Supporting Information

Synergistic effect between rare-earth and copper species enhances hydrothermal stability of Cu-SSZ-13 for NO abatement

Liu Yang a, 1, Yuanjiang Wang a, 1, Tiantian Zhang a, Hao Qu a, Xin Guo a, Cheng Zhang a, Yan Wang a, *, Mi Yan a, d, and Pengfei Xiea, b, c*

a State Key Laboratory of Baiyunobo Rare Earth Resource Researches and Comprehensive Utilization, Baotou Research Institute of Rare Earths, Baotou 014030, China

b Key Laboratory of Biomass Chemical Engineering of Ministry of Education, College of Chemical and Biological Engineering, Zhejiang University, Hangzhou 310058, China

c Institute of Zhejiang University-Quzhou, Quzhou 324000, China

d Zhejiang Province Key Laboratory of Advanced Information Materials, School of Materials Science and Engineering, Zhejiang University, Hangzhou 310058, China

1 Liu Yang and Yuanjiang Wang contributed equally to this work.

* Corresponding Authors Email: pfxie@zju.edu.cn; wy_brire@brire.com.

## Text S1. Catalyst Characterization

X-ray Fluorescence Spectrometer (XRF) was employed to analyze the contents of Si and Al in the samples, utilizing a Shimadzu EDX-7000 instrument. ICP (Inductive Coupled Plasma Emission Spectrometer) was used to analyze other elements content used Agilent 725ES & Agilent 5110 instrument. X-ray powder diffraction (XRD) tests were collected on a Rigaku SmartLab SE diffractometer with Cu Kα radiation at a scanning range from 5 to 55o. X-ray photoelectron spectroscopy (XPS) was performed on a Thermo ESCALAB 250XI spectrometer using Al Kα X-ray radiation. The binding energies of C 1s (284.6 eV) were corrected all XPS spectrum. Electron paramagnetic resonance (EPR) spectroscopy was performed using a Bruker A300 instrument to analyze Cu2+ species at -150 ℃ and room temperature.

Temperature programmed reduction of hydrogen (H2-TPR) and Temperature programmed desorption of ammonia (NH3-TPD) tests were conducted on a Antom Paar Chem 3000 instrument. For H2-TPR test, 100mg of 60 ~ 100 mesh catalyst was pretreated under pure helium (He) at 300 ℃ for 1 h and then cooled down to 30 ℃, which was heated to 900 ℃ at 10 ℃ min−1 in a 5% H2/Ar at a flow rate of 100 ml/min. For NH3-TPD teat, 50 mg catalyst was pretreated by nitrogen for 1 h at 400 ℃. Then, the sample was adsorbed by 6000 ppm NH3/He at 100 ℃ for 150 min and purged by N2 for 40 min. Desorption signal was collected from 150 to 900 ℃ at a heating rate of 10 ℃/min. Luo[1] indicate that each ZCu(OH)+ site can adsorb 1 NH3 molecule, while each Z2Cu site can adsorb up to 2 NH3 molecules.

The diffuse reflectance infrared Fourier transform spectroscopy (DRIFTS) experiments were implemented on a Fourier transform infrared spectrometer (FTIR, Nicolet iS50) with the MCT/A detector. For the NH3 adsorption, the catalyst was pretreated at 450 ℃ in 20% O2/N2 for 60 min and subsequently cooled to 50 ℃. After the background spectra were collected under pure N2, 500 ppm of NH3 in N2 was introduced. In the transient studies, each catalyst was first at 450 ℃ for 60 min with 100 mL/min N2 and then cooled to 170 ℃ to collect the background spectra. Subsequently, 500 ppm NH3/N2 was introduced 60 min and then the gas was switched to 500 ppm NO + 5 vol% O2, in order to collect the changes of the pre-adsorbed NH3 species. By altering the sequence of gas introduction, the spectrum corresponding to the process where NO & O2 are first adsorbed, followed by the introduction of NH3 for the reaction, was obtained.

## Fig. S1. Structural schematics of various RECuSSZ-13 catalysts.

## Fig. S2. XRD patterns of Cu-SSZ-13 and RECuSSZ-13 catalysts.

## Fig. S3. NOx conversion of Cu-SSZ-13 and RECuSSZ-13 samples.

## Fig. S4. (a) N2O formation and (b) N2 selectivity of Cu-SSZ-13 and RECuSSZ-13 catalysts. Reaction conditions: 500 ppm NO, 500 ppm NH3, 10% O2, and 5% H2O, balance N2; GHSV = 100000 h−1.

## Fig. S5. NOx conversions at 150 ℃ (a) and 175 ℃ (b) over Cu-SSZ-13 and RECuSSZ-13 samples before and after high-temperature hydrothermal ageing.

## Fig. S6. Comparison of the T50 values for Cu-SSZ-13HT and RECuSSZ-13HT samples.

## Fig. S7. NOx conversions at 400~600 ℃ over Cu-SSZ-13 and RECuSSZ-13 samples before and after high-temperature hydrothermal ageing.

## Fig. S8. The corresponding T90 temperature window of Cu-SSZ-13HT and RECuSSZ-13HT catalysts.

## Fig. S9. In situ DRIFTS spectra after NH3 adsorption saturation (T-O-T vibrations portion) over Cu-SSZ-13HT and RECuSSZ-13HT. Reaction conditions: 500 ppm NH3 balanced with N2.

## Fig. S10. The percentage of ZCu(OH)+ based on quadratic integration of H2-TPR profiles.

## Fig. S11. In situ DRIFT spectra of the reaction between 500 ppm NO + 5% O2 and pre-adsorbed NH3 at 170 ℃ on the NdCuSSZ-13HT catalyst.

## Fig. S12. In situ DRIFT spectra of the reaction between 500 ppm NO + 5% O2 and pre-adsorbed NH3 at 170 ℃ on the CeCuSSZ-13HT catalyst.

## Fig. S13. In situ DRIFT spectra of the reaction between 500 ppm NO + 5% O2 and pre-adsorbed NH3 at 170 ℃ on the LaCuSSZ-13HT catalyst.

## Fig. S14. In situ DRIFT spectra of the reaction between 500 ppm NO + 5% O2 and pre-adsorbed NH3 at 170 ℃ in the 3500~3000 cm-1 region.

## Fig. S15. In situ DRIFT spectra of the reaction between 500 ppm NH3 and pre-adsorbed NO + O2 at 170 ℃ on the YCuSSZ-13HT catalyst.

## Fig. S16. In situ DRIFT spectra of the reaction between 500 ppm NH3 and pre-adsorbed NO + O2 at 170 ℃ on the NdCuSSZ-13HT catalyst.

## Fig. S17. In situ DRIFT spectra of the reaction between 500 ppm NH3 and pre-adsorbed NO + O2 at 170 ℃ on the CeCuSSZ-13HT catalyst.

## Fig. S18. In situ DRIFT spectra of the reaction between 500 ppm NH3 and pre-adsorbed NO + O2 at 170 ℃ on the Cu-SSZ-13HT catalyst.

## Fig. S19. In situ DRIFT spectra of the reaction between 500 ppm NH3 and pre-adsorbed NO + O2 at 170 ℃ on the LaCuSSZ-13HT catalyst.

## Fig. S20. The pCOHP and ICOHP results for (a) NdCuSSZ-13, (b) CeCuSSZ-13, and (c) LaCuSSZ-13 systems.

## Fig. S21. Configuration from AIMD revealing a Cu(OH)2 unit within the NdCuSSZ-13 framework.

## Fig. S22. Configuration from AIMD revealing a Cu(OH)2 unit within the CeCuSSZ-13 framework.

## Fig. S23. Configuration from AIMD revealing a Cu(OH)2 unit within the LaCuSSZ-13 framework.

## Table S1. Characterization of the Si/Al ratio and elemental composition of the catalysts.

| Samples | Si/Ala | Cub | REb |
| --- | --- | --- | --- |
| LaCuSSZ-13 | 6.4 | 3.4% | 0.5% |
| CeCuSSZ-13 | 6.2 | 3.5% | 0.5% |
| PrCuSSZ-13 | 6.2 | 3.2% | 0.4% |
| NdCuSSZ-13 | 6.2 | 3.6% | 0.4% |
| SmCuSSZ-13 | 6.3 | 3.7% | 0.5% |
| EuCuSSZ-13 | 6.1 | 3.5% | 0.4% |
| YCuSSZ-13 | 6.1 | 3.2% | 0.4% |

a: Calculated by XRF.

b: Calculated by ICP.

## Table S2. Data results related to Fig. 2e.

| ## Catalysts | ## C175 a | ## C600 b | ## △T90 c | ## △CF-A d | ## △S95 e |
| --- | --- | --- | --- | --- | --- |
| ## YCuSSZ-13HT | ## 89.9 | ## 80.5 | ## 379.4 | ## -1.1 | ## 450 |
| ## NdCuSSZ-13HT | ## 88.6 | ## 75.7 | ## 358.9 | ## 2.2 | ## 450 |
| ## EuCuSSZ-13HT | ## 83.1 | ## 77.7 | ## 364.2 | ## 2.9 | ## 450 |
| ## CeCuSSZ-13HT | ## 79.2 | ## 79 | ## 352.8 | ## 4.6 | ## 400 |
| ## SmCuSSZ-13HT | ## 78 | ## 81.2 | ## 382.6 | ## 4.1 | ## 450 |
| ## Cu-SSZ-13HT | ## 76 | ## 59.1 | ## 281.7 | ## 8.7 | ## 300 |
| ## PrCuSSZ-13HT | ## 73.8 | ## 75.6 | ## 349.1 | ## 2.7 | ## 450 |
| ## LaCuSSZ-13HT | ## 70.8 | ## 78.4 | ## 359.1 | ## 5.4 | ## 450 |

a: The NOx conversion at 175 ℃;

b: The NOx conversion at 600 ℃;

c: Temperature window corresponding to 90 % conversion;

d: The average value of the decrease in NOx conversions for the fresh catalysts and the hydrothermal-aged catalysts within the temperature range of 150 to 600 ℃;

e: The temperature range of N2 selectivity ≥95%.

## Table S3. Representative rare earth modified Cu-zeolites for the NH3-SCR reaction.

| Catalyst | NOx Conv. (175 ℃) -HT (%) | NOₓ Conv. (550 ℃) -HT (%) | ΔT90 (HT) | Ref. |
| --- | --- | --- | --- | --- |
| YCuSSZ-13HT | 90 | 80 | 380 | This work |
| Cu-Sm-SSZ-13 | 35 | 80 | 120 | [2] |
| Cu-Pr-SSZ-13 | 33 | 78 | 100 | [3] |
| Cu-Cd-SSZ-13 | 85 | 80 | 340 | [4] |
| CM/CSZ-BM | 50 | 70 | 190 | [5] |
| Cu-Fe-SSZ-13 | 85 | 80 | 100 | [6] |
| CuLa0.5-SAPO34 | 95 | 72 | 290 | [7] |
| Cu/Y-S | 65 | 70 | 180 | [8] |
| Cu/SSZ-13@CeO2 | 32 | 60 | 0 | [9] |

The references (2~9) are consistent with those cited in Fig. 2f in the manuscript.

## Table S4. EPR results of catalysts.

| Samples | Total peak area of the curve (Hydrate-Dehydrate) | Percentage increase upon RE incorporation (%) |
| --- | --- | --- |
| YCuSSZ-13HT | 916029.5 | 19.3 |
| NdCuSSZ-13HT | 832503.3 | 8.5 |
| CeCuSSZ-13HT | 827794.9 | 7.8 |
| Cu-SSZ-13HT | 767646.5 | - |
| LaCuSSZ-13HT | 742274.0 | -3.3 |

## Table S5. Integral results of the NH3-TPD profile.

| Samples | Relative Proportion of Integrated Peak Area (%) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Peak position |  |  |  |  | Peak Area |  |  |  |
| YCuSSZ-13HT | 231.7 | 274.5 | 337.2 | 463.5 | 677.4 |  | 2086.6 | 3376.4 | 2565.1 |
| NdCuSSZ-13HT | 235.8 | 276.0 | 344.7 | 466.3 | 886.5 |  | 2447.4 | 2983.2 | 2363.2 |
| CeCuSSZ-13HT | 234.8 | 275.7 | 348.5 | 464.0 | 600.0 |  | 2622.4 | 2721.7 | 2581.3 |
| Cu-SSZ-13HT | 236.6 | 288.3 | 352.1 | 482.6 | 1200.0 |  | 2754.6 | 2504.6 | 2568.4 |
| LaCuSSZ-13HT | 238.2 | 295.0 | 358.2 | 480.8 | 1735.3 |  | 2803.1 | 2410.9 | 2064.4 |

## Table S6. Comparison of the occurrence times of various nitrate species in in-situ DRIFT spectra.

| Samples | Monodentate nitrate |  |  | Bidentate nitrate |  | Nitrate |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Occurrence time |  | Disappearance time | Occurrence times of nitrate species (min) |  |  |  |
| YCuSSZ-13HT | 2 | 20 |  |  | 4 |  | 25 |
| NdCuSSZ-13HT | 6 | 40 |  |  | 4 |  | 25 |
| CeCuSSZ-13HT | 8 | 40 |  |  | 6 |  | 40 |
| Cu-SSZ-13HT | 4 | 40 |  |  | 4 |  | 40 |
| LaCuSSZ-13HT | 20 | 40 |  |  | 15 |  | - |

## Reference

[1] Luo J, et al. New Insights into Cu/SSZ-13 SCR Catalyst Acidity. Part I: Nature of Acidic Sites Probed by NH3 Titration. J. Catal. 348, 291-299 (2017).

[2] Chen MY, et al. Unveiling secondary-ion-promoted catalytic properties of Cu-SSZ-13 zeolites for selective catalytic reduction of NOx. J. Am. Chem. Soc. 144, 12816-12824 (2022).

[3] Chen MY, et al. Improving the hydrothermal stability of Al-rich Cu-SSZ-13 zeolite via Pr-ion modification. Chem. Sci. 15, 5548-5554 (2024).

[4] Li M, et al. The preferential occupying effect regulated atomically dispersed Cu site over Cu-SSZ-13 for enhancing NH3-SCR performance. Fuel 380, 133202 (2025).

[5] Andana T, et al. Selective catalytic reduction of NOx with NH3 over Ce-Mn oxide and Cu-SSZ-13 composite catalysts – low temperature enhancement. Appl. Catal. B Environ. 316, 121522 (2022).

[6] Tan MJ, et al. Introduction of iron by a feasible way to regulate Cu sites of Cu-SSZ-13 with enhanced hydrothermal stability and SO2 resistance for NH3-SCR. Micropor Mesopor Mat. 394, 113668 (2025).

[7] Li GB, et al. One stone four birds: The redox and acid-basic site integral regulation by La in Cu-SAPO-34 for boosting NO reduction. Appl. Catal. B Environ. 378, 125647 (2025).

[8] Gao LY, et al. Boosting low-temperature and high-temperature hydrothermal stability of Cu/SAPO-34 for NO removal via Yttrium decoration. Chem. Eng. J. 455, 140520 (2023).

[9] Zhang JN, et al. Enhancing hydrothermal stability in Cu/SSZ-13 catalyst for diesel SCR applications through a novel core-shell structure. Chin. Chem. Lett. 36, 110516 (2025).