Supplementary Information

Supplementary Figure SI1. SEM images of citrate-reduced gold nanoparticles. The nanoparticles were deposited on to Si wafers and imaged using a Hitachi S-4800 SEM.

Supplementary Figure SI2. Zeta potential distribution of citrate-reduced gold nanoparticles measured using the Malvern Zetasizer Nano ZS (Malvern Panalytical, Malvern, UK) fitted with a 532 nm laser.

Supplementary Figure SI3. Results from a Zetasizer of the average hydrodynamic diameter of citrate-reduced gold nanoparticles measured using the Malvern Zetasizer Nano ZS (Malvern Panalytical, Malvern, UK) fitted with a 532 nm laser. Histograms display size distribution from intensity.

Supplementary Figure SI4. Image of three palm oil samples from the study, highlighting the variation in colour between samples.

Palm oil naturally ranges in colour from pale orange to deep red, a variation largely driven by its differing levels of β-carotene. This natural variability means that two legitimate, unadulterated oils can look strikingly different from one another. When colourant dyes such as Sudan IV are added, they generally intensify the redness of the oil. Yet the effect is not always dramatic: low levels of added dye may shift the appearance only slightly - from light orange toward a somewhat deeper hue - making visual inspection unreliable. Complicating matters further, an oil that is naturally rich in β-carotene may appear redder than an oil that has been adulterated but contains relatively little dye. These overlapping colour ranges highlight the limitations of colour-based assessments and underscore the need for analytical techniques capable of reliably detecting the presence of Sudan dyes in palm oil. As shown, even though the sample on the left has been adulterated, it still presents a paler appearance compared with the middle sample. This highlights the overlap between natural colour variability and dye-induced colour changes.

Supplementary Figure SI5. Raman and SERS spectra of negative and positive control samples are shown for the glass vial, citrate-reduced gold nanoparticles, aggregated nanoparticles (water + NaCl), and extracted palm oil samples spiked with Sudan IV at three concentrations, including a dye-free control. The spectra of the 3 different levels of spiked Sudan dye were taken after extraction and drying.

Table SI1. Predicted concentrations from SERS analysisof Sudan IV dye (mg/mL) for each sample from Cameroon, as well as the average and standard deviation.

| Samples | Predicted Concentration (mg/mL) | Predicted Concentration (mg/mL) |
| --- | --- | --- |
|  | Repeats | Averages (standard deviation) |
|  | 0.0009 |  |
| 1 | 0.0012 | 0.0010 (0.0002) |
|  | 0.0009 |  |
|  | 0.0006 |  |
| 2 | 0.0009 | 0.0007 (0.0002) |
|  | 0.0006 |  |
|  | 0.0011 |  |
| 3 | 0.0005 | 0.0012 (0.0008) |
|  | 0.0021 |  |
|  | 0.0003 |  |
| 4 | 0.0004 | 0.0006 (0.0005) |
|  | 0.0012 |  |
|  | 0.0012 |  |
| 5 | 0.0008 | 0.0011 (0.0003) |
|  | 0.0013 |  |
|  | 0.0005 |  |
| 6 | 0.0007 | 0.0009 (0.0006) |
|  | 0.0015 |  |
|  | -0.0006 |  |
| 7 | 0.0004 | –0.0002 (0.0005) |
|  | -0.0004 |  |
|  | 0.0006 |  |
| 8 | 0.0011 | 0.0010 (0.0004) |
|  | 0.0013 |  |
|  | 0.0020 |  |
| 9 | 0.0014 | 0.0014 (0.0006) |
|  | 0.0008 |  |
|  | 0.0012 |  |
| 10 | 0.0005 | 0.0009 (0.0004) |
|  | 0.0011 |  |
|  | 0.0014 |  |
| 11 | 0.0015 | 0.0015 (0.0001) |
|  | 0.0015 |  |
|  | 0.0005 |  |
| 12 | 0.0010 | 0.0009 (0.0004) |
|  | 0.0013 |  |
|  | 0.0013 |  |
| 13 | 0.0006 | 0.0009 (0.0004) |
|  | 0.0008 |  |
|  | 0.0001 |  |
| 14 | 0.0021 | 0.0007 (0.0013) |
|  | 0.0000 |  |
|  | 0.0012 |  |
| 15 | 0.0004 | 0.0009 (0.0005) |
|  | 0.0011 |  |
|  | 0.0003 |  |
| 16 | 0.0013 | 0.0010 (0.0006) |
|  | 0.0013 |  |
|  | 0.0010 |  |
| 17 | 0.0010 | 0.0009 (0.0002) |
|  | 0.0007 |  |
|  | 0.0004 |  |
| 18 | 0.0015 | 0.0009 (0.0006) |
|  | 0.0008 |  |
|  | 0.0012 |  |
| 19 | 0.0012 | 0.0011 (0.0001) |
|  | 0.0010 |  |
|  | 0.0006 |  |
| 20 | 0.0017 | 0.0011 (0.0006) |
|  | 0.0011 |  |
|  | 0.0005 |  |
| 21 | 0.0019 | 0.0011 (0.0008) |
|  | 0.0008 |  |
|  | 0.0005 |  |
| 22 | 0.0008 | 0.0008 (0.0003) |
|  | 0.0011 |  |
|  | 0.0023 |  |
| 23 | 0.0015 | 0.0014 (0.0010) |
|  | 0.0004 |  |
|  | 0.0000 |  |
| 24 | 0.0005 | 0.0003 (0.0003) |
|  | 0.0004 |  |
|  | 0.0012 |  |
| 25 | −0.0001 | 0.0007 (0.0008) |
|  | 0.0011 |  |
|  | 0.0012 |  |
| 26 | 0.0010 | 0.0010 (0.0002) |
|  | 0.0008 |  |
|  | 0.0011 |  |
| 27 | 0.0010 | 0.0013 (0.0004) |
|  | 0.0017 |  |
|  | 0.0008 |  |
| 28 | 0.0004 | 0.0011 (0.0009) |
|  | 0.0021 |  |
|  | 0.0021 |  |
| 29 | 0.0018 | 0.0017 (0.0004) |
|  | 0.0013 |  |
|  | 0.0004 |  |
| 30 | 0.0011 | 0.0007 (0.0004) |
|  | 0.0006 |  |
|  | 0.0010 |  |
| 31 | 0.0014 | 0.0010 (0.0004) |
|  | 0.0006 |  |
|  | 0.0010 |  |
| 32 | 0.0006 | 0.0007 (0.0002) |
|  | 0.0006 |  |
|  | 0.0003 |  |
| 33 | 0.0006 | 0.0005 (0.0002) |
|  | 0.0006 |  |
|  | 0.0010 |  |
| 34 | 0.0019 | 0.0012 (0.0006) |
|  | 0.0007 |  |
|  | 0.0008 |  |
| 35 | -0.0003 | 0.0006 (0.0008) |
|  | 0.0013 |  |
|  | 0.0009 |  |
| 36 | 0.0007 | 0.0008 (0.0001) |
|  | 0.0007 |  |
|  | -0.0002 |  |
| 37 | 0.0007 | 0.0002 (0.0005) |
|  | 0.0001 |  |
|  | 0.0007 |  |
| 38 | 0.0004 | 0.0006 (0.0002) |
|  | 0.0007 |  |
|  | 0.0005 |  |
| 39 | 0.0007 | 0.0006 (0.0001) |
|  | 0.0005 |  |
|  | -0.0007 |  |
| 40 | 0.0014 | 0.0004 (0.0011) |
|  | 0.0004 |  |
|  | 0.0009 |  |
| 41 | 0.0005 | 0.0008 (0.0003) |
|  | 0.0009 |  |
|  | 0.0006 |  |
| 42 | 0.0017 | 0.0014 (0.0007) |
|  | 0.0019 |  |
|  | 0.0005 |  |
| 43 | 0.0011 | 0.0007 (0.0003) |
|  | 0.0006 |  |
|  | -0.0002 |  |
| 44 | 0.0002 | -0.0002 (0.0004) |
|  | -0.0005 |  |
|  | 0.0014 |  |
| 45 | 0.0004 | 0.0008 (0.0005) |
|  | 0.0005 |  |
|  | 0.0019 |  |
| 46 | 0.0005 | 0.0010 (0.0008) |
|  | 0.0006 |  |
|  | 0.0009 |  |
| 47 | 0.0011 | 0.0011 (0.0003) |
|  | 0.0014 |  |
|  | 0.0011 |  |
| 48 | 0.0017 | 0.0014 (0.0003) |
|  | 0.0013 |  |
|  | 0.0011 |  |
| 49 | 0.0008 | 0.0012 (0.0005) |
|  | 0.0017 |  |
|  | 0.0005 |  |
| 50 | 0.0009 | 0.0009 (0.0005) |
|  | 0.0014 |  |
|  | 0.0004 |  |
| 51 | 0.0003 | 0.0004 (0.0001) |
|  | 0.0004 |  |
|  | 0.0016 |  |
| 52 | 0.0015 | 0.0015 (0.0001) |
|  | 0.0013 |  |
|  | 0.0017 |  |
| 53 | 0.0019 | 0.0016 (0.0003) |
|  | 0.0013 |  |
|  | 0.0008 |  |
| 54 | -0.0008 | 0.0000 (0.0008) |
|  | 0.0001 |  |
|  | 0.0004 |  |
| 55 | 0.0010 | 0.0011 (0.0003) |
|  | 0.0008 |  |
|  | 0.0023 |  |
| 56 | 0.0012 | 0.0015 (0.0008) |
|  | 0.0009 |  |
|  | 0.0012 |  |
| 57 | 0.0002 | 0.0004 (0.0007) |
|  | -0.0001 |  |
|  | 0.0008 |  |
| 58 | 0.0001 | 0.0006 (0.0004) |
|  | 0.0008 |  |
|  | 0.0006 |  |
| 59 | 0.0005 | 0.0006 (0.0001) |
|  | 0.0007 |  |
|  | 0.0005 |  |
| 60 | 0.0011 | 0.0006 (0.0004) |
|  | 0.0003 |  |
|  | 0.0003 |  |
| 61 | 0.0016 | 0.0012 (0.0008) |
|  | 0.0016 |  |
|  | 0.0004 |  |
| 62 | 0.0013 | 0.0012 (0.0007) |
|  | 0.0018 |  |
|  | 0.0008 |  |
| 63 | 0.0009 | 0.0006 (0.0004) |
|  | 0.0002 |  |
|  | 0.0014 |  |
| 64 | 0.0005 | 0.0009 (0.0005) |
|  | 0.0008 |  |