SUPPLEMENTARY MATERIAL

SDS–Chitosan Flocculant Systems in Oily Produced Water Treatment: Performance and Influence of Chitosan Properties

Anny Marry Teixeira Marques1,2 · Gabriele Braz Anhalo1,3 · Allan da Silva Santos1 · Claudia Regina Elias Mansur1,2

1 Laboratório de Macromoléculas e Coloides na Indústria de Petróleo (LMCP), Instituto de Macromoléculas Professora Eloisa Mano (IMA), Universidade Federal do Rio de Janeiro (UFRJ), Rio de Janeiro, RJ, Brazil

2 Programa de Engenharia Metalúrgica e de Materiais (PEMM/COPPE), Universidade Federal do Rio de Janeiro (UFRJ), Rio de Janeiro, RJ, Brazil

3 Universidade do Estado do Rio de Janeiro (UERJ), Rio de Janeiro, RJ, Brazil

Corresponding author: Claudia Regina Elias Mansur – E-mail: celias@ima.ufrj.br – ORCID: 0000-0001-8736-7363 - Address: Laboratório de Macromoléculas e Coloides na Indústria de Petróleo (LMCP), Instituto de Macromoléculas Professora Eloisa Mano (IMA), Universidade Federal do Rio de Janeiro (UFRJ), Rua Moniz Aragão, 360, Bloco 8G-CT2, LIMC, Cidade Universitária, Rio de Janeiro, RJ, CEP 21941-594, Brazil

Table S1 Composition of the saline solution used in the study

| Brine (proportion 90% injection water/ 10% formation water) |  |
| --- | --- |
| Salt | Concentration (mg/L) |
| NaCl | 41621 |
| Anhydrous CaCl2 | 4171 |
| MgCl2.6H2O | 3184 |
| KCl | 1159 |
| Na2(SO)4 | 65 |
| SrCl2.6H2O | 851 |
| TDS | 49014 |

Figure S1 Calibration curve of 14° API crude oil in distilled toluene

Figure S2 ¹H NMR spectrum of low-molecular-weight chitosan (LC)

Figure S3 ¹H NMR spectrum of high-molecular-weight chitosan (HC)

Figure S4 Reduced Viscosity as a function of LC Concentration

Figure S5 Reduced Viscosity as a function of QH concentration

Figure S6 Surface tension as a function of SDS concentration for CMC determination

Table S2 Matrix of coded variables, real variables and responses obtained from design of experiments using the SDS and LC flocculant system

| Experiments | SDS Concentration (ppm) | Flocculant Concentration (LC) (ppm) | pH of Flocculant System (LC) | Residual Oil Concentration (ppm) | Oil Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | 87 (−1) | 65.2 (−1) | 4 (-1) | 74,5 | 0 |
| 2 | 261 (+1) | 65.2 (−1) | 4 (-1) | 88,6 | 0 |
| 3 | 87 (−1) | 195.7 (+1) | 4 (-1) | 69,3 | 0 |
| 4 | 261 (+1) | 195.7 (+1) | 4 (-1) | 16,0 | 75,4 |
| 5 | 87 (−1) | 65.2 (−1) | 5 (1) | 73,7 | 0 |
| 6 | 261 (+1) | 65.2 (−1) | 5 (1) | 84,4 | 0 |
| 7 | 87 (−1) | 195.7 (+1) | 5 (1) | 65,4 | 0 |
| 8 | 261 (+1) | 195.7 (+1) | 5 (1) | 65,4 | 0 |
| 9 | 27.7 (−1.68) | 130.5 (0) | 4,5 (0) | 83,9 | 0 |
| 10 | 320.3 (+1.68) | 130.5 (0) | 4,5 (0) | 23,3 | 68,9 |
| 11 | 174 (0) | 20.8 (−1.68) | 4,5 (0) | 73,7 | 0 |
| 12 | 174 (0) | 240.2 (+1.68) | 4,5 (0) | 75,5 | 0 |
| 13 | 174 (0) | 130.5 (0) | 3,7 (-1,68) | 79,5 | 0 |
| 14 | 174 (0) | 130.5 (0) | 5,3 (1,68) | 79,6 | 0 |
| 15 | 174 (0) | 130.5 (0) | 4,5 (0) | 70,6 | 0 |
| 16 | 174 (0) | 130.5 (0) | 4,5 (0) | 63,0 | 0 |
| 17 | 174 (0) | 130.5 (0) | 4,5 (0) | 77,6 | 0 |
| 18 | 174 (0) | 130.5 (0) | 4,5 (0) | 72,2 | 0 |

Table S3 Matrix of coded variables, real variables and responses obtained from design of experiments using the SDS and HC flocculant system

| Experiments | SDS Concentration (ppm) | Flocculant Concentration (HC) (ppm) | pH of Flocculant System (HC) | Residual Oil Concentration (ppm) | Oil Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | 87 (−1) | 65.2 (−1) | 4 (-1) | 45,3 | 34,5 |
| 2 | 261 (+1) | 65.2 (−1) | 4 (-1) | 26,5 | 61,7 |
| 3 | 87 (−1) | 195.7 (+1) | 4 (-1) | 73,2 | 0 |
| 4 | 261 (+1) | 195.7 (+1) | 4 (-1) | 7,2 | 89,6 |
| 5 | 87 (−1) | 65.2 (−1) | 5 (1) | 57,9 | 0 |
| 6 | 261 (+1) | 65.2 (−1) | 5 (1) | 78,0 | 0 |
| 7 | 87 (−1) | 195.7 (+1) | 5 (1) | 57,1 | 0 |
| 8 | 261 (+1) | 195.7 (+1) | 5 (1) | 13,5 | 75,0 |
| 9 | 27.7 (−1.68) | 130.5 (0) | 4,5 (0) | 60,9 | 0 |
| 10 | 320.3 (+1.68) | 130.5 (0) | 4,5 (0) | 5,0 | 91,0 |
| 11 | 174 (0) | 20.8 (−1.68) | 4,5 (0) | 68,8 | 0 |
| 12 | 174 (0) | 240.2 (+1.68) | 4,5 (0) | 53,0 | 5,7 |
| 13 | 174 (0) | 130.5 (0) | 3,7 (-1,68) | 26,5 | 62,5 |
| 14 | 174 (0) | 130.5 (0) | 5,3 (1,68) | 69,0 | 2,5 |
| 15 | 174 (0) | 130.5 (0) | 4,5 (0) | 40,8 | 41,1 |
| 16 | 174 (0) | 130.5 (0) | 4,5 (0) | 38,2 | 48,9 |
| 17 | 174 (0) | 130.5 (0) | 4,5 (0) | 47,1 | 16,2 |
| 18 | 174 (0) | 130.5 (0) | 4,5 (0) | 36,5 | 48,5 |

Figure S7 Contour plot for removal efficiency as a function of SDS and HC concentrations

Figure S8 Contour plot for removal efficiency as a function of HC solution pH and SDS concentration

Table S4 Responses obtained for optimization CCRD using the SDS and LC flocculant system

| Experiments | SDS Concentration (ppm) | Flocculant Concentration LC (ppm) | Residual Oil Concentration (ppm) | Oil Removal Efficiency (%) | Ratio Between Charges of Dosed Concentrations |
| --- | --- | --- | --- | --- | --- |
| 1 | 261 (−1) | 195.7 (−1) | 22,9 | 69,1 | 0.75 |
| 2 | 435 (+1) | 195.7 (−1) | 73,3 | 1,5 | 0.45 |
| 3 | 261 (−1) | 326.2 (+1) | 30,2 | 59,4 | 1.24 |
| 4 | 435 (+1) | 326.2 (+1) | 12,8 | 82,7 | 0.75 |
| 5 | 225 (−1.41) | 261 (0) | 64,2 | 0 | 1.15 |
| 6 | 471 (+1.41) | 261 (0) | 12,3 | 74,0 | 0.55 |
| 7 | 348 (0) | 168.7 (−1.41) | 15,9 | 66,3 | 0.48 |
| 8 | 348 (0) | 353.2 (+1.41) | 46,5 | 1,7 | 1.01 |
| 9 | 348 (0) | 261 (0) | 13,9 | 81,3 | 0.75 |
| 10 | 348 (0) | 261 (0) | 14,5 | 69,7 | 0.75 |
| 11 | 348 (0) | 261 (0) | 9,5 | 78,1 | 0.75 |
| 12 | 348 (0) | 261 (0) | 14,3 | 85,6 | 0.75 |

Table S5 Responses obtained for optimization planning using the SDS and HC flocculant system

| Experiments | SDS Concentration (ppm) | Flocculant Concentration HC (ppm) | Residual Oil Concentration (ppm) | Oil Removal Efficiency (%) | Ratio Between Charges of Dosed Concentrations |
| --- | --- | --- | --- | --- | --- |
| 1 | 261 (−1) | 195.7 (−1) | 9,5 | 83,8 | 0.75 |
| 2 | 435 (+1) | 195.7 (−1) | 30,3 | 48,2 | 0.45 |
| 3 | 261 (−1) | 326.2 (+1) | 30,7 | 47,8 | 1.24 |
| 4 | 435 (+1) | 326.2 (+1) | 3,4 | 94,2 | 0.75 |
| 5 | 225 (−1.41) | 261 (0) | 64,9 | 22,8 | 1.15 |
| 6 | 471 (+1.41) | 261 (0) | 6,9 | 91,8 | 0.55 |
| 7 | 348 (0) | 168.7 (−1.41) | 6,7 | 92,4 | 0.48 |
| 8 | 348 (0) | 353.2 (+1.41) | 24,8 | 70,5 | 1.01 |
| 9 | 348 (0) | 261 (0) | 3,1 | 87,2 | 0.75 |
| 10 | 348 (0) | 261 (0) | 8,5 | 91,7 | 0.75 |
| 11 | 348 (0) | 261 (0) | 5,5 | 94,6 | 0.75 |
| 12 | 348 (0) | 261 (0) | 5,2 | 93,8 | 0.75 |