“Phytoconstituent Effect on Morphology of ZnO nanostructure: Synthesis, characterisation and photocatalytic degradation of Methylene blue, Malachite green, Brilliant cresyl blue, Rb171, Eosin yellow and Congo red dye”

Suneel a*,Haroon b,  Mohd. Shabeerc, Zainab Ferozd, Nafees Ahmada, Qazi Inamur Rahman a*

Supplementary File

Table. S1 Structural parameter of syntheised ZnO NSa

| ZnO Ns Sample | 2θ (°) | hkl | FWHM (°) | Crystalline size calculated by D=kλ/βCosθ (nm) | (101/002) Intensity ratio | Inter Planar spacing (A°) | Lattice constant (A°)) |  |  | Unit cell volume (A°)3 | Dislocation density (x10-3 nm-2) | Strain ε (x10-3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | a | c | c/a |  |  |  |
| S | 31.979 | 100 | 1.122 | 7.245 | 2.397 | 2.796 | 3.23 ±0.01 | 5.16 ±0.02 | 1.597 | 46.06 ±0.33 | 19.70 | 17.1 |
|  | 34.795 | 002 | 1.099 | 7.446 |  | 2.579 |  |  |  |  | 18.0 | 14.3 |
|  | 36.448 | 102 | 1.304 | 6.321 |  | 2.463 |  |  |  |  | 25.0 | 16.0 |
|  | 47.762 | 110 | 1.334 | 6.397 |  | 1.904 |  |  |  |  | 24.4 | 12.7 |
|  | 56.825 | 103 | 1.501 | 5.934 |  | 1.620 |  |  |  |  | 28.4 | 12.4 |
| P | 31.92 | 100 | 0.462 | 16.394 | 2.24 | 2.81 | 3.23 ±0.006 | 5.18±0.012 | 1.069 | 47.09 ±0.22 | 3.72 | 7.04 |
|  | 34.567 | 002 | 0.368 | 19.856 |  | 2.60 |  |  |  |  | 2.54 | 4.79 |
|  | 36.399 | 101 | 0.443 | 16.894 |  | 2.47 |  |  |  |  | 3.50 | 5.43 |
|  | 47.687 | 102 | 0.475 | 16.174 |  | 1.91 |  |  |  |  | 3.82 | 4.41 |
|  | 56.727 | 110 | 0.532 | 15.353 |  | 1.62 |  |  |  |  | 4.24 | 4.38 |
| M | 31.745 | 100 | 0.660 | 11.969 | 1.584 | 2.816 | 3.250 ± 0.004 | 5.19±0.012 | 1.064 | 47.52 ± 0.16 | 6.98 | 8.86 |
|  | 34.515 | 002 | 0.627 | 12.638 |  | 2.597 |  |  |  |  | 6.26 | 8.31 |
|  | 36.216 | 101 | 0.620 | 12.702 |  | 2.478 |  |  |  |  | 6.20 | 7.63 |
|  | 47.47 | 102 | 0.573 | 13.863 |  | 1.914 |  |  |  |  | 5.20 | 5.43 |
|  | 56.57 | 110 | 0.696 | 12.191 |  | 1.626 |  |  |  |  | 6.73 | 5.83 |
| A | 31.698 | 100 | 0.583 | 13.384 | 1.899 | 2.820 | 3.256 ± 0.0028 | 5.22±0.013 | 1.603 | 47.99 ±0.08 | 5.58 | 8.73 |
|  | 34.3 | 002 | 0.545 | 14.309 |  | 2.612 |  |  |  |  | 4.88 | 7.08 |
|  | 36.16 | 101 | 0.560 | 13.881 |  | 2.482 |  |  |  |  | 5.18 | 6.91 |
|  | 47.41 | 102 | 0.584 | 13.642 |  | 1.916 |  |  |  |  | 5.37 | 5.46 |
|  | 56.48 | 110 | 0.605 | 13.767 |  | 1.627 |  |  |  |  | 5.27 | 5.13 |

Fig.S1 W-H plot of linear fitting of(a) S (b) P (c) M and (d) A for the estimation of Size and lattice strain (microstrain)

Fig.S2 Illustration of (a) XRD and (b) FTIR spectra of ZnO NS, sample S after reusability test

Table xxx Photodegradation performance of ZnO nanostructure derived from S, P, M and A, exposure to 120 min of open sunlight

| Catalytic and |  |  |  | Kinetics Parameter |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model Pollutants (dye) | Nanomaterial (sample) | Conc of dyes and its Volume | Degradation efficiency (%) | Kapp (min-1) | Half-life (t1/2) min | Regression coefficient (R2) |
| MB | S | 10 ppm, 100mL | 93.6 | 0.0252 | 30.08 | 0.98942 |
|  | P |  | 92.80 | 0.0204 | 33.96 | 0.96166 |
|  | M |  | 93.28 | 0.0024 | 30.86 | 0.99062 |
|  | A |  | 93.71 | 0.0231 | 29.98 | 0.98853 |
| MG | S |  | 66.83 | 0.0088 | 78.59 | 0.99745 |
|  | P |  | 68.26 | 0.0090 | 76.76 | 0.99692 |
|  | M |  | 44.57, | 0.0047 | 145.3 | 0.99776 |
|  | A |  | 60.72 | 0.0074 | 92.92 | 0.97471 |
| BCB | S |  | 57.27 | 0.00651 | 106.48 | 0.99072 |
|  | P |  | 47.16 | 0.00508 | 136.45 | 0.9883 |
|  | M |  | 41.98 | 0.00446 | 155.42 | 0.98367 |
|  | A |  | 58.28 | 0.00708 | 97.90 | 0.9831 |
| Rb171 | S |  | 46.74 | 0.00474 | 146.24 | 0.92729 |
|  | P |  | 41.38 | 0.00428 | 161.96 | 0.99695 |
|  | M |  | 70.37 | 0.00807 | 85.89 | 0.96279 |
|  | A |  | 54.16 | 0.00567 | 122.31 | 0.9466 |
| EY | S |  | 43.72 | 0.00472 | 146.8 | 0.99673 |
|  | P |  | 38.52 | 0.00382 | 181.5 | 0.98503 |
|  | M |  | 52.19 | 0.00551 | 125.8 | 0.99823 |
|  | A |  | 66.47 | 0.00506 | 136.9 | 0.96907 |
| CR | S |  | 50.52 | 0.0056 | 138.8 | 0.98555 |
|  | P |  | 42.58 | 0.0046 | 150.3 | 0.98211 |
|  | M |  | 37.33 | 0.0039 | 174.2 | 0.9369 |
|  | A |  | 56.07 | 0.0071 | 97.6 | 0.9397 |

Table 5. Comparative catalytic performance of plant fabricated ZnO nanostructure with reported research

| Photocatalyst size (nm) and shape | Source of Reducing / stabilizing, capping agent | Band gap (eV) | Pollutants & degradation (%) | Conc. of Pollutant /Volume of solution (mL) | Time (min) | Source of illumination | Kapp (min-1) | Half-life (t1/2) min | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cu2S, 17.77 nm Hexagonal | Chemical | 3.13 | RhB,53 | 5 ppm,50 mL | 180 | 70W mercury lamp | 0.0062 | 111.8 | 16 |
| FeO-MNPs 16.5, spherical | A. indica (leaf extract) | 3.27 | RY176 95.18 | 30 ppm/L pH=4 | 250 | 500 W Xenon lamp | 0.0212 | 3.26 | 17 |
| α-Fe2O3,32.50 nm spherical ZnO,37.50 triangular S P M A | Livistona chinensis S. cumuni P. guajava M. oleifera A. indica | 2.25 2.98 2.90 2.66 2.74 2.92 | MG, 68 MG, 79 MG,66.83 68.26 44.57, 60.72 | 10ppm, 100 mL 10ppm, 100mL | 90 120 | Visible light Open sunlight | 0.0109 0.0136 0.0088 0.0090 0.0047 0.0074 | 63.59 50.97 78.59 76.76 145.3 92.92 | 18 PW |
| CeO2 NPs S P M A | Aegle marmelos S. cumuni P. guajava M. oleifera S. cumuni | 2.90 2.66 2.74 2.92 | MB,98 MB ,93.6 92.80 93.28 93.71 | 10 ppm,50mL 10 ppm, 100mL | 180 120 | 500‐W lamp Open sunlight (OSL) | 0.2038 0.0252 0.0204 0.0024 0.0231 | 3.40 30.08 33.96 30.86 29.98 | 19 PW |
| ZnOW,23.6 nm Hexagonal | Water |  | CR ,70.04 | 50 ppm, 100mL | 60 | Solar light | 0.0132 | 52.51 | 22 |
| ZnO-SG, 50 nm HxR ZnO-PP,100nm HxW | chemical | 3.26 3.28 | Phenol,85 100 | 50 ppm | 120 | Solar Light photo radiometer (PMA2200 at 90 W/m2 ) | 0.0155 0.0312 | 44.72 22.21 | 23 |
| PVA/ZnO, ~70 | PVA | 3.09 | CV, 48 | 1mg/100mL | 90 | sunlight | 0.00694 | 100.4 | 24 |
| S P M A | S. cumuni P. guajava M. oleifera S. cumuni | 2.90 2.66 2.74 2.92 | CR ,50.52 42.58 37.33 56.07 | 10 ppm, 100mL | 120 | OSL | 0.0056 0.0046 0.0039 0.0071 | 138.8 150.3 174.2 97.6 | PW |
| ZnO,250-500 nm Nest like | NH4OH Hydrothermal | - | MB, 95.34 | 100ppm, 100 mL | 150 | UV-light. | 0.064 | 10.83 | 26 |
| Zn/Ag (1%) | chitosan | 3.22 | MB, 79.1 | 6.4 ppm, 100mL | 240 | Hg, lamp | 0.0067 | 103.5 | 29 |
| ZnO, spherical | egg white | 3.28 | MB, 100 | 10ppm, 50mL | 55 | 8 W, UV lamps | 0.158 | 0.158 | 30 |
| ZnO ,56 ,Hx W | Hylocereus polyrhizus | 3.36 | MB, 95 | 20ppm, 50mL | 120 | Sunlight | 0.0145 | 47.80 | 31 |
| ZnO, 40-60 nm spherical | Clerodendrum phlomidis | 3.1 | MB, 86 | 6.39 ppm, 20 | 60 | 500 W Xe lamp | ND | - | 33 |
| ZnO-J1, 20-40 | Hibiscus sabdariffa | 2.96 | MB, 97 | 15 ppm, | 150 | 500 W,UV lamp | 0.0182 | 38.08 | 34 |
| ZnO,32.8 nm HxW | Garcinia Cambogia | 3.24 | CV, 76 PR, 83 | 15ppm,30 mL | 90 120 | 25W, UV lamp | 0.011 0.0067 | 63.01 103.4 | 35 |
| ZnO, 42.23, Hx | Myristica fragrans | 3.29 | MB, 88 | 20 ppm, 45 | 140 | UV light | ND |  | 36 |
| ZnO,21, spherical; | Garcinia mangostana | 3.32 | MG, 99 | 10ppm ,50 mL | 180 | Solar light | 0.0245 | 28.29 | 38 |
| ZnO,19, spherical | Zizyphus jujuba | 3.36 | ECBT, 86 | 100ppm,15mL | 300 | Sunlight | 0.0067 | 103.4 | 39 |
| Al-ZnO, 50 nm tetrameric | Amomum longiligulare | ND | MG, 38.1 | 50μM, | 60 | UV light (CL-1000) | 0.008 | 86.65 | 40 |
|  |  |  | MB, 66 |  |  |  | 0.014 | 49.51 |  |
| ZnO, nano Flower | C.haematocephala | ND | MB, 88, | 20ppm,100mL | 270 | Solar light | 0.01 | 69.32 | 43 |
| ZnO,14 nm spherical | Brassica oleracea L | 4.09 | PR, 71 MB, 74 | 5x10-2 M 25 mL | 180 | 250 W He (Helium) lamp | 0.0066 0.0073 | 105.0 94.95 | 45 |
| ZnO,15.6 spherical | Phoenix roebelenii | 3.24 | MB,98 | 10 ppm | 105 | 250W ,UV lamp | 0.037 | 18.8 | 47 |
| ZnO, 10-20 nm spherical | Morinda umbellata | 2.75 | MG, 98.9 CR,92.8 | 20,10ppm,0.1L, at pH 10&6 | 90 | UV light | 0.0204 0.0123 | 33.98 56.35 | 48 |
| ZnO,20.17nm Flower like S P M A | H. hamnoides S. cumuni P. guajava M. oleifera S. cumuni | ND 2.90 2.66 2.74 2.92 | MG,89 EY,95 EY, 43.72 38.52 52.19 66.47 | 10 ppm 10 ppm 100 mL | 180 120 | UV OSL | ND 0.00472 0.00382 0.00551 0.00506 | - 146.8 181.5 125.8 136.9 | 50 PW |
| ZnO,20 nm cauliflower | Alchemilla vulgaris | 3.27 | RhB,75 | 10 ppm,80 mL | 120 | 500 W Xe lamp SHBC XSS-5XD | ND | - | 51 |
| ZnO pure ZnO-Cu(3%) | Synadium grantii | 3.10 3.20 | IC,26.5 IC,78.2 | 10 ppm, 100 mL | 80 | 30 W UV (254nm) | 0.0192 0.0301 | 36.10 23.02 | 52 |
| ZnO,19.31 | Epipremnum aureum | 3.73 | CR,56.6 | 10 ppm | 100 | UV | 0.014 | 49.51 | 53 |
| ZnO ,26.14 | Salvia officinalis | 2.96 | MO, 92.47 | 5 ppm,100mL | 120 | 500W Hg lamp | 0.02134 | 32.48 | 54 |
| ZnO ,11.35 nm | S. Cumini | 3.32 | MB,91.4 | 40ppm,50 mL | 180 | UV–vis | 0.004 | 173.3 | 55 |
| ZnF-CA-LP | P. guajava | - | MB, 96 | 5 ppm,50mL | 120 | UV lamp | 0.0165 | 42.01 | 57 |
| ZnO ,40.05 nm | M. oleifera | 3.02 | MB,80 | 3.2ppm,50 mL | 60 | 300 W, Halogen | 0.013 | 53.32 | 60 |
| gCN/ZnO (50%) M A | ZAD and Urea M. oleifera S. cumuni | 2.03 2.74 2.92 | Rb171,89.2 Rb171,70.4 54.16 | 10ppm,100mL | 140 120 | Sunlight OSL | 0.0150 0.00807 0.00567 | 46.21 85.89 122.3 | 71 PW |
| ZnO,9-18 | corriandrum sativum | ND | C14H10, 96 | 0.1ppm | 240 | 2 UV lamps,20W | 0.009 | 77.02 | 72 |
| Ag/ZnO sf | Hydrothermal | 3.09 | MO,99.7 RhB,99.3 | 10ppm,80mL at 8.8 and 8.7 pH | 35 | UV, Xenon lamp | 0.1104 0.0542 | 6.27 12.78 | 73 |
| ZnO (C3%),47 nm | Laser method | 3.30 | RhB, ≈13.8 | 9.58ppm, | 20 | Hg UV | 0.0074 | 93.5 | 74 |
| ZnO, 20-25 nm HxW | Chemical | ND | MO,99.7 CR,97.5 DB38,89.5 | 30ppm 50 mL | 30 | 1000-W UV lamp | 0.1578 0.1119 0.0803 | 4.39 6.19 8.63 | 75 |
| ZnO (disklike) | Sol gel, NH4OH |  | RhB,85.14 | ~4.8 ppm,20mL | 80 | 360 W, UV | 0.0431 | 16.08 | 76 |

a CR F3BS= coraleneredF3BS, RY =Reactive yellow, Hxw= Hexagonal wurtzite, AR27= Acid red 27, DB38=Direct blue, CV= crystal violet, Acid Blue 92, AB92, TY= Titan Yellow, AMP= acetaminophen, SDZ =sulfadiazine

OSL= open sunlight, RBB= Remazol Brilliant Blue, MOR=Mordenite