# Supplementary Information

# A Systematic Investigation into the Influence of Zeolite Framework Differences on the Catalytic Performance of Copper Sites in Ammonia Oxidation

# Sisi Deng a, Fuming Liu a, Shuqing Denga, Ruifeng Miao a, Changqiu Chen a, Dingding Liu a*.

a. Department of Environmental Science & Engineering, College of Chemical Engineering, Huaqiao University, Xiamen, Fujian 361021, China.

Section 1

Table S1. Physicochemical properties of proton and copper containing catalysts prepared in this study.

| Sample | IZA code | Pore topology | Pore size (A) | ICP elemental analysis Si/Al Cu(wt%) |  |
| --- | --- | --- | --- | --- | --- |
| H-BETA | BEA | 3D,12-ring | 6.5×6.7，5.6×5.6 | 20 |  |
| H-ZSM-5 | MFI | 3D,10-ring | 5.1×5.5，5.3×5.6 | 25 |  |
| H-SSZ-13 | CHA | 3D,8-ring | 3.8×3.8 | 20 |  |
| Cu/BETA |  |  |  | 20 | 1.90 |
| Cu-ZSM-5 |  |  |  | 25 | 1.74 |
| Cu-SSZ-13 |  |  |  | 20 | 1.94 |

Section 2

Table S2. The results of integrating the peak areas of Cu/SSZ-13, Cu/ZSM-5 and Cu/BETA catalysts by H2-TPR.

| Sample | Peak I | Peak II | Peak III |
| --- | --- | --- | --- |
| Cu/SSZ-13 | 0.044 | 0.037 | 0.047 |
| Cu/ZSM-5 | 0.036 | 0.047 | 0.030 |
| Cu/BETA | 0.030 | 0.035 | 0.023 |

Section 3

Fig. S1. XRD patterns of H-SSZ-13,H-BETA and H-ZSM-5.

Section 4

Fig. S2. The N2 selectivity of Cu-SSZ-13, Cu-ZSM-5, and Cu-BETA.

Section 5

Fig. S3. EDS results of the Cu/SSZ-13 (a-d), Cu/ZSM-5 (e-h), and Cu/BETA (i-l) catalysts.

Section 6

Fig. S4. In-situ infrared spectra of Cu/ZSM-5, Cu/BETA and Cu/SSZ-13 molecular sieves