Experimental section

Materials and reagents.

Deionized (DI) water was obtained by an 18 MΩ cm (SHRO-plus DI) system. Phosphate buffer solution (PBS) and bovine serum albumin (BSA) were purchased from Thermo-Fisher (USA). Polyvinyl pyrrolidone (MW: 10 000), iron (III) chloride hexahydrate (FeCl3·6H2O, 99%), ethylene glycol (EG), anhydrous sodium acetate (NaAc, 99%), Paraformaldehyde (PFA), 1, 1’-dioctadecyl-3, 3, 3’, 3’-tetramethylindocarbocyanine perchlorates (Dil), and cell counting kit-8 (CCK-8) were obtained from Sigma-Aldrich (USA). Sulfur powder (S, 99%) was obtained from Shanghai Rongtai Pharmatech Co., Ltd. JC-1 Mitochondrial Membrane Potential Assay Kit was purchased from Yeasen Biotechnology (Shanghai) Co., Ltd. The γ-H2AX antibody was purchased from Abcam Company. The other reagents used in this work were purchased from Sinopharm Chemical Reagent (China) and Aladdin-Reagent (China).

Preparation of pyrite nanozymes (FeS2).

The pyrite nanozymes with a size of 151 nm were prepared by a one-pot solvothermal method(1). In a typical synthesis, 0.7 g of PVP was dispersed into 30 mL of EG solution, and then 0.5 g of FeCl3·6H2O was added under

constant magnetic stirring. Next, 3.6 g of NaAc was added into above mixture under vigorous stirring. After that, 0.4 g of S powder was added, and the resultant mixture was ultrasonicated for 1 h to form a homogeneous dispersion. Then, the reaction mixture was transferred into a 40 mL Teflon-lined stainless-steel autoclave, which was sealed and maintained at 473 K for 12 h. After the reaction was cooled to room temperature naturally, the resultant black precipitates were collected by centrifugation at 10 000 rpm for 10 min. Then, the collected black products were washed with CHCl3 to remove the excess S and using absolute alcohol and ultrapure water several times to remove impurities. After centrifugation, the products were dried in a vacuum lyophilizer overnight for further characterization.

Preparation of cancer exosome (CDE) biomimetic FeS2 nanoparticles (CF). The pure CDE were prepared according to the standard protocol of Exosome Isolation Reagent (RIBOBIO biotechnology co. LTD, China)(2). For CF preparation, 4T1 cancer cells were cultured for 3 days and then the growth medium was rinsed out, replaced with fresh medium containing 1mg FeS2 and incubated for 2 days at 37 °C and 5% CO2 atmosphere. Then the medium was replaced by the fresh medium without FBS and the cells were incubated at 37 °C and 5% CO2 atmosphere for another 2 days. Then all the supernatant was collected and centrifuged at 1125 g for 5 min to eliminate the cells and debris. The CF in supernatant isolated by centrifuged at 10000 rpm for 5 min. CF was stored at 4℃ for further use.

Preparation of erythrocyte membranes biomimetic FeS2 nanoparticles (RF).

The red blood cell-vesicles were obtained by using low-osmosis method(3). The RF were obtained by using an extrusion method(4). Briefly, 0.1 mg of CF were mixed with 1 mg of red blood cell-vesicles, which were quantified by lyophilization and extruded through 100 nm polycarbonate membranes.

The RF were stored in PBS at 4 °C for the following experiments.

Characterization of prepared formulations.

XRD was measured on a D8 Advance (Bruker-AXS, Germany). The morphology of nanoparticles (NPs) was observed by TEM (JEM-2010HT, Japan) at an accelerating voltage of 120 keV. The hydrodynamic diameter and zeta potential of nanoparticles suspended in 1 × PBS or FBS were measured by dynamic light scattering (DLS) (Nano-Zen 3600, Malvern Instruments, and UK). UV/vis-NIR spectrophotometer (UV-3600, Shimadzu, Japan) was used to measure the light absorption spectrum.

Western blotting for the key proteins in CDE and CF.

The CDE and CF were lysed in RIPA lysis buffer and then subjected to western blot analysis. The primary antibodies used included anti-CD63 (Abcam, ab216130) and anti-CD9 (Santa Cruz, SC-7964). All primary antibodies were diluted to 1:2000.

Cell lines and animal model.

4T1 mouse breast cancer cell lines was provided by the College of Life Science of Wuhan University. All the cells were cultured in the standard cell medium recommended by American Type Culture Collection. Female BALC/c mice aged 4-5 weeks were purchased from Vital River Company (Beijing, China). 1×106 4T1 cells suspended in 100 μL PBS were subcutaneously injected into each mouse to establish the tumor models. After the tumor volume reached around 200 mm3, the tumor bearing mice were used for further experiments. The animal experiments were carried out according to the protocol approved by the Ministry of Health in the People’s Republic of PR China and were approved by the Administrative Committee on Animal Research of the Wuhan University.

In vitro tumor-specific uptake.

At first, Dil labeled CF and RF (Containing100 μg/mL FeS2) were incubated with 4T1 cells for 2 h at 37 °C. The cells were then washed with PBS several times, fixed with PFA for 30 min at room temperature, stained with Lyso-Tracker Green and then imaged by using a fluorescence microscope (IX81, Olympus, Japan). The fluorescence intensity was measured by IamgeJ software.

In vitro Immune Evasion Study

RAW 264.7 were seeded in 12-well plates and cultured for 12 h. Different concentrations of FeS2 and CF (i.e., FeS2 dose of 25, 50, and 100 mg/mL) were added the medium, and the cells grown without any particles were used as control. Then the cells were washed three times and then incubated for 4 h at 37 ℃, 5% CO2, and then washed with PBS three times. To quantify nanoparticle uptake, 1 mL aqua regia was added to the cells. The mixture was left at room temperature for 12 h, followed by annealing at 70 ℃ for 6 h to remove the acids. The sample was then resuspended with 1 mL DI water and the Fe content in each sample was determined by using an inductively coupled plasma-atomic emission spectrometer (ICP-AES; iris Intrepid II XSP, Thermo Elemental, United States).

γ-H2AX immunofluorescence analysis.

4T1 cells were seeded in 24-well plates and then cultured for 24 h at 37 °C under hypoxia condition. Then the cells were treated with 1) Control (PBS); 2) Radiotherapy (RT, 2Gy); 3) RF+RT; 4) High dose RT (6Gy); 5) CF+RT. The FeS2 concentration was 200 μg/mL in groups 3, and 5. After RT treatment for 2 h, the cells were fixed with 4% paraformaldehyde for 10 min, rinsed with PBS, permeabilized with methanol for 15 min at -20 °C and then rinsed with PBS again. Then the cells were exposed to a blocking buffer (1% bovine serum albumin (BSA) in PBS solution) for 1 h at room temperature and further incubated with anti- phospho-histone γ-H2AX mouse monoclonal antibody (dilution 1:500) overnight at 4 °C. After washing with PBS, the cells were incubated with Cy5-conjugated sheep anti-mouse secondary antibody (dilution 1:500) for 1 h at room temperature. Excess antibody was removed by rinsing the coverslips in PBS. Cell nuclei were stained by DAPI for 5 min at room temperature. The cells were imaged via confocal fluorescence microscopy (IX81). Quantitative analysis of γ-H2AX foci density (foci/100 μm2) was performed by automatic counting using the ImageJ software for n = 100 cells in each treatment group.

JC-1 mitochondrial membrane potential assay

For the JC-1 assay, 4T1 cells were co-incubated with five different groups: 1) Control (PBS); 2) Radiotherapy (RT, 2Gy); 3) RF+RT; 4) High dose RT (6Gy); 5) CF+RT. The cells were stained with JC-1 for 30 min before washing with PBS. Then, the mitochondrial damage/disruption was detected by fluorescence microscopy (IX81).

GSH depletion activity of CF

The GSH depletion activity assay was carried out employing DTNB as a probe, which can react with thiol groups (−SH) in GSH to produce a yellow product with maximal absorption at 412 nm. All the experiments need to be examined in the dark because GSH is easily oxidized in light. Specifically, different formulations reacted with GSH solution (0.4 mM) in 0.2 M HAc−NaAc buffer (pH 4.5). Subsequently, the nanoparticles were separated by centrifugation. The supernatants were added with DTNB (0.2 mM) solution to react thoroughly. The mixture was detected for the absorbance of 412 nm.

Clonogenic assay.

4T1 cells were seeded in 6-well plates with a different amount (125, 250, 500, 1000 and 2000) per well and incubated at 37 ℃ for 24 h Then the cells were treated with five groups: 1) Control (PBS); 2) Radiotherapy (RT, 2Gy); 3) RF+RT; 4) High dose RT (6Gy); 5) CF+RT. The FeS2 concentration was 200 μg/mL in groups 3, and 5. After that, cells were washed with PBS and fresh medium was replaced every three days for 10 days. The colonies were fixed by 4% paraformaldehyde and then stained with Giemsa dye. Only colonies containing at least 50 cells were counted. At last, an evaluation of the effects of different treatments was conducted by counting the survival fraction of the colonies. Each treatment was performed in triplicate.

In vivo pharmacokinetics, and distribution study

24 BALB/c mice bearing 4T1 tumor xenografts (n = 3) received an intravenous (i.v.) injection of 100 μL PBS containing FeS2, RF, or CF at the concentration of 2.5 mg Fe/kg. At various time points after the injection (i.e.,0, 1, 2, 4, 6, 12, 24, and 48 h), 20 μL blood was collected from the tail veins, treated with aqua regia, and then on heated at 70 °C until to obtain clear solutions. And the resultant mixture was left standing still at room temperature for 12 h and then kept in oil bath at 70 °C for 6 h to remove acids, yielding samples for Fe content quantification by using an ICP-AES (iris Intrepid II XSP, Thermo Elemental, USA). To study the biodistribution of particles in various organs, at 24 h after the injection, all mice were euthanized and their hearts, livers, spleens, kidneys, lungs, and tumors were carefully collected, weighted, and finally quantitatively analyzed with ICP-AES as described above.

In vivo antitumor study.

1×106 4T1 cells suspended in 100 μL PBS were subcutaneously injected into each mouse to establish the tumor models. When tumor size reached approximately 200 mm3, the mice were divided randomly into 5 groups (each group included 5 mice): 1) Control (PBS); 2) Radiotherapy (RT, 2Gy); 3) RF+RT; 4) High dose RT (6Gy); 5) CF+RT. The FeS2 dose was 5mg/kg in groups 3 and 5. The treatment was conducted every 4 days for 16 days. Mice body weight and tumor volume in all groups were monitored every 2 days. A caliper was employed to measure the tumor length and tumor width and the tumor volume was calculated according to the following formula. Tumor volume = tumor length × tumor width 2 / 2. After 16 days of treatment, all the mice were sacrificed. Their blood samples and major organs (i.e., hearts, livers, spleens, lungs, and kidneys) were collected. Three important hepatic indicators (i.e., ALT: alanine aminotransferase, AST: aspartate aminotransferase, and ALP: alkaline phosphatase) and two indicators for kidney functions (i.e., BUN: blood urea nitrogen and CRE: creatinine) were measured by using a blood biochemical autoanalyzer (7080, HITACHI, Japan). And the tumor tissues were weighed, and fixed in 4% neutral buffered formalin, processed routinely into paraffin, and sectioned at 4 μm. Then the sections were stained with hematoxylin and eosin (HE) and TUNEL staining and finally examined by using an optical microscope (BX51, Olympus, Japan). Part of their organs were stained with H&E and examined as described above.

Statistical analysis.

Data analyses were conducted using the GraphPad Prism 5.0 software. Significance between every two groups was calculated by the Student’s t-test. *P < 0.05, **P < 0.01, ***P < 0.005.

Figure S1. Nanoparticle uptake by RAW 264.7 cells at different incubated concentration (FeS2 dose of 25, 50 and 100 μg/mL)

1.	X. Meng, D. Li, L. Chen, H. He, Q. Wang, C. Hong, J. He, X. Gao, Y. Yang, B. Jiang, G. Nie, X. Yan, L. Gao and K. Fan: High-Performance Self-Cascade Pyrite Nanozymes for Apoptosis-Ferroptosis Synergistic Tumor Therapy. ACS Nano (2021) doi:10.1021/acsnano.1c01248

2.	D. Zhu, M. Lyu, Q. Huang, M. Suo, Y. Liu, W. Jiang, Y. Duo and K. Fan: Stellate Plasmonic Exosomes for Penetrative Targeting Tumor NIR-II Thermo-Radiotherapy. ACS Appl. Mater. Interfaces, 12(33), 36928-36937 (2020) doi:10.1021/acsami.0c09969

3.	D. M. Zhu, W. Xie, Y. S. Xiao, M. Suo, M. H. Zan, Q. Q. Liao, X. J. Hu, L. B. Chen, B. Chen, W. T. Wu, L. W. Ji, H. M. Huang, S. S. Guo, X. Z. Zhao, Q. Y. Liu and W. Liu: Erythrocyte membrane-coated gold nanocages for targeted photothermal and chemical cancer therapy. Nanotechnology, 29(8), 084002 (2018) doi:10.1088/1361-6528/aa9ca1

4.	D. Zhu, M. Lyu, W. Jiang, M. Suo, Q. Huang and K. Li: A biomimetic nanozyme/camptothecin hybrid system for synergistically enhanced radiotherapy. J Mater Chem B, 8, 5312-5319 (2020) doi:10.1039/d0tb00676a