Supplementary Material:

A ZIF-8 Derived Nano-Porous Carbon as Solid Transducing Layer in High-Performance All-Solid-State Sodium Ion Selective Electrodes

Peike Wang1,2,† · Shuheng Fan1,2,† · Haipeng Liu1,2 · Shiqiang Zhou1,2 · Jingjing Luo1,2 · Yuan Meng1,2 · Jin Ning1,2 · Suzhu Yu1,2 · Jun Wei1,2,3

E-mail: 
Suzhu Yu

szyu@hit.edu.cn

Jun Wei

junwei@hit.edu.cn

1 Shenzhen Key Laboratory of Flexible Printed Electronics Technology, Harbin Institute of Technology (Shenzhen), Shenzhen 518055, China

2 School of Materials Science and Engineering, Harbin Institute of Technology (Shenzhen), Shenzhen 518055, China

3 State Key Laboratory of Advanced Welding and Joining, Harbin Institute of Technology (Shenzhen), Shenzhen 518055, China

†These authors contributed equally to this work.

Fig. S1. XRD spectrum of ZIF-8 ZIF-8 template.

Fig. S2. XRD spectrum of (a) graphene and (b)MWCNTs.

Fig. S3. Raman spectrum of (a) graphene and (b) MWCNTs.

Fig. S4. Pore size distribution curve of the NPC.

Fig. S5. C 1s and O 1s XPS spectra of (a, b) graphene and (c, d) MWCNTs, respectively

Fig. S6. FTIR spectra of (a) graphene and (b) MWCNTs.

Fig. S7. CV curves of (a) NPC, (b) graphene and (c) MWCNT at different scan rates. GCD curves of (d) NPC, (e) graphene and (f) MWCNT at different current densities.

Table S1. XPS results

| Samples | C (at.%) | N (at.%) | O (at.%) |
| --- | --- | --- | --- |
| MWCNT | 97.6 | 0 | 2.4 |
| Graphene | 90.1 | 0 | 9.9 |
| NPC | 89.1 | 7.6 | 3.0 |

Table S2. Comparison of the Calculated Sensitivity Results of manufactured Sensors

| Sensors | Sensitivity (mV·dec−1) | Range (M) | R2 |
| --- | --- | --- | --- |
| Bare GCE | 32.9 | 10−2.3~10−1 | 0.79959 |
| MWCNT | 59.85 | 10−4.5~10−1 | 0.9865 |
| Graphene | 61.21 | 10−4.8~10−1 | 0.98688 |
| NPC | 64.11 | 10−4.7~10−1 | 0.96462 |

Table S3. Comparison of the solid transducing layers reported in previous publications

| SC | Support | Target ion | Sensitivity (mV·dec−1) | Range (M) | Ref. |
| --- | --- | --- | --- | --- | --- |
| CNT | CNT | Na+ | 56 ± 3 | 7×10–7~1 | [1] |
| Graphene | Carbon | Na+ | 60.2 ± 0.9 | 1×10−6~1 | [2] |
| CB | SPE | Na+ | 58 ± 3 | 1×10−7~1 | [3] |
| 3DOMC | Ni mesh | K+ | 56.4 | 1.6×10-7~1 | [4] |
| PC-SMSs | GCE | K+ | 57.8 | 1×10−6~1 | [5] |
| Fullerenes | GCE | K+ | 55 | - | [6] |
| NPC | GCE | Na+ | 64.11 | 10-4.7~10-1 | This work |

CNT: carbon nanotube; CB: carbon black; SPE: screen-printed electrode; 3DOMC: three-dimensionally ordered microporous carbon; GCE: glassy carbon electrode; PC-SMSs: porous carbon sub-microns.