Supporting Information:

Sustainable biosorption of Methylene Blue using highly-efficient activated Mediterranean macroalgae: a comparative mechanistic study

Ali Jaber,1 Loubna Bitar,2 Mohammad Mazloum,1 Leila Ghannam,3 Walid Malaeb,1 Ali Yassin*1 and Ahmad Houri*1

1 Department of Physical Sciences, School of Arts and Sciences, Lebanese American University, Beirut 1102-2801, Lebanon

2 RDMPN Laboratory, Faculty of Pharmacy, Lebanese University, Beirut BP 14/6573, Lebanon

3 Department of Chemistry and Biochemistry, Faculty of Science I, Lebanese University, Hadath, Beirut, Lebanon

* Correspondence to: (A.H) ahouri@lau.edu.lb, (A.Y) ali.yassin02@lau.edu.lb

Table S1. Effect of initial concentration on the % removal efficiency of MB, at initial pH: 5.0, with 100 mg/L biomass of Ulva Lactuca, Ulva Prolifera, Bryopsis, and Corallina treated with CaCl2.

| [MB] mg/L | Ulva Lactuca | Ulva Prolifera | Bryopsis | Corallina |
| --- | --- | --- | --- | --- |
|  | % R | % R | % R | % R |
| 1.25 | 73.1 | 97.9 | 88.63 | 78.33 |
| 5 | 82.45 | 98.04 | 90.34 | 89.33 |
| 10 | 87.76 | 98.52 | 88.5 | 90.78 |
| 20 | 94.53 | 95.7 | 90.72 | 93.24 |
| 80 | 97.25 | 97.53 | 94.19 | 94.34 |
| 120 | 97.72 | 97.89 | 94.11 | 94.87 |
| 180 | 96.12 | 97 | 85.61 | 84.98 |
| 220 | 97.59 | 98.17 | 86.96 | 86.74 |
| 260 | 97.4 | 97.23 | 81.83 | 83.67 |
| 300 | 97.42 | 91.22 | 83.34 | 85.03 |
| 600 | 93.17 | 94.117 | 45.69 | 62.58 |
| 900 | 94.83 | 95.92 | 24.74 | 42.42 |

Table S2. Effect of contact time on the removal efficiency (%) of MB: Ulva Lactuca, Ulva Prolifera, Bryopsis, and Corallina treated with CaCl2, with initial solution pH:5.0, MB concentration:10 mg/L, time taken at 5, 10, 15, 25, 30, 60, 90, and 120 min.

| time (min) | Ulva Lactuca | Ulva Prolifera | Bryopsis | Corallina |
| --- | --- | --- | --- | --- |
|  | + CaCl2 | +CaCl2 | +CaCl2 | +CaCl2 |
|  | %R | %R | %R | %R |
| 0 | 0 | 0 | 0 | 0 |
| 5 | 62.1 | 63 | 94.8 | 46.8 |
| 10 | 66.8 | 71.4 | 95.5 | 55.9 |
| 15 | 71.4 | 73.9 | 96.4 | 64.2 |
| 25 | 71.9 | 75.3 | 96.2 | 65.4 |
| 30 | 71.4 | 93.4 | 86.9 | 89.8 |
| 60 | 70.5 | 94.2 | 87.1 | 90.9 |
| 90 | 70.7 | 97.6 | 88.8 | 90.9 |
| 120 | 70.3 | 97.1 | 88.6 | 92 |

(a)

(b)

(c)

(d)

Figure S1. Langmuir and Freundlich Isotherm models for the MB biosorption: (a) Ulva Lactuca +CaCl2, (b) Ulva Prolifera +CaCl2, (c) Bryopsis +CaCl2, (d) Corallina +CaCl2 ; initial solution pH:5; algae dosage: 100 mg/L; Time: 120 min.

Table S3. Kinetic parameters estimated by a) the pseudo-first-order, b) pseudo-second-order and c) intra-particle diffusion for MB biosorption on to Ulva Lactuca, Ulva Prolifera, Bryopsis and Corallina treated with CaCl2.

(a)

| Algae Model | Pseudo-first order |  |  |
| --- | --- | --- | --- |
|  | K1 | Qe | R2 |
|  | (1/min) | (mg/g) |  |
| Ulva Lactuca + CaCl2 | 0.6126 | 2.8284 | 0.99997 |
| Ulva Prolifera + CaCl2 | 0.1132 | 3.8562 | 0.99984 |
| Bryopsis + CaCl2 | 0.1393 | 3.5292 | 0.99995 |
| Corallina + CaCl2 | 0.1375 | 3.653 | 0.9997 |

(b)

| Algae Model | Pseudo-second order |  |  |
| --- | --- | --- | --- |
|  | K2 | Qe | R2 |
|  | (g/mg.min) | (mg/g) |  |
| Ulva Lactuca + CaCl2 | 1.02613 | 2.8285 | 0.9988 |
| Ulva Prolifera + CaCl2 | 0.1392 | 3.9427 | 0.9986 |
| Bryopsis + CaCl2 | 0.3212 | 3.5685 | 0.9998 |
| Corallina + CaCl2 | 0.33215 | 3.6893 | 0.9999 |

(c)

| Algae Model | Intraparticle Diffusion |  |  |
| --- | --- | --- | --- |
|  | Kid | C | R2 |
|  | (mg/g.min) | (mg/L) |  |
| Ulva Lactuca + CaCl2 | 0.0186 | 1.1438 | 0.8249 |
| Ulva Prolifera + CaCl2 | 0.02648 | 1.46948 | 0.8294 |
| Bryopsis + CaCl2 | 0.0239 | 1.3781 | 0.8277 |
| Corallina + CaCl2 | 0.0246 | 1.4289 | 0.8275 |

(a)

(b)

(c)

(d)

(e)

Figure S2. a, b, c, and d) pseudo-first-order, and pseudo-second-order, and (e) intra-particle diffusion, kinetic models for the MB biosorption (Ulva Lactuca, Ulva Prolifera, Bryopsis and Corallina treated with CaCl2): initial solution pH: 5, algae dosage: 100 mg/L, MB concentration: 10 mg/L.

qt = qe (1- e (K1.t))				(1)

qt = qe2 x k2 x t/1+ qe x k2 x t		(2)

The parameters of pseudo-first-order and pseudo-second-order kinetic models are defined as follows: qt (mg/g): the amount of MB adsorbed by algae at time t, K1 (1/min): the constant of the pseudo-first-order model, t (min): time, and K2 (g/mg.min): the rate constant of the pseudo-second-order model.

Qt = Kid x t 0.5 + C                               (3)

Where qt (mg/g) is the amount of MB sorbed at time t, C is the intercept (that corresponds to the exponential phase when resistance to film diffusion contributes to controlling uptake kinetics), and Kid (mg/g.min0.5 ) is the intra-particle diffusion rate constant.