# 7. Appendix

Table A1: List of gun tilt angle, average power, and average discharge voltage (Vd) used in the four depositions.  A zero degree angle indicates that the sputter gun has been tilted away from factory setting and points down to the bottom of the chamber to decrease rate of deposition for associated species.  Discharge voltages are averages obtained from the Lesker datalog recorded during deposition (values obtained every 1 sec).

| Deposition ID | Gun tilt angles for Pt:Au (deg) | Sputter Power to Pt (Watts) | Sputter Power to Au (Watts) | Vd for Pt (Volts) | Vd for Au (Volts) |
| --- | --- | --- | --- | --- | --- |
| 1 | 20:0 | 150 | 50 | 432 | 311 |
| 2 | 20:20 | 100 | 100 | 399 | 352 |
| 3 | 20:20 | 150 | 50 | 430 | 311 |
| 4 | 0:20 | 50 | 150 | 376 | 340 |