Supplementary Information

Intact metal/metal halide van der Waals junction enables reliable memristive switching with high endurance

Joo-Hong Lee1,†, June-Mo Yang2,†, So-Yeon Kim2, Sungpyo Baek1, Sungjoo Lee1, Sung-Joon Lee3,*, Nam-Gyu Park2,*, Jin-Wook Lee1,*

1SKKU Advanced Institute of Nanotechnology (SAINT) and Department of Nanoengineering, Sungkyunkwan University, Suwon 16419, Republic of Korea.

2School of Chemical Engineering, Sungkyunkwan University, Suwon 16419, Republic of Korea.

3U.S. Naval Research Laboratory, Washington, DC 20375, United States.

†These authors contributed equally to this work.

*Corresponding authors:

S.-J.L. email: sungjoon.lee.ctr.ks@nrl.navy.mil

N.-G.P. email: npark@skku.edu

J-W.L. email: jw.lee@skku.edu

This supplement contains

Supplementary Figures 1-14

Supplementary Tables 1-4

Supplementary Fig. 1 | Photoluminescence emission spectra of FAPbI3 film annealed at 110 ℃ for 10 min.

Supplementary Fig. 2 | a-f, X-ray photoelectron spectroscopy (XPS) data of bare FAPbI3 film and the film after peeling off the EVC. Wide range XPS (a) and high resolution XPS spectra of C 1s (b), Ag 3d (c), Pb 4f (d), I 3d (e), and N 1s (f).

Supplementary Fig. 3 | a, Ultraviolet photoelectron spectroscopy (UPS) data of the bare δ-FAPbI3 film and the film after peeling off the EVC (EVC-off). b, A Tauc plot of the δ-FAPbI3 film. c, Energy band structure of the bare δ-FAPbI3 film and EVC-off film determined from the UPS data.

Supplementary Fig. 4 | a,b, Schematics of switching mechanism in the memristors based on EVC (a) and vdWC (b).

Supplementary Fig. 5 | a,b, Space charge limited current measurement of the devices with the ITO/FAPbI3/Au structure based on EVC (a) and vdWC (b). c, A Box plot of the trap filling voltage (VTFL) extracted from 20 different cells for each condition. d,e, Optical microscopy images of the Au EVC (d) and vdWC (e).

Supplementary Fig. 6 | A ln(I/T2)-1000/T plot of FAPbI3 memristors based on EVC and vdWC in HRS region with different applied voltage. Filled symbols are measured data and dashed lines are linear fitting of the data.

Supplementary Fig. 7 | a,b, Optical microscopy images of the EVC devices on different substrates in a same batch. The devices with intensive reaction between the EVC and FAPbI3 (a). and the devices with the relatively less reaction (b). c, The I-V characteristics of the intensely reacted EVC devices.

Supplementary Fig. 8 | Box plot of the forming voltages obtained from 30 different devices in 3 different batches based on the EVC and vdWC.

Supplementary Fig. 9 | a,b, X-ray diffraction patterns of fresh and aged (10 days) FAPbI3 memristors based on EVC (a) and vdWC (b).

Supplementary Fig. 10 | a,b, Optical microscopy images of FAPbI3 memristors based on EVC (a) and vdWC (b) with different aging times.

Supplementary Fig. 11 | a, Current-voltage (I-V) characteristics of the EVC device with relatively less reaction between the EVC and FAPbI3 layer measured at various temperature from 296 K to 356 K. Optical microscopy images of different spots in a single substrate. b,c, Optical microscopy images of thermally unstable devices (b) and stable devices (c).

Supplementary Fig. 12 | The retention measurement of the FAPbI3 memristors based on vdWC.

Supplementary Fig. 13 | Multi-level switching ability of FAPbI3 memristor based on vdWC measured by changing the compliance current (CC). a, Current-voltage (I-V) characteristics of the device. b, Retention property of the multi-level storage capability with corresponding CC.

Supplementary Fig. 14 | a,b, log(I)-log(V) plot with linear fitting lines for the forming scan of Cs3Cu2I5 memristors based on EVC (a) and vdWC (b).

Supplementary Table 1 | Statistical parameters of the operating voltage measured from 350 cells in the same batch

| Condition | Voltage | Mean(V) | Median(V) | Max(V) | Min(V) | Std(V) |
| --- | --- | --- | --- | --- | --- | --- |
| EVC | Forming | 0.27 | 0.26 | 0.42 | 0.17 | 0.051 |
|  | Set | 0.19 | 0.19 | 0.34 | 0.10 | 0.050 |
|  | Reset | -0.20 | -0.20 | -0.080 | -0.45 | 0.060 |
| vdWC | Forming | 0.36 | 0.37 | 0.54 | 0.21 | 0.049 |
|  | Set | 0.16 | 0.15 | 0.29 | 0.10 | 0.036 |
|  | Reset | -0.23 | -0.24 | -0.090 | -0.38 | 0.060 |

Supplementary Table 2 | Statistical parameters of the forming voltage measured from 30 cells each in three different batches

| Condition | Batch | Mean(V) | Median(V) | Max(V) | Min(V) | Std(V) |
| --- | --- | --- | --- | --- | --- | --- |
| EVC | 1 | 0.31 | 0.31 | 0.40 | 0.22 | 0.041 |
|  | 2 | 0.26 | 0.25 | 0.39 | 0.18 | 0.062 |
|  | 3 | 0.31 | 0.33 | 0.42 | 0.18 | 0.049 |
| vdWC | 1 | 0.37 | 0.37 | 0.45 | 0.29 | 0.036 |
|  | 2 | 0.41 | 0.41 | 0.52 | 0.34 | 0.041 |
|  | 3 | 0.42 | 0.42 | 0.5 | 0.33 | 0.045 |

Supplementary Table 3 | Statistical parameters of the set voltage measured from 30 cells each in three different batches

| Condition | Batch | Mean(V) | Median(V) | Max(V) | Min(V) | Std(V) |
| --- | --- | --- | --- | --- | --- | --- |
| EVC | 1 | 0.17 | 0.15 | 0.28 | 0.11 | 0.050 |
|  | 2 | 0.16 | 0.16 | 0.28 | 0.07 | 0.052 |
|  | 3 | 0.19 | 0.18 | 0.3 | 0.1 | 0.053 |
| vdWC | 1 | 0.17 | 0.17 | 0.23 | 0.10 | 0.035 |
|  | 2 | 0.17 | 0.17 | 0.21 | 0.13 | 0.023 |
|  | 3 | 0.17 | 0.17 | 0.22 | 0.11 | 0.029 |

Supplementary Table 4 | Statistical parameters of the reset voltage measured from 30 cells each in three different batches

| Condition | Batch | Mean(V) | Median(V) | Max(V) | Min(V) | Std(V) |
| --- | --- | --- | --- | --- | --- | --- |
| EVC | 1 | -0.22 | -0.21 | -0.1 | -0.42 | 0.075 |
|  | 2 | -0.24 | -0.24 | -0.08 | -0.38 | 0.067 |
|  | 3 | -0.25 | -0.23 | -0.16 | -0.43 | 0.071 |
| vdWC | 1 | -0.24 | -0.24 | -0.11 | -0.33 | 0.048 |
|  | 2 | -0.22 | -0.22 | -0.13 | -0.34 | 0.051 |
|  | 3 | -0.22 | -0.24 | -0.1 | -0.41 | 0.078 |