Supplementary Information for

Bright and stable Cr3+-activated protoenstatite near-infrared emitter

Lei Zhonga, Yuefei Xianga, Zhe Wua, Junfu Tanga, Shidan Raoa, Chunyan Jianga,b*, Lei Zhoua,c*, Xiaojun Wangd, Mingmei Wua

a Zhuhai Key Laboratory of Optoelectronic Functional Materials and Membrane Technology, School of Chemical Engineering and Technology, Sun Yat-sen University, Zhuhai 519082, China

b Centre for Optical and Electromagnetic Research, Guangdong Engineering Research Centre of Optoelectronic Intelligent Information Perception, South China Academy of Advanced Optoelectronics, South China Normal University, Guangzhou 510006, China

c Southern Marine Science and Engineering Guangdong Laboratory (Zhuhai), Sun Yat-sen University, Zhuhai 519082, China

d Department of Physics, Georgia Southern University, Statesboro, GA 30460, USA

* Corresponding authors: jiangchy0119@m.scnu.edu.cn (C. Jiang); zhoul8@mail.sysu.edu.cn (L. Zhou)

Supplementary Fig. 1 a XRD patterns under different doping conditions. b XRD patterns of single-doped sample before and after aging. c XRD patterns of Cr3+, Li+ co-doped sample before and after aging.

Supplementary Fig. 2 XRD Rietveld refinement plot of MgSiO3:x%Cr,Li.

Supplementary Fig. 3 XPS spectrum of MgSiO3:Cr,Li.

Supplementary Fig. 4 a SEM image and b energy dispersive spectrum of MgSiO3:Cr,Li.

Supplementary Fig. 5 Diffuse reflection spectra MgSiO3:x%Cr,Li.

Supplementary Fig. 6 Determination of the optical band gap.

Supplementary Fig. 7 a-f Deconvolution plots of the PL spectra of MgSiO3:x%Cr,Li upon 450 cm excitation.

Supplementary Fig. 8 a Decay curves of MgSiO3:x%Cr,Li monitoring the emission of Cr1 at room temperature. b Average decay time of MgSiO3:x%Cr,Li.

Supplementary Fig. 9 Decay curve of MgSiO3:0.25%Cr,Li and MgSiO3:2%Cr,Li at 83 K.

Supplementary Fig. 10 IQE, AE, and EQE for MgSiO3:x%Cr,Li.

Supplementary Fig. 11 Dq/B and Mg1–O bond length with difference Cr3+ doping concentration.

Supplementary Fig. 12 a-h XRD Rietveld refinement of MgSiO3: Cr,y%Li.

Supplementary Fig. 13 The Calculated formation energies for the four models. Model 1: Cr→Mg2 + Li→Mg2; model 2: Cr→Mg2 + Li→Mg1; model 3: Cr→Mg1 + Li→Mg2; model 4: Cr→Mg1 + Li→Mg1.

Supplementary Fig. 14 Bond length of Mg–O of MgSiO3:Cr,y%Li versus Li+ content.

Supplementary Fig. 15 EPR spectra of MgSiO3:x%Cr,y%Li measured at room temperature.

Supplementary Fig. 16 XRD patterns after 7 days of immersion in different liquids.

Supplementary Fig. 17 Thermal images of NIR pc-LED device at different driving currents.

Supplementary Fig. 18 a Driven current-dependent emission spectra of the fabricated NIR pc-LED. The inset shows a photograph of the fabricated pc-LED device on a fingertip. b Electro-optical conversion efficiency and blue-to-NIR light conversion efficiency versus driving currents. c Output powers versus driving currents.

Supplementary Table 1 Rietveld refinement structural data of MgSiO3:x%Cr,Li.

|  | x = 0.25 | x = 0.5 | x = 1 | x = 1.5 | x = 2 | x = 2.5 |
| --- | --- | --- | --- | --- | --- | --- |
| a (Å) | 9.2563 | 9.2545 | 9.2521 | 9.2494 | 9.2468 | 9.2449 |
| b (Å) | 8.7474 | 8.7461 | 8.7440 | 8.7418 | 8.7390 | 8.7366 |
| c (Å) | 5.3213 | 5.3209 | 5.3203 | 5.3193 | 5.3186 | 5.3182 |
| V (Å3) | 430.8574 | 430.6828 | 430.4105 | 430.1032 | 429.7854 | 429.5440 |
| Rwp (%) | 12.5 | 10.9 | 10.3 | 10.1 | 9.63 | 9.39 |
| Rp (%) | 8.09 | 7.29 | 6.96 | 7.01 | 6.48 | 6.23 |
| χ2 | 2.57 | 1.89 | 1.72 | 1.62 | 1.54 | 1.51 |

Supplementary Table 2 The atom positions, fraction factors, and thermal vibration parameters of MgSiO3:Cr,y%Li.

| Atom (y = 4) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.26441 | 0.25000 | 1 | 7.271 |
| Mg2 | 4c | 0.00000 | 0.09690 | 0.75000 | 1 | 5.906 |
| Si1 | 8d | 0.29488 | 0.09156 | 0.07063 | 1 | 7.187 |
| O1 | 8d | 0.11775 | 0.09248 | 0.07618 | 1 | 5.541 |
| O2 | 8d | 0.37637 | 0.25540 | 0.07530 | 1 | 6.396 |
| O3 | 8d | 0.35173 | -0.02430 | 0.29530 | 1 | 6.228 |

| Atom (y = 4.5) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.26317 | 0.25000 | 1 | 6.542 |
| Mg2 | 4c | 0.00000 | 0.09699 | 0.75000 | 1 | 4.877 |
| Si1 | 8d | 0.29577 | 0.09165 | 0.06992 | 1 | 5.970 |
| O1 | 8d | 0.12105 | 0.09207 | 0.07587 | 1 | 4.705 |
| O2 | 8d | 0.37829 | 0.25353 | 0.07301 | 1 | 5.259 |
| O3 | 8d | 0.35195 | -0.02450 | 0.29468 | 1 | 4.868 |

| Atom (y = 5) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.26067 | 0.25000 | 1 | 6.693 |
| Mg2 | 4c | 0.00000 | 0.09663 | 0.75000 | 1 | 5.406 |
| Si1 | 8d | 0.29420 | 0.09234 | 0.07309 | 1 | 6.276 |
| O1 | 8d | 0.11887 | 0.09209 | 0.08333 | 1 | 5.037 |
| O2 | 8d | 0.37725 | 0.25230 | 0.07186 | 1 | 5.638 |
| O3 | 8d | 0.35265 | -0.02050 | 0.29694 | 1 | 5.536 |

| Atom (y = 5.5) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.26024 | 0.25000 | 1 | 6.932 |
| Mg2 | 4c | 0.00000 | 0.09637 | 0.75000 | 1 | 5.741 |
| Si1 | 8d | 0.29347 | 0.09233 | 0.07351 | 1 | 6.632 |
| O1 | 8d | 0.11828 | 0.09200 | 0.08404 | 1 | 5.403 |
| O2 | 8d | 0.37710 | 0.25180 | 0.07172 | 1 | 5.935 |
| O3 | 8d | 0.35218 | -0.01980 | 0.29861 | 1 | 6.119 |

| Atom (y = 6) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.25980 | 0.25000 | 1 | 6.685 |
| Mg2 | 4c | 0.00000 | 0.09680 | 0.75000 | 1 | 5.424 |
| Si1 | 8d | 0.29350 | 0.09220 | 0.07260 | 1 | 6.172 |
| O1 | 8d | 0.11830 | 0.09230 | 0.08400 | 1 | 5.316 |
| O2 | 8d | 0.37640 | 0.25070 | 0.07080 | 1 | 5.606 |
| O3 | 8d | 0.35270 | -0.01900 | 0.29670 | 1 | 5.711 |

| Atom (y = 6.5) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.25913 | 0.25000 | 1 | 6.564 |
| Mg2 | 4c | 0.00000 | 0.09659 | 0.75000 | 1 | 5.352 |
| Si1 | 8d | 0.29378 | 0.09223 | 0.07291 | 1 | 6.183 |
| O1 | 8d | 0.11867 | 0.09248 | 0.08266 | 1 | 5.199 |
| O2 | 8d | 0.37662 | 0.25230 | 0.07186 | 1 | 5.486 |
| O3 | 8d | 0.35354 | -0.01820 | 0.29619 | 1 | 5.931 |

| Atom (y = 7) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.25902 | 0.25000 | 1 | 6.273 |
| Mg2 | 4c | 0.00000 | 0.09625 | 0.75000 | 1 | 4.990 |
| Si1 | 8d | 0.29419 | 0.09266 | 0.07299 | 1 | 5.955 |
| O1 | 8d | 0.11889 | 0.09228 | 0.08402 | 1 | 4.973 |
| O2 | 8d | 0.37660 | 0.25160 | 0.06882 | 1 | 5.163 |
| O3 | 8d | 0.35295 | -0.01740 | 0.29698 | 1 | 5.632 |

| Atom (y = 7.5) | Wyck. | x | y | z | Occ. | B (iso.) |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | 4c | 0.00000 | 0.25863 | 0.25000 | 1 | 6.570 |
| Mg2 | 4c | 0.00000 | 0.09594 | 0.75000 | 1 | 5.305 |
| Si1 | 8d | 0.29383 | 0.09239 | 0.07333 | 1 | 6.296 |
| O1 | 8d | 0.11869 | 0.09260 | 0.08473 | 1 | 5.348 |
| O2 | 8d | 0.37696 | 0.25085 | 0.06937 | 1 | 5.317 |
| O3 | 8d | 0.35264 | -0.01730 | 0.29718 | 1 | 6.029 |

Supplementary Table 3 Mg1-O bond length in MgSiO3:Cr,y%Li.

|  | y = 4 | y = 4.5 | y = 5 | y = 5.5 | y = 6 | y = 6.5 | y = 7 | y = 7.5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mg1-O3Ⅰ | 2.3087 | 2.3195 | 2.3620 | 2.3728 | 2.3786 | 2.3840 | 2.3939 | 2.3985 |
| Mg1-O2Ⅱ | 2.0780 | 2.0602 | 2.0576 | 2.0569 | 2.0559 | 2.0504 | 2.0466 | 2.0462 |
| Mg1-O1Ⅲ | 2.0759 | 2.0860 | 2.0413 | 2.0337 | 2.0302 | 2.0296 | 2.0280 | 2.0204 |
| Mg1-O3Ⅳ | 2.3087 | 2.3195 | 2.3620 | 2.3728 | 2.3786 | 2.3840 | 2.3939 | 2.3985 |
| Mg1-O1Ⅴ | 2.0759 | 2.0860 | 2.0413 | 2.0337 | 2.0302 | 2.0296 | 2.0280 | 2.0204 |
| Mg1-O2Ⅵ | 2.0780 | 2.0602 | 2.0576 | 2.0569 | 2.0559 | 2.0504 | 2.0466 | 2.0462 |
| D of [Mg1-O] | 4.782% | 5.081% | 6.452% | 6.756% | 6.920% | 7.096% | 7.350% | 7.532% |

Supplementary Table 4 Several excellent Cr3+-doped NIR phosphors.

| Number | Material | λex (nm) | λem (nm) | IQE (%) | EQE (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Y2CaAl4SiO12:Cr3+ | 440 | 744 | 75.9 | 28.1 | 1 |
| 2 | Ca2LuZr2Al3O12:Cr3+ | 460 | 750 | 69.1 | 31.5 | 2 |
| 3 | SrGa12O19:Cr3+ | 415 | 765 | 98.2 | 45 | 3 |
| 4 | Na3ScF6:Cr3+ | 436 | 774 | 91.5 | 40.8 | 4 |
| 5 | AlP3O9:Cr3+ | 450 | 780 | 75 | 36 | 5 |
| 6 | KAlP2O7:Cr3+ | 450 | 790 | 78.8 | 31.1 | 6 |
| 7 | Ga1.6In0.4O3:Cr3+ | 450 | 800 | 88 | 44 | 7 |
| 8 | LuCa2ScZrGa2GeO12:Cr3+ | 456 | 815 | 68.75 | 26.11 | 8 |
| 9 | GaTaO4:Cr3+ | 460 | 840 | 91.2 | 31.3 | 9 |
| 10 | Mg4Ta2O9:Cr3+ | 450 | 842 | 87.5 | 61.25 | 10 |
| 11 | Mg1.2Ga1.8O3.8F0.2:Cr3+ | 420 | 870 | 93.2 | 60.6 | 11 |
| 12 | LiInGe2O6:Cr3+ | 460 | 880 | 81.2 | 39.8 | 12 |
| 13 | LiScGe2O6:Cr3+ | 480 | 886 | 72.6 | 39.9 | 13 |
| 14 | LiInO2:Cr3+ | 468 | 897 | 42.4 | 24.5 | 14 |
| 15 | Ga2GeO5 | 428 | ~910 | 71.25 | 18.95 | 15 |
| 16 | Mg0.8Zn0.2Ga2O4:Cr3+ | 420 | 913 | 83.9 | 35.7 | 16 |
| 17 | Mg2GeO4:Cr3+ | 465 | 940 | 48 | 16.38 | 17 |
| 18 | CaSc0.8Al1.15SiO6:Cr3+ | 460 | 950 | 30 | 9.3 | 18 |
| 19 | Mg2SiO4:Cr3+,Li+ | 468 | 960 | 70 | 48 | 19 |
| 20 | LiIn2SbO6:Cr3+ | 492 | 970 | 7 | 3.44 | 20 |
| 21 | MgSiO3:Cr3+,Li+ | 450 | 880 | 96 | 64 | This work |

Supplementary Table 5 Detailed performances of the fabricated NIR pc-LED (COB).

| Drive Current (mA) | Voltage (V) | Blue output power (mW) | NIR output power (mW) | NIR electro-optical conversion efficiency (%) |
| --- | --- | --- | --- | --- |
| 20 | 7.706 | 2.756 | 42.999 | 27.958 |
| 50 | 7.816 | 7.028 | 106.316 | 27.212 |
| 100 | 7.929 | 14.102 | 213.073 | 26.886 |
| 200 | 8.092 | 28.064 | 419.230 | 25.91 |
| 300 | 8.227 | 41.911 | 621.552 | 25.184 |
| 400 | 8.351 | 55.516 | 818.578 | 24.508 |
| 500 | 8.466 | 68.915 | 1008.032 | 23.814 |
| 600 | 8.577 | 82.012 | 1193.500 | 23.197 |
| 700 | 8.682 | 94.964 | 1371.805 | 22.574 |
| 800 | 8.785 | 107.619 | 1548.144 | 22.031 |
| 900 | 8.885 | 120.555 | 1723.849 | 21.559 |
| 1000 | 8.983 | 132.390 | 1883.017 | 20.964 |
| 1100 | 9.078 | 144.675 | 2053.324 | 20.562 |
| 1200 | 9.172 | 155.706 | 2204.716 | 20.032 |
| 1300 | 9.264 | 167.161 | 2360.296 | 19.599 |
| 1400 | 9.355 | 178.100 | 2505.874 | 19.133 |
| 1500 | 9.445 | 188.897 | 2645.951 | 18.677 |
| 1600 | 9.535 | 198.946 | 2768.753 | 18.149 |

Supplementary Table 6 Detailed performances of the fabricated NIR pc-LED (SMD).

| Drive Current (mA) | Voltage (V) | Blue output power (mW) | NIR output power (mW) | NIR electro-optical conversion efficiency (%) |
| --- | --- | --- | --- | --- |
| 10 | 2.609 | 1.032 | 8.595 | 32.905 |
| 20 | 2.656 | 2.034 | 16.76 | 31.533 |
| 40 | 2.724 | 4.013 | 32.667 | 29.997 |
| 60 | 2.779 | 5.926 | 48.089 | 28.83 |
| 80 | 2.829 | 7.773 | 62.25 | 27.508 |
| 100 | 2.877 | 9.564 | 75.828 | 26.357 |
| 120 | 2.922 | 11.276 | 88.652 | 25.286 |
| 140 | 2.964 | 12.97 | 100.296 | 24.162 |
| 160 | 3.005 | 14.591 | 111.578 | 23.202 |
| 180 | 3.045 | 16.132 | 121.535 | 22.166 |
| 200 | 3.084 | 17.579 | 130.673 | 21.189 |
| 220 | 3.122 | 18.952 | 139.249 | 20.272 |
| 240 | 3.160 | 20.213 | 146.241 | 19.285 |
| 260 | 3.197 | 21.39 | 152.394 | 18.330 |
| 280 | 3.234 | 22.464 | 157.587 | 17.403 |
| 300 | 3.271 | 23.423 | 161.666 | 16.473 |

(1)

(2)

(3)

(4)

Supplementary Equation 1–4. The calculation formula of Dq/B, where Dq is the crystal field splitting energy, the Racah parameter B indicates the repulsion between 3d orbital electrons, and ΔE represents the energy difference between the 4T1 and 4T2 states as determined from the PL and PLE spectra. ΔS is the Stokes shift obtained from the energy difference between E(4A2 → 4T2) in the PLE spectrum and E(4T2 → 4A2) in the PL spectrum.

(5)

Supplementary Equation 5. The calculation formula of distortion index (Ddis), where n is the coordination number. di is the distance from Mg to the i-th coordinating O atoms, and dav is the average Mg–O distance.

(6)

(7)

Supplementary Equation 6–7. The fitting formulas of decay curves, where I(t) represents the luminescence intensity at time t, A1, A2, and I0 are the fitting constants, and τ1 and τ2 represent the lifetime for exponential components.

(8)

Supplementary Equation 8. The calculation formula of activation energy, where 𝐼0 and 𝐼𝑇 represent emission intensity at temperature 123 K and T, respectively; C is the constant of host; k represents the Boltzmann's constant.

(9)

Supplementary Equation 9. The calculation formula of Huang-Rhys factor (S), where FWHM(T) is acquired from emission spectra at each temperature T, ℎ𝑣𝑣 is the photon energy and k is the Boltzmann's constant.

# References

1.	Mao M., et al. Broadband near-infrared (NIR) emission realized by the crystal-field engineering of Y3−xCaxAl5−xSixO12:Cr3+ (x = 0–2.0) garnet phosphors. J. Mater. Chem. C 8, 1981-1988 (2020).

2.	Zhang L., et al. A high efficiency broad-band near-infrared Ca2LuZr2Al3O12:Cr3+ garnet phosphor for blue LED chips. J. Mater. Chem. C 6, 4967-4976 (2018).

3.	Liu S., et al. Site engineering strategy toward enhanced luminescence thermostability of a Cr3+-doped broadband NIR phosphor and its application. Mater. Chem. Front. 5, 3841-3849 (2021).

4.	He F., et al. A general ammonium salt assisted synthesis strategy for Cr3+-doped hexafluorides with highly efficient near infrared emissions. Adv. Funct. Mater. 31, 2103743 (2021).

5.	Huang D., et al. Efficient and thermally stable broadband near-infrared emission from near zero thermal expansion AlP3O9:Cr3+ phosphors. Inorg. Chem. Front. 9, 1692-1700 (2022).

6.	Zhang H., et al. Efficient and thermally stable broad-band near-infrared emission in a KAlP2O7:Cr3+ phosphor for nondestructive examination. ACS Appl. Mater. Interfaces 14, 11663-11671 (2022).

7.	Zhong J., et al. Efficient and tunable luminescence in Ga2–xInxO3:Cr3+ for near-infrared imaging. ACS Appl. Mater. Interfaces 13, 31835-31842 (2021).

8.	Xie J., et al. Near-infrared LuCa2ScZrGa2GeO12:Cr3+ garnet phosphor with ultra-broadband emission for NIR LED applications. Inorg. Chem. 62, 10772-10779 (2023).

9.	Zhong J., et al. Efficient broadband near-infrared emission in the GaTaO4:Cr3+ phosphor. Adv. Opt. Mater. 10, 2101800 (2022).

10.	Wang S., et al. Achieving high quantum efficiency broadband NIR Mg4Ta2O9:Cr3+ phosphor through lithium-ion compensation. Adv. Mater. 35, e2300124 (2023).

11.	Yao L., et al. Simultaneous absorption and near-infrared emission enhancement of Cr3+ ions in MgGa2O4 spinel oxide via anionic F-substitution. Adv. Opt. Mater. 11, 2202458 (2023).

12.	Liu T., et al. Efficient near-infrared pyroxene phosphor LiInGe2O6:Cr3+ for NIR spectroscopy application. J. Am. Ceram. Soc. 104, 4577-4584 (2021).

13.	Chen X. H., et al. Distorted octahedral site occupation-induced high-efficiency broadband near-infrared emission in LiScGe2O6:Cr3+ phosphor. J. Mater. Chem. C 9, 13640-13646 (2021).

14.	Qin Y., et al. Efficient near-infrared luminescence in LiInO2:Cr3+ phosphor for light-emitting-diodes. Opt. Mater. 143, 114284 (2023).

15.	Peng C.-Y., et al. Six- and five-coordinated Cr3+ in Ga2GeO5 invokes tunable broadband near-infrared emission toward night-vision applications. Rare Metals 42, 3787-3796 (2023).

16.	Chen G., et al. Unlocking Cr3+–Cr3+ coupling in spinel: Ultrabroadband near-infrared emission beyond 900 nm with high efficiency and thermal stability. ACS Appl. Mater. Interfaces 16, 30185-30195 (2024).

17.	Cai H., et al. Tuning luminescence from NIR-I to NIR-II in Cr3+-doped olivine phosphors for nondestructive analysis. J. Mater. Chem. C 9, 5469-5477 (2021).

18.	Liu G., et al. Structural rigidity control toward Cr3+-based broadband near-infrared luminescence with enhanced thermal stability. Chem. Mater. 34, 1376-1384 (2022).

19.	Zhong L., et al. Valence and site engineering enable efficient broadband near-infrared emission at 960 nm in Cr3+-activated forsterite. Adv. Mater. 37, 2508768 (2025).

20.	Liu G., et al. Li/Na substitution and Yb3+ co-doping enabling tunable near-infrared emission in LiIn2SbO6:Cr3+ phosphors for light-emitting diodes. iScience 24, 102250 (2021).