Optoelectronic and Thermoelectric Properties of High-Performance AlSb Semiconductors

Dilshod Nematov a,b*, Amondulloi Burkhonzodaa**, Iskandar Raufov a, Sherali Murodzoda a, Saidjafar Murodzoda a, Sakhidod Sattorzoda a, Anushervon Ashurov a, Makhsud Barot Islomzoda c, Kholmirzo Kholmurodov a

a S.U. Umarov Physical-Technical Institute of NAST, Dushanbe 734063, Tajikistan

b School of Optoelectronic Engineering & CQUPT-BUL Innovation Institute, Chongqing University of Posts and Telecommunications, Chongqing 400065, China

c  Tajik National University, Dushanbe 734025, Tajikistan

Corresponding author’s E-mail: *dilnem@mail.ru (D. Nematov), ** amondullo.burkhonzoda@mail.ru (A. Burkhonzoda)

Figure S1. Convergence of total energy for (a) the cubic and (b) the hexagonal phases of AlSb as a function of plane-wave cutoff energy (ENCUT), calculated using Monkhorst-Pack (red) and Γ-centered (black) k-point sampling schemes.

Figure S2. Convergence of the total energy for (a) the cubic and (b) the hexagonal phases of AlSb as a function of k-point mesh density, calculated using the Monkhorst-Pack (red) and Γ-centered (black) sampling schemes.

Table S1. Comparison of SCAN-calculated crystal lattice parameters of cubic and hexagonal phases of AlSb with experimental data.

| AlSb | Lattice constants | SCAN | Experimental |
| --- | --- | --- | --- |
| F43m | a (Å) | 6.17 | 6.14 [37, 38] |
|  | α=β=γ , o | 90.00 |  |
|  | V (Å3) | 235.11 |  |
| P63mc | a (Å) | 4.35 |  |
|  | b (Å) | 3.76 |  |
|  | c (Å) | 7.17 |  |
|  | α= β≠γ, o | 90, 12 |  |
|  | V (Å3) | 117.55 |  |