Electronic Supplementary materials

A Zn(II)-organic framework as a fluorescent probe for the aqueous phase detection of nitroaromatic explosive and Cr(III) ion

Samrah Kamal,a M. Shahnawaz Khan,a Mohd Khalid,a* M. Shahida, Musheer Ahmadb

aFunctional Inorganic Materials Lab (FIML), Department of Chemistry, Aligarh Muslim University, Aligarh, 202002, India

bZHCET Aligarh Muslim University, Aligarh, 202002, India

*Corresponding author, Email:    khalid215@gmail.com

Formula for calculating the percentage of Trinitrophenol (TNP) fluorescence intensity quenching:

(Io-I)/Io x 100%

Where, Io = initial fluorescence intensity,

I = intensity of Zn-MOF-1 containing Trinitrophenol (TNP) solution.

Stern-Volmer equation:

Io/I = Ksv[A] + 1

Where, Io = fluorescent intensity of Zn-MOF-1 before the addition of the analyte

I = fluorescent intensity after the addition of the respective analyte

Ksv = Stern-Volmer constant

[A] = molar concentration of the analyte (M-1).

Reference: (a) S. Pramanik, C. Zheng, X. Zhang, T. J. Emge and J. Li, J. Am. Chem. Soc., 2011, 133, 4153; (b) D. Banerjee, Z. Hu and J. Li, Dalton Trans., 2014, 43, 10668.

Scheme 1. Different coordination modes of carboxylate (COO‒ ) group [i.e., asymmetric monodentate (a), symmetric bidentate (b) and asymmetric bidentate (c & d)].

Table S1. Selected bond lengths (Å) and bond angles (degree) for Zn-MOF-1

| Zn1- O1 | 2.0486(14) |
| --- | --- |
| Zn1- O4 | 2.1405(15) |
| Zn1- O5 | 2.1799(16) |
| Zn1- O8 | 2.1387(16) |
| Zn1- O9 | 2.0699(15) |
| Zn1 -N1 | 2.1154(17) |
| Zn2 -O2 | 1.9734(16) |
| Zn2- O4 | 2.0079(15) |
| Zn2 -O6 | 2.0765(16) |
| Zn2- O7 | 2.0738(15) |
| Zn2- N2 | 2.1043(19) |
| Zn2- O4- Zn1 | 112.88(7) |
| O4- Zn1- O8 | 87.47(6) |
| O9- Zn1- O8 | 93.11(6) |
| O9- Zn1- O4 | 166.81(6) |
| O5 -Zn1- O8 | 177.78(6) |
| O5- Zn1- O4 | 90.34(6) |
| O5- Zn1- O9 | 89.11(6) |
| O1- Zn1- O8 | 93.56(6) |
| O1- Zn1- O4 | 97.07(6) |
| O1- Zn1- O9 | 96.05(6) |
| O1- Zn1- O5 | 86.30(6) |
| N1- Zn1- O8 | 94.04(6) |
| N1- Zn1- O4 | 77.00(6) |
| N1- Zn1- O9 | 89.81(6) |
| N1- Zn1- O5 | 85.86(6) |
| N1- Zn1- O1 | 170.13(7) |
| O7- Zn2- O4 | 100.38(6) |
| O2- Zn2- O4 | 101.55(6) |
| O2 -Zn2- O7 | 96.34(6) |
| O6- Zn2- O4 | 87.40(6) |
| O6- Zn2- O7 | 159.25(7) |
| O6- Zn2- O2 | 100.93(7) |
| N2- Zn2- O4 | 147.84(7) |
| N2- Zn2- O7 | 77.48(7) |
| N2- Zn2- O2 | 110.59(7) |
| N2- Zn2- O6 | 85.69(7) |

Figure S1: The change in fluorescence intensity of Zn-MOF-1 upon incremental addition of (a) ONA (b) MNA solution.

Figure S2: The change in fluorescence intensity of Zn-MOF-1 upon incremental addition of (a) MDNB (b) ONP solution.

Figure S3: Linear region of fluorescence intensity of Zn-MOF-1 upon addition of TNP in water (05 ‒ 50 μL, 1 mM stock solution) (upon λex= 272nm) (R2= 0.97).

Figure S4: Linear region of fluorescence intensity of Zn-MOF-1 upon addition of Cr3+ in water (50 ‒ 500 μL, 1 mM stock solution) (upon λex= 272nm) (R2= 0.93).

Calculation  of  Standard deviation (σ):

Table S2: Standard deviation of  Zn-MOF-1

| Blank readings (only Zn-MOF-1) | Intensity of Zn-MOF-1 |
| --- | --- |
| Reading 1 | 2411.04 |
| Reading 2 | 2400.27 |
| Reading 3 | 2409.49 |
| Reading 4 | 2414.03 |
| Reading 5 | 2410.500 |
| Standard deviation (σ) | 4.65 |

Calculation of detection limit:

Table S3: Detection limit calculation of Zn-MOF-1 for TNP

| Compound | Slope from graph (m) | Detection limit (3σ)/m |  |
| --- | --- | --- | --- |
| Zn-MOF-1 | 25600 | (µM) | ppb |
|  |  | 5.4×10-4 | 0.12 |

Table S4: Detection limit calculation of Zn-MOF-1 for Cr3+

| Compound | Slope from graph (m) | Detection limit (3σ)/m |  |
| --- | --- | --- | --- |
| Zn-MOF-1 | 5920 | (µM) | ppb |
|  |  | 2.3×10-3 | 0.62 |