Confinement and Molecular Polarity Effects on Adsorption in Microporous Carbons: A 2D-NLDFT Mapping Study

Ana Claudia Pina1,2*, Alejandro Amaya1, Conchi Ania2*

Supplementary Information

# S1. Complete adsorption kinetics data

Table S1. Time-dependent adsorption data for SMX.

| C-KOH |  |  | C-240 |  |  | C-120 |  |  | C-60 |  |  | C-30 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qt (mmol/g) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| t (min) | S1 | S2 | t (min) | S1 | S2 | t (min) | S1 | S2 | t (min) | S1 | S2 | t (min) | S1 | S2 |
| 20 | 0.75509 | 0.77389 | 30 | 1.01807 | 1.02877 | 20 | 0.50945 | 0.57952 | 20 | 0.34052 | 0.33844 | 20 | 0.24269 | 0.30719 |
| 40 | 1.46937 | 1.41978 | 40 | 1.27566 | 1.35362 | 30 | 0.54294 | 0.59947 | 30 | 0.33492 | 0.34411 | 30 | 0.25488 | 0.31110 |
| 60 | 1.83441 | 1.72963 | 50 | 1.45558 | 1.56648 | 40 | 0.56834 | 0.64697 | 40 | 0.34784 | 0.36354 | 40 | 0.26959 | 0.34486 |
| 120 | 1.86478 | 1.76626 | 60 | 1.70893 | 1.72148 | 50 | 0.50151 | 0.68445 | 50 | 0.33988 | 0.33935 | 50 | 0.28926 | 0.37133 |
| 180 | 1.87624 | 1.78145 | 120 | 1.73930 | 1.74925 | 60 | 0.61141 | 0.63362 | 60 | 0.33350 | 0.36129 | 60 | 0.30763 | 0.39867 |
| 270 | 1.88556 | 1.79750 | 180 | 1.75076 | 1.76331 | 120 | 0.65744 | 0.79042 | 120 | 0.37941 | 0.39764 | 120 | 0.33067 | 0.42768 |
| 360 | 1.89287 | 1.81110 | 360 | 1.76739 | 1.77994 | 180 | 0.70190 | 0.76520 | 180 | 0.38233 | 0.41306 | 180 | 0.37202 | 0.43236 |
| 1440 | 1.90635 | 1.83915 | 1440 | 1.78087 | 1.79587 | 1440 | 0.88483 | 1.00577 | 1440 | 0.46219 | 0.52692 | 1440 | 0.40258 | 0.42875 |
| 2880 | 1.91953 | 1.84255 | 2880 | 1.78077 | 1.74185 | 2880 | 0.99431 | 1.02580 | 2880 | 0.49177 | 0.56049 | 2880 | 0.44025 | 0.43344 |
| 5760 | 1.92664 | 1.84773 | 4320 | 1.78079 | 1.74205 | 4320 | 0.98672 | 1.01278 | 4320 | 0.50026 | 0.52662 | 4320 | 0.44746 | 0.43096 |

Table S2. Time-dependent adsorption data for MNZ.

|  | C-KOH |  | C-240 |  | C-120 |  | C-60 |  | C-30 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qt (mmol/g) |  |  |  |  |  |  |  |  |  |
| t (min) | S1 | S2 | S1 | S2 | S1 | S2 | S1 | S2 | S1 | S2 |
| 10 | 0.81640 | 0.81166 | 0.80074 | 0.79116 | 0.70663 | 0.68679 | 0.61637 | 0.62963 | 0.03548 | 0.03975 |
| 15 | 1.03040 | 1.01078 | 0.91199 | 0.98625 | 0.84877 | 0.85528 | 0.76370 | 0.77800 | 0.07217 | 0.07012 |
| 30 | 1.03745 | 1.00964 | 0.96448 | 0.98703 | 0.85431 | 0.85431 | 0.79109 | 0.82163 | 0.35789 | 0.34715 |
| 45 | 1.03859 | 1.01348 | 0.96557 | 0.98724 | 0.84876 | 0.84876 | 0.81247 | 0.82730 | 0.46221 | 0.44840 |
| 60 | 1.03932 | 1.01652 | 0.96515 | 0.98768 | 0.84803 | 0.85353 | 0.81708 | 0.84070 | 0.48123 | 0.46672 |
| 120 | 1.03986 | 1.01768 | 0.96495 | 0.98612 | 0.84536 | 0.85416 | 0.81807 | 0.84050 | 0.50598 | 0.49080 |
| 180 | 1.04158 | 1.01426 | 0.96502 | 0.98752 | 0.85786 | 0.85042 | 0.80953 | 0.83998 | 0.51468 | 0.49923 |
| 240 | 1.04159 | 1.01920 | 0.96611 | 0.98695 | 0.85433 | 0.85006 | 0.81893 | 0.84222 | 0.53096 | 0.51503 |
| 300 | 1.04175 | 1.01313 | 0.96591 | 0.98713 | 0.84837 | 0.85757 | 0.82167 | 0.84086 | 0.53338 | 0.51724 |
| 360 | 1.04162 | 1.01415 | 0.96515 | 0.98705 | 0.84969 | 0.85632 | 0.82612 | 0.84064 | 0.53398 | 0.51796 |
| 1440 | 1.04214 | 1.01421 | 0.96535 | 0.98701 | 0.85196 | 0.85126 | 0.82235 | 0.83950 | 0.53299 | 0.51653 |

Table S3. Non-linearised Fitting kinetic data for SMX and MNZ (1.0 mmolL-1) adsorption onto the carbon adsorbents.

| SMX |  |  |  |  |  | MNZ |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C-KOH | C-240 | C-120 | C-60 | C-30 | C-KOH | C-240 | C-120 | C-60 | C-30 |
| PFO |  |  |  |  |  |  |  |  |  |  |
| k1 (min-1) | 0.034 | 0.033 | 0.028 | 0.042 | 0.145 | 0.175 | 0.181 | 0.188 | 0.149 | 0.031 |
| %MRD | 4.61 | 7.45 | 15.5 | 13.5 | 10.3 | 2.04 | 1.52 | 1.26 | 1.79 | 11.6 |
| χ2 | 0.014 | 0.029 | 0.028 | 0.007 | 0.005 | 0.001 | 0.001 | 0.001 | 0.001 | 0.004 |
| RSS | 0.143 | 0.434 | 0.278 | 0.071 | 0.052 | 0.014 | 0.008 | 0.007 | 0.005 | 0.044 |
| PSO |  |  |  |  |  |  |  |  |  |  |
| k2 (g mmol-1min-1) | 0.029 | 0.032 | 0.044 | 0.139 | 0.161 | 0.553 | 0.619 | 0.609 | 0.451 | 0.07 |
| %MRD | 7.32 | 7.18 | 10.4 | 9.22 | 7.99 | 2.88 | 2.42 | 2.44 | 2.80 | 14.45 |
| χ2 | 0.039 | 0.029 | 0.013 | 0.003 | 0.002 | 0.003 | 0.002 | 0.002 | 0.001 | 0.008 |
| RSS | 0.394 | 0.429 | 0.130 | 0.003 | 0.002 | 0.033 | 0.022 | 0.018 | 0.015 | 0.070 |

# S2. Equilibrium adsorption datasets

Table S4. Equilibrium adsorption data for SMX, average values from three determinations.

| KOH |  | 240 |  | 120 |  | 60 |  | 30 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) |
| 8.02E-04 | 4.54E-01 | 1.75E-03 | 3.09E-01 | 6.00E-03 | 1.01E-01 | 5.00E-06 | 2.48E-01 | 4.70E-02 | 1.09E-01 |
| 3.17E-03 | 6.74E-01 | 6.29E-03 | 5.77E-01 | 2.57E-02 | 3.82E-01 | 5.81E-03 | 4.80E-01 | 1.20E-01 | 1.38E-01 |
| 7.88E-03 | 9.03E-01 | 1.95E-02 | 8.35E-01 | 2.93E-02 | 2.81E-01 | 4.46E-02 | 6.06E-01 | 1.44E-01 | 1.48E-01 |
| 1.27E-02 | 1.15E+00 | 5.58E-02 | 1.07E+00 | 8.29E-02 | 7.62E-01 | 7.13E-02 | 6.68E-01 | 2.51E-01 | 1.73E-01 |
| 2.12E-02 | 1.36E+00 | 1.00E-01 | 1.28E+00 | 1.17E-01 | 9.30E-01 | 2.23E-01 | 6.86E-01 | 3.19E-01 | 1.99E-01 |
| 4.76E-02 | 1.63E+00 | 1.62E-01 | 1.49E+00 | 1.88E-01 | 1.03E+00 | 3.30E-01 | 7.05E-01 | 4.11E-01 | 2.11E-01 |
| 6.24E-02 | 1.71E+00 | 1.88E-01 | 1.58E+00 | 2.14E-01 | 1.13E+00 | 4.38E-01 | 7.05E-01 | 5.16E-01 | 2.21E-01 |
| 8.00E-02 | 1.73E+00 | 2.42E-01 | 1.88E+00 | 3.24E-01 | 1.19E+00 | 5.37E-01 | 7.00E-01 | 6.12E-01 | 2.23E-01 |
| 9.77E-02 | 1.76E+00 | 3.09E-01 | 1.90E+00 | 4.31E-01 | 1.20E+00 | 6.47E-01 | 7.06E-01 | 7.15E-01 | 2.20E-01 |
| 9.68E-02 | 1.75E+00 | 3.68E-01 | 1.90E+00 | 5.20E-01 | 1.20E+00 | 7.43E-01 | 7.15E-01 | 8.00E-01 | 2.25E-01 |
| 9.63E-02 | 1.74E+00 | 3.65E-01 | 1.89E+00 | 5.13E-01 | 1.19E+00 | 7.43E-01 | 7.15E-01 | 9.15E-01 | 2.21E-01 |

Table S5. Equilibrium adsorption data for MNZ, average values from three determinations.

| C-KOH |  | C-240 |  | C-120 |  | C-60 |  | C-30 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) | Ce(mmolL-1) | qe (mmolg-1) |
| 9.18E-03 | 2.26E-01 | 4.24E-02 | 5.16E-01 | 7.00E-03 | 2.24E-01 | 1.30E-03 | 2.47E-01 | 1.25E-03 | 1.91E-01 |
| 2.93E-02 | 4.28E-01 | 7.41E-02 | 7.23E-01 | 2.25E-02 | 4.42E-01 | 2.49E-02 | 4.29E-01 | 5.07E-02 | 3.39E-01 |
| 5.02E-02 | 6.24E-01 | 1.43E-01 | 9.55E-01 | 6.19E-02 | 6.03E-01 | 8.99E-02 | 5.35E-01 | 1.23E-01 | 4.42E-01 |
| 7.45E-02 | 7.72E-01 | 1.94E-01 | 1.07E+00 | 1.01E-01 | 7.50E-01 | 1.35E-01 | 6.81E-01 | 2.01E-01 | 5.00E-01 |
| 1.19E-01 | 9.47E-01 | 3.04E-01 | 1.11E+00 | 1.77E-01 | 8.05E-01 | 1.82E-01 | 8.01E-01 | 2.70E-01 | 5.25E-01 |
| 1.54E-01 | 1.08E+00 | 3.53E-01 | 1.16E+00 | 2.84E-01 | 8.66E-01 | 2.84E-01 | 8.47E-01 | 3.10E-01 | 5.37E-01 |
| 2.63E-01 | 1.16E+00 | 3.80E-01 | 1.14E+00 | 3.34E-01 | 8.79E-01 | 4.05E-01 | 8.66E-01 | 3.40E-01 | 5.37E-01 |
| 3.27E-01 | 1.16E+00 | 4.21E-01 | 1.20E+00 | 3.86E-01 | 8.86E-01 | 5.11E-01 | 8.70E-01 | 3.96E-01 | 5.38E-01 |
| 3.80E-01 | 1.20E+00 | 4.64E-01 | 1.20E+00 | 4.38E-01 | 8.91E-01 | 5.96E-01 | 8.63E-01 | 4.92E-01 | 5.37E-01 |
| 4.19E-01 | 1.20E+00 | 5.14E-01 | 1.20E+00 | 4.90E-01 | 8.96E-01 | 6.91E-01 | 8.66E-01 | 5.23E-01 | 5.38E-01 |

S3. Adsorption model fitting parameters

Empirical adsorption models were used to describe equilibrium data and support comparison between samples. The isotherms were fitted to the Langmuir and the Freundlich models (Equations 1 and 2, respectively).

qe= qmKLCe1+KLCe 									     Equation 1.

qe= KFCen		 	        					 	    Equation 2.

where qe (mmolg-1) is the amount adsorbed per carbon mass unit at the equilibrium, qm (mmolg-1) is the maximum adsorption capacity, Ce (mmolL-1) is the concentration of the pollutant after equilibrium, KL (Lmmol-1) is the Langmuir constant, KF (molkg-1) (molL-1)-n is the Freundlich constant, and n is the Freundlich exponent.

Table S6. Nonlinear fitting of the Langmuir and Freundlich isotherm models to SMX and MNZ adsorption on the carbon adsorbents studied.

|  | SMX |  |  |  |  |  | MNZ |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | C-KOH | C-240 | C-120 | C-60 | C-30 | C-KOH | C-240 | C-120 | C-60 | C-30 |
| LANGMUIR |  |  |  |  |  |  |  |  |  |  |  |
| KL a |  | 149.4 | 30.71 | 15.56 | 343.4 | 12.34 | 17.24 | 15.29 | 36.64 | 27.59 | 34.50 |
| qmax.b |  | 1.85 | 1.95 | 1.39 | 0.702 | 0.246 | 1.39 | 1.37 | 0.94 | 0.92 | 0.57 |
| %MRD |  | 18.4 | 36.9 | 4.21 | 1867 | 4.84 | 4.67 | 1.70 | 3.35 | 0.001 | 0.004 |
| χ2 |  | 0.020 | 0.053 | 0.002 | 0.011 | 0.0001 | 0.002 | 0.001 | 0.001 | 0.014 | 0.006 |
| RSS |  | 0.090 | 0.267 | 0.007 | 0.064 | 0.001 | 0.010 | 0.004 | 0.004 | 0.069 | 0.029 |
| FREUNDLICH |  |  |  |  |  |  |  |  |  |  |  |
| KF c |  | 3.490 | 2.716 | 1.687 | 0.7535 | 0.2435 | 1.732 | 1.525 | 1.136 | 1.003 | 0.6365 |
| n |  | 0.27 | 0.32 | 0.34 | 0.08 | 0.24 | 0.34 | 0.28 | 0.24 | 0.21 | 0.18 |
| %MRD |  | 6.58 | 4.97 | 16.4 | 3.99 | 4.76 | 11.2 | 5.16 | 8.03 | 6.49 | 3.53 |
| χ2 |  | 0.012 | 0.007 | 0.025 | 0.001 | 0.0002 | 0.016 | 0.007 | 0.007 | 0.006 | 0.001 |
| RSS |  | 0.052 | 0.038 | 0.113 | 0.007 | 0.001 | 0.081 | 0.035 | 0.033 | 0.029 | 0.004 |
| a: KL, Lmmol-1 b: qm, mmolg-1 c: qmax., mmolg-1 c: values are reported considering Cein mmol L⁻¹ and qein mmol g⁻¹ |  |  |  |  |  |  |  |  |  |  |  |

S4. Construction of the contour plot

The contour plots represent adsorption uptake as a function of cumulative pore volume within selected pore-width intervals, with pore volume derived from pore-size distribution (PSD) analysis. For a fixed equilibrium concentration, uptake is calculated using the corresponding adsorption model and subsequently correlated with the pore volume for each pore-width domain. For every pore interval, the goodness of fit between pore volume and uptake is quantified using the adjusted coefficient of determination (adj-R²) and the residual sum of squares (RSS).

The resulting contour map visualises the distribution of these fitness values across the evaluated pore-width domains. An illustrative example of the contour plot construction is provided for an equilibrium concentration of 0.1 mmol L⁻¹.

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure S1. Correlation between the uptake of SMX for an equilibrium concentration of 0.1 mmolL-1 as a function of the size of the pores: (a) up to 0.7 nm, (b) up to 1.5 nm, (c) up to 2.0 nm, and (d) up to 3.0 nm.

Table S7. Fitting parameters for the SMX uptake at an equilibrium concentration of 0.1 mmolL-1 as a function of the pore size distribution for pores of selected ranges.

| Pore Size Range | 0.7 nm | 1.5 nm | 2.0 nm | 3.0 nm |
| --- | --- | --- | --- | --- |
| adj-R2 | 0.5295 | 0.9666 | 0.9765 | 0.9723 |
| RSS | 0.0594 | 0.3593 | 0.0560 | 0.0002 |

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure S2. MNZ uptake for equilibrium concentrations of 0.1 mmolL-1 as a function of the volume of pores below (a) 0.7 nm, (b) 1.5 nm, (c) 2.0 nm, and (d) 3.0 nm.

Table S8. Fitting parameters for the MNZ uptake for Ceq 0.1 mmolL-1 as a function of the volume of pores plots for 0.7, 1.5, 2.0 and 3.0 nm.

|  | 0.7 nm | 1.5 nm | 2.0 nm | 3.0 nm |
| --- | --- | --- | --- | --- |
| R2 | 0.1266 | 0.8414 | 0.9124 | 0.9115 |
| RSS | 0.1236 | 0.0224 | 0.0124 | 0.0125 |