Supplementary Information

An electrochemically stable defect-free glassy electrolyte formed at room temperature for all-solid-state sodium batteries

Xiaowei Chi1,2‡, Ye Zhang1‡, Fang Hao1‡, Steven Kmiec3‡, Hui Dong1, Rong Xu,4 Kejie Zhao4, Liang Wang5, †, Lihong Zhao1, Liqun Guo1, Huolin Xin6, Steve W. Martin3*, Yan Yao1*

1Department of Electrical and Computer Engineering and Texas Center for Superconductivity at the University of Houston, University of Houston, Houston, TX, 77204, USA

2Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai 200050, China 3Department of Materials Science & Engineering, Iowa State University, Ames, IA 50011, USA

4School of Mechanical Engineering, Purdue University, West Lafayette, IN 47907, USA

5Department of Physics, Northern Illinois University, Dekalb, IL 60115, USA

6Department of Physics and Astronomy, University of California, Irvine, Irvine, CA, USA

‡ X. C., Y. Z., F. H., S.K. contribute equally to this work.

† Current address: Institute of Advanced Structure Technology and School of Materials Science and Engineering, Beijing Institute of Technology, Beijing 100081, China

* Email: yyao4@uh.edu (Y.Y.), swmartin@iastate.edu (S.M.)

Supplementary Table S1 | Assignments of the peaks in the Fourier-transform infrared spectroscopy (FTIR) spectra of Na3PS4–xOx SEs

| Position (cm-1) | Assignment |
| --- | --- |
| 445 | P–S linkage |
| 560 | Asymmetric stretching of P–S |
| 590 | Stretching of P–O–P |
| 634 | Bending vibration of O–P–O |
| 685 | Symmetric stretching of P–O–P |
| 720 | Symmetric stretching of P–O–P |
| 895 | Asymmetric stretching of P–O–P |
| 996 | Symmetric stretching of –O–P–O– non-bridging oxygen |
| 1030 | Motion of the P=O or P–O– non-bridging oxygen |
| 1090 | Symmetric stretching of –O–P–O– non-bridging oxygen |
| 1150 | Symmetric stretching of –O–P–O– non-bridging oxygen |

Note: P–O connections are also observed in x=0 sample, which may result from the oxygen contamination during synthesis.

Supplementary Table S2 | Fitting results of EIS spectra of Na3PS4−xOx (x=0, 0.15, 0.30, and 0.60) SEs for symmetric cells before and after contact Na metals for 5 h.

| x value | ASR [Ω∙cm2] | Rb [Ω∙cm2] | Cb [pF] | Ri [Ω∙cm2] | Ci [μF] | Rct [Ω∙cm2] | Cct [mF] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.00 before | 1596.7 | 1240 | 1.20 | 272 | 0.16 | 84.7 | 9.90 |
| 0.00 after | 1753.0 | 1350 | 2.90 | 304 | 0.19 | 99.0 | 6.30 |
| 0.15 before | 253.1 | 216 | 0.24 | 6 | 4.50 | 31.1 | 53.0 |
| 0.15 after | 341.7 | 254 | 0.58 | 16 | 0.32 | 71.2 | 1.53 |
| 0.30 before | 367.2 | 334 | 0.24 | 24 | 0.45 | 8.9 | 0.45 |
| 0.30 after | 376.7 | 332 | 0.13 | 28 | 1.20 | 16.4 | 3.30 |
| 0.60 before | 664.9 | 644 | 0.79 | - | - | 20.9 | 1.30 |
| 0.60 after | 662.2 | 640 | 0.89 | - | - | 21.4 | 1.60 |

Note: The obtained EIS spectra from high frequency to middle frequency to low frequency can be fitted into bulk resistance and capacitance (Rb + Rgb, Cb + Cgb) of the SEs, interfacial resistance and capacitance (Ri, Ci) between Na and SEs with characteristic capacitance of 10–6~10–7 F, and the charge-transfer resistance and capacitance (Rct, Cct).

Supplementary Table S3 | Comparison of reported solid-state Na–S batteries with this work

| Electrolyte | Cathode | Anode | Voltage (V) | Cathode capacity (Cc, mAh g−1) |  | Full cell capacity (C, mAh g−1) |  | Specific energy (Wh/kg) |  | Cycling life |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Na3.1Zr1.95Mg0.05Si2PO12 (RT) | S | Na | 1.75 | 527 | 363 |  | 635 |  | 10 |  | 1 |  |
| PEO-NaCF3SO3 (90 °C) | S | Na | 1.75 | 505 | 352 |  | 617 |  | 10 |  | 2 |  |
| PEO−NaN(SO2F)2−1% TiO2 (60 °C) | S | Na | 1.40 | 713 | 442 |  | 619 |  | 100 |  | 3 |  |
| Na3PS4 (RT) | S | Na15Sn4 | 1.10 | 1522 | 544 |  | 599 |  | 2 |  | 4 |  |
| Na3PS4 (RT) | S | Na15Sn4 | 1.30 | 1112 | 481 |  | 625 |  | 25 |  | 5 |  |
| Na3PS4 (60 °C) | Na2S | Na15Sn4 | 1.25 | 869 | 429 |  | 536 |  | 50 |  | 6 |  |
| Na3PS4 (60 °C) | Na2S | Na15Sn4 | 1.25 | 800 | 411 |  | 514 |  | 50 |  | 7 |  |
| Na3SbS4 (RT) | S | Na3Sb | 0.5 | 1560 | 464 |  | 232 |  | 55 |  | 8 |  |
| Na3PS4-xOx (60 °C) | S | Na | 1.42 | 1281 | 610 |  | 866 |  | 150 |  | This work |  |

Note: The cell specific energy (Es) is calculated by Es = E × (Cc−1 + Ca−1)−1, where E is the average discharge voltage, Cc is cathode specific capacity. The anode specific capacity (Ca) for Na, Na15Sn4 and Na3Sb are 1165, 847 and 660 mAh g−1, respectively. The full cell capacity (C) is calculated by C = (Cc−1 + Ca−1)−1.

Supplementary Figure 1 | Lab-based X-ray diffraction patterns of Na3PS4–xOx SEs.

Supplementary Figure 2 | Differential scanning calorimeter (DSC) curves of Na3PS4–xOx SEs. Tg and Tc represent the glass transition temperature and crystallization temperature, respectively.

Supplementary Figure 3 | Transmission electron microscope (TEM) image and selected area electron diffraction (SAED) patterns of Na3PS3.85O0.15 SE.

Supplementary Figure 4 | Gaussian fitting results of PS4 mode in Raman spectra of Na3PS4–xOx SEs.

Supplementary Figure 5 | Galvanostatic cycling of Na|HT-Na3PS4|Na symmetric cells at 60 °C under current density of 0.1 mA cm−2 with a stripping/plating capacity of 0.1 mAh cm−2.

Supplementary Figure 6 | SEM images of cross-sectional Na3PS4 SE pressed at (a) 150 MPa and (b) at 375 MPa, in comparison with Na3PS3.4O0.6 SE pressed at (c) 150 MPa and (d) at 375 MPa (scale bar: 20 μm).

Supplementary Figure 7 | SEM images of (a) Na3PS4 glass and (b) Na3PS3.4O0.6 glass powders (scale bar: 5 μm).

Supplementary Figure 8 | Nano-indentation loading curves of Na3PS3.85O0.15 and Na3PS3.7O0.3 glass SEs;

Supplementary Figure 9 | Areal Specific Resistance (ASR) change of Na3PS4–xOx SEs before and after in contact with Na metal for 5 hours.

Supplementary Figure 10 | P 2p and S 2p orbitals in XPS spectra of pristine Na3PS4–xOx SEs.

Supplementary Figure 11 | Electrochemical impedance spectra (EIS) of Na3PS4–xOx SEs in a Cu|SE|Cu cell at 60 °C.

Supplementary Figure 12 | Plots of activation energies (Ea) and conductivity at 60 °C in Na3PS4–xOx SEs.

Supplementary Figure 13 | Cross-sectional SEM images of the tri-layer electrolyte.

Supplementary Fig. S14 | Comparison of reported Na|SE|Na symmetric cell performance with this work in terms of the capacity of Na metal plated per cycle (circle area), current density, cycling time. SEs include sulfide-based (Na3PS4, Na3SbS4, Na2.9375PS3.9375Cl0.0625)9-11, oxide-based (Na3.1Zr1.95Mg0.05Si2PO12, heat-treated Na3Zr2(PO4)(SiO4)2)1,12, boride-based (Na2(B12H12)0.5(B10H10)0.5)13, polymer-based (poly(ethylene oxide) (PEO), hollow mesoporous organic polymer-PEO composite)14,15, and polymer-oxide composite (cross-linked poly(ethylene glycol) methyl ether acrylate (CPMEA)–Na3Zr2(PO4)(SiO4)2)12.

Supplementary Fig. S15 | Symmetric cell performances: (a) Scheme of tri-layer electrolyte composed of Na3PS3.4O0.6|HT-Na3PS4|Na3PS3.4O0.6; (b) SEM image of the tri-layer electrolyte; (c) SEM image of enlarged interface between Na3PS3.4O0.6 (top layer) and HT-Na3PS4 (bottom layer); (d) and (e) galvanostatic cycling of Na|Na3PS3.4O0.6|HT-Na3PS4|Na3PS3.4O0.6|Na symmetric cells at 60 °C under current densities of 0.2 mA cm−2 and 0.5 mA cm−2, respectively.

Supplementary Figure 16 | Voltage profiles of Na-S full cells at 60 °C under current densities from 0.05 mA cm−2 to 0.35 mA cm−2.

References

1	Song, S., Duong, H. M., Korsunsky, A. M., Hu, N. & Lu, L. A Na+ Superionic Conductor for Room-Temperature Sodium Batteries. Sci. Rep. 6, 32330, doi:10.1038/srep32330 (2016).

2	Park, C.-W. et al. Discharge properties of all-solid sodium-sulfur battery using poly(ethylene oxide) electrolyte. J. Power Sources 165, 450-454, doi:https://doi.org/10.1016/j.jpowsour.2006.11.083 (2007).

3	Zhu, T. et al. An All-Solid-State Sodium–Sulfur Battery Using a Sulfur/Carbonized Polyacrylonitrile Composite Cathode. ACS Applied Energy Materials 2, 5263-5271, doi:10.1021/acsaem.9b00953 (2019).

4	Nagata, H. & Chikusa, Y. An All-solid-state Sodium-Sulfur Battery Operating at Room Temperature Using a High-sulfur-content Positive Composite Electrode. Chem. Lett. 43, 1333-1334, doi:10.1246/cl.140353 (2014).

5	Tanibata, N., Deguchi, M., Hayashi, A. & Tatsumisago, M. All-Solid-State Na/S Batteries with a Na3PS4 Electrolyte Operating at Room Temperature. Chem. Mater. 29, 5232-5238, doi:10.1021/acs.chemmater.7b01116 (2017).

6	Yue, J. et al. High-Performance All-Inorganic Solid-State Sodium–Sulfur Battery. ACS Nano 11, 4885-4891, doi:10.1021/acsnano.7b01445 (2017).

7	Fan, X. et al. High-Performance All-Solid-State Na–S Battery Enabled by Casting–Annealing Technology. ACS Nano 12, 3360-3368, doi:10.1021/acsnano.7b08856 (2018).

8	Ando, T., Sakuda, A., Tatsumisago, M. & Hayashi, A. All-solid-state sodium-sulfur battery showing full capacity with activated carbon MSP20-sulfur-Na3SbS4 composite. Electrochem. Commun. 116, 106741, doi:https://doi.org/10.1016/j.elecom.2020.106741 (2020).

9	Wan, H. et al. Nanoscaled Na3PS4 Solid Electrolyte for All-Solid-State FeS2/Na Batteries with Ultrahigh Initial Coulombic Efficiency of 95% and Excellent Cyclic Performances. ACS Appl. Mater. Interfaces 10, 12300-12304, doi:10.1021/acsami.8b01805 (2018).

10	Wang, H. et al. An Air-Stable Na3SbS4 Superionic Conductor Prepared by a Rapid and Economic Synthetic Procedure. Angew. Chem. Int. Ed. 55, 8551-8555, doi:10.1002/anie.201601546 (2016).

11	Wu, E. A. et al. New Insights into the Interphase between the Na Metal Anode and Sulfide Solid-State Electrolytes: A Joint Experimental and Computational Study. ACS Appl. Mater. Interfaces 10, 10076-10086, doi:10.1021/acsami.7b19037 (2018).

12	Zhou, W., Li, Y., Xin, S. & Goodenough, J. B. Rechargeable Sodium All-Solid-State Battery. ACS Cent. Sci. 3, 52-57, doi:10.1021/acscentsci.6b00321 (2017).

13	Duchêne, L. et al. A highly stable sodium solid-state electrolyte based on a dodeca/deca-borate equimolar mixture. Chem. Commun. 53, 4195-4198, doi:10.1039/c7cc00794a (2017).

14	Ma, Q. et al. A new Na[(FSO2)(n-C4F9SO2)N]-based polymer electrolyte for solid-state sodium batteries. J. Mater. Chem. A 5, 7738-7743, doi:10.1039/c7ta01820g (2017).

15	Zhou, W., Gao, H. & Goodenough, J. B. Low-Cost Hollow Mesoporous Polymer Spheres and All-Solid-State Lithium, Sodium Batteries. Adv. Energy Mater. 6, 1501802, doi:doi:10.1002/aenm.201501802 (2016).