Supplementary Information for

The Meissner effect in high-temperature hydrogen-rich superconductors under high pressure

V. S. Minkov, S. L. Bud’ko, F. F. Balakirev, V. B. Prakapenka, S. Chariton, R. J. Husband, H. P. Liermann, M. I. Eremets

Correspondence to: m.eremets@mpic.de; v.minkov@mpic.de

This PDF file includes:

Supplementary Text

Figs. SI1 to SI11

Figure SI1.

M(T) magnetization data of the sandwiched sample with S and NH3BH3 pressurized at PD = 167±7 GPa at 2, 4 and 10 mT (lower panel), the heated sample with the superconducting Im-3m-H3S phase at PS = 155±5 GPa (PD = 162±3 GPa, PH = 155 GPa) at 2, 4, 10 mT (middle panel), and the difference plot (upper panel). The blue and red circles correspond to the zero-field-cooled (ZFC) and filed-cooled (FC) measurements.

Figure SI2.

M(T) magnetization data of the sandwiched sample with LaH3 and NH3BH3 pressurized at PD = 168±7 GPa at 2, 4 and 10 mT (lower panel), the heated sample with the superconducting Fm-3m-LaH10 phase at PS = 130±8 GPa (PD = 157±3 GPa) at 2, 4, 10 mT (middle panel), and the difference plot (upper panel). The blue and red circles correspond to the zero-field-cooled (ZFC) and filed-cooled (FC) measurements.

Figure SI3.

Photos of the sandwiched sample with S and NH3BH3 after clamping at PD 1 GPa (left panel) and pressurizing to PD = 167±7 GPa (central panel), and the heated sample with the superconducting Im-3m-H3S phase at PS = 155±5 GPa (PD = 162±3 GPa, PH = 155 GPa). The photos are taken in transmitted (top), transmitted and reflected (center), and reflected (bottom) light.

Figure SI4.

Photos of the sandwiched sample with LaH3 and NH3BH3 after clamping at PD 3 GPa (left panel) and pressurizing to PD = 168±7 GPa (second panel), and the sample with the superconducting Fm-3m-LaH10 phase at PS = 130±8 GPa (PD = 157±3 GPa) after heating by a pulse laser at 1000 K (third panel) and 2000 K (right panel). The photos are taken in transmitted (top), transmitted and reflected (center), and reflected (bottom) light.

Figure SI5.

Raman spectra of the sandwiched sample with S and NH3BH3 upon pressurizing from PD 1 GPa (black Raman spectrum) to PD = 167±7 GPa (red Raman spectrum), demonstrating the metallization of sulfur. The blue Raman spectrum on the top corresponds to the sample with the superconducting Im-3m-H3S phase, which was synthesized after heating at 700 K by a pulse laser. The wavenumber of the hydrogen vibron, which was appeared in the Raman spectrum after heating of NH3BH3, corresponds to a pressure value of PH = 155 GPa, slightly lower than PD = 162±3 GPa estimated by the diamond scale(37).

Figure SI6.

Centering of a sample residing in the miniature DAC using a ferromagnetic signal of the steel piece with a size of 14010025 m3 attached to the rhenium gasket. The red, black and blue circles and green curve correspond to the DC scans of the miniature DAC with and without steel piece, the difference, and Gauss fit, respectively. Here is the centering of the sample with the Fm-3m-LaH10 phase in the DAC at 295 K and 2 mT.

Figure SI7.

M(H) magnetization data of the heated sample with the Im-3m-H3S at PS = 155±5 GPa (PD = 162±3 GPa, PH = 155 GPa) at several temperatures: in a normal metallic state above Tc at 200 K, and in a superconducting state below Tc at 180, 140, 100 and 80 K. The left panel shows the full range of hysteresis and the right panel shows the enlarged magnetic field range of -0.1 – 0.1 T.

Figure SI8.

M(H) magnetization data of the heated sample with the Fm-3m-LaH10 phase at PS = 130±8 GPa (PD = 157±3 GPa) at several temperatures: in a normal metallic state above Tc at 240 K, and in a superconducting state below Tc at 180, 140, 100 and 80 K. The left panel shows the full range of hysteresis and the right panel shows the enlarged magnetic field range of -0.1 – 0.1 T.

Figure SI9.

Temperature-dependence of the London penetration depth, L, of Im-3m-H3S at PS = 155±5 GPa, a, and Fm-3m-LaH10 at PS = 130±8 GPa, b. The black circles correspond to the L values, which were determined using the sample thickness of 2.8 m for H3S and 1.9 m for LaH10 samples estimated from the optical microscopy data. The red and blue stars correspond to maximum and minimum L values, which were estimated using the theoretical calculated maximum and minimum values of sample thickness.

Figure SI10.

Magnetic measurements of the test materials in a SQUID. M(T) magnetization data for powder MgB2 sample, a and b, single crystal MgB2 sample, c and d, and single crystal Bi2Sr2CaCu2O8 sample, e and f, housing in the miniature DACs and the standard nonmagnetic plastic tube. Black and red cycles correspond to ZFC and FC magnetization curves. g, M(H) magnetization data of the single crystal Bi2Sr2CaCu2O8 sample in the DAC at different temperatures. h and i, Hp(T) and Hc1(T) plots of the single crystal Bi2Sr2CaCu2O8 sample in the DAC built from the M(H) data without effective demagnetizing factor N and with the estimated N = 0.8556, respectively. Red circles and black rhombuses are the present data and the data from Ref(48), respectively.

Figure SI11.

Estimation of a thickness of the superconducting samples in the miniature DACs at high pressure. a and b, Expansion of the hole in the rhenium gasket restraining the sandwiched samples with H3S at PS = 155±5 GPa and LaH10 at PS = 130±8 GPa, respectively. The inner red circles show the starting size of the hole in the rhenium gasket at PD 1 and 3 GPa. Photos are taken with 90%-transmitting and 10%-reflecting light.