Development, Hirshfeld surface analysis, DFT calculations and biological evaluation of neratinib loaded Co-crystals for solubility enhancement.
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Figure S1: Scanning Absorbance Maxima of Neratinib in Methanol (264 nm)
Calibration Curve Determination
Table 4: Calibration Curve Data of Neratinib in Methanol
	Sr. No.
	Concentration (μg/mL)
	Absorbance

	1
	2
	0.182

	2
	4
	0.364

	3
	6
	0.559

	4
	8
	0.728

	5
	10
	0.910

	6
	12
	1.092

	Slope
	0.091

	Intercept
	0.0019

	Correlation Coefficient (R²)
	0.9998

	Absorption Maxima (λmax)
	264 nm



Table S1: Cumulative Percentage In Vitro Drug Release (mean ± SD, n = 3) from Neratinib–3-Hydroxybenzoic Acid Cocrystal Batches PF1–PF9 and Pure Neratinib
	Time (min)
	Pure Neratinib
	PF1
	PF2
	PF3
	PF4
	PF5
	PF6
	PF7
	PF8
	PF9

	0
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00
	0.00 ± 0.00

	5
	3.8 ± 0.34
	6.4 ± 0.48
	7.9 ± 0.54
	9.2 ± 0.61
	10.1 ± 0.68
	12.8 ± 0.76
	14.6 ± 0.84
	11.4 ± 0.72
	15.8 ± 0.88
	17.2 ± 0.94

	10
	6.9 ± 0.47
	11.8 ± 0.66
	14.2 ± 0.74
	16.4 ± 0.82
	17.9 ± 0.86
	22.4 ± 1.08
	25.6 ± 1.16
	20.3 ± 0.98
	27.8 ± 1.24
	30.4 ± 1.32

	15
	9.4 ± 0.58
	16.6 ± 0.82
	19.8 ± 0.91
	22.7 ± 0.98
	25.1 ± 1.12
	31.6 ± 1.34
	36.2 ± 1.48
	28.4 ± 1.22
	39.4 ± 1.56
	43.8 ± 1.64

	20
	11.6 ± 0.68
	20.8 ± 0.96
	24.9 ± 1.04
	28.4 ± 1.12
	31.8 ± 1.28
	41.2 ± 1.54
	47.1 ± 1.68
	36.6 ± 1.38
	51.2 ± 1.76
	57.4 ± 1.84

	30
	14.2 ± 0.76
	26.4 ± 1.14
	31.6 ± 1.28
	36.1 ± 1.36
	40.8 ± 1.48
	52.4 ± 1.78
	59.6 ± 1.88
	46.2 ± 1.62
	63.8 ± 1.94
	69.4 ± 2.02

	45
	16.8 ± 0.88
	32.6 ± 1.38
	38.4 ± 1.46
	43.2 ± 1.58
	48.6 ± 1.72
	61.4 ± 1.86
	67.8 ± 1.96
	54.8 ± 1.84
	72.6 ± 2.08
	77.8 ± 2.16

	60
	18.4 ± 1.24
	38.4 ± 1.74
	43.6 ± 1.58
	48.2 ± 1.86
	54.3 ± 1.94
	66.8 ± 2.02
	73.4 ± 1.96
	61.2 ± 2.08
	78.4 ± 2.14
	84.6 ± 1.92
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