Supplementary Information (SI)

Remediation of Heavy Metals from Industrial Calcium-Rich Waste Generated during Sugar Beet Processing by Optimization of Chemical Precipitation Parameters

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

1:

Dilution ratio (-)

Fig. S1 The removal efficiency (%) of HMs during the precipitation method by applying different dilution ratios after a contact time of 180 minutes and at a pH level of 9.0

Table S1 The analysis of variance (ANOVA) results (F and P-values) of the removal efﬁciency (%) for the HMs at different dilution ratios under optimal conditions

| Element | F | P-value |
| --- | --- | --- |
| Al | 1893.215 | 1.21E-07 |
| Cr | 1378.219 | 2.67E-07 |
| Cu | 1438.307 | 2.4E-07 |
| Fe | 1934.208 | 1.15E-07 |
| Hg | 933.6071 | 7.05E-07 |
| Mg | 579.5624 | 2.3E-06 |
| Mn | 661.4894 | 1.66E-06 |
| Pb | 1793.469 | 1.39E-07 |
| Si | 1715.277 | 1.55E-07 |
| Ti | 1544.653 | 2.01E-07 |
| Zn | 1534.382 | 2.04E-07 |

Contact time (min)

Fig. S2 The removal efficiency (%) of HMs in the precipitation method by applying different contact times.

Table S2 The ANOVA results (F and P-values) of the removal efﬁciency (%) for the HMs at different contact times under optimal conditions

| Element | F | P-value |
| --- | --- | --- |
| Al | 3.959831 | 0.140693 |
| Cr | 3.700423 | 0.150099 |
| Cu | 3.217358 | 0.170754 |
| Fe | 3.672952 | 0.151157 |
| Hg | 4.434624 | 0.125862 |
| Mg | 8.489389 | 0.061813 |
| Mn | 8.006509 | 0.066213 |
| Pb | 7.199482 | 0.074846 |
| Si | 3.67111 | 0.151229 |
| Ti | 2.706037 | 0.198519 |
| Zn | 3.05837 | 0.178638 |

EDTA concentration (M)

Fig. S3 The removal efficiency (%) of HMs in the precipitation method by applying different chelating agent concentrations.

Table S3 The ANOVA results (F and P-values) of the removal efﬁciency (%) for the HMs at different concentrations of EDTA under optimal conditions

| Element | F | P-value |
| --- | --- | --- |
| Al | 101.3642 | 3.09E-03 |
| Cr | 91.5943 | 3.98E-03 |
| Cu | 96.5221 | 3.49E-03 |
| Fe | 108.3953 | 2.62E-03 |
| Hg | 97.5002 | 3.41E-03 |
| Mg | 72.5541 | 6.26E-03 |
| Mn | 66.2831 | 8.71E-03 |
| Pb | 66.4548 | 8.53E-03 |
| Si | 102.0671 | 3.07E-03 |
| Ti | 83.9484 | 4.95E-03 |
| Zn | 77.3903 | 5.99E-03 |

pH

Fig. S4 The removal efficiency (%) of HMs in the precipitation method by applying different pH levels and contact times.

Table S4 The ANOVA results (F and P-values) of the removal efﬁciency (%) for the HMs under different pH levels under optimal conditions

| Element | F | P-value |
| --- | --- | --- |
| Al | 187.7143 | 3.72E-05 |
| Cr | 160.7652 | 5.42E-05 |
| Cu | 258.3835 | 1.7E-05 |
| Fe | 187.2765 | 3.74E-05 |
| Hg | 167.9446 | 4.88E-05 |
| Mg | 56.95569 | 0.000647 |
| Mn | 56.32469 | 0.000664 |
| Pb | 62.40975 | 0.000523 |
| Si | 180.2077 | 4.11E-05 |
| Ti | 156.8024 | 5.76E-05 |
| Zn | 150.9452 | 6.32E-05 |