Supplemental Information

Visualization of Long-Range Order in Self-Assembled Ion Barriers for Stable Perovskite Tandems

This Supplementary Information includes:

Supplementary Text

Supplementary Figs. 1–24

Supplementary Tables 1–12

# Supplementary Text

Note 1: SCLC method

The Nt can be calculated using the following equation 1

Nt=2εε0VTFLqL2 #S1

Where q is the elementary charge, L is the perovskite film thickness, ε0 is the vacuum permittivity, ε is the relative dielectric constant, and VTFL is the onset voltage of the trap-filled limit region.

The charge carrier mobility of the HTM films was measured using the SCLC technique. Hole-only devices were fabricated in a structure of ITO/C60/ETL/Ag. The device characteristics were extracted by modeling the dark current under forward bias using the Mott-Gurney law 2:

J=98εrε0μV2L3#S2

Here, εr is the average dielectric constant of the film, ε0 is the permittivity of the free space, μ is the carrier mobility, L is the thickness of the film, and V is the applied voltage.

Note 2: TRPL method

TRPL was performed on Delta Flex TCSPC system (Horiba, Japan), recorded at 800 nm using excitation with a 520 nm light pulse. The glass substrate was sequentially ultrasonicated in isopropyl alcohol and deionized water for 15 minutes each, followed by a 20-minute UV-ozone treatment. Front-side excitation was employed for all measurements. The PL decay time and amplitudes are modeled using a biexponential expression 3:

ft=iAi exp-tτi+K#S3

where Ai  is the decay amplitude, τi is the decay time and K is a constant for the base-line offset. The average PL decay times (τave) are further estimated using the τi and Ai  values from the fitted data:

τave=Aiτi2Aiτi#S4

Supplementary Figures and Tables：

Supplementary Fig. 1. (a). Thermogravimetric analysis (TGA) curve of PTCDA. (b). Differential scanning calorimetry (DSC) heat-flow curve of PTCDA as a function of temperature.

Supplementary Fig. 2. (a, b) High-resolution STM images of self-assembled C60 and PTCDA on Ag(111) at 77 K. (a) C60 images were acquired at scan sizes of 20 nm × 20 nm (0.9 V, 74 pA; right: FFT pattern). (b) PTCDA images were acquired at 50 nm × 50 nm (1.0 V, 110 pA; right: FFT pattern). (c) Large-area STM image of PTCDA showing long-range ordering (100 nm × 100 nm, V = 1.0 V, I = 49 pA).

Supplementary Fig. 3. GIWAXS profiles of C60 (a) and PTCDA (b) plotted as a function of the scattering vector q.

Supplementary Fig. 4. XPS I 3d spectra of PSK (a), PSK/C60 (b), and PSK/PTCDA (c).

Supplementary Fig. 5. AES spectra of C60 (a) and PTCDA (b) measured on Ag substrates. Characteristic C and Ag Auger features are marked.

Supplementary Fig. 6. Normal distributions of the Ag signal proportion derived from the total C and Ag counts in AES spectra for C60 (a) and PTCDA (b).

Supplementary Fig. 7. ToF-SIMS depth profiling of Pb2+ distribution in w/o SAIB (a) and w/ SAIB (b) PSCs after 72 h of MPPT operation.

Supplementary Fig. 8. ToF-SIMS depth profiling of I- distribution in w/o SAIB (a) and w/ SAIB (b) PSCs after 72 h of MPPT operation.

Supplementary Fig. 9. Top-view Pb2+ distribution maps (from five depths: 50, 100, 150, 400, and 600 nm). a–e correspond to the w/o SAIB sample, and f–j correspond to the w/ SAIB sample.

Supplementary Fig. 10. Top-view I- distribution maps (from five depths: 50, 100, 150, 400, and 600 nm). a–e correspond to the w/o SAIB sample, and f–j correspond to the w/ SAIB sample.

Supplementary Fig. 11. Migration energy barriers of Ag+ ions along the migration pathway in the presence of C60 and PTCDA.

Supplementary Fig. 12. PiFM mapping of w/o and w/ SAIB samples. (a) PiFM mapping of the w/o SAIB sample at wavenumbers 1024 cm-1, and 1772 cm-1. (b) PiFM mapping of the w/ SAIB sample at wavenumbers 1024 cm-1, and 1772 cm-1.

Supplementary Fig. 13. PiFM imaging and spectra of w/o and w/ SAIB samples. (a, b) Surface and bulk PiFM of w/o SAIB samples; (c, d) Surface and bulk PiFM of w/ SAIB samples.

Supplementary Fig. 14. Statistical photovoltaic parameters of wide bandgap PSCs with different SAIB thicknesses; box plots show median and interquartile range, whiskers denote full data spread (n = 22 per group).

Supplementary Fig. 15. Independent efficiency verification of PSK/ Si tandem solar cells. The efficiency is verified by the NREL.

Supplementary Fig. 16. J–V characteristics of the PSK/Si tandem solar cell measured under forward and reverse scan directions.

Supplementary Fig. 17. Changes in the μe of PTCDA caused by Ag+ migration during 0~120 h.

Supplementary Fig. 18. Changes in the μe of C60 caused by Ag+ migration during 0~120 h.

Supplementary Fig. 19. Changes in the μe of PTCDA/C60 caused by Ag+ migration during 0~120 h.

Supplementary Fig. 20. SCLC characteristics of C60-based electron-only devices during 0~120 h.

Supplementary Fig. 21. SCLC characteristics of PTCDA/C60-based electron-only devices during 0~120 h.

Supplementary Fig. 22. Evolution of the TRPL decay curves of PSK/AgI during 0~120 h.

Supplementary Fig. 23. Evolution of the TRPL decay curves of PSK/C60/AgI during 0~120 h.

Supplementary Fig. 24. Evolution of the TRPL decay curves of PSK/PTCDA/C60/AgI during 0~120 h.

Supplementary Table 1. Summary of the characteristic scattering peaks (q) and corresponding d-spacing values of C60 and PTCDA films.

| Sample | q (Å-1) | d (Å) |
| --- | --- | --- |
| C60 | 0.78 | 8.05 |
|  | 1.40 | 4.48 |
|  | 2.02 | 3.11 |
| PTCDA | 0.62 | 10.13 |
|  | 0.88 | 7.14 |
|  | 1.80 | 3.49 |
|  | 1.98 | 3.17 |

Supplementary Table 2. Ag 3d XPS fitting parameters of the perovskite surface with different interfacial layers.

| Sample | Ag+/(Ag+ + Ag0) (%) | 3d3/2 (eV) |  | 3d5/2 (eV) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Ag0 | Ag+ | Ag0 | Ag+ |
| Metal silver layer | 15.21 | 374.69 | 375.51 | 368.65 | 369.35 |
| 2 nm C60 | 9.63 | 374.63 | 375.30 | 368.66 | 369.40 |
| 2 nm PTCDA | 1.30 | 374.80 | 375.65 | 368.78 | 369.70 |

Supplementary Table 3. Pb 4f XPS fitting parameters of the perovskite surface with different interfacial layers.

| Sample | Pb0/( Pb0 + Pb2) (%) | 4f5/2 (eV) |  | 4f7/2 (eV) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Pb0 | Pb2 | Pb0 | Pb2 |
| PSK | 20.12 | 142.85 | 143.40 | 137.71 | 138.45 |
| PSK/C60 | 3.96 | 142.84 | 143.39 | 137.74 | 138.44 |
| PSK/PTCDA | 0 | none | 143.52 | none | 138.60 |

Supplementary Table 4. Statistical photovoltaic parameters of w/o SAIB WBG PSCs.

| Sample | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| SAIB-free | 1.22 | 20.71 | 81.99 | 20.68 |
|  | 1.22 | 21.98 | 82.81 | 22.22 |
|  | 1.21 | 20.89 | 81.73 | 20.66 |
|  | 1.21 | 20.93 | 81.39 | 20.54 |
|  | 1.20 | 20.63 | 81.88 | 20.32 |
|  | 1.23 | 21.93 | 82.07 | 22.06 |
|  | 1.19 | 21.33 | 81.61 | 20.70 |
|  | 1.18 | 20.61 | 80.85 | 19.68 |
|  | 1.22 | 21.28 | 81.78 | 21.26 |
|  | 1.23 | 20.64 | 82.67 | 21.04 |
|  | 1.22 | 21.28 | 81.78 | 21.26 |
|  | 1.22 | 20.55 | 82.56 | 20.64 |
|  | 1.21 | 21.44 | 81.20 | 21.13 |
|  | 1.23 | 21.38 | 81.50 | 21.36 |
|  | 1.21 | 21.27 | 80.88 | 20.81 |
|  | 1.21 | 21.65 | 81.12 | 21.23 |
|  | 1.22 | 21.57 | 80.33 | 21.17 |
|  | 1.24 | 21.24 | 80.34 | 21.16 |
|  | 1.21 | 20.92 | 81.65 | 20.74 |
|  | 1.23 | 20.97 | 81.42 | 21.07 |
|  | 1.23 | 22.09 | 80.48 | 21.83 |
|  | 1.23 | 22.17 | 82.06 | 22.43 |

Supplementary Table 5. Statistical photovoltaic parameters of 1 nm SAIB WBG PSCs.

| Sample | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| 1 nm SAIB | 1.23 | 21.45 | 82.87 | 21.80 |
|  | 1.23 | 21.52 | 83.08 | 22.03 |
|  | 1.22 | 21.60 | 82.92 | 21.90 |
|  | 1.24 | 21.82 | 82.97 | 22.49 |
|  | 1.24 | 20.99 | 82.38 | 21.48 |
|  | 1.25 | 21.67 | 83.65 | 22.63 |
|  | 1.24 | 21.87 | 83.52 | 22.65 |
|  | 1.24 | 21.40 | 82.97 | 21.98 |
|  | 1.22 | 21.47 | 82.22 | 21.61 |
|  | 1.24 | 21.95 | 82.14 | 22.37 |
|  | 1.25 | 21.76 | 83.19 | 22.58 |
|  | 1.22 | 21.19 | 82.73 | 21.38 |
|  | 1.22 | 20.99 | 82.33 | 21.09 |
|  | 1.23 | 21.74 | 82.98 | 22.15 |
|  | 1.25 | 21.80 | 83.43 | 22.67 |
|  | 1.21 | 21.20 | 81.87 | 21.03 |
|  | 1.22 | 21.01 | 82.08 | 21.05 |
|  | 1.22 | 21.20 | 81.92 | 21.27 |
|  | 1.24 | 21.32 | 81.97 | 21.60 |
|  | 1.23 | 21.29 | 81.38 | 21.32 |
|  | 1.24 | 21.77 | 82.65 | 22.40 |
|  | 1.24 | 21.37 | 82.52 | 21.84 |

Supplementary Table 6. Statistical photovoltaic parameters of 2 nm SAIB WBG PSCs.

| Sample | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| 2 nm SAIB | 1.24 | 22.00 | 84.06 | 22.89 |
|  | 1.24 | 22.00 | 83.15 | 22.72 |
|  | 1.27 | 21.85 | 84.39 | 23.36 |
|  | 1.27 | 22.00 | 83.82 | 23.33 |
|  | 1.23 | 21.93 | 82.68 | 22.30 |
|  | 1.23 | 22.47 | 82.19 | 22.70 |
|  | 1.26 | 22.21 | 81.79 | 22.83 |
|  | 1.25 | 20.68 | 84.27 | 21.75 |
|  | 1.24 | 22.60 | 83.24 | 23.33 |
|  | 1.25 | 21.75 | 83.34 | 22.62 |
|  | 1.27 | 21.85 | 84.57 | 23.41 |
|  | 1.24 | 22.12 | 82.22 | 22.59 |
|  | 1.25 | 21.78 | 82.66 | 22.41 |
|  | 1.24 | 22.50 | 83.24 | 23.22 |
|  | 1.26 | 22.12 | 83.72 | 23.35 |
|  | 1.23 | 21.97 | 82.42 | 22.34 |
|  | 1.23 | 22.29 | 82.48 | 22.58 |
|  | 1.23 | 22.17 | 82.06 | 22.43 |
|  | 1.24 | 22.12 | 83.92 | 23.06 |
|  | 1.21 | 21.46 | 84.76 | 22.08 |
|  | 1.23 | 22.47 | 82.19 | 22.70 |
|  | 1.26 | 21.35 | 84.62 | 22.67 |

Supplementary Table 7. Statistical photovoltaic parameters of 3 nm SAIB WBG PSCs.

| Sample | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| 3 nm SAIB | 1.20 | 21.43 | 81.36 | 20.92 |
|  | 1.22 | 21.48 | 82.57 | 21.55 |
|  | 1.21 | 20.74 | 80.28 | 20.09 |
|  | 1.21 | 20.73 | 80.61 | 20.15 |
|  | 1.21 | 21.58 | 81.37 | 21.17 |
|  | 1.21 | 21.03 | 81.45 | 20.75 |
|  | 1.19 | 21.29 | 81.11 | 20.61 |
|  | 1.20 | 21.33 | 81.17 | 20.81 |
|  | 1.20 | 21.71 | 81.54 | 21.21 |
|  | 1.20 | 20.51 | 81.82 | 20.21 |
|  | 1.21 | 20.17 | 82.23 | 20.08 |
|  | 1.20 | 20.30 | 81.92 | 20.01 |
|  | 1.20 | 21.18 | 82.74 | 21.10 |
|  | 1.21 | 21.24 | 82.80 | 21.30 |
|  | 1.21 | 21.14 | 82.76 | 21.17 |
|  | 1.20 | 21.33 | 80.37 | 20.49 |
|  | 1.19 | 21.59 | 81.45 | 21.00 |
|  | 1.19 | 21.13 | 81.11 | 20.36 |
|  | 1.21 | 21.21 | 80.17 | 20.57 |
|  | 1.19 | 20.11 | 80.54 | 19.34 |
|  | 1.21 | 21.17 | 80.82 | 20.67 |
|  | 1.19 | 21.13 | 81.54 | 20.54 |

Supplementary Table 8. Statistical photovoltaic parameters of w/ SAIB PSK/Si tandem.

| Sample |  | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | Forword | 2.006 | 20.37 | 84.36 | 34.48 |
|  | Reverse | 2.007 | 20.37 | 84.57 | 34.58 |
| 2 | Forword | 2.003 | 20.36 | 83.76 | 34.14 |
|  | Reverse | 2.004 | 20.34 | 83.90 | 34.20 |
| 3 | Forword | 2.009 | 20.43 | 83.78 | 34.39 |
|  | Reverse | 2.010 | 20.42 | 84.03 | 34.50 |
| 4 | Forword | 2.009 | 20.43 | 83.47 | 34.26 |
|  | Reverse | 2.010 | 20.43 | 83.70 | 34.38 |
| 5 | Forword | 2.007 | 20.29 | 84.27 | 34.32 |
|  | Reverse | 2.008 | 20.28 | 84.49 | 34.42 |
| 6 | Forword | 2.007 | 20.39 | 84.02 | 34.39 |
|  | Reverse | 2.008 | 20.39 | 84.19 | 34.48 |
| 7 | Forword | 2.007 | 20.31 | 83.43 | 34.02 |
|  | Reverse | 2.008 | 20.31 | 83.56 | 34.09 |
| 8 | Forword | 2.008 | 20.43 | 83.49 | 34.26 |
|  | Reverse | 2.009 | 20.42 | 83.70 | 34.35 |
| 9 | Forword | 2.005 | 20.38 | 83.94 | 34.31 |
|  | Reverse | 2.006 | 20.38 | 84.07 | 34.37 |
| 10 | Forword | 2.003 | 20.38 | 82.98 | 33.89 |
|  | Reverse | 2.004 | 20.38 | 83.13 | 34.97 |

Supplementary Table 9. Photovoltaic parameters of the PSK/Si tandem solar cell, measured under forward and reverse J–V scans.

| Sample |  | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| Reverse |  | 2.007 | 20.37 | 84.57 | 34.58 |
|  | Forword | 2.006 | 20.37 | 84.36 | 34.48 |

Supplementary Table 10. Evolution of electron mobility (μe) in C60, PTCDA/ C60, and PTCDA films induced by Ag-ion migration during aging from 0 to 120 h.

| Sample | C60 | PTCDA-C60 |
| --- | --- | --- |
|  | ×10-4 cm2 V-1 s-1 |  |
| 0 h | 1.052 | 1.118 |
| 12 h | 1.055 | 1.118 |
| 24 h | 1.060 | 1.118 |
| 36 h | 1.100 | 1.202 |
| 48 h | 1.162 | 1.235 |
| 60 h | 1.188 | 1.262 |
| 72 h | 1.225 | 1.277 |
| 84 h | 1.227 | 1.282 |
| 96 h | 1.230 | 1.290 |
| 108 h | 1.233 | 1.298 |
| 120 h | 1.234 | 1.300 |

Supplementary Table 11. Evolution of defect density (Nₜ) in C60 and PTCDA/ C60 films induced by Ag-ion migration during aging from 0 to 120 h.

| Sample | C60 | PTCDA-C60 |
| --- | --- | --- |
|  | ×1015 cm3 |  |
| 0 h | 1.98 | 1.85 |
| 12 h | 1.96 | 1.86 |
| 24 h | 2.02 | 1.87 |
| 36 h | 2.18 | 1.91 |
| 48 h | 2.39 | 2.07 |
| 60 h | 2.47 | 2.05 |
| 72 h | 2.62 | 2.18 |
| 84 h | 2.66 | 2.22 |
| 96 h | 2.77 | 2.21 |
| 108 h | 2.95 | 2.24 |
| 120 h | 3.01 | 2.25 |

Supplementary Table 12. Evolution of TRPL lifetimes of perovskite films with PSK/Ag, PSK/C60/Ag, and PSK/PTCDA/C60/Ag architectures during aging from 0 to 120 h.

| Sample | PSK/C60/AgI | PSK/PTCDA/C60/AgI |
| --- | --- | --- |
|  | ns |  |
| 0 h | 80.22 | 75.21 |
| 12 h | 78.76 | 73.22 |
| 24 h | 75.79 | 68.57 |
| 36 h | 70.81 | 65.61 |
| 48 h | 62.77 | 64.53 |
| 60 h | 59.81 | 64.45 |
| 72 h | 53.88 | 63.84 |
| 84 h | 46.89 | 62.92 |
| 96 h | 42.90 | 60.16 |
| 108 h | 38.17 | 57.51 |
| 120 h | 35.62 | 52.63 |

References and Notes

- Shi, D. et al. Low trap-state density and long carrier diffusion in organolead trihalide perovskite single crystals. Science 347, 519–522 (2015).

- Herz, L. M. Charge-carrier mobilities in metal halide perovskites: Fundamental mechanisms and limits. ACS Energy Lett. 2, 1539–1548 (2017).

- de Quilettes, D. W. et al. Impact of microstructure on local carrier lifetime in perovskite solar cells. Science 348, 683–686 (2015).