Supplementary material for

Multivariate synthesis optimization, comprehensive characterization, and surface ligand determination of palladium nanoparticles

Eduardo Sidinei Chaves1,3*, Morgana Lurdes da Rocha1, Isabella Tavernaro2,

Ute Resch-Genger2* and Björn Meermann3*

1Federal University of Santa Catarina, Department of Chemistry, Florianópolis, Brazil.

2Federal Institute for Materials Research and Testing, Division 1.2- Biophotonics, Berlin, Germany.

3Federal Institute for Materials Research and Testing, Division 1.1- Inorganic Trace Analysis (ITALab), Berlin, Germany.

* Corresponding authors:  ute.resch@bam.de

bjoern.meermann@bam.de

eduardo.chaves@ufsc.br

Content:

Tables S1 to S10

Figures S1 to S7

Table S1. Experiments, real and coded values for PdNP optimization 25-1 fractionated factorial design.

Experiment; Temperature oC; Time Min.; Pd µmol; Ligand mmol; Ascorbic Acid mmol; 1-PDI. 1; 25 (-1); 30 (-1); 2 (-1); 0.02 (-1); 0.25 (+1); 0.800. 2; 25 (-1); 30 (-1); 2 (-1); 0.14 (+1); 0.05 (-1); 0.793. 3; 25 (-1); 30 (-1); 16 (+1); 0.02 (-1); 0.05 (-1); 0.700. 4; 25 (-1); 30 (-1); 16 (+1); 0.14(+1); 0.25 (+1); 0.731. 5; 25 (-1); 180 (+1); 2 (-1); 0.02 (-1); 0.05 (-1); 0.802. 6; 25 (-1); 180 (+1); 2 (-1); 0.14 (+1); 0.25 (+1); 0.792. 7; 25 (-1); 180 (+1); 16 (+1); 0.02 (-1); 0.25 (+1); 0.711. 8; 25 (-1); 180 (+1); 16 (+1); 0.14 (+1); 0.05 (-1); 0.755. 9; 75 (+1); 30 (-1); 2 (-1); 0.02 (-1); 0.05 (-1); 0.719. 10; 75 (+1); 30 (-1); 2 (-1); 0.14 (+1); 0.25 (+1); 0.752. 11; 75 (+1); 30 (-1); 16 (+1); 0.02 (-1); 0.25 (+1); 0.818. 12; 75(+1); 30 (-1); 16 (+1); 0.14 (+1); 0.05 (-1); 0.838. 13; 75 (+1); 180 (+1); 2 (-1); 0.02 (-1); 0.25 (+1); 0.747. 14; 75 (+1); 180 (+1); 2 (-1); 0.14 (+1); 0.05 (-1); 0.631. 15; 75(+1); 180 (+1); 16 (+1); 0.02 (-1); 0.05 (-1); 0.833. 16; 75 (+1); 180 (+1); 16 (+1); 0.14 (+1); 0.25 (+1); 0.841. 17; 50 (0); 105 (0); 9 (0); 0.080 (0); 0.15 (0); 0.833. 18; 50 (0); 105 (0); 9 (0); 0.080 (0); 0.15 (0); 0.824. 19; 50 (0); 105 (0); 9 (0); 0.080 (0); 0.15 (0); 0.805.

Ligand: 3-mercaptopropionic acid (MPA)

Figure S1. Pareto´s Chart for the fractionated factorial design 25-1 optimization of the water-based PdNPs synthesis.  Effect of the synthesis´ parameters of the PdNPs, at a confidence level of 95%, significant effect on the PDI showed p<0.05.

Table S2. ANOVA of the factorial 25-1 design optimization of the PdNPs synthesis capped with thiol-based ligand.

| Fator | SS | df | MS | F | p |
| --- | --- | --- | --- | --- | --- |
| Curvature | 0.006760 | 1 | 0.006760 | 33.0841 | 0.028921 |
| (1) Temperature, oC | 0.001139 | 1 | 0.001139 | 5.5745 | 0.142120 |
| (2) Time, min | 0.000000 | 1 | 0.000000 | 0.0003 | 0,987634 |
| (3) Pd, µ mol | 0.001425 | 1 | 0.001425 | 6.9742 | 0.118445 |
| (4) Ligand, m mol | 0.000116 | 1 | 0.000116 | 0.5656 | 0.530487 |
| (5) Ascorbic acid, m mol | 0.000410 | 1 | 0.000410 | 2.0068 | 0.292291 |
| 1 by 2 | 0.000315 | 1 | 0.000315 | 1.5419 | 0,340203 |
| 1 by 3 | 0.033398 | 1 | 0.033398 | 163.4465 | 0.006063 |
| 1 by 4 | 0,000333 | 1 | 0.000333 | 1.6300 | 0.329899 |
| 1 by 5 | 0.000798 | 1 | 0.000798 | 3.9057 | 0.186770 |
| 2 by 3 | 0.000689 | 1 | 0.000689 | 3.3722 | 0.207715 |
| 2 by 4 | 0.000770 | 1 | 0.000770 | 3.7687 | 0.191731 |
| 2 by 5 | 0.000028 | 1 | 0.000028 | 0.1349 | 0.748637 |
| 3 by 5 | 0.001661 | 1 | 0.001661 | 8.1267 | 0.104175 |
| 3 by 5 | 0.001073 | 1 | 0.001073 | 5.2491 | 0.149058 |
| 4 by 5 | 0.000086 | 1 | 0.000086 | 0.4187 | 0.583919 |
| Pure error | 0.000409 | 2 | 0.000204 |  |  |
| Total SS | 0.006760 | 18 |  |  |  |

R2:0.99173; Adj.: 0.92556; MS Pure error:0.0002043.

Ligand: 3-mercaptopropionic acid

Table S3. ANOVA of the Doehlert design optimization of the PdNPs synthesis capped with 3-mercaptopropionic acid (MPA) based on the 1-PDI.

| Fator | SS | df | MS | F | p |
| --- | --- | --- | --- | --- | --- |
| (1) Pd, µ mol (L) | 0.001752 | 1 | 0.001752 | 2.666794 | 0.244063 |
| Pd, µ mol (Q) | 0.000389 | 1 | 0.000389 | 0.591781 | 0.522161 |
| (2) Temperature, oC(L) | 0.001482 | 1 | 0.001482 | 2.256088 | 0.271931 |
| Temperature, oC(Q) | 0.000128 | 1 | 0.000128 | 0.195028 | 0.701923 |
| 1L by 2L | 0.000020 | 1 | 0.000020 | 0.030822 | 0.876805 |
| Lack of fit | 0.000840 | 1 | 0.000840 | 1.278792 | 0.375485 |
| Pure error | 0.001314 | 2 | 0.000657 |  |  |
| Total SS | 0.006040 | 8 |  |  |  |

R2:0.64366; Adj.: 0.04897; 2 factors;1 block, 9 runs; MS Pure error:0.000657.

Table S4. ANOVA of the Doehlert design optimization of the PdNPs synthesis capped with L-cysteine based on the 1-PDI.

| Fator | SS | df | MS | F | p |
| --- | --- | --- | --- | --- | --- |
| (1) Pd, µ mol (L) | 0.016576 | 1 | 0.016576 | 12.10540 | 0.073604 |
| Pd, µ mol (Q) | 0.002803 | 1 | 0.002803 | 2.04722 | 0.288780 |
| (2) Temperature, oC(L) | 0.000121 | 1 | 0.000121 | 0. 08836 | 0.794300 |
| Temperature, oC(Q) | 0.005603 | 1 | 0.005603 | 4.09202 | 0.180426 |
| 1L by 2L | 0.000784 | 1 | 0.000784 | 0.57254 | 0.528239 |
| Lack of fit | 0.000451 | 1 | 0.000451 | 0.32911 | 0.624095 |
| Pure error | 0.002739 | 2 | 0.001369 |  |  |
| Total SS | 0.027776 | 8 |  |  |  |

R2:0.88518; Adj.: 0.69381; 2 factors;1 block, 9 runs; MS Pure error:0.0013693.

Figure S2. Sulfur concentration in the PdNP-MPA and PdNP-Cys supernatant according to the washing cycles.

Table S5. ANOVA from pared t-test with 95% of confidence, comparing NTA and DLS data

|  | DLS | NTA |
| --- | --- | --- |
| Mean | 136 | 127,5 |
| Variance | 1250 | 480,5 |
| Observations | 2 | 2 |
| Pearson Correlation | 1 |  |
| Hypothesized Mean Difference | 0 |  |
| df | 1 |  |
| T Stat t | 0.894737 |  |
| P(T<=t) one-tail | 0.267666 |  |
| t critical one-tail | 6.313752 |  |
| P(T<=t) two-tail | 0.535331 |  |
| t critical two-tail | 12.7062 |  |

Figure S3. DLS number-based size distribution for PdNP-MPA and PdNP-Cys.

Figure S4. NTA particle size distribution for PdNP-MPA and PdNP-Cys.

Figure S5. Size, size distribution and particle number obtained by (A) sp-ICP-MS and (B) NTA for reference material of PtNP.

Figure S6. Dilution effect in the (A) particle size and (B) number obtained by sp-ICP-MS.

Table S6. ANOVA from pared t-test with 95% of confidence, comparing NTA and sp-ICP-MS data

|  | Sp-ICP-MS | NTA |
| --- | --- | --- |
| Mean | 1.63E+13 | 1.68E+15 |
| Variance | 1.01E+25 | 1.35E+29 |
| Observations | 2 | 2 |
| Pearson Correlation | 1 |  |
| Hypothesized Mean Difference | 0 |  |
| df | 1 |  |
| T Stat t | -6.4549 |  |
| P(T<=t) one-tail | 0.048924 |  |
| t critical one-tail | 6.313752 |  |
| P(T<=t) two-tail | 0.097848 |  |
| t critical two-tail | 12.7062 |  |

Table S7. ANOVA one-way with 95% of confidence, comparing the ligand density considering PdNP with different morphologies.

| Source of Variation | SS | Df | MS | F | P-value | F crit |
| --- | --- | --- | --- | --- | --- | --- |
| Between Groups | 18.30525742 | 4 | 4.576314354 | 1.609253 | 0.246545 | 3.47805 |
| Within Groups | 28.43750867 | 10 | 2.843750867 |  |  |  |
| Total | 46.74276609 | 14 |  |  |  |  |

Table S8. Variables, coded values, and levels for PdNPs synthesis by 25-1 fractionated factorial design.

Variables; Levels. -1; 0; +1. Temperature, oC; 25; 50; 75. Time, min.; 30; 105; 180. Pd, µmol; 2; 9; 16. Ligand, mmol; 0.02; 0.08; 0.14. Ascorbic acid, mmol; 0.05; 0.15; 0.25.

Table S9.  Coded and real variables for Doehlert design optimization of the PdNPs synthesis capped with 3-mercaptopropionic acid (MPA) and L-cysteine (Cys), based on the PDI results.

| Experiment | Factors |  | MPA |  | Cys |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | X1(Pd, µ mol) | X2 (T, oC) | PDI | 1-PDI | PDI | 1-PDI |
| 1 | -1 (10) | 0 (60) | 0.237 | 0.763 | 0.181 | 0.819 |
| 2 | -0.5 (15) | -0.866 (40) | 0.244 | 0.756 | 0.229 | 0.771 |
| 3 | -0.5 (15) | 0.866 (80) | 0.201 | 0.799 | 0.212 | 0.788 |
| 4 | 0.5 (25) | -0.866 (40) | 0.239 | 0.761 | 0.258 | 0.742 |
| 5 | 0.5 (25) | 0.866 (80) | 0.205 | 0.795 | 0.297 | 0.703 |
| 6 | 1 (30) | 0 (60) | 0.165 | 0.835 | 0.347 | 0.653 |
| 7 | 0 (20) | 0 (60) | 0.243 | 0.757 | 0.289 | 0.711 |
| 8 | 0 (20) | 0 (60) | 0.222 | 0.778 | 0.293 | 0.707 |
| 9 | 0 (20) | 0 (60) | 0.192 | 0.808 | 0.355 | 0.645 |

Figure S7. Schematic representation of the unbounded ligand removal of the PdNP-MPA and PdNP-Cys

Table S10. Instrumental parameters for the ICP-MS and sp-ICP-MS measurements.

| RF power, W | 1550 |  |
| --- | --- | --- |
| Plasma gas flow rate, L min-1 | 15.0 |  |
| Auxiliary gas flow rate L min-1 | 0.90 |  |
| Nebulizer | Concentric |  |
| sample uptake, mL min-1 | 0.346 |  |
|  | sp-ICP-MS mode | ICP-MS mode |
| Torch injector | 1.5 mm | 2.5 mm |
| Dwell time, ms | 100 | 0.1 |
| Collision / Reaction gas | No gas | He: 5.5 mL min-1(Pd) O2: 0.3 mL min-1 (S) |
| Gas flow nebulizer, L min-1 | 0.80 | 1.07 |
| Monitored isotopes | 105Pd, 194Pt | 32S, ³²S¹⁶O⁺, 105Pd, 103Rh (IS) |
| Limit of detection | LODsize 30 nm | Pd 10 ng L-1 |
|  | LODconc. 1.3 ng L-1 | Pd 17 ng L-1 |

.