Supplementary Material

# Mechano-Carbonation of Portland Cement Paste: Simultaneous Milling and Aqueous Carbonation to Accelerate Carbonation Process

Jonathan Smith1, Kiersten Williams1, Juan Pablo Gevaudan 1, †

1Department of Architectural Engineering, The Pennsylvania State University, 408 ECORE Building, 556 White Course Dr, University Park, PA 16801, USA. †Corresponding Author: jp.gevaudan@psu.edu

Appendix A:

The Type 1 OPC sample provided by Heidelberg Materials has 3.1%wt limestone and 1.86%wt gypsum already added, as identified by the manufacturer’s mill test report. To ensure the LS batch has exactly 15% limestone, 5% gypsum, and 80% OPC the following system of equations was developed to calculate paste mixtures. The same system was used for preparing the cOPC batches while adjusting for the difference in density of cOPC samples (2.634 g/cm3 limestone, 2.431 g/cm3 cOPC [Table 6]). This ensures the same volumes of OPC, gypsum, and filler (cOPC or limestone) are present across all samples, ensuring a controlled comparison of the fresh-state properties of the fillers. The calculation procedure utilized in this paper is shown in equations 1-7 and mixture proportions are shown in Table A1.

OPCLS=0.801-0.031-0.0186=84.18%#1

FillerLS=0.15-0.8418*0.031=12.39%#2

GypsumLS=0.05-0.8418*0.0186=3.43%#3

Fillerequal volume=FillerLS*ρcOPCρLS=0.1239*2.4312.634=11.44%#4

OPCcOPC=OPCLSOPCLS+Fillerequalvolume+GypsumLS=0.84180.9905=84.99%#5

FillercOPC=Fillerequal volumeOPCLS+Fillerequal volume+GypsumLS=0.11440.9905=11.55%#6

GypsumcOPC=GypsumLSOPCLS+Fillerequalvolume+GypsumLS=0.03430.9905=3.46%#7

Table A1. Mixture proportions table for samples studied in this study.

|  | Paste Mixtures (wt.%) |  |  |  |
| --- | --- | --- | --- | --- |
| Sample Name | OPC | Limestone | Gypsum | cOPC |
| LS | 84.18 | 12.39 | 3.43 | - |
| cOPC | 84.99 | - | 3.46 | 11.55 |

Appendix B:

Carbonation calculations for the samples presented in this study are as follows. Data for the calculation of ThCO2(%max) was obtained from XRF data in Table 2 and adjusted with LOI obtained from TGA. ΔmonsetTGA was obtained from TGA-DSC data detailed in 2.4.9 and analyzed using the standardized onset method established by Chiang and Pan21.  mOPC limestone was obtained from the mill test report provided by Heidelberg Materials.

Table B1: XRF data with LOI from Table 2 (this study)

|  | CaO | SiO2 | Al2O3 | Fe2O3 | SrO | K2O | TiO2 | MgO | SO3 | Na2O | Other | LOI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 28-day OPC | 44.7 | 13.5 | 3.7 | 1.52 | 0 | 0.74 | 0 | 2.03 | 2.24 | 0.18 | 2.19 | 29.2 |

ThCO2%max=M CO2M CaO*CaO=0.785*CaO

ThCO2%max=0.785*44.7

ThCO2%max=0.351 kgCO2/kg

Δmmax=ThCO21+ThCO2*100=0.3511+0.341*100=26.0%wt

ΔmCO2MC=ΔmonsetTGA-mOPC limestoneMCO2MCaCO3=25.04-3.144.009100.0869=23.7%wt

DOCMC=ΔmCO2Δmmax*100=23.7%26.0%*100=91.2%

Degree of carbonation calculations for the samples presented in Teune et al. are as follows7. Data for the calculation of ThCO2(%max) was obtained from XRF data in Table 2, ΔmonsetTGA from TGA-DSC data presented in figure 1 and analyzed using the standardized onset method established by Chiang and Pan21.  mHP-I limestone was taken from Table 3 QXRD results. The XRF data presented in Teune et al is copied below in Table B27.

Table B2: XRF Data from 7.

| XRF (wt%) | LOI | CaO | SiO2 | Al2O3 | MgO | SO3 | Fe2O3 | Other |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HP-1 | 26.2 | 50.6 | 13.1 | 3.0 | 0.9 | 2.7 | 2.9 | 0.5 |

ThCO2%max=0.785*CaO

ThCO2%max=0.785*50.6

ThCO2%max=0.397 kgCO2/kg

Δmmax=ThCO21+ThCO2*100=0.3971+0.397*100=28.4%wt

ΔmCO2ACH-I=ΔmonsetTGA-mHP-1 limestoneQXRDMCO2MCaCO3=(22-2.544.009100.0869)=20.9%wt

DOCACH-I=ΔmCO2Δmmax*100=20.9%28.4%*100=73.6%

ΔmCO2ACNa-I=ΔmonsetTGA-mHP-1 limestoneQXRDMCO2MCaCO3=23-2.544.009100.0869=21.9%wt

DOCACH-I=ΔmCO2Δmmax*100=21.9%28.4%*100=77.1%

ΔmCO2DC-I=ΔmonsetTGA-mHP-1 limestoneQXRDMCO2MCaCO3=13-2.544.009100.0869=11.9%wt

DOCDC-I=ΔmCO2Δmmax*100=11.9%28.4%*100=38.7%