Supporting Information

Synergy of Single Atoms Pd and Oxygen Vacancies on In2O3 for Highly Selective C1 Oxygenates Production from Methane under Visible Light

Lei Luo, Lei Fu, Huifen Liu, Youxun Xu, Jialiang Xing, Junwang Tang*

Figure S1. XRD patterns of In2O3, Pd-In2O3 and Pd-def-In2O3.

Figure S2. (a, b) HRTEM images of Pd-In2O3. In the region marked by yellow dash in panel b, no defective layer was observed on the edge of the Pd-In2O3 nanorods, suggesting the defect-lean structure of Pd-In2O3.

Figure S3. In-situ Pd3d XPS spectra of Pd-def-In2O3 in dark and under light.

Figure S4. Photocurrent responses of In2O3, Pd-In2O3 and Pd-def-In2O3.

Figure S5. Time-decay PL spectra of In2O3, Pd-In2O3 and Pd-def-In2O3.

Table S1. Fitted PL lifetime from time-decay PL spectra of In2O3, Pd-In2O3 and Pd-def-In2O3.

| Sample | α1 | τ1 [ns] | α2 | τ2 [ns] | τ [ns] |
| --- | --- | --- | --- | --- | --- |
| In2O3 | 0.98 | 49.9 | 6.21 | 50.1 | 3.60 |
| Pd-In2O3 | 1.03 | 44.4 | 6.87 | 55.6 | 4.28 |
| Pd-def-In2O3 | 1.00 | 36.8 | 7.32 | 63.2 | 4.99 |