Samarium-Promoted Ni/YSZ Catalysts for Enhanced CO2 Dry Reforming: Insights into Reducibility and Surface Basicity

Supplementary Information

Table S1. Deconvolution results of Zr 3d XPS spectra for the 5Ni/8YZr and 5Ni+xSm/8YZr (x=0.5, 1, 2 wt.%) catalysts, showing binding energies (eV) and corresponding peak area percentages (%) for each chemical state.

| Catalysts |  | 5Ni/8YZr | 5Ni+0.5Sm/8YZr | 5Ni+1Sm/8YZr | 5Ni+2Sm/8YZr |
| --- | --- | --- | --- | --- | --- |
| Zr 3d Peak 1 | B.E. (eV) | 182.2 | 181.3 | 181.3 | 181.3 |
|  | % Area | 79.8 | 79.9 | 80.6 | 74.9 |
| Zr 3d Peak 2 | B.E. (eV) | 184.7 | 183.8 | 183.8 | 183.7 |
|  | % Area | 20.2 | 20.1 | 19.4 | 25.1 |

Table S2. Deconvolution results of Y3d XPS spectra for the catalysts 5Ni/8YZr and 5Ni+xSm/8YZr (x=0.5, 1, 2 wt.%), showing binding energies (eV) and corresponding peak area percentages (%) for each chemical state.

| Catalysts |  | 5Ni/8YZr | 5Ni+0.5Sm/8YZr | 5Ni+1Sm/8YZr | 5Ni+2Sm/8YZr |
| --- | --- | --- | --- | --- | --- |
| Y 3d Peak 1 | B.E. (eV) | 157.5 | 156.6 | 156.5 | 156.5 |
|  | % Area | 86.9 | 85.7 | 87.9 | 79.1 |
| Y 3d Peak 2 | B.E. (eV) | 159.7 | 158.8 | 158.7 | 158.6 |
|  | % Area | 13.1 | 14.3 | 12.1 | 20.9 |

Table S3. Deconvolution results of Sm 3d XPS spectra for the catalysts 5Ni/8YZr and 5Ni+xSm/8YZr (x=0.5, 1, 2 wt.%), showing binding energies (eV) and corresponding peak area percentages (%) for each chemical state.

| Catalysts |  | 5Ni/8YZr | 5Ni+0.5Sm/8YZr | 5Ni+1Sm/8YZr | 5Ni+2Sm/8YZr |
| --- | --- | --- | --- | --- | --- |
| Sm 3d5/2 Peak 1 | B.E. (eV) | 1081.5 | 1081.3 | 1081.4 | 1081.3 |
|  | % Area | 65.0 | 62.1 | 62.8 | 59.1 |
| Sm 3d5/2 Peak 2 | B.E. (eV) | 1108.5 | 1108.5 | 1108.5 | 1108.4 |
|  | % Area | 35.0 | 37.9 | 37.2 | 40.9 |

Table S4. Deconvolution results of Ni 2p XPS spectra for the 5Ni/8YZr and 5Ni+xSm/8YZr (x=0.5, 1, 2 wt.%) catalysts, showing binding energies (eV) and corresponding peak area percentages (%) for each chemical state.

| Catalysts |  | 5Ni/8YZr | 5Ni+0.5Sm/8YZr | 5Ni+1Sm/8YZr | 5Ni+2Sm/8YZr |
| --- | --- | --- | --- | --- | --- |
| Ni 2p Peak 1 | B.E. (eV) | 854.1 | 854.2 | 854.0 | 853.6 |
|  | % Area | 46.0 | 34.2 | 33.2 | 32.8 |
| Ni 2p Peak 2 | B.E. (eV) | 860.2 | 860.5 | 860.1 | 860.0 |
|  | % Area | 32.6 | 27.6 | 32.3 | 30.8 |
| Ni 2p Peak 3 | B.E. (eV) | 872.1 | 871.8 | 871.8 | 871.4 |
|  | % Area | 13.9 | 18.6 | 16.9 | 17.1 |
| Ni 2p Peak 4 | B.E. (eV) | 877.9 | 878.6 | 878.3 | 878.3 |
|  | % Area | 7.5 | 19.6 | 17.6 | 19.3 |

Table S5. Deconvolution results of O 1s XPS spectra for the 5Ni/8YZr and 5Ni+xSm/8YZr (x=0.5, 1, 2 wt.%) catalysts, showing binding energies (eV) and corresponding peak area percentages (%) for each chemical state.

| Catalysts |  | 5Ni/8YZr | 5Ni+0.5Sm/8YZr | 5Ni+1Sm/8YZr | 5Ni+2Sm/8YZr |
| --- | --- | --- | --- | --- | --- |
| O 1s Peak 1 | B.E. (eV) | 528.2 | 527.7 | 527.4 | 527.7 |
|  | % Area | 20.1 | 16.3 | 22.2 | 24.3 |
| O 1s Peak 2 | B.E. (eV) | 529.5 | 529.0 | 529.0 | 529.0 |
|  | % Area | 73.6 | 77.1 | 70.8 | 56.5 |
| O 1s Peak 3 | B.E. (eV) | 531.9 | 531.3 | 531.1 | 530.8 |
|  | % Area | 6.2 | 6.6 | 7.0 | 19.2 |