Supplementary Information

Non-Radiative Recombination of Triplet Charge-Transfer State as the Key of Limiting Efficiency Mediates the Positive Relevance of JSC and VOC

Yue Ren,a Ming-Yang Li,a Yun Geng,b Yi-Zhou Xu,a Guang-Yan Sun,*a Ming-Yue Sui*a and Zhong-Min Sua,b

a.	Department of Chemistry, Faculty of Science, Yanbian University, Yanji 133002, Jilin, P. R. China; Email: gysun@ybu.edu.cn

b.	Institute of Functional Material Chemistry, Faculty of Chemistry, Northeast Normal University, Changchun 130024, Jilin, P. R. China

METHODS

Decay rate and parameter calculation

Non-radiative energy loss (ΔE3) is essentially linked to the external electroluminescence quantum efficiency (EQEEL) of device, as follows:1

(1)

where EQEEL is related to the radiative and non-radiative recombination rate (kr and knr):

(2)

The kr is obtained from the Einstein coefficient relation:2

(3)

where μtr is the average transition dipole moment; ε0 is the vacuum permittivity; h is the Planck constant; and c is the speed of light in vacuum. In classical Marcus electrons hopping model, non-radiative recombination rate (knr) of 1CT and 3CT state is defined as:3

(4)

where Vel denotes the electronic coupling; σ is the energetic disorder; and λ is the reorganization energy. ƒ(n) depends on the refractive index (n) of the blend by ƒ(n) = n(n2+2)2/9. Following the Lorentz virtual cavity model, the value of refractive index is n=1.8. Energetic disorder σ is given by σ2 = 2λkBT, where λ refer to the reorganization energy.4 Three-state model was applied to account for the electronic couplings, reorganization energy, and other parameters in the decay rate.

Reorganization Energy

The total reorganization energy λ includes internal reorganization energy (λint) and external reorganization energy (λext), λ = λint+λext.5 The λint derives from the changes in the ground state structures of donor and acceptor when they gain or lose charge upon electron transfer, which is expressed as:5

(5)

(6)

(7)

However, the λext is due to electronic and nuclear polarization from the surrounding medium, which can be approximately evaluated by:3

(8)

where a1, a2, R, εOP, and ε0 are donor radii, acceptor radii, distance between the center of donor and acceptor, and optical and zero-frequency dielectric constants of surrounding media, respectively. Considering the reconciliation between the computational cost and accuracy, εOP and ε0 are estimated to be 1.96 and 3.4 by Troisi6 and Jérôme,5 respectively.

Electronic Coupling

For the calculation of kr and knr, the electronic coupling can be approximated from the generalized Mulliken-Hush (GMH) formalism in adiabatic description, which could be written as below:7

(9)

where µtr is the average transition dipole moment, Δµ is the dipole moment difference between initial state S0 and final state Sn, and ΔE corresponds to the vertical excitation energy. The Δµ can be estimated directly from a finite field method on the excitation energy.8

Figure 1. The HOMO energy levels of donor copolymer (PM6)n (n=1, 1.5, 2, 2.5, 3, 3.5, 4).

Figure 2. Schematic diagrams of interfacial stacking sites of the molecular clusters. D and A represent the D and A unit in the A-D-A structure, respectively.

Figure 3. NTO maps and the lowest 1CT- and 3CT-state energies for PM6/acceptor blends.

Figure 4. Schematic diagrams of non-radiative recombination rates of 1CT→GS and 3CT→3LE pathway in PM6/IT-4F and PM6/IOM-4F blends. The top dotted box denotes the 3CT state decay to 3LE state of donor, and the bottom denotes to T1 state of acceptor.

Table 1. Experimental photovoltaic parameters of the PM6/acceptor blends.9

|  | VOC (V) | JSC (mA cm-2) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| PM6/IT-4F | 0.85 | 20.02 | 75.22 | 12.80 |
| PM6/IOM-4F | 0.86 | 21.66 | 72.00 | 13.41 |
| PM6/IM-4F | 0.88 | 22.12 | 72.79 | 14.17 |
| PM6/PC71BM | 1.02 | 9.30 | 56.00 | 5.30 |

Table 2. 1CT-state energies (E(1CT)), transition dipole moments (μtr), electron couplings (Vel), recombination energies (λ), energetic disorders (σ), radiative recombination rates (kr1CT), and non-radiative recombination rates (knr1CT) of 1CT→S0 pathway for PM6/acceptors blends.

|  | Vel (eV) | λ (eV) | σ (eV) | E(1CT) (eV) | μtr (debye) | kr1CT (s-1) | knr1CT (s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PM6/IT-4F | 0.108 | 0.759 | 0.198 | 2.114 | 1.272 | 8.87×103 | 4.36×103 |
| PM6/IOM-4F | 1.162 | 0.749 | 0.197 | 2.405 | 6.121 | 3.02×105 | 3.18 |
| PM6/IM-4F | 1.397 | 0.757 | 0.198 | 2.963 | 0.217 | 7.11×102 | 1.15×10-11 |
| PM6/PC71BM | 0.402 | 0.694 | 0.189 | 2.599 | 2.970 | 8.98×104 | 1.08×10-07 |

Table 3. T1-state energies of donor (E(3LED)) and acceptors (E(3LEA)), and the lowest 3CT-state energies (E(3CT)).

|  | E(3LED) (eV) | E(3LEA) (eV) | E(3CT) (eV) |
| --- | --- | --- | --- |
| PM6/IT-4F | 1.518 | 1.276 | 2.112 |
| PM6/IOM-4F | 1.518 | 1.264 | 2.409 |
| PM6/IM-4F | 1.518 | 1.256 | 2.964 |
| PM6/PC71BM | 1.518 | 1.411 | 2.618 |

Table 4. Energy differences between 3CT- and T1-state energies of donor (ΔE(3CT-3LED)), electron couplings (Vel), recombination energies (λ), energetic disorders (σ), and non-radiative recombination rates (knr3CT→3LED) of 3CT→T1 pathway for PM6/acceptors blends.

|  | Vel (eV) | λ (eV) | σ (eV) |  | ΔE(3CT-3LED) (eV) | knr3CT→3LED (s-1) |
| --- | --- | --- | --- | --- | --- | --- |
| PM6/IT-4F | 0.302 | 1.067 | 0.235 | 0.594 |  | 8.42×1013 |
| PM6/IOM-4F | 0.012 | 1.101 | 0.239 | 0.891 |  | 4.20×1011 |
| PM6/IM-4F | 0.150 | 1.090 | 0.237 | 1.446 |  | 1.16×1013 |
| PM6/PC71BM | 0.117 | 1.079 | 0.236 | 1.100 |  | 6.18×1013 |

Table 5. Energy differences between the 3CT- and T1-state energies of acceptor (ΔE(3CT-3LEA)), electron couplings (Vel), recombination energies (λ), energetic disorders (σ), and non-radiative recombination rates (knr3CT→3LEA) of 3CT→T1 pathway for PM6/acceptors blends.

|  | Vel (eV) | λ (eV) | σ (eV) | ΔE(3CT-3LEA) (eV) | knr3CT→3LEA (s-1) |
| --- | --- | --- | --- | --- | --- |
| PM6/IT-4F | 0.011 | 0.976 | 0.225 | 0.836 | 5.01×1011 |
| PM6/IOM-4F | 0.217 | 0.940 | 0.220 | 1.145 | 1.48×1014 |
| PM6/IM-4F | 0.017 | 1.020 | 0.230 | 1.708 | 1.48×1010 |
| PM6/PC71BM | 0.179 | 0.977 | 0.225 | 1.208 | 9.06×1013 |

Table 6. Experimental photovoltaic parameters (VOC and JSC) and their increments (ΔVOC and ΔJSC) of the five groups of NFA-based blends.

| Donor | Acceptor | VOC (V) | JSC (mA cm-2) | ΔVOC (V) | ΔJSC (mA cm-2) | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| FTAZ | F5IC | 0.73 | 14.49 | 0.009 | 3.810 | 10 |
|  | F7IC | 0.74 | 18.30 |  |  |  |
|  | F7IC | 0.74 | 18.30 | 0.115 | 1.420 |  |
|  | F9IC | 0.86 | 19.72 |  |  |  |
| PM6 | IT-4F | 0.85 | 20.02 | 0.010 | 1.640 | 9 |
|  | IOM-4F | 0.86 | 21.66 |  |  |  |
|  | IOM-4F | 0.86 | 21.66 | 0.020 | 0.460 |  |
|  | IM-4F | 0.88 | 22.12 |  |  |  |
| PTB7-Th | F6IC | 0.61 | 18.07 | 0.029 | 7.050 | 11 |
|  | F8IC | 0.64 | 25.12 |  |  |  |
|  | F6IC | 0.61 | 18.07 | 0.121 | 2.760 |  |
|  | F10IC | 0.73 | 20.83 |  |  |  |
| PBDB-T | BDCPDT-IC | 0.86 | 16.56 | 0.060 | 0.190 | 12,13 |
|  | ITIC | 0.92 | 16.75 |  |  |  |
|  | ITIC | 0.92 | 16.75 | 0.020 | 3.150 |  |
|  | ITBC | 0.94 | 19.90 |  |  |  |
| PBDB-T | BDCPDT-IC | 0.86 | 16.56 | 0.080 | 1.160 | 12,13 |
|  | BDCPDT-TTC | 0.94 | 17.72 |  |  |  |
|  | BDCPDT-IC | 0.86 | 16.56 | 0.060 | 1.990 |  |
|  | BDCPDT-BC | 0.92 | 18.55 |  |  |  |

References

1	Rau, U. Reciprocity Relation between Photovoltaic Quantum Efficiency and Electroluminescent Emission of Solar Cells. Phys. Rev. B 76, 085303 (2007).

2	Hilborn, R. C. Erratum: ‘‘Einstein coefficients, cross sections, f values, dipole moments, and all that’’ [Am. J. Phys. 50, 982 (1982)]. Am. J. Phys. 51, 471-471 (1983).

3	Marcus, R. A. On the Theory of Oxidation-Reduction Reactions Involving Electron Transfer. I. J. Chem. Phys. 24, 966-978 (1956).

4	Sánchez-Carrera, R. S., Paramonov, P., Day, G. M., Coropceanu, V. & Brédas, J.-L. Interaction of Charge Carriers with Lattice Vibrations in Oligoacene Crystals from Naphthalene to Pentacene. J. Am. Chem. Soc. 132, 14437-14446 (2010).

5	Lemaur, V., Steel, M., Beljonne, D., Brédas, J.-L. & Cornil, J. Photoinduced Charge Generation and Recombination Dynamics in Model Donor/Acceptor Pairs for Organic Solar Cell Applications:  A Full Quantum-Chemical Treatment. J. Am. Chem. Soc. 127, 6077-6086 (2005).

6	Liu, T. & Troisi, A. Absolute Rate of Charge Separation and Recombination in a Molecular Model of the P3HT/PCBM Interface. J. Phys. Chem. C 115, 2406-2415 (2011).

7	Voityuk, A. A. Estimation of Electronic Coupling in π-Stacked Donor-Bridge-Acceptor Systems: Correction of the Two-State Model. J. Chem. Phys. 124, 064505 (2006).

8	Li, Y., Pullerits, T., Zhao, M. Y. & Sun, M. T. Theoretical Characterization of the PC60BM:PDDTT Model for an Organic Solar Cell. J. Phys. Chem. C 115, 21865-21873 (2011).

9	Zhang, Z. H. et al. Modification on the Indacenodithieno[3,2-b]thiophene Core to Achieve Higher Current and Reduced Energy Loss for Nonfullerene Solar Cells. Chem. Mater. 32, 1297-1307 (2020).

10	Dai, S. X. et al. Effect of Core Size on Performance of Fused-Ring Electron Acceptors. Chem. Mater. 30, 5390-5396 (2018).

11	Dai, S. X. et al. Enhancing the Performance of Polymer Solar Cells via Core Engineering of NIR-Absorbing Electron Acceptors. Adv. Mater. 30, 1706571 (2018).

12	Chang, S.-L. et al. New Thieno[3,2-b]thiophene-Based Acceptor: Tuning Acceptor Strength of Ladder-Type N-Type Materials to Simultaneously Achieve Enhanced Voc and Jsc of Nonfullerene Solar Cells. ACS Energy Lett. 3, 1722-1729 (2018).

13	Chang, S.-L. et al. Isomerically Pure Benzothiophene-Incorporated Acceptor: Achieving Improved Voc and Jsc of Nonfullerene Organic Solar Cells via End Group Manipulation. ACS Appl. Mat. Interfaces 11, 33179-33187 (2019).