Efficient tetracycline removal from aqueous solutions using ionic liquid modiﬁed magnetic activated carbon (IL@mAC)

Edris Bazrafshan1,2, Amin Allah Zarei2, Leili Mohammadi3,*, Muhammad Nadeem Zafar4,*, Maryam Foroughi1,2, Summan Aman4, Faezeh Sabri1,2, Amir Hossein Mahvi5, Farahnaz Barahuie6

1Health Sciences Research Center, Torbat Heydariyeh University of Medical Sciences, Torbat Heydariyeh 33787 95196, Iran

2Department of Environmental Health Engineering, Torbat Heydariyeh University of Medical Sciences, Torbat Heydariyeh 33787 95196, Iran

3Infectious Diseases and Tropical Medicine Research Center, Resistant Tuberculosis Institute, Zahedan University of Medical Sciences, Zahedan 98167-43463, Iran

4Department of Chemistry, University of Gujrat, Gujrat 50700, Pakistan

5Department of Environmental Health Engineering, Tehran University of Medical Sciences, Tehran, Iran

6Faculty of Industry and Mining (Khash), University of Sistan and Baluchestan, Zahedan 98167 45845, Iran

Supplementary data

Table S1. Levels and factors of the operational parameters

| Parameters | Level of parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | -2 | -1 | 0 | +1 | +2 |
| A: Dose of IL@mAC (g/50 mL) | 0.01 | 0.027 | 0.06 | 0.08 | 0.1 |
| B: pH | 3 | 5 | 7 | 9 | 11 |
| C: Conc. of TC (mg/L) | 50 | 412.5 | 775 | 1137 | 1500 |
| D: Reaction time (min) | 30 | 82.5 | 135 | 187.5 | 240 |

Table S2. Model summary of the experimental design for TC removal onto IL@mAC

| Standard deviation | 5.63 | R2 | 0.8950 |
| --- | --- | --- | --- |
| Mean | 75.77 | R2adj | 0.7970 |
| CV (%) | 7.43 | R2pred | 0.4297 |
| PRESS* | 2581.03 | Adeq. Precision** | 11.338 |

*Indicating the conformity degree of the model with the observations not included in the model estimation

**Adeq Precision determines the signal to noise ratio. The >4 values are desirable. A ratio of 11.338 suggests an adequate signal. This model is applicable for the design space navigation.

Fig. S1. The zero-point charge of IL@mAC

Fig. S2. Effect of TCy concentration on adsorption capacity and removal efficiency of IL@mAC (pH 7, Temperature 303 K, IL@mAC dose 1.2g/L, Time 135 min)

S1. Adsorption isotherms

The following equations 1, 2, and 3 show the linear relationship of Langmuir, Freundlich, and Temkin, respectively [1-3].

1qeq= 1qL+ 1bLqLCeq										          1

logqeq=log kF+ 1nlogCeq									          2

qeq=BlnaT+BlnCeq, where B= RTbT							          3

Where, qL (mg/g): maximum monolayer Langmuir adsorption capacity of TC onto IL@mAC, bL (L/g): Langmuir constant (related to affinity of adsorption energy and binding sites), kF ((mg/g)(mg/L)1/n): Freundlich constant, n: adsorption intensity, aT (L/mg) and bT: Temkin constants (belongs to heat of adsorption and equilibrium binding constant respectively).

Fig. S3. Langmuir (a), Freundlich (b), and Temkin (c) isotherm plots for tetracycline adsorption onto IL@mAC

[1] I. Langmuir, Adsorption of gases on plane surfaces of glass, mica and platinum, Journal of the American Chemical Society, 40 (1918) 1361-1403.

[2] H. Freundlich, Adsorption in solutions, Journal of Physical Chemistry, 57 (1906) 384-410.

[3] M.J. Temkin, V. Pyzhev, Recent modifications to Langmuir isotherms., Acta Physiochimica USSR, 12 (1940) 217-222.