Supplementary Information - Improving ALD-Al2O3 surface passivation of Si using native SiOx

Michael N. Getz, Marco Povoli, Eduard Monakhov

| Table S1: Thickness measured by SE before and after Al2O3 deposition on single-side polished Si substrates. |  |  |  |
| --- | --- | --- | --- |
| Pretreatment | Tdep (˚C) | Thickness before dep. (nm) | Thickness post dep. (nm) |
| HF-dip | 150 | 0.7 ± 0.06 | 20.7 ± 0.05 |
| HF-dip | 200 | 0.6 ± 0.04 | 19.9 ± 0.4 |
| HF-dip | 250 | 0.6 ± 0.06 | 18.4 ± 0.2 |
| HF-dip | 300 | 0.6 ± 0.04 | 16.9 ± 0.2 |
| … | 150 | 1.9 ± 0.2 | 21.3 ± 0.2 |
| … | 200 | 1.54 ± 0.06 | 20.2 ± 0.2 |
| … | 250 | 1.6 ± 0.1 | 18.8 ± 0.1 |
| … | 300 | 1.6 ± 0.1 | 17.3 ± 0.2 |
| Table S2: Thickness measured by SE before and after Al2O3 deposition of samples deposited on double-side polished Si substrates. |  |  |  |
| Pretreatment | Tdep (˚C) | Thickness before dep. (nm) | Thickness post dep. (nm) |
| HF-dip | 150 | 0.6 ± 0.04 | 19.5 ± 0.6 |
| HF-dip | 200 | 0.6 ± 0.04 | 19.7 ± 0.1 |
| HF-dip | 250 | 0.6 ± 0.06 | 18.4 ± 0.1 |
| HF-dip | 300 | 0.6 ± 0.04 | 17.4 ± 0.2 |
| … | 150 | 1.6 ± 0.1 | 20.0 ± 0.8 |
| … | 200 | 1.6 ± 0.1 | 19.8 ± 0.3 |
| … | 250 | 1.6 ± 0.1 | 18.2 ± 0.08 |
| … | 300 | 1.6 ± 0.1 | 17.3 ± 0.2 |

Figure S1: Auger-corrected inverse lifetime 8 months after annealing of no-HF samples (a) and HF-dipped (b). Dashed lines show the linear fits used to extract J0s.

Series resistance correction and effective charge extraction:

The measured capacitance, Cm, and conductance, Gm as a function of applied gate voltage, V. Cm, and Gm, obtained from parallel conductance mode were corrected for series resistance, Rs, before extracting any parameters. Rs was determined by[1]:

|  | Rs= GmaGma2+ ω2Cma2, | (1) |
| --- | --- | --- |

where Cma and Gma are the measured capacitance and conductance in accumulation, respectively, and ω is the angular frequency, 2πf. The series corrected capacitance and conductance, C and G, respectively, were determined by:[1]

|  | C= Gm2+ ω2Cm2Cma2+ ω2Cm2, G= Gm2+ ω2Cm2aa2+ ω2Cm2, | (2) (3) |
| --- | --- | --- |

where a is:

|  | a= Gm-Gm2+ ω2Cm2Rs. | (4) |
| --- | --- | --- |

The presented CV and GV characteristics in the paper and in the supplementary materials section have been corrected for series resistance.

The effective interface charge, Qeff, was determined by first calculating the flatband capacitance, CFB, given by:

|  | CFB= CoxεSiA/λCox+ εSiA/λ, | (5) |
| --- | --- | --- |

where Cox is the Al2O3 capacitance and is equal to Cma. εSi is the relative dielectric constant of silicon assumed to be 1.03 × 10-12 F/cm,[2] A is the area of the gate electrode, and λ is the Debye length given by:

|  | λ= εSikBTq2NA, | (6) |
| --- | --- | --- |

where kB is the Boltzmann constant, T is the measurement temperature, q is the electron charge, and NA is the doping of the substrate. The substrate doping was determined from the slope of the 1/C2 data of the annealed samples and was determined to be 2 × 1016 cm-3. The flatband voltage, VFB, was then extracted by reading out the voltage at CFB. Qeff was finally calculated from:[3]

|  | Qeff= Cox(φms-VFB)q, | (7) |
| --- | --- | --- |

where φms is given by:

|  | φms=Fm-χSi-Eg2-kBTqln⁡(NAni), | (8) |
| --- | --- | --- |

where Fm = 4.08 eV[4] is the work function of Al, and χSi, Eg, and ni are the electron affinity (4.05 eV),[5] band gap (1.12 eV), and intrinsic doping (8.2 × 109 cm-3 at 298 K) of silicon, respectively. φms was determined to be -0.9 eV for the samples used in this study.

Figure S2: Calculated Qeff for each frequency in Figure 5a in the main article and fitted to a double exponential.

Figure S3: CV of a no-HF sample deposited at 200 ˚C. The gate voltage was swept from inversion to accumulation (blue) and then back again (red).

9

Figure S4: 500 Hz GV characteristics of samples deposited at 150 – 300 ˚C for a) no-HF as deposited, b) HF-dip as-deposited, c) no-HF annealed, and d) HF-dip annealed.

Figure S5: GV of a no-HF sample (a) and HF-dipped sample (b) deposited at 250 ˚C.

| Table S3: Qfix and Dit of as-deposited. |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | no-HF |  | HF-dipped |  |
| Tdep (˚C) | Qfix (cm-2) | Dit (ev-1 cm-2) | Qfix(cm-2) | Dit (ev-1 cm-2) |
| 150 | -4.7 × 1012 | 2.0 × 1012 | -4.0 × 1012 | 2.7 × 1012 |
| 200 | -4.6 × 1012 | 2.1 × 1012 | -4.5 × 1012 | 2.4 × 1012 |
| 250 | -4.4 × 1012 | 2.1 × 1012 | -3.6 × 1012 | 3.3 × 1012 |
| 300 | -4.8 × 1012 | 2.6 × 1012 | -4.4 × 1012 | 4.4 × 1012 |

| Table S4: Qfix and Dit of no-HF and HF-dipped samples after FG anneal at 435 ˚C. |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | no-HF |  | HF-dipped |  |
| Tdep (˚C) | Qfix (cm-2) | Dit (ev-1 cm-2) | Qfix (cm-2) | Dit (ev-1 cm-2) |
| 150 | -3.5 × 1012 | 1.0 × 1010 | -3.6 × 1012 | 2.6 × 1010 |
| 200 | -4.2 × 1012 | 9.8 × 109 | -4.0 × 1012 | 2.8 × 1010 |
| 250 | -3.7 × 1012 | 6.5 × 1010 | -2.9 × 1012 | 3.8 × 1010 |
| 300 | -3.2 × 1012 | 6.4 × 1010 | -2.4 × 1012 | 7.0 × 1010 |

References

[1]	E. H. Nicollian, J. R. Brews, MOS (Metal Oxide Semiconductor) Physics and Technology, Wiley, New York, 1982.

[2]	M. Wolf, The Physics of Computing, Elsevier, Cambridge, United States, 2017.

[3]	D. K. Schroder, Semiconductor Material and Device Characterization, 3rd ed., John Wiley & Sons, Inc., New Jersey, 2005.

[4]	P. A. Tipler, R. A. Llewellyn, Modern Physics, 5th ed., W. H. Freeman, 2008.

[5]	B. El-Kareh, Silicon Devices and Processes, Springer, 2009.