Supplementary Information

Predicting Carbon Deposition on Rh-Based Catalysts in Ethanol Oxidative Steam Reforming

Hao Liu1,2,3, Xue Han2,*, HaoZhe Feng1,2,3, Haoyu Li1,2,3, Qinghe Yu2

1.National Engineering Research Center of Nonferrous Metals Materials and Products for New Energy, China GRINM Group Co., Ltd., Beijing 100088, China；

2. GRIMAT Engineering Institute Co., Ltd., Beijing 101407, China；

3. General Research Institute for Nonferrous Metals, Beijing 100088, China

Corresponding authors:

*GRIMAT Engineering Institute Co., Ltd., Beijing 104107, China

E-mail addresses: hanxuehit@126.com (X. Han)

S1 N2 adsorption-desorption characterization

The BET surface area, average pore size and total pore volume of catalysts are shown in Table S1, and the pore size distribution of these samples are shown in Figure S1. 1%Rh/TiO2 and 1%Rh/MgO get obviously higher surface area comparing to 1%Rh/ZrO2, 1%Rh/CeO2 and 1%Rh/ZnO; while 1%Rh/ZnO and 1%Rh/MgO catalysts have no typical pore size distribution mode, which is very different from 1% Rh/ZrO2, 1%Rh/CeO2 and 1%Rh/TiO2. Considering ammonia produced by urea decomposition is a weak alkaline precipitant, the formation process of strong alkaline ZnO and MgO supports and weak alkaline TiO2, CeO2 and ZrO2 supports should have a certain difference. Hence, although 1%Rh/TiO2 and 1%Rh/MgO have similar larger specific surface area, their pore structures are great difference.

Table 1 Physical properties of the samples

| Catalyst | Surface area（m2·g-1） | Pore diameter（nm） | Pore volume（cm3·g-1） | Crystallite size（nm） |
| --- | --- | --- | --- | --- |
| 1%Rh/MgO | 119 | 21.4 | 0.632 | 13.2 |
| 1%Rh/ZnO | 27.7 | 26.4 | 0.184 | 32.7 |
| 1%Rh/TiO2 | 121 | 10.2 | 0.309 | 11.8 |
| 1%Rh/ZrO2 | 53.7 | 4.87 | 0.065 | 15.2 |
| 1%Rh/CeO2 | 28.4 | 6.32 | 0.045 | 20.6 |

Figure S1. BJH pore size distribution of metal oxides supported Rh catalysts. Pore size distribution curves of 1%Rh/MgO (■), 1%Rh/ZnO (●), 1%Rh/TiO2 (▲), 1%Rh/ZrO2 (▽), and 1%Rh/CeO2 (☆) catalysts prepared by urea homogeneous precipitation method. Measurements were conducted using N2 adsorption–desorption isotherms at −196 °C.