PYROLYSIS OF AGRICULTURAL WASTE MATERIALS

From Agricultural Waste to Potential Radiation Shielding Materials: Linking Thermochemical Reactivity and Solid Product Availability

- Onset temperature (Tonset): Decomposition starts

- Heating Rate: 2.7 – 8.3 oCmin-1

- Residence Time

- Final Temperature (Tf)

- Thermal Reactivity Index (TRI)

TRI= Tf- Totf-to

TRI Range: 0.7 - 7.0 oCmin-1

THERMOCHEMICAL REACTIVITY INDICATORS

THERMOCHEMICAL CONVERSION

COMBUSTION OF AWM

(Ash production)

- Temperature: 400 – 700OC

- Product: Mineral-Rich bio-ash

PYROLYSIS OF AWMs

(Oxygen-limited)

- Temperature: Ambient to 800OC

- Residence time: Controlled

- Product: Biochar + Volatiles

- Low-moderate reactivity

Higher solid yields

- High reactivity

Faster decomposition

Lower char yield

- Energy demand inversely           proportional to reactivity

(SGC: 0.29 – 1.22 kg kg-1)

PERFORMANCE AND ENERGY INSIGHT

ENGINEERING APPLICATIONS

SUPPLEMENTARY CEMENT REPLACEMENT

Pozzolanic ash

CONCRETE FILLERS

(Lightweight aggregates)

RADIATION SHIELDING MATERIAL

Biochar and Ashes Composites

SUSTAINABLE CONSTRUCTION MATERIALS

SOLID RESIDUES (PRODUCTS)

BIOCHAR

YIELD: 10 – 34%

Highest yield:

- Fisch Scale (~33.8%)

- Cocoa bean husk (~30.3%)

- Cow Hooves (~21.5%)

ASH

YIELD: 0 – 12%

Highest yield:

- Tropical Almond leaves (~11.5%)

- Plantain leaves (~9.1%)

- Rice straw (~6.8%)

- Cutting larger samples – size reduction

- Cleaning Samples - impurity removal

- Drying Samples – moisture control

FEEDSTOCK PREPARATION

FEEDSTOCK

(Agricultural Waste Materials)