Supplementary Materials

Adsorption of volatile organic compounds and microwave regeneration on self-prepared high-surface-area beaded activated carbon

Shih-Ying Hsiao 1, Shu-Wen You 1, Can Wang 2,3, Ji-Guang Deng 4, and Hsing-Cheng Hsi 1,

1 Graduate Institute of Environmental Engineering, National Taiwan University, No. 1, Sec. 4, Roosevelt Rd., Da'an Dist., Taipei 10617, Taiwan

2 School of Environmental Science and Engineering, Tianjin University, Tianjin 300072, China

3 Tianjin Key Lab of Indoor Air Environmental Quality Control, Tianjin 300072, China

4 College of Environmental and Energy Engineering, Beijing University of Technology, Beijing, 100124, China

- Langmuir, Freundlich, and Dubinin-Radushkevich (D-R) isotherms

The Langmuir isotherm was primarily designed to describe gas-solid phase adsorption. It assumed the adsorption was monolayer and in dynamic equilibrium, the Langmuir equation can be written in the following form:

|  | qqs= b∙P1+bP | (S1) |
| --- | --- | --- |

where q (mg g-1) is the adsorption capacity, qs (mg g-1) the saturated adsorption capacity, b (Pa-1) the Langmuir constant representing the strength of the adsorbate-adsorbent interactions, and P (Pa) stands for the partial pressure of the adsorbate in the bulk phase.

The Freundlich isotherm is an empirical equation which is applicable to adsorption processes occurred on heterogeneous interfaces. The form of Freundlich isotherm is as follows:

|  | q = KF∙P1nF | (S2) |
| --- | --- | --- |

where KF and nF are empirical constants that are generally temperature dependent.

The Dubinin-Radushkevich isotherm is a semi-empirical equation adapted from the earlier Polanyi potential theory and has been widely applied to describe the adsorption in microporous materials (Nguyen and Do, 2001), having the form of:

|  | q =ρW0 exp-εE0β2 | (S3) |
| --- | --- | --- |

and

|  | ε= RTlnP0P | (S4) |
| --- | --- | --- |

where W0 is the pore volume filled, β the affinity coefficient (β = 1 for the reference vapor), ε the adsorption potential, E0 the so-called characteristic energy for a reference vapor (usually benzene), R the universal gas constant (8.314 J mole-1 K-1), T the absolute temperature (K), and P0 the saturated vapor pressure of the adsorbate.

- Supplementary figures

Figure S1 The scheme diagram of the microwave regeneration system

Figure S2 DTG of MEK-SBAC at various heating rates. (a) DTG peaks; (b) linear form providing the heat of desorption.

Figure S3 DTG of MEK-KBAC at various heating rates. (a) DTG peaks; (b) linear form providing the heat of desorption.

Figure S4 DTG of TOL-SBAC at various heating rates. (a) DTG peaks; (b) linear form providing the heat of desorption.

Figure S5 DTG of TOL-KBAC at various heating rates. (a) DTG peaks; (b) linear form providing the heat of desorption

- Supplementary tables

Table S1 Peak desorption temperatures at different heating rates and activation energies for desorption

|  | Peak desorption temperatures (K) at different heating rates |  |  | Ed (kJ mol-1) | ∆Hvap (kJ mol-1) |
| --- | --- | --- | --- | --- | --- |
|  | 20 oC min-1 | 10 oC min-1 | 5 oC min-1 |  |  |
| MEK-SBAC | 488 | 461 | 432 | 36.45 | 31.21 |
| MEK-KBAC | 488 | 468 | 441 | 46.41 |  |
| TOL-SBAC | 494 | 459 | 430 | 30.40 | 32.80 |
| TOL-KBAC | 520 | 476 | 446 | 27.15 |  |

Table S2 Langmuir parameters for different adsorbate-adsorbent systems at different temperatures

| Langmuir parameter |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Integration method |  |  |  |  |  |
| Adsorbate | Adsorbent | T (°C) | R2 | qs (mg g-1) | KL |
| MEK | SBAC | 30 | 0.9571 | 1956.8 | 40.2 |
|  |  | 40 | 0.9559 | 1701.5 | 60.3 |
|  |  | 50 | 0.9904 | 2382.2 | 29.9 |
|  | KBAC | 30 | 0.9321 | 547.6 | 230.6 |
|  |  | 40 | 0.8572 | 538.9 | 419.2 |
|  |  | 50 | 0.9730 | 568.3 | 238.8 |
| TOL | SBAC | 30 | 0.8669 | 1686.0 | 64.6 |
|  |  | 40 | 0.8551 | 1222.0 | 168.6 |
|  |  | 50 | 0.9405 | 1433.7 | 105.4 |
|  | KBAC | 30 | 0.9902 | 593.1 | 176.3 |
|  |  | 40 | 0.9838 | 557.1 | 218.9 |
|  |  | 50 | 0.9866 | 555.6 | 362.9 |
| Gravimetric method |  |  |  |  |  |
| Adsorbate | Adsorbent | T (°C) | R2 | qs (mg g-1) | KL |
| MEK | SBAC | 30 | 0.9683 | 962.7 | 112.5 |
|  |  | 40 | 0.9906 | 770.2 | 100.4 |
|  |  | 50 | 0.8936 | 610.1 | 211.3 |
|  | KBAC | 30 | 0.9924 | 365.1 | 368.0 |
|  |  | 40 | 0.9849 | 358.8 | 286.0 |
|  |  | 50 | 0.9652 | 377.4 | 255.3 |
| TOL | SBAC | 30 | 0.9612 | 1323.9 | 71.7 |
|  |  | 40 | 0.9343 | 997.3 | 147.5 |
|  |  | 50 | 0.9456 | 978.2 | 123.7 |
|  | KBAC | 30 | 0.9944 | 421.8 | 468.6 |
|  |  | 40 | 0.9995 | 413.0 | 491.5 |
|  |  | 50 | 0.9912 | 400.9 | 653.6 |

Table S3 Freundlich parameters for different adsorbate-adsorbent systems at different temperatures

| Freundlich parameter |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Integration method |  |  |  |  |  |
| Adsorbate | Adsorbent | T (°C) | R2 | n | KF |
| MEK | SBAC | 30 | 0.9657 | 2.302 | 4243.3 |
|  |  | 40 | 0.9896 | 2.309 | 4431.1 |
|  |  | 50 | 0.9999 | 1.746 | 7927.5 |
|  | KBAC | 30 | 0.9822 | 4.778 | 890.8 |
|  |  | 40 | 0.9410 | 4.995 | 954.2 |
|  |  | 50 | 0.9931 | 3.352 | 1360.9 |
| TOL | SBAC | 30 | 0.9486 | 3.942 | 2426.1 |
|  |  | 40 | 0.9825 | 4.496 | 2013.0 |
|  |  | 50 | 0.9669 | 3.041 | 3060.9 |
|  | KBAC | 30 | 0.9927 | 7.886 | 737.1 |
|  |  | 40 | 0.9925 | 6.382 | 783.6 |
|  |  | 50 | 0.9967 | 6.662 | 824.7 |
| Gravimetric method |  |  |  |  |  |
| Adsorbate | Adsorbent | T (°C) | R2 | n | KF |
| MEK | SBAC | 30 | 0.9483 | 3.336 | 1793.6 |
|  |  | 40 | 0.9769 | 2.531 | 2005.2 |
|  |  | 50 | 0.9637 | 3.105 | 1569.8 |
|  | KBAC | 30 | 0.9960 | 6.784 | 518.7 |
|  |  | 40 | 0.9946 | 4.407 | 656.4 |
|  |  | 50 | 0.9947 | 3.386 | 905.4 |
| TOL | SBAC | 30 | 0.9555 | 3.824 | 1988.3 |
|  |  | 40 | 0.9900 | 3.902 | 1777.6 |
|  |  | 50 | 0.9857 | 3.187 | 2107.6 |
|  | KBAC | 30 | 0.9989 | 15.97 | 475.8 |
|  |  | 40 | 0.9960 | 12.42 | 494.1 |
|  |  | 50 | 0.9890 | 10.67 | 515.3 |

Table S4 D-R parameters for different adsorbate-adsorbent systems at different temperature

| D-R parameter |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Integration method |  |  |  |  |  |  |  |  |  |  |  |  |  |
| adsorbate | adsorbent |  | T (°C) | R2 |  | W0 (cm3 g-1) |  |  | E0 (kJ mol-1) | E (kJ mol-1) |  | x0 (nm) |  |
| MEK |  | SBAC | 30 | 0.9685 |  | 2.711 |  |  | 7.44 | 7.20 |  | 1.747 |  |
|  |  |  | 40 | 0.9778 |  | 2.536 |  |  | 8.17 | 7.92 |  | 1.592 |  |
|  |  |  | 50 | 0.9949 |  | 3.367 |  |  | 7.30 | 7.09 |  | 1.780 |  |
|  |  | KBAC | 30 | 0.9709 |  | 0.787 |  |  | 11.09 | 10.74 |  | 1.172 |  |
|  |  |  | 40 | 0.9200 |  | 0.808 |  |  | 12.52 | 12.14 |  | 1.039 |  |
|  |  |  | 50 | 0.9954 |  | 0.927 |  |  | 10.67 | 10.36 |  | 1.218 |  |
| TOL |  | SBAC | 30 | 0.9020 |  | 2.014 |  |  | 7.45 | 8.88 |  | 1.745 |  |
|  |  |  | 40 | 0.9559 |  | 1.590 |  |  | 9.12 | 10.88 |  | 1.425 |  |
|  |  |  | 50 | 0.9636 |  | 1.962 |  |  | 7.84 | 9.36 |  | 1.658 |  |
|  |  | KBAC | 30 | 0.9956 |  | 0.724 |  |  | 10.19 | 12.15 |  | 1.276 |  |
|  |  |  | 40 | 0.9935 |  | 0.710 |  |  | 10.21 | 12.18 |  | 1.273 |  |
|  |  |  | 50 | 0.9974 |  | 0.728 |  |  | 11.45 | 13.66 |  | 1.136 |  |
| Gravimetric method |  |  |  |  |  |  |  |  |  |  |  |  |  |
| adsorbate | adsorbent |  | T (°C) | R2 | W0 (cm3 g-1) |  |  | E0 (kJ mol-1) |  |  | E (kJ mol-1) |  | x0 (nm) |
| MEK |  | SBAC | 30 | 0.9690 | 1.389 |  |  | 9.22 |  |  | 8.92 |  | 1.410 |
|  |  |  | 40 | 0.9932 | 1.219 |  |  | 8.67 |  |  | 8.41 |  | 1.500 |
|  |  |  | 50 | 0.9477 | 1.008 |  |  | 10.34 |  |  | 10.04 |  | 1.258 |
|  |  | KBAC | 30 | 0.9998 | 0.510 |  |  | 13.14 |  |  | 12.72 |  | 0.989 |
|  |  |  | 40 | 0.9990 | 0.540 |  |  | 11.44 |  |  | 11.10 |  | 1.136 |
|  |  |  | 50 | 0.9936 | 0.618 |  |  | 10.77 |  |  | 10.46 |  | 1.207 |
| TOL |  | SBAC | 30 | 0.9768 | 1.635 |  |  | 7.83 |  |  | 9.34 |  | 1.659 |
|  |  |  | 40 | 0.9834 | 1.342 |  |  | 8.41 |  |  | 10.03 |  | 1.546 |
|  |  |  | 50 | 0.9811 | 1.368 |  |  | 8.13 |  |  | 9.70 |  | 1.599 |
|  |  | KBAC | 30 | 0.9982 | 0.505 |  |  | 14.84 |  |  | 17.68 |  | 0.876 |
|  |  |  | 40 | 0.9982 | 0.505 |  |  | 14.23 |  |  | 16.98 |  | 0.913 |
|  |  |  | 50 | 0.9905 | 0.503 |  |  | 14.53 |  |  | 17.34 |  | 0.895 |

Table S5 Kinetic parameters of desorption and correlation coefficient R2 obtained from PFO and IPD kinetic models

| Adsorbate | Adsorbent | Irradiation power (W) | PFO model |  | IPD model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | k1 (min-1) | R2 | kp (mg g-1 s-1/2) | I (mg g-1) | R2 |  |
| MEK | SBAC | 400 | 0.328 ± 0.030 | 0.889 – 0.921 | 9.17 ± 0.49 | -8.23 ± 4.40 | 0.889 – 0.912 |  |
|  |  | 600 | 0.372 ± 0.027 | 0.900 – 0.934 | 9.50 ± 0.20 | -7.67 ± 5.55 | 0.886 – 0.916 |  |
|  |  | 800 | 0.350 ± 0.009 | 0.895 – 0.926 | 8.60 ± 1.65 | -7.97 ± 6.86 | 0.881 – 0.912 |  |
|  |  | 1000 | 0.309 ± 0.030 | 0.875 – 0.904 | 8.75 ± 0.64 | -3.35 ± 6.15 | 0.877 – 0.893 |  |
|  | KBAC | 400 | 0.064 ± 0.017 | 0.953 – 0.975 | 4.03 ± 0.67 | -25.30 ± 6.39 | 0.973 – 0.985 |  |
|  |  | 600 | 0.068 ± 0.007 | 0.842 – 0.987 | 3.87 ± 0.67 | -17.87 ± 8.32 | 0.949 – 0.988 |  |
|  |  | 800 | 0.138 ± 0.036 | 0.902 – 0.973 | 5.83 ± 0.55 | -24.30 ± 21.61 | 0.901 – 0.955 |  |
|  |  | 1000 | 0.204 ± 0.021 | 0.904 – 0.937 | 7.17 ± 0.12 | -23.43 ± 6.95 | 0.907 – 0.940 |  |
| TOL | SBAC | 400 | 0.158 ± 0.044 | 0.868 – 0.951 | 18.07 ± 1.72 | -20.17 ± 49.80 | 0.896 – 0.944 |  |
|  |  | 600 | 0.230 ± 0.012 | 0.887 – 0.926 | 22.20 ± 0.98 | 7.23 ± 18.65 | 0.874 – 0.905 |  |
|  |  | 800 | 0.212 ± 0.019 | 0.803 – 0.870 | 19.90 ± 0.85 | 54.53 ± 13.78 | 0.799 – 0.850 |  |
|  |  | 1000 | 0.232 ± 0.031 | 0.814 – 0.895 | 20.43 ± 0.32 | 33.70 ± 42.86 | 0.817 – 0.888 |  |
|  | KBAC | 400 | 0.026 ± 0.007 | 0.949 – 0.972 | 4.30 ± 1.18 | -35.50 ± 7.66 | 0.958 – 0.976 |  |
|  |  | 600 | 0.078 ± 0.026 | 0.981 – 0.985 | 9.33 ± 1.62 | -64.70 ± 8.22 | 0.975 – 0.987 |  |
|  |  | 800 | 0.126 ± 0.042 | 0.963 – 0.990 | 11.20 ± 0.70 | -56.93 ± 20.97 | 0.928 – 0.982 |  |
|  |  | 1000 | 0.170 ± 0.009 | 0.899 – 0.947 | 11.33 ± 0.64 | -10.13 ± 17.22 | 0.866 – 0.908 |  |

Reference

- Nguyen C, Do DD. The Dubinin–Radushkevich equation and the underlying microscopic adsorption description. Carbon. 2001;39(9):1327-36.

Correspondence: hchsi@ntu.edu.tw