Supplementary information

Hybrid PEO–hydrothermal–silane coating with synergistic Ce–8HQ inhibitor sealing for durable corrosion protection of AZ31 magnesium alloy

Majid Shahsanaei a, c, Nastaran Farahbakhsh a, Masoud Atapour b, Morteza Shamanian b, Benjamin Butz c, Christian Pritzel a, and Manuela S. Killian a*

a) Chemistry and Structure of novel Materials, Department of Chemistry and Biology, University of Siegen, Paul-Bonatz-Str. 9-11, 57076 Siegen, Germany

b) Department of Materials Engineering, Isfahan University of Technology, Isfahan 84156-83111, Iran

c) Micro- and Nano Analytics Group, University of Siegen, Adolf-Reichwein-Straße 28, 57076 Siegen, Germany

* Corresponding author, Email: Manuela Killian, manuela.killian@uni-siegen.de

Figure S 1: SEM images of PEO coatings at different magnifications. The images clearly show cracks and pores formed during plasma electrolytic oxidation.

Figure S 2: SEM images of PEO/HT coatings at different magnifications, showing that cracks and pores are effectively sealed by Ce-based components.

Figure S 3: SEM images of (a) PEO/HT/Silane and (b) PEO/HT/Silane+8HQ show that the surface is covered with a silane layer.

Figure S 4: Water contact angle measurements of various samples: (a) AZ31 magnesium, (b) PEO, (c) PEO/HT, (d) PEO/HT/Silane, and (e) PEO/HT/Silane+8HQ.

Figure S 5: Parameters calculated using the Young’s equation and Neumann equation, including work of adhesion, surface free energy, and water contact angle for different samples.

Figure S 6: Positive ToF-SIMS signals of molecular fragments: (a) Mg+, (b) C2H5NO+, (c) C9H9NO+/ SiC5H13NO2+, and (d) SiO2C9H9NO+ for PEO/HT and PEO/HT/silane+8HQ samples.

Table S 1: Peak list applied for PCA of positive-ion ToF-SIMS spectra from PEO/HT and PEO/HT/silane+8HQ samples. Fragment assignments were obtained from the corresponding loading plot shown in Figure 5e.

| m/z | Ion |
| --- | --- |
| 15.02 | CH3+ |
| 23.98 | Mg+ |
| 27.97 | Si+ |
| 40.99 | MgOH+ |
| 41.03 | C3H5+ |
| 44.02 | C2H4O+ |
| 45.03 | CH3NO+ |
| 58.03 | C2H4NO+ |
| 59.03 | C2H5NO+ |
| 73.04 | SiC2H5O+ |
| 87.04 | SiC2H5NO+ |
| 91.02 | NaC5H8+ |
| 139.91 | Ce+ |
| 140.91 | Na2PO4+ |
| 147.09 | C9H9NO+/SiC5H13NO2+ |
| 155.91 | CeO+ |
| 156.92 | CeOH+ |
| 207.03 | SiO2C9H9NO+ |