Table S1. Iron and alumina oxides contents of Marwit El Sweiqat original quartz samples (RER feeding samples)

| Sample | Wt.% | Fe2O3% | Al2O3% |
| --- | --- | --- | --- |
| Unclassified -0.6+0.1 mm | 100.00 | 0.104 | 0.0875 |
| -0.6+0.3mm fraction | 49.50 | 0.105 | 0.086 |
| -0.3+0.1 mm fraction | 50.50 | 0.103 | 0.089 |

Table S2. The design variables and their coded/ actual levels

| Overall -0.6+0.1 mm |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Factor | Name |  | Units | Type |  |  | Low actual |  |  | High actual | Low coded | High coded |
| A | Splitter Angle |  | Degree | Numeric |  |  | 85 |  |  | 95 | -1 | 1 |
| B | Belt Speed |  | rpm | Numeric |  |  | 200 |  |  | 250 | -1 | 1 |
| -0.6+0.3 mm coarse fraction |  |  |  |  |  |  |  |  |  |  |  |  |
| A |  | Splitter Angle | Degree |  |  | Numeric |  | 85 | 95 |  | -1 | 1 |
| B |  | Belt Speed | rpm |  |  | Numeric |  | 200 | 250 |  | -1 | 1 |
| -0.3+0.1 mm fine fraction |  |  |  |  |  |  |  |  |  |  |  |  |
| A |  | Splitter Angle | Degree |  | Numeric |  |  | 85 |  | 95 | -1 | 1 |
| B |  | Belt Speed | rpm |  | Numeric |  |  | 200 |  | 250 | -1 | 1 |

Table S3.The results of analysis of variance (ANOVA) for the all fractions (Marwit El Sweiqat)

| Marwit El Sweiqat overall quartz sample, -0.6+0.1 mm, (Ov.S.) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Conc. Wt., % |  |  | Fe2O3 Red. % |  |  |  | Al2O3 Red. % |  |  |
| Source | F Value | Prob > F | Source | F Value | Prob > F |  | Source | F Value | Prob > F |
| Model A B A2 B2 AB | 1273.70 5205.35 24.14 1058.09 0.61 41.32 | < 0.0001 < 0.0001 0.0080 < 0.0001 0.4768 0.0030 | Model A B A2 B2 AB | 444.19 177.8 1064.91 16.31 383.14 0.28 | <0.0001 0.0002 < 0.0001 0.0156 <0.0001 0.6232 |  | Model A B A2 B2 AB | 11.28 8.46 31.69 6.89 3.73 3.58 | 0.0179 0.0438 0.0049 0.0585 0.1257 0.1316 |
| Pure error | 0 |  | Pure error | 0 |  |  | Pure error | 0 |  |
| -0.6 +0.3 mm coarse fraction (C.S.) |  |  |  |  |  |  |  |  |  |
| Model A B A2 B2 AB | 2037.67 7601.29 43.35 2461.78 0.24 3.10 | < 0.0001 < 0.0001 0.0028 < 0.0001 0.6528 0.1530 | Model A B A2 B2 AB | 13.33 2.57 59.60 1.25 3.07 0.71 | 0.0132 0.1838 0.0015 0.3264 0.1548 0.4478 | Model A B A2 B2 AB |  | 82.80 39.57 287.92 0.48 71.93 10.06 | 0.0004 0.0033 < 0.0001 0.5284 0.0011 0.0338 |
| Pure error | 0 |  | Pure error | 0 |  | Pure error |  | 0 |  |
| -0.3 +0.1 mm fine fraction (F.S.) |  |  |  |  |  |  |  |  |  |
| Model A B A2 B2 AB | 1540.77 5913.00 93.42 1603.40 7.21 3.92 | < 0.0001 < 0.0001 0.0006 < 0.0001 0.0549 0.1187 | Model A B A2 B2 AB | 34.12 53.27 86.28 4.88 16.95 5.49 | 0.0022 0.0019 0.0007 0.0916 0.0146 0.0792 | Model A B A2 B2 AB |  | 91.46 80.05 185.05 14.7 56.06 0.05 | 0.0003 0.0009 0.0002 0.0186 0.0017 0.8345 |
| Pure error | 0 |  | Pure error | 0 |  | Pure error |  | 0 |  |

Table S4. Significance model terms for El Sweiqat Quartz Samples

| Marwit El Sweiqat quartz overall sample, -0.6+0.1 mm, (Ov.S.) |  |
| --- | --- |
| Conc. Wt., % | A, B, A2 and AB |
| Fe2O3 Reduction % | A, B, A2 and B2 |
| Al2O3 Reduction % | B |
| -0.6 +0.3 mm coarse fraction (C.S.) |  |
| Conc. Wt., % | A, B and A2 |
| Fe2O3Reduction % | B |
| Al2O3Reduction % | A, B, B2, AB |
| -0.3 +0.1 mm fine fraction (F.S.) |  |
| Conc. Wt., % | A and A2 |
| Fe2O3Reduction % | A, B and B2 |
| Al2O3Reduction % | A, B, A2 and B2 |

Table S5.Optimization test scheme constraints for the Magnaroll separation of Marwit El-Sweiqat ground quartz sample.

| Name | Goal | Lower Limit | Upper Limit | Lower Weight | Upper Weight | Importance |
| --- | --- | --- | --- | --- | --- | --- |
| The unclassified sample, (OV.S.) |  |  |  |  |  |  |
| Splitter Angle, degree | Is in range | 85o | 95o | 1 | 1 | 3 |
| Belt Speed, rpm | Is in range | 200 | 250 | 1 | 1 | 3 |
| Fe2O3 Red., % | Maximum | 94.17 | 98.73 | 1 | 1 | 3 |
| Al2O3 Red., % | Maximum | 86.62 | 98.76 | 1 | 1 | 3 |
| The -0.6+0.3 mm coarse fraction, (C.S.) |  |  |  |  |  |  |
| Splitter Angle, degree | Is in range | 85o | 95o | 1 | 1 | 3 |
| Belt Speed, rpm | Is in range | 200 | 250 | 1 | 1 | 3 |
| Fe2O3 Red., % | Maximum | 94.95 | 98.85 | 1 | 1 | 3 |
| Al2O3 Red., % | Maximum | 89.53 | 97.79 | 1 | 1 | 3 |
| The -0.3+0.1 mm fine fraction, (F.S.) |  |  |  |  |  |  |
| Splitter Angle, degree | Is in range | 85o | 95o | 1 | 1 | 3 |
| Belt Speed, rpm | Is in range | 200 | 250 | 1 | 1 | 3 |
| Fe2O3 Red., % | Maximum | 89.12 | 97.76 | 1 | 1 | 3 |
| Al2O3 Red., % | Maximum | 50.58 | 85.95 | 1 | 1 | 3 |