(Supporting Information)

A Hierarchical Au@PDA-PdCu Nanozyme for Signal-Amplified Immunochromatographic Detection of Carbofuran in Leafy Vegetables

Haofeng Lao†, a, Xuhui Yue†, a, Xiaoqing Weng†, a, Shaokang Zhanga, Jiachen Shi*, a ,Yuanfeng Wang*, a

a Development Center of Plant Germplasm Resources, College of Life Sciences, Shanghai Normal University, Shanghai 200234, China

† These authors contributed equally to this work.

* Corresponding author.

Figure S1. Optimization of DA·HCl dosage for the synthesis of Au@PDA-PdCu nanozymes.

Figure S2. Optimization of Pd and Cu feeding amounts: (a) optimization of Pd addition; (b) optimization of Cu addition; (c) comparison of absorbance change rates between Au@PDA-Pd and Au@PDA-PdCu nanozymes.

Figure S3. Optimization of the solid content in lyophilized probe conjugates.

Figure S4. Optimization of the lyophilization time for probe preparation.

Figure S5. Accelerated aging stability test of ICA strips prepared with liquid, sprayed, and lyophilized probes.

Figure S6. Optimization of sample extraction reagents: (a) comparison of extraction solvent ratios; (b) colorimetric performance of extracts on ICA strips prepared with three probe types.

Figure S7. Calibration curves of three types of carbofuran ICA strips— (a, b, c) liquid, (d, e, f) sprayed, and (g, h, i) lyophilized—tested with Chinese cabbage, chive, and spinach samples.

Table S1. Optimization results of liquid-type probe-based ICA parameters determined by the checkerboard titration method.

| Probe quantity (μL) | Concentration (mg/mL) | T-line | T/C | inhibition ratio (%) |
| --- | --- | --- | --- | --- |
| 10 | 0.4 | 2125.9±319.8 | 0.54±0.04 | 44.3±14.5 |
| 20 |  | 3534.8±717.0 | 0.47±0.04 | 51.3±6.5 |
| 30 |  | 5555.3±376.2 | 0.76±0.01 | 27.4±3.0 |
| 10 | 0.5 | 1388.8±240.1 | 0.37±0.08 | 62.8±17.1 |
| 20 |  | 2666.2±267.5 | 0.46±0.08 | 55.8±5.7 |
| 30 |  | 3134.9±812.8 | 0.57±0.09 | 51.1±1.7 |
| 10 | 0.6 | 2271.5±113.9 | 1.04±0.02 | 41.7±1.2 |
| 20 |  | 4735.7±131.7 | 1.13±0.03 | 41.2±3.0 |
| 30 |  | 5130.4±239.3 | 1.25±0.20 | 32.0±7.5 |

Table S2. Optimization results of sprayed-type probe-based ICA parameters determined by the checkerboard titration method.

| Probe quantity (μL/cm) | Concentration (mg/mL) | T-line | T/C | inhibition ratio (%) |
| --- | --- | --- | --- | --- |
| 3 | 0.4 | 1138.8±57.8 | 0.28±0.07 | 86±3.8 |
| 3.5 |  | 2041.3±336.1 | 0.46±0.04 | 69.8±14 |
| 4 |  | 2922±1219.6 | 0.58±0.24 | 27.4±3.0 |
| 3 | 0.5 | 1639.4±454.1 | 0.28±0.06 | 81.1±5.7 |
| 3.5 |  | 3307.3±654.1 | 0.46±0.06 | 78.3±3.5 |
| 4 |  | 4097.4±401.8 | 0.49±0.03 | 75.2±1.6 |
| 3 | 0.6 | 1475.8±933.1 | 0.31±0.18 | 82.5±8.8 |
| 3.5 |  | 2436.6±1196.9 | 0.43±0.17 | 78.2±7.2 |
| 4 |  | 1804.4±307.4 | 0.35±0.03 | 77.8±5.1 |

Table S3. Optimization results of lyophilized-type probe-based ICA parameters determined by the checkerboard titration method.

| Probe quantity (μL) | Concentration (mg/mL) | T-line | T/C | inhibition ratio (%) |
| --- | --- | --- | --- | --- |
| 5 | 0.1 | 1166.9±212.3 | 0.22±0.03 | 94.4±0.5 |
| 10 |  | 1654.8±70.9 | 0.22±0.01 | 91.4±0.2 |
| 15 |  | 2308.7±190 | 0.25±0.02 | 90.0±0.9 |
| 5 | 0.2 | 1078.7±104.9 | 0.22±0.01 | 94.0±1.2 |
| 10 |  | 2130.5±211 | 0.33±0.05 | 91.2±0.8 |
| 15 |  | 2313.9±172.2 | 0.29±0.03 | 91.2±1.1 |
| 5 | 0.3 | 1159±87.5 | 0.26±0.03 | 95.8±1.1 |
| 10 |  | 1927.1±112.2 | 0.30±0.02 | 92.1±1.6 |
| 15 |  | 2438.7±466 | 0.39±0.08 | 88.1±1.2 |

Table S4. Analytical performance of three carbofuran ICA strips for detection in three vegetable matrices.

| Test strip type | Vegetable species | Detection mode | IC50(ng/ml) | LOD(ng/ml) |
| --- | --- | --- | --- | --- |
| Liquid probe strip | Chinese cabbage | Direct | 0.469 | 0.053 |
|  |  | DAB-enhanced | 1.061 | 0.107 |
|  | Chive | Direct | 0.119 | 0.008 |
|  |  | DAB-enhanced | 0.373 | 0.014 |
|  | Spinach | Direct | 0.368 | 0.081 |
|  |  | DAB-enhanced | 0.454 | 0.081 |
| Sprayed probe strip | Chinese cabbage | Direct | 0.117 | 0.002 |
|  |  | DAB-enhanced | 0.839 | 0.035 |
|  | Chive | Direct | 0.936 | 0.190 |
|  |  | DAB-enhanced | 0.560 | 0.069 |
|  | Spinach | Direct | 0.599 | 0.100 |
|  |  | DAB-enhanced | 2.608 | 0.240 |
| Lyophilized probe strip | Chinese cabbage | Direct | 0.371 | 0.067 |
|  |  | DAB-enhanced | 0.464 | 0.090 |
|  | Chive | Direct | 0.414 | 0.090 |
|  |  | DAB-enhanced | 0.371 | 0.067 |
|  | Spinach | Direct | 0.422 | 0.139 |
|  |  | DAB-enhanced | 0.856 | 0.153 |