Supporting Information

An unexpected phenomenon of intense luminescence of aqueous solutions of macromolecular europium complexes

Elena L. Krasnopeeva, Tatiana N. Nekrasova, Elena Yu. Melenevskaya, Elena N. Vlasova, Anna V. Kashina, Michael A. Smirnov, Alexander V. Yakimansky*

Branch of Petersburg Nuclear Physics Institute Named by B.P. Konstantinov of National Research Centre “Kurchatov Institute” – Institute of Macromolecular Compounds, 31 Bolshoy pr. V.O., St. Petersburg, 199004 Russia

Polymer synthesis[1]

Synthesis of Macroinitiator, Cell-BiB

0.4 g of MCC was dissolved in 10 g of an ionic liquid – BMIMCl, at 80 °C, 5 mL of bromo-anhydride of 2-bromo-isobutyric acid was added dropwise to the solution, the reaction the mixture was kept for 8 h, after which the macroinitiator was planted in an excess of deionized water, filtered, washed, and dried under vacuum to constant weight.

Polymerization of TBMA on a Macroinitiator

0.035 g of Cell-BiB was dissolved in 10 g of BMIMCl at 80 °C. The resulting solution was degassed under vacuum, after which 0.01 g of CuBr and 1.5 mL of TBMA was added to it. Before the reaction, TBMA was degassed by threefold repetition of freeze– thaw cycles. The reaction was carried out with stirring on a magnetic stirrer for 7 h and left overnight at room temperature. The resulting product, Cell-g-PTBMA, was precipitated in an excess of distilled water and purified with acetone on a Soxhlet extraction apparatus.

Molecular Cellulose Brushes with Poly(methacrylic Acid) Side Chains

Freshly distilled trifluoroacetic acid was introduced into a solution of a cellulose-based brush with PTBMA side chains with a concentration of 4 wt% in pre-distilled CH2Cl2. The reaction was carried out at a temperature of 25 °C with constant stirring for a day, then the solvent was distilled off, the precipitated Cell-g-PMAA was purified by reprecipitation from ethyl alcohol into methylene chloride, and subsequently dried at 40 °C under vacuum.

Cleavage of grafted PTBMA chains from Cell-g-PTBMA

0.1 g Cell-g-PTBMA of is dissolved in 15 ml of freshly distilled THF, then 10 ml of a 5 wt% methanol solution of KOH is added. The reaction mixture is maintained in a glass container with a screw cap (Schott Duran, Germany) for three days at 90 °C. After completion of the reaction, the mixture is neutralized with hydrochloric acid, then the product is concentrated and precipitated in water, washed multiply with water, and dried at 40 °C under vacuum.

Reference

1 Krasnopeeva EL, Melenevskaya EY, Klapshina LG, Shilyagina NY, Balalaeva IV, Smirnov NN, Smirnov MA, Yakimansky AV (2021) Poly(methacrylic Acid)-Cellulose Brushes as Anticancer Porphyrazine Carrier. Nanomaterials 11:1997. https://doi.org/10.3390/nano11081997