Supplementary Table S1|. Representative optical ratiometric thermometry methods with emission bands lying within the NIR biological window.

| Materials | T Range (K) | Sr (%/ K) | Mode ( nm) | Ref. |
| --- | --- | --- | --- | --- |
| Sc2(MoO4)3:Yb3+/Er3+ | 298-623 | 12.9 | Lifetime1538 | This work |
| LiLaP4O12:Yb3+/Cr3+ | 100-475 | 1.2 | FIR820/975 | 1 |
| LiLaP4O12:Nd3+/Cr3+ | 293-323 | 4.89 | FIR810/1048 | 2 |
| LaF3:Tm3+ | 297-361 | 1.90 | FIR1470/1230 | 3 |
| LuVO4:Yb3+/Er3+@SiO2 | 298-523 | 0.182 | FIR1469/1527 | 45 |
| TTA-NaYF4: Nd3+ | 283-323 | 7.1 | FIR540/1060 | 4 |
| Al4B2O9:Yb3+/Nd3+ | 298-333 | 2.6 | FIR800/920 | 5 |
| LaF3:Yb3+/Er3+@LaF3:Yb3+/Tm3+ | 293-323 | 5 | FIR1000/1550 | 46 |
| YVO4:Yb3+/Tm3+ | 300-1009 | 2.13 | FIR940/800 | 6 |
| YAlO3:Nd3+ | 293-611 | 1.83 | FIR820/890 | 7 |
| Na2K(Lu3Si6O18):Yb3+/Er3+ | 12-450 | 2.6 | FIR1125/1640 | 8 |

Supplementary Figure 1| Structural characterization. a. XRD patterns of Sc2(MoO4)3:xYb/1%Er crystals with different Yb3+ doped concentrations at room temperature. b. XRD patterns of Sc2(MoO4)3:20%Yb/yEr crystals with different Er3+ doped concentrations at room temperature.

Supplementary Figure 2| Morphology and chemical compositions. a. Typical SEM images of the Sc2(MoO4)3:20%Yb/1%Er phosphors. The scale bar is 1 μm. b. EDX data taken from a single particle. c. Elemental maps of Sc, Mo, O, Yb and Er in Sc2(MoO4)3:20%Yb/1%Er particle. The scale bar is 5 μm.

Supplementary Figure 3| Lattice changes with temperature. Temperature-dependent unit cell parameters a, b, and c of the Sc2(MoO4)3:20%Yb/1%Er phosphors derived from in situ SXRD patterns.

Supplementary Figure 4| Emission spectra in Yb2WO6:1%Er3+ phosphor. a. Upconversion emission spectra of the Yb2WO6:1%Er3+ crystals as a function of temperature under 980 nm excitation. b. Integral emission intensity of Yb2WO6: 1%Er3+ crystals as a function of temperature.

Supplementary Figure 5| Spectra in Yb2WO6:1%Er phosphor. a. Downshifting emission spectra of Yb2WO6:1%Er. b. Integral emission intensity of Yb2WO6:1%Er crystals as a function of temperature.

Supplementary Figure 6| Emission spectra in Sc2(MoO4)3:5%Er3+ phosphor. a. Simplified energy level diagram showing upconversion process via excited-state absorption of Er3+. b. Upconversion emission spectra of the Sc2(MoO4)3:5%Er3+ crystals as a function of temperature under 980 nm excitation. c. Integral emission intensity of Sc2(MoO4)3:5%Er3+ crystals as a function of temperature.

Supplementary Figure 7| Temperature-dependent spectra in Sc2(MoO4)3:5%Er phosphor. a. Downshifting emission spectra of Sc2(MoO4)3:5%Er under 980 nm excitation. b Normalized NIR emission intensities of Sc2(MoO4)3:5%Er3+as a function of temperature.

Supplementary Figure 8| Temperature-dependent luminescence decay curves of 2F5/2 excited state of Yb3+. a. and b. Temperature-dependent luminescence decay curves of 2F5/2 excited state of Yb3+ in Yb3+/Er3+-codoped and Yb3+-single doped SMO, respectively.

Supplementary Figure 9| Temperature-dependent luminescence decay curves of 2H11/2 and 4I11/2 excited states of Er3+. a. and b. Temperature-dependent luminescence decay curves of 2H11/2 and 4I11/2 excited states of Er3+ in Yb3+/Er3+-codoped SMO, respectively.

References

- Marciniak, L. et al. Nanocrystalline NIR-to-NIR luminescent thermometer based on Cr3+,Yb3+ emission, Sens. Actuators, B, 243, 388-393 (2017).

- Marciniak, L. et al. A new generation of highly sensitive luminescent thermometers operating in the optical window of biological tissues, J. Mater. Chem. C, 4, 5559-5563 (2016).

- Ximendes, E. C. et al. Thulium doped LaF3 for nanothermometry operating over 1000 nm, Nanoscale, 11, 8864-8869 (2019).

- Xu, M. et al. Ratiometric nanothermometer in vivo based on triplet sensitized upconversion, Nat. Commun. 9, 2698 (2018).

- Silva, A. F. et al. Thermal sensitivity of frequency upconversion in Al4B2O9:Yb3+/Nd3+ nanoparticles, J. Mater. Chem. C, 5, 1240-1246 (2017).

- Runowski, M. et al. Luminescent nanothermometer operating at very high yemperature-sensing up to 1000 K with upconverting nanoparticles (Yb3+/Tm3+), ACS Appl. Mater. Interf. 12, 43933-43941 (2020)

- Hernandez-Rodríguez, M. A. et al. Comparison of the sensitivity as optical temperature sensor of nano-perovskite doped with Nd3+ ions in the first and second biological windows. Sens. Actuators, B 255, 970-976 (2018).

- Ananias, D. et al. Near-infrared ratiometric Luminescent thermometer based on a new lanthanide silicate, Chem. Eur. J., 24, 11926-11935 (2018).