Supporting Information

Switchable Structure Promoted Leaching Free Atomically Dispersed Pt Catalyst for Low Carbon Biomass Polyol Oxidation

Hao Yana, Mingyue Zhaoa, Xin Zhoua, Siming Zhaoa, Shangfeng Lia, Minghao Zhaa, Fanyu Menga, Xiang Fenga*, Xiaobo Chena, Yibin Liua*, De Chenb*, Ning Yanc, Chaohe Yanga

aState Key Laboratory of Heavy Oil Processing, China University of Petroleum,

Qingdao 266580, China

bDepartment of Chemical Engineering, Norwegian University of Science and Technology,

Trondheim 7491, Norway

c Department of Chemical and Biomolecular Engineering, National University of Singapore, 4 Engineering Drive 4, 117585, Singapore

*Corresponding author: E-mail address: xiangfeng@upc.edu.cn (X. Feng); liuyibin@upc.edu.cn (Y. Liu); de.chen@ntnu.no (D. Chen);

1. Supplementary Experimental Procedures	1

1.1 Chemicals	1

1.2 Catalyst preparation	1

1.3 Catalyst characterization	2

1.4 Catalytic test	3

1.5 Density functional theory (DFT) calculations	4

2. Supplementary Data Items	5

2.1 XRD patterns	5

2.2 HAADF-STEM images and particle size distribution	6

2.3 N2-physisorption	7

2.4 Coordination structure and bond length of Pt1/HAP catalyst	7

2.5 Detailed discussion on H2-TPR and CO2-TPD	8

2.6 Characterization of the used catalyst	10

2.7 Configuration and charge distribution of C-H bond activation	11

2.8 Supplementary free energy diagram	12

2.9 In-situ FT-IR on Pt/AC	14

2.10 SEM images of the Pt1/HAP catalyst	14

2.11 Kinetics determination	14

I. Elimination of the diffusion limitations	14

II. The results of apparent reaction kinetics	16

III. Entropy change analysis of apparent reaction kinetics	18

IV. Combining experiment with DFT calculation	19

2.12 Physicochemical properties of the catalysts	21

2.13 EXAFS parameters	21

2.14 Quantitative analysis of H2-TPR, NH3-TPD and CO2-TPD	22

2.15 Results of catalytic oxidation of low carbon polyols	23

2.16 Summary of activation energy calculated by DFT calculation and reaction kinetics	26

1. Supplementary Experimental Procedures

1.1 Chemicals

Ammonium dihydrogen phosphate (98% ACS, NH4H2PO4), calcium nitrate tetrahydrate (98% ACS, Ca(NO3)2·4H2O), ammonia solution tetrahydrate (25%-28%, NH3·H2O), chloroplatinic acid (99.9% ACS, H2PtCl6·6H2O), glycerol (99%, C3H8O3) and activated carbon (AC) were purchased from Sigma-Aldrichk. Deuterated glycerol (CD2OHCDOHCD2OH) and D2O were purchased from J&K scientific.

1.2 Catalyst preparation

Hydroxyapatite (HAP) support: HAP material was synthesized according to the previous reports.1 Briefly, 1.4 g NH4H2PO4 was first dissolved in 50 mL deionized water, and the pH of this solution was adjusted to 12 via the addition of NH3·H2O. Subsequently, 4.7 g Ca(NO3)2·4H2O in 80 mL deionized water was dropwise to the above solution with the fixed pH value of 12. After stirring for 2 h at 80 °C, this mixture was transferred into a Teflon-lined autoclave and hydrothermal crystallized at 110 °C for 24 h. The obtained sample was filtered by deionized water, dried (at 70 oC for 2 h) and calcined (at 550 oC for 6 h).

Pt1/HAP catalyst: Atomically dispersed Pt1/HAP catalyst was prepared by green and convenient in-situ doping method. The synthesis process was as follows: 1.4 g NH4H2PO4 together with a certain amount of H2PtCl6·6H2O was mixed in 50 mL deionized water and stirred at 0 oC for 12 h. Then, 4.7 g Ca(NO3)2·4H2O in 80 mL deionized water was dropwise added slowly and the pH of this solution was adjusted to 12. After stirring for 12 h at 0 °C, this mixture was transferred into a Teflon-lined autoclave and hydrothermal crystallized at 110 °C for 24 h. The as-formed sample was filtered by deionized water, dried (at 70 oC for 2 h) and calcined (at 550 oC for 6 h) to obtain Pt1/HAP catalyst. The Pt metal content determined by inductively coupled plasma optical emission spectrometry (ICP-OES) was 0.14 wt%. The final sample was reduced by 10 vol% H2 in Ar (60 mL/min) for 3 h at 300oC.

Pt/AC catalyst: Pt/AC catalyst was prepared by equivalent-volumetic impregnation methods. A certain amount of H2PtCl6·6H2O solution was added to 1 g AC (purchased from Sigma-Aldrichk), allowing to stand at room temperature for 6 h. The as-formed sample was dried (at 100 °C for 2 h), then calcined in static air (at 550 °C for 2 h). The Pt metal content measured by ICP was 0.84%. The final sample was reduced by 10 vol% H2 in Ar (60 mL/min) for 3 h at 300oC.

1.3 Catalyst characterization

X-ray diffraction (XRD) was analyzed on X’pert PRO MPD with a CuKα radiation (1.5418 Å). ICP-OES was performed using VARIAN 720-ES. Transmission electron microscopy (TEM) was carried out on a JEM 2100F. High-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) was performed on the Titan 80-300 scanning/transmission electron microscope equipped with a probe spherical aberration corrector. Valence state of metal surface was measured by X-ray photoelectron spectroscopy (XPS) on the Thermo ESCALAB 250Xi with the C 1s binding energy of 284.8 eV. N2 physisorption was determined on Micromeritics ASAP 2020, and the surface area was calculated by Brunauer-Emmet-Teller (BET) method. X-ray absorption spectroscopy (XAS) measurements were carried out in the Advanced Photon Source at Argonne National Laboratory (fluorescence mode on beamline 12-BM). The ATHENA module was used to fit the data of extended X-ray absorption fine structure spectroscopy (EXAFS) and X-ray absorption near edge structure (XANES). NH3-TPD, CO2-TPD, H2-TPD and H2-TPR were conducted in the Micromeritics AutoChem II 2920 instrument. For NH3-TPD, CO2-TPD, CO-TPD and H2-TPD, the sample (0.1 g) was pretreated by 60 mL/min of He gas (or 10 vol.% H2 in Ar in H2-TPD) for 1 h at 300oC. Then, the as-reduced sample was cooled down to 50oC, and NH3 (or CO2, CO/H2) gas (30 mL/min) was introduced into the samples for 1 h. Afterwards, the quartz tube was heated to 600 oC at a rate of 20 oC/min. The signal is collected by TCD detector. For H2-TPR, the un-reduced catalyst was treated by 10 vol% H2 in Ar (60 mL/min), and the quartz tube was heated to 600 oC in a heating rate of 15oC/min. The signal is collected by TCD detector.

In situ diffuse reflectance infrared Fourier transform spectroscopy (DRIFTS) was performed on the Thermo Scientific Nicolet iS50 FT-IR. The samples were pretreated with 50 mL/min of 10 vol.% H2 in Ar at 300oC for 1 h. Then, N2 (40 mL/min) is used to purge the sample and cool to 30oC. Pure CO (40 mL/min) was purged for 20 min to reach adsorption saturation. A N2 purge at a flow rate of 40 40 mL/min was performed to remove gas phase CO from the DRIFTS cell. All the spectra were recorded using 128 scans with a resolution of 4 cm-1. In situ FTIR spectra was measured on the Bruker Vector 22 spectrometer. In detail, the catalysts with 1 mL mixed solution of glycerol and sodium hydroxide (0.05 mol/L) was freeze-dried for 24 h. Then, the sample is filled in the in situ cell in N2 (30 mL/min) at 25oC for 1h (record background). Switching the gas into O2 (5 vol% O2 and He mixture gas) with a 30 mL/min ﬂow rate, the in situ cell was heated to 200oC, and the data was collected every 20 oC and every 1 min when the reaction temperature was reached. For the FT-IR of HAP support, Pt1/HAP and used Pt1/HAP catalysts, samples were mixed with pre-dried FT-IR grade KBr and pressed into disks for test. Then, transmission infrared spectra of disks were recorded in the range of 4000-400 cm-1 with a 0.3 cm-1 resolution.

1.4 Catalytic test

The selective oxidation of low carbon polyols was performed in the 50 mL autoclave. 0.2 g catalyst, 0.5 g substrate, 25 mL deionized water were added. After several times of O2 gas washing, the pressure was fixed at 1.0 MPa. The gas product was analyzed by a Scion 456-GC Chromatography equipped with a TCD detector. The liquid product was analyzed by a Shimadzu LC-20AT high performance liquid chromatography (HPLC) with UV and refractive index (RID-10A) detectors. The chromatographic column was Rezex ROA-Organic Acid H+ (8%), and the mobile phase was 0.005M H2SO4 solution. The turnover frequency (TOF), conversion (X) and product selectivity (S) were calculated by the following formula:

TOF was calculated as mole of polyol converted per mole of surface atoms per hour. M, T and N represent the number of surface active sites, reaction time and the number of polyol moles converted during the reaction time, respectively. It should be noted that TOF is estimated at conversions less than 10%, which could ensure that the average reaction rate equaled the instantaneous reaction rate. In addition, K0 is the initial concentration of polyol (mol/L), Kt is the concentration after the polyol oxidation (mol/L), and Ct is the concentration of carboxylic acid product formed in the reaction (mol/L). The initial reaction rate is expressed as the number of moles of polyols converted per unit time per unit mass of Pt metal.

1.5 Density functional theory (DFT) calculations

DFT calculations were performed in the Dmol3 program. The Perdew-Burke-Ernzerhof (PBE) functional from the generalized gradient approximation (GGA) was used to obtain the correlation energies. Monkhorst-Pack method was selected for sampling brillouin zone (3×3×1) after convergence test. The double numerical plus polarization (DNP) together with effective core potentials was used to describe the iron electrons. The real space atomic cutoff radius was chosen as 4.5 Å, and the TS parameters for van der Waals dispersion correction was also considered in the calculation process. All the energies obtained in this work have been corrected by zero point energy. The transition state was determined by LST/QST method, and the vibrational frequency analysis was used to ensure that there is only one virtual frequency from reactant to product. Allowable deviations for displacement, gradient and total energy are 0.005 Ǻ, 0.002 Ha/Ǻ and 1.0×10-5 Ha respectively. Single Pt atom was supported on the HAP (001) model (with 4-layer p(1×1)) in the 20 Å vacuum layer. The whole configuration was in relaxation. The adsorption energy of substrate could be defined as: Eads=EPt+HAP(001)+substrate-EPt+HAP(001)-Esubstrate, where EPt+HAP(001)+substrate,  EPt+HAP(001) and Esubstrate are the total energy of the calculation system, the isolated energy of calculation model and substrate, respectively.

All energy correction terms are extracted from the normal mode analyses of the optimized reactant and transition state at different temperatures. Outputs from Dmol3 calculations include corrections to bring bare electronic energies and Gibbs free energies. Gibbs free energies correction also has contained the zero-point vibrational energy correction.

The activation barrier with zero-point vibrational energy correction (), the activation barrier () and free energy presented () herein are obtained using the following calculation scheme:

(1)

(2)

(3)

(4)

(5)

Whereandare the electronic ground state energies of the transition and reactant state, respectively. andare the free energy corrections of the transition and reactant state, respectively. Theandare the respective zero point vibrational energy (ZPE) corrections.

2. Supplementary Data Items

2.1 XRD patterns

Figure S1. XRD patterns of the Pt/AC, Pt1/HAP catalysts and HAP support. The XRD peaks of the Pt1/HAP catalyst and HAP support are almost identical, indicating that the catalyst has a stable HAP structure. The Pt/AC catalyst exhibits a diffraction peak of Pt (111) at ~40o.

2.2 HAADF-STEM images and particle size distribution

Figure S2. HAADF-STEM images and particle size distribution of a) 0.32 wt% Pt/HAP, b) 0.96 wt% Pt/HAP, c) 1.45 wt% Pt/HAP and d) Pt/AC catalysts. The preparation method of the 0.32 wt% Pt/HAP, 0.96 wt% Pt/HAP and 1.45 wt% Pt/HAP were the same as the Pt1/HAP catalyst. The increase of Pt metal loading results in the increase of particle size from single atom to 2.2 nm. The Pt/AC catalyst prepared by impregnation method with the Pt metal loading of 0.8 wt% exhibits a particle size of 3.9 nm.

2.3 N2-physisorption

Figure S3. N2-physisorption isotherms and pore size distribution for the (a) Pt1/HAP, HAP and (b) Pt/AC catalyst. BET specific surface area and pore volume were summarized in Table S1.

2.4 Coordination structure and bond length of Pt1/HAP catalyst

Figure S4. (a) Coordination structure and (b) bond length of Pt1/HAP catalyst shown by DFT calculation.

Figure S5. a) Side and b) top view of Pt1/HAP(001) calculation model.

Figure S6. FT-IR spectra of HAP support, Pt1/HAP catalysts and used Pt1/HAP catalysts (after 20 recycles).

2.5 Detailed discussion on H2-TPR and CO2-TPD

Figure S7. (a) H2-TPR of the HAP and Pt1/HAP catalysts in the temperature range of 0 to 250oC. (b) H2-TPR of the HAP, Pt1/HAP, 0.32wt% Pt/HAP, 0.96 wt% Pt/HAP and 1.45 wt% Pt/HAP catalysts.

Fig. S7a shows that the Pt1/HAP catalyst exhibit a characteristic reduction peak near 180oC (Pt12+→Pt10) after increasing the signal strength eight times [Appl. Catal. B. 2020, 277, 119280; Angew. Chem. Int. Ed. 2016, 55, 8319 –8323; Angew. Chem. 2020, 132, 20872 – 20877; Nat. Com. 2017, 8, 16100]. In addition, Fig. S7b shows that there are four reduction peaks of bare HAP supports centered at ~330oC, ~480oC, ~560oC and ~620oC. The reduction peak at 330oC could be assigned to the reduction of surface oxygen species, and the peaks at ≥480 oC could be attributed to the desorption of CO2 (m/z: 44) under reducing atmosphere, indicating the decomposition of surface carbonates species [ACS Catal. 2016, 6, 775-783; Appl. Catal. B. 2017, 201, 189-201]. The reduction peaks of bare HAP decreases with the increase of Pt metal loading [Appl. Catal. B. 2020, 270, 118851; Appl. Catal. A. 2019, 580, 34-45; Fuel Process. Technol. 2020, 202, 106359], and the reduction peaks of Pt metal clusters begin to appear and increase. Meanwhile, the H2 consumption of the Pt/HAP samples with different metal loading was further analyzed during the reduction process. Table S3 shows that the bare HAP support could consume relatively more hydrogen (293.0 μmol/g) due to the existence of oxygen species on the surface and in the bulk phase. Notablely, the introduction of Pt can reduce the hydrogen consumption of HAP since the Pt could stabilize the skeleton structure of HAP during the calcination process [Appl. Catal. B. 2020, 277, 119280]. The amount of hydrogen consumed in the reduction of Pt metal can be determined by the relative proportion of the reduction peak at < 300oC. Obviously, with the increase of Pt metal loading, the amount of hydrogen consumed and the ratio of H2 to Pt began to increase rapidly over the Pt/HAP catalysts. It should be noted that the H2 consumption of Pt in Pt1/HAP is only 0.7 μmol/g, and the ratio of H2 to Pt (< 300oC) is only 0.05, which is much lower than that of Pt/AC (2.56). Furthermore, Table S4 shows that the catalytic performance of calcined Pt1/HAP catalyst is similar to that of reduced Pt1/HAP catalyst, indicating that the isolated Pt atoms entering HAP framework are difficult to be reduced.

Figure S8. (a) NH3-TPD and (b) CO2-TPD profiles for the Pt1/HAP and HAP samples.

Fig. S8a and Table S3 show that the total NH3 consumption of the HAP and Pt1/HAP samples and the relative content of acid sites with different strength are similar, confirming that the isolated Pt does not affect the acid properties of HAP. However, for the CO2-TPD of the two samples, the total CO2 consumption of the Pt1/HAP is slightly lower than that of HAP (Fig. S8b), which is mainly because the introduction of Pt could reduce the content of medium strength alkaline sites (Table S3).

2.6 Characterization of the used catalyst

Figure S9. XPS spectra of Pt 4f on the (a) fresh Pt/AC and (b) used Pt/AC catalysts (after 20 recycles). TEM and HAADF-STEM images (b) used Pt/AC and (c) used Pt1/HAP catalysts (after 20 recycles).

2.7 Configuration and charge distribution of C-H bond activation

Figure S10. (a) Schematic diagram of catalytic cycle of the Pt-(O-P) linkage over the Pt1-OPO43- switch active site. (b) Configuration diagrams and Mulliken charge (|e|) of CH2OHCHOHCH2O* + * →CH2OHCHOHCHO* + H* in the oxidation of glycerol to glycolic acid. (c) Configuration diagrams and Mulliken charge of CH2OHCHOHCOOH*→ COOH* +CH2OHCHOH* over Pt1/HAP and Pt (111) models.

Fig. S10a shows the typical process of the catalytic cycle that the Pt-(O-P) linkage in the Pt1-OPO43- switch active site opens and closes during the reaction (including O2 direct dissociation, water assisted O2 activation and dehydrogenation of O-H and C-H bonds as well as OH oxidation). The Pt1-OPO43- switch active site that did not participate in the reaction was in the off state, and the charges of the three PO43- ligands are about 1.0 |e|. Once involved in the reaction, the Pt1-OPO43- switch active site will be open. Previous bottom Pt-(O-P) linkage breaks with the formation of new top Pt-(O-R) linkage. Meanwhile, the negative charge of three PO43- ligands increases rapidly. The strong electron transfer between oxygenated substrate (O-R), Pt1 and PO43- promotes the progress of reaction. After the product desorption, the Pt-(O-P) linkages in the Pt1-OPO43- switch active site and the charge of PO43- ligands return to a level close to the previous state.

In addition, it is found that Pt1-OPO43- switch could assist the C-H bond activation of CH2OHCHOHCH2O* intermediate (Fig. S10b).The C-C bond cleavage could be suppressed by this Pt1-OPO43- switch (compared to the Pt-Pt active sites). Fig. S10c shows that the bond length of C-C on the Pt1-OPO43- switch is shorter than that on the Pt-Pt active sites. Meanwhile, the electronegativity between the two C atoms on the Pt-Pt active sites is significantly higher than that on the Active site. This provides a favorable environment for the fracture of C-C bond on the Pt-Pt active sites.

2.8 Supplementary free energy diagram

Figure S11. a) Free energy diagrams for the oxidation of glycerol (GLY) to a-1) glyceric acid (GLYA) and a-2) dihydroxyacetone (DHA) over Pt(111) model at 298K. b) Free energy diagrams for the oxidation of glyceric acid (GLYA) to glycolic acid (GLYOA), formic acid (FA) or tartronic acid (TA) over Pt(111) model. [Appl. Surf. Sci. 497 (2019) 143661].

In addition, we compared the free energy diagram for the oxidation of glycerol over the Pt(111) and Pt1/HAP(001) models. Fig. S11a-1 and Fig. 4a-2 shows that the free energy level of the rate-determining step of glycerol oxidation to glyceric acid on Pt(111) [RCH2O*→RCHO*+H*, 0.39 eV] is similar to than that of Pt1/HAP(001) [0.38 eV]. This indicate that the dehydrogenation ability of the Pt1-OPO43- switch in the Pt1/HAP catalyst is no less than that of Pt-Pt metal active sites in the Pt/AC catalyst. Moreover, Fig. S11b shows that the ability of C-C bond cleavage on Pt1/HAP(001) model (1.75 eV) is much higher than that on Pt(111) model (0.83 eV), and the desorption energy of glyceric acid product on Pt1/HAP(001) model (0.31 eV) is much lower than that on Pt(111) model (0.74 eV). This indicates that the product of glyceric acid is easier to be desorbed on the Pt1/HAP catalyst, thus avoiding the side reactions such as C-C bond cleavage.

Figure S12. Free energy diagrams for the oxidation of glyceric acid (GLYA) to glycolic acid (GLYOA), formic acid (FA) or tartronic acid (TA) over Pt1/HAP (001) model at 298K.

2.9 In-situ FT-IR on Pt/AC

Figure S13. In situ FT-IR spectra of glycerol oxidation over Pt/AC at (a) carbonyl region (1500-1900 cm-1) and (b) νCO region (1000-1200 cm-1).

2.10 SEM images of the Pt1/HAP catalyst

Figure S14. SEM images of the Pt1/HAP catalyst.

2.11 Kinetics determination

I. Elimination of the diffusion limitations

The Pt1/HAP catalyst was used to study the internal and external mass transfer, and the oxidation of glycerol to glyceric acid was used as a model reaction for the selective oxidation of low carbon polyols. It is ensured that all the catalysts were evaluated with negligible mass transfer limitations.

(1) Effect of external diffusion on EG oxidation

(Reaction conditions: 50 oC, 1MPa O2, 0.05M Glycerol, 0.7 g Cat.)

(a) At 700 RPM, (10 min) Roxidation = 0.074 kmol/m3∙h; kmol/m3∙h

(b) At 1000 RPM, (10 min) Roxidation = 0.071 kmol/m3∙h;

(c) At 1200 RPM, (10 min) Roxidation = 0.075 kmol/m3∙h;

(2) Interphase Mass Transfer Limitation for Oxygen

(a) Gas-Liquid Mass Transfer Limitation: (Three phase catalytic reactors, Ramachandran & Chaudhari, 1983; J. Chem Eng Data. 1984, 29, 286-287; Chem. Eng. Process, 2004, 43, 823-830; J. Catal. 2016, 337, 272-283; J. Catal. 2008, 257, 1-4)

Roxidationdbubble6∙ε∙kg-l∙Co2, b=0.071 (kmol/m3∙h)∙0.000002(m)6∙0.09∙1.44(m/h)∙0.01(kmol/m3)=1.83×10-5< 0.1

(b) Liquid-Solid Mass Transfer Limitation: (J. Catal. 2016, 337, 272-283; Three phase catalytic reactors, Ramachandran & Chaudhari, 1983; HAP, assume 100 nm, see Fig. S8)

Roxidationρp∙dp6∙ωcat∙kl-s∙Co2, b*=0.071kmol/m3∙h∙2000kg/m3∙10-7m6∙8kg/m3∙72.1m/h∙0.01kmol/m3=4.10×10-7< 0.1

(c) Internal Diffusion: (J. Catal. 2016, 337, 272-283; Three phase catalytic reactors, Ramachandran & Chaudhari, 1983; Perry’s Handbook: Table 5-16)

Roxidationρp∙dp24∙ωcat∙De∙Co2, *=0.071(kmol/m3∙h)∙2000kg/m3∙(10-7m)24∙8(kg/m3)∙0.094(m2/h)∙0.01(kmol/m3)=×10-9<  1

(3) Interphase Mass Transfer Limitation for Glycerol

(a) Liquid-Solid Transfer Limitation: (J. Catal. 2016, 337, 272-283; AIChE J. 1980, 26, 177-201; Three phase catalytic reactors, Ramachandran & Chaudhari, 1983)

Roxidationρp∙dp6∙ωcat∙kl-s∙Cgly=0.071kmol/m3∙h∙2000kg/m3∙10-7m6∙8kg/m3∙0.6m/h∙0.05kmol/m3=9.86×10-6< 0.1

(b) Intraparticle Transfer Limitation: (J. Catal. 2016, 337, 272-283; AIChE J. 1980, 26, 177-201; Three phase catalytic reactors, Ramachandran & Chaudhari, 1983)

dp6[(m+1)∙Roxidationρp2∙ωcat∙De∙Cgly]0.5=10-7m6[0.071kmol/m3∙h∙2000kg/m38∙kg/m3∙0.036m2/h∙0.05kmol/m3]0.5=1.66×10-6 < 0.2

II. The results of apparent reaction kinetics

Figure S15. (a) Arrhenius-type plot for the oxidation of glycerol to glyceric acid (GLYA) (Reaction 1), glycolic acid (GLYOA) (Reaction 2) and tartronic acid (TA) (Reaction 3). (b) Activation energy calculated from intrinsic kinetic equation over the Pt1/HAP and Pt/AC catalysts. (c) Product distribution of the selective oxidation of DHA and GLYAD.

As shown in Fig. S15, the selective oxidation of glycerol to glyceric acid (r1), tartronic acid (r2), formic acid and carbon dioxide (r3) is a sequential parallel reaction:

r1 = rGLYA + r2 + r3 (Global Reaction)

r2 = rFA + rGLYOA

r3 = rTA

Then, the power function type reaction kinetic equation was used to investigate the oxidation of glycerol over the Pt/AC and Pt1/HAP catalysts. The equation can be expressed as:

ri= -dC0dt=A exp-EaiRTCGaPOb

PO and CG are the initial concentration of O2 pressure and glycerol (in mol gPt-1) respectively; a and b are the corresponding reaction order. T, r, R, A and Eai are the reaction temperature (K), the initial reaction rate of one substrate (in mol gPt −1 h−1), ideal gas constant (8.314 × 10-3 kJ mol-1 K-1), the pre-exponential factor and activation energy (kJ mol-1).The concentration of oxygen at the surface equals its bulk concentration (calculated by Henry’s law). [J. Chem. Thermodyn. 2000, 32, 1145; J. Phys. Chem. C, 2010, 114, 1164–1172; J. Phys. Chem. 1996, 100, 5597].The initial reaction rate is almost constant in the range of 1-1.8 MPa O2, suggesting that the reaction order of oxygen partial pressure could be considered as zero. The reaction order of glycerol (GLY) for the Pt/AC and Pt1/HAP catalysts are 0.42 and 0.44 respectively. The final dynamic equations for glycerol oxidation to glyceric acid are as follows:

Pt/AC catalyst: r1= -dC0dt=2.68×105exp-34.90×103RTCG0.42

Pt1/HAP catalyst: r1= -dC0dt=5.53×105exp-34.55×103RTCG0.44

Fig. S15 a-b and Table S12 clearly show that the apparent activation energy of GLY oxidation to glyceric acid (GLYA) on the Pt1/HAP catalyst (34.5 kJ/mol) is similar to that on the Pt/AC catalyst (34.9 kJ/mol), further indicating that the activation ability of glycerol over these two catalysts is close. Differently, the Pt1/HAP catalyst (5.53×105) displays more than twice the pre exponential factor than the Pt/AC catalyst (2.68×105). It is worth mentioning that the unit of concentration in the calculation of apparent kinetics is mol/gPt. The larger pre exponential factor indicates that the Pt1/HAP catalyst has more active sites than the Pt/AC catalyst. Therefore, the atomically dispersed Pt1/HAP catalyst greatly improves the utilization efficiency of Pt metal and promotes the dispersion and utilization of more Pt active sites. In addition, the Ea2 (76.26 kJ/mol) and Ea3 (57.20 kJ/mol) on the Pt1/HAP catalyst are significantly higher than Ea1 (34.55 kJ/mol), meaning that the deep oxidation reactions such as C-C bond cleavage are hardly occurred over the Pt1-OPO43- switch active sites. On the contrary, the Ea2 (42.48 kJ/mol) and Ea3 (63.2 kJ/mol) on the Pt/AC catalyst are only slightly higher than Ea1 (34.90 kJ/mol), indicating that the Pt-Pt active sites tend to break the C-C bond.

Meanwhile, we used GLYAD (primary hydroxyl) and DHA (secondary hydroxyl) as the common intermediates for the oxidation reaction. Fig. S15c clearly shows that GLYAD and DHA could be transformed rapidly under alkaline conditions due to the existence of OH-. It is worth mentioning that in the presence of Pt based catalyst (especially Pt1/HAP catalyst), GLYAD tends to be converted to GLYA, and other deep oxidation reactions are inhibited. However, the presence or absence of Pt catalysts has little effect on the distribution of DHA oxidation products. This further indicates that the Pt based catalyst (especially Pt1/HAP catalyst) tends to oxidize the primary hydroxyl group rather than the secondary hydroxyl group.

III. Entropy change analysis of apparent reaction kinetics

Experimentally measured TOF value on the Pt/AC and Pt1/HAP catalysts could be can be obtained from the rate equation of apparent reaction kinetics:

TOF=kCGn=A exp⁡(-EaRT)CGn

where k, CG, A, Ea, R and T are the rate constant, substrate concentration, pre exponential factor, apparent activation energy reaction order, universal gas constant and reaction temperature, respectively.

Meanwhile, based on the transition state theory, TOF value could be also expressed in the Eyring form:

TOF=kBThexp⁡(ΔSR)exp⁡(-ΔHRT)

where kB, h, ΔS, and ΔH are the Boltzmann constant, Planck constant, entropy of activation, and enthalpy of activation, respectively. Ea is simplified to be close to ΔH.

The entropy change in the activation step of the chemical reaction is closely related to the thermodynamics of the rate constant, which results in the following equation:

ΔS=R(lnA-lnkBTh )

The detailed results, including pre exponential factors, entropy change and activation energy of three reactions of glycerol oxidation over the Pt/AC and Pt1/HAP catalysts, have been summarized in Table S12. The entropy change of Reaction 1 (-148.7 kJ/mol) on the Pt1/HAP catalyst is significantly higher than that of Reaction 2 (-35.8 kJ/mol) and 3 (-87.1 kJ/mol), indicating that the Pt1-OHAP active site mainly binds to glycerol reactant. However, the entropy change of Reaction 1 (-148.9 kJ/mol) and 2 (-122.6 kJ/mol) on the Pt/AC catalyst is similar. This shows that the Pt-Pt active site has a strong binding state to both glycerol and its carboxylic acid products, resulting in C-C bond cleavage more easily than Pt1-OHAP active site.

IV. Combining experiment with DFT calculation

(1)RCH2OH(g)+O2(g)+2H2O(g)+4*→RCH2OH*+O2+2H2O*

(2)O2*+2H2O*+*→4OH*

(3)RCH2OH*+OH*→RCH2O*+H2O*

(4)RCH2O*→RCHO*+H*    Rate determining step

(5)RCHO*+OH*→RCHOOH*

(6)RCHOOH*→RCOOH*+H*

(7)RCOOH*+2H*+H2O*+2OH*→RCOOH(g)+3H2O(g)

if we treat ES4(RCH2O*+H2O*+3OH*→RCHO*+H*+H2O*+3OH*) as rate-determining step and other steps as quasi-equilibrated. Then the reaction involving elementary steps before ES6, namely, RCH2OH(g)+O2(g)+2H2O(g)+5*→RCH2O*+H2O*+3OH* could be assumed to be at equilibrium, with the equilibrium constant written as:

(1)

where θ is the surface coverage, P is pressure, T is temperature, and kB is Boltzmann's constant. ΔG represents the free energy change for reaction.

The forward reaction rate of ES4 is:

(2)

(3)

where h denotes Planck's constant. ∆G4+ is the free energy of activation for ES4.

With the combination of Eqs. (1) and (3), Eq. (2) could be expressed as:

Figure S16. Arrhenius plot and apparent activation energy for glycerol oxidation to glyceric acid generated from experiment and DFT over (a) Pt1/HAP and (b) Pt/AC. Reaction conditions: 0.78 kmol/m3 O2 solution, 50 kmol/m3 glycerol solution,

In conclusion, our DFT theoretical calculation and apparent reaction kinetics have reached the consistent conclusions:

1. Atomic dispersed Pt1/HAP catalyst has more sufficient utilization efficiency of Pt metal.

2. Pt1-OPO43- switch active site has higher glycerol selectivity than Pt-Pt active site.

3. Pt-based catalysts prefer to directly oxidize primary hydroxyl rather than secondary hydroxyl to produce glyceric acid.

2.12 Physicochemical properties of the catalysts

Table S1. Results of N2-physisorption, metal loading and dispersion of these catalysts

| Catalyst | BET surface area (m2/g) | Pore volume (cm3/g) | Loading (wt%)a |  | Dispersion (%)b |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Pt | Ca/P |  |
| HAP | 46.0 | 0.35 | - | 1.8 | - |
| Pt/AC | 1387.5 | 0.39 | 0.84 | - | 37.9 |
| Pt1/HAP | 48.9 | 0.69 | 0.14 | 1.8 | 100 |

a. Determined by ICP-OES analysis.

b. Determined by CO-TPD.

2.13 EXAFS parameters

Table S2. EXAFS parameters of Pt foil, Pt1/HAP and PtO2 catalystsa.

| Samples | Shell | N | ΔE(eV) | R (Å) | 103ⅹσ2(Å2) |
| --- | --- | --- | --- | --- | --- |
| Pt foil | Pt-Pt | 12 (fixed) | 0.7 (0.5) | 2.7 (0.0) | 4.7 (0.2) |
| Pt1/HAP | Pt-O | 4.97(0.49) | 10.5 (1.2) | 2.0 (0.1) | 3.7 (1.4) |
| PtO2 | Pt-O | 6 (fixed) | 0.0 (1.6) | 2.1 (0.1) | 2.9 (0.5) |

aN, ΔE, R and σ2 are the coordination number, shift in the edge energy, interatomic distance and Debye−Waller factor.

2.14 Quantitative analysis of H2-TPR, NH3-TPD and CO2-TPD

Table S3. Quantitative analysis of H2-TPR

| Sample | H2-TPR |  |  |
| --- | --- | --- | --- |
|  | Total H2 consumption (μmol/g) | T < 300oC (μmol/g) | H2/Pt for T< 300 oC |
| HAP | 293.0 | 0 | - |
| Pt1/HAP | 107.0 | 0.7 | 0.05 |
| 0.32wt% Pt/HAP | 61.9 | 3.9 | 0.24 |
| 0.96wt% Pt/HAP | 74.5 | 11.2 | 0.24 |
| 1.48wt% Pt/HAP | 139.6 | 61.7 | 0.81 |
| Pt/AC | 167.7 | 110.3 (~310oC) | 2.56 |

Table S4. Quantitative analysis of NH3-TPD and CO2-TPD

| Sample | NH3-TPD |  |  |  | CO2-TPD |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Total NH3 consumption (μmol/g) | Weak acid sites ~150oC (%) | Medium acid sites ~220oC (%) | Strong acid sites ~380oC (%) | Total CO2 consumption (μmol/g) | Weak basic sites ~150oC (%) | Medium basic sites ~220oC (%) | Medium strong basic sites ~380oC (%) | Strong basic sites ~900oC (%) |
| HAP | 43.7 | 48.7% | 27.3% | 24.0% | 26.6 | 27.4% | 29.3% | 12.8% | 30.5% |
| Pt1/HAP | 43.5 | 49.6% | 27.9% | 22.6% | 24.3 | 32.7% | 24.9% | 12.4% | 30.0% |

Table S5. Quantitative analysis of CO-TPD

| Sample | CO chemisorption (μmolCO/g) |
| --- | --- |
| AC | 40.9 |
| Pt/AC | 2.3 |
| HAP | 11.0 |
| Pt1/HAP | 10.8 |

2.15 Results of catalytic oxidation of low carbon polyols

The initial reaction rate was calculated as moles of polyol molecules converted per gram of Pt metal per hour. In each trial, the conversion was all less than 20% to ensure that the average reaction rate equaled the instantaneous reaction rate. In addition, the evaluation results of the initial reaction rate were repeated three times to take the average value. We take the calculation process of initial reaction rate over Pt1/HAP catalyst in glycerol oxidation as an example:

(Reaction conditions: 50 oC, 1MPa O2, 25 mL, 0.05M Glycerol, 0.7 g Cat, 0.5 g NaOH)

(1) (6 min) Initial reaction rate1= (0.025 L × 0.05 mol/L ×0.126)/(0.7 g ×0.14wt% ×0.1 h) =1.61 mol/gPt/h;kmol/m3∙h

(2) (6 min) Initial reaction rate2= (0.025 L × 0.05 mol/L ×0.143)/(0.7 g ×0.14wt% ×0.1 h) =1.82 mol/gPt/h;

(3) (6 min) Initial reaction rate3 = (0.025 L × 0.05 mol/L ×0.151)/(0.7 g ×0.14wt% ×0.1 h) =1.93 mol/gPt/h;

Therefore, initial reaction rate = (1.61+1.82+1.93)/3 = 1.78mol/gPt/h ≈ 1.8mol/gPt/h

Table S6. Oxidation of glycerol over these catalystsa

| Catalyst | Selectivity (%)c |  |  | Conversion (%) | Carbon balance (%) | Glyceric acid yield (%) | TOF (h-1)b |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Glyceric acid | Tartronic acid | Glycolic acid |  |  |  |  |
| HAP | - | - | - | - | - | - | - |
| Pt/AC | 47.8 | 4.1 | 29.1 | 86.8 | 95.3 | 35.8 | 343.7 |
| Pt1/HAP | 86.7 | 7.8 | 2.7 | 92.5 | 98.5 | 80.2 | 351.1 |
| Pt1/HAP (Unreduced) | 87.1 | 6.1 | 4.9 | 91.8 | 98.1 | 80.0 | 344.9 |
| Pt/HAP (1.45 wt%)d | 52.0 | 3.2 | 32.8 | 88.1 | 94.0 | 41.6 | 378.3 |
| Used Pt/HAP (1.45 wt%)e | 50.1 | 2.3 | 35.1 | 43.2 | 91.3 | 21.6 | - |

a. Reaction conditions: 0.7 g HAP/ Pt1/HAP or 0.2 g Pt/AC or 0.1 g Pt/HAP (1.45 wt%), 25 mL aqueous solution of glycerol (0.05 M), 0.5 g NaOH, 50oC, 1MPa O2, 16h

b. The metal dispersion of Pt/AC is 31.2% (determined by CO-TPD).

c. CO2 products is not listed in the table.

d. Catalytic performance of fresh Pt/HAP (1.45 wt%) catalyst.

e. Catalytic performance of used Pt/HAP (1.45 wt%) catalyst after 20 cycles.

Table S1 shows that the Pt/HAP (1.45 wt%) catalyst with 2.2 nm Pt nanoparticles exhibits similar conversion and glyceric acid selectivity compared to the Pt/AC catalyst. Moreover, the glyceric acid selectivity of the Pt/HAP (1.45 wt%) catalyst (52.0%) is much lower than that of the Pt1/HAP catalyst (86.7%). On these foundation, it can be inferred that HAP and AC as the supports of Pt nanoparticles display no significant effect on the catalytic activity and selectivity of glycerol oxidation due to the strong alkaline solution (NaOH). In addition, we also investigated the catalytic performance of the Pt/HAP (1.45 wt%) catalyst after 20 cycles. It is found that the yield of glyceric acid decreases significantly (from 41.6% to 21.6%). Meanwhile, the Pt metal loading of the used Pt/HAP (1.45 wt%) catalyst decreases to 0.95 wt%. Obviously, it does not exhibits the same leaching free characteristic as Pt1/HAP catalyst. In other words, only atomically dispersed Pt stabilized in HAP framework could show the unique leaching free characteristic in polyol aqueous phase oxidation reaction.

Table S7. Oxidation of ethylene glycol over these catalysta

| Catalyst | Selectivity (%) |  |  | Conversion (%) | Carbon balance (%) | Glycolic acid yield (%) | TOF (h-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Glycolic acid | Glycolaldehyde | Formic acid |  |  |  |  |
| HAP | - | - | - | 0.2 | 98.1 | - | - |
| Pt/AC | 68.5 | - | 21.8 | 58.7 | 90.3 | 43.1 | 3874.4 |
| Pt1/HAP | 98.3 | - | 0.2 | 79.1 | 98.5 | 77.8 | 4531.8 |

a. Reaction conditions: 0.25 g HAP/ Pt1/HAP or 0.1 g Pt/AC, 25 mL aqueous solution of ethylene glycol (0.05 M), 0.5 g NaOH, 60oC, 1MPa O2, 16 h

Table S8. Oxidation of 1,2-propylene glycol over these catalysta

| Catalyst | Selectivity (%) |  |  | Conversation (%) | Carbon balance (%) | Lactic acid yield (%) | TOF (h-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Lactic acid | Acetic acid | Formic acid |  |  |  |  |
| HAP | - | - | - | - | - | - | - |
| Pt/AC | 50.0 | 25.9 | 16.2 | 84.2 | 92.1 | 50.5 | 3874.4 |
| Pt1/HAP | 80.1 | 6.7 | 3.0 | 89.5 | 89.8 | 71.7 | 4914.0 |

a. Reaction conditions: 0.25 g HAP/ Pt1/HAP or 0.1 g Pt/AC, 25 mL 1,2- propylene glycol solution (0.05 M), 0.5 g NaOH, 160oC, 1MPa O2, 16 h

Table S9. Oxidation of 1,2- butanediol over these catalysta

| Catalyst | Selectivity (%) |  |  | Conversation (%) | Carbon balance (%) | 2-Hydroxybutyric acid yield (%) | TOF (h-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 2-Hydroxybutyric acid | Oxalic acid | CO2 |  |  |  |  |
| HAP | - | - | - | - | - | - | - |
| Pt/AC | 62.4 | 20.8 | 8.8 | 81.5 | 92.0 | 63.1 | 2874.5 |
| Pt1/HAP | 91.8 | 2.7 | 3.4 | 88.7 | 97.9 | 81.4 | 2511.6 |

a. Reaction conditions: 0.7 g HAP/ Pt1/HAP or 0.2 g Pt/AC, 25 mL aqueous solution of 1,2- butanediol (0.05 M), 0.5 g NaOH, 140oC, 1MPa O2, 16 h

Table S10. Oxidation of glycerol over the Pt1/HAP catalyst and other reported Pt-based catalystsa

| Pt-based Catalyst |  |  | Selectivity (%) |  |  |  |  | Conversion (%) | GLYA Yield (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | GLYAD |  | GLYA |  | DHA | GLYOA |  |  |  |
| Pt0.8Ru0.8/MCM-41a |  | 2.5 |  | 80.4 | 6.2 |  | 3.9 | 78.2 | 62.9 | Appl. Catal. B. 2019, 259: 118070. |
| 2%Pt9Sn1/C-Rb |  | 1.1 |  | 55.4 | 7.2 |  | 8.0 | 91.1 | 50.5 | Appl. Catal., B 180 (2016) 78-85. |
| 1%Au1Pt3/MgOc |  | - |  | 72.2 | - |  | 3.3 | 42.9 | 31.0 | Angew. Chem., Int. Ed. 50 (2011) 10136-10139. |
| 5%PtCu/Cd |  | 1.5 |  | 70.8 | 10.1 |  | 9.2 | 86.2 | 61.0 | Catal. Commun. 12 (2011) 1059-1062. |
| 1% Au−Pt−Pd/TiO2e |  | - |  | 55.0 | - |  | 7.0 | 37.0 | 20.4 | ChemSusChem 7 (2014) 1326-1334. |
| 1% PtFe/CeO2f |  | - |  | 77.1 | - |  | - | 57.1 | 44.0 | J Catal. 337 (2016) 272–283. |
| 1% Pt/Cg |  | - |  | 42.4 | - |  | 43.1 | 50.0 | 21.2 | Catal. Today. 102–103 (2005) 203–212. |
| Pt-CeO2/CNT |  | 4.7 |  | 78.0 | 3.1 |  | 3.5 | 96.1 | 74.9 | ACS Catal. 2020, 10, 3832−3837 |
| Pt1/HAP |  | - |  | 86.7 | - |  | 4.7 | 92.5 | 80.2 | This work |

a. Reaction conditions: glycerol/Pt molar ratio 700, 80℃, 1MPa O2, 12 h;

b. Reaction conditions: glycerol/Pt molar ratio 1000, 60℃, Oxygen flow (15 mL/min), 8 h;

c. Reaction conditions: glycerol/Pt molar ratio 1000, 60℃, 1MPa O2, 4 h;

d. Reaction conditions: glycerol/Pt molar ratio 500, 60℃, Oxygen flow (150 mL/min), 6 h;

e. Reaction conditions: glycerol/Au molar ratio 2728, 100℃, 4 h.

f. Reaction conditions: glycerol/Pt molar ratio 4000, NaOH/glycerol = 4, 60℃, Oxygen flow 0.1MPa O2, 2 h;

g. Reaction conditions: glycerol/Pt molar ratio 500, NaOH/glycerol = 4, 50℃, Oxygen flow 0.3MPa O2;

Note: GLY, GLYA, GLYAD, GLYOA and DHA represent glycerol, glyceric acid, glyceraldehyde, glycolic acid and dihydroxyacetone, respectively. In addition, we selected the optimal GLYA yield data over the optimal catalysts in these literature in Table S8.

2.16 Summary of activation energy calculated by DFT calculation and reaction kinetics

Table S11. Activation barriers (eV) for the dissociation of O2 and H2O on Pt(111) and Pt1/HAP models.

| Reaction | Pt(111) | Pt1/HAP |
| --- | --- | --- |
| O2*+H2O* → OOH* + OH* | 0.47 | 0.39 |
| OOH*+H2O* → HOOH* + OH* | 0.40 | 0.32 |
| HOOH*+* → 2OH* | 0.11 | 0.28 |

The dissociation of O2 and H2O on Pt(111) has been studied in detail in our previous work [Applied Surface Science 497 (2019) 143661; Appl. Catal. B 2019, 259, 118070]. Zope et al. [Science 2010, 330, 74-78] has demonstrated that O2 could react with H2O to form a reaction cycle, and finally get OH to participate in the subsequent liquid-phase oxidation of glycerol and other alcohols. It should be noted that the OH in NaOH solution could first participate in the oxidation reaction, and the subsequent cycle of O2 and H2O will continue to supplement the OH [Science 2010, 330, 74-78; ACS Catal. 2020, 10, 3832−3837]. In other words, O2 and H2O are proposed to participate in the catalytic cycle by regenerating hydroxide ions (OH) formed. Moreover, it has been widely accepted that this activation steps of O2 and H2O are not rate-determining steps under alkaline conditions [Science 2010, 330, 74-78; Chemical Engineering Science 203 (2019) 228–236], which is also proved by our KIE experiment.

Table S12 Summary of pre exponential factors, entropy change and activation energy of three reactions of glycerol oxidation over the Pt/AC and Pt1/HAP catalysts.

| Catalysts | Reaction 1 |  |  |  |
| --- | --- | --- | --- | --- |
|  | Aa | Ab | ΔS (kJ/mol) | Ea (kJ/mol) |
| Pt/AC | 2.68×105 | 2.89×103 | -148.9 | 34.9 |
| Pt1/HAP | 5.53×105 | 2.95×103 | -148.7 | 34.5 |
| Catalysts | Reaction 2 |  |  |  |
|  | Aa | Ab | ΔS (kJ/mol) | Ea (kJ/mol) |
| Pt/AC | 4.78×105 | 6.83×104 | -122.6 | 42.5 |
| Pt1/HAP | 4.33×1010 | 2.34×109 | -35.8 | 76.3 |
| Catalysts | Reaction 3 |  |  |  |
|  | Aa | Ab | ΔS (kJ/mol) | Ea (kJ/mol) |
| Pt/AC | 5.25×108 | 7.50×107 | -64.4 | 63.2 |
| Pt1/HAP | 9.08×107 | 4.92×106 | -87.1 | 57.2 |

a. Pre exponential factor was estimated based on moles per hour per unit mass Pt.

b. Pre exponential factor was estimated based on TOF (the dispersions of Pt/AC and Pt1/HAP catalysts are 37.9% and 100%, respectively).