Optimizing Oxygen Ion Transport in Pyrochlore Structures: A Doping Strategy by DFT and Experimental Validation

A Ajayraj a, Anjana P Anantharaman a*

a Department of Chemical Engineering, National Institute of Technology Warangal, 506004, Telangana, India

Corresponding Author Information:

*

Dr. Anjana P Anantharaman, Ph. D.

Assistant Professor, Chemical Engineering Department

National Institute of Technology Warangal,

Warangal-506004, India

E-mail: anjanapa@nitw.ac.in

Table S1: Parameters used for the DFE calculations

| Parameter | NZO | NMgZO | NMoZO | NSMoZO |
| --- | --- | --- | --- | --- |
| Max run time (s) | 86400 | 86400 | 86400 | 86400 |
| Bravais lattice index | 1 | 1 | 1 | 1 |
| Plane-wave cutoff energy (Ry) | 38 | 58.12 | 49 | 49 |
| Cutoff energy (Ry) for charge density | 341.95 | 523.08 | 440.53 | 440.53 |
| Electron occupation | smearing | smearing | smearing | smearing |
| Smearing width (eV/Å) | 0.01 | 0.01 | 0.01 | 0.01 |
| Convergence threshold (eV) | 1.00e-05 | 1.00e-05 | 1.00e-05 | 1.00e-05 |
| Maximum number of SCF iterations | 1001 | 1001 | 1001 | 1001 |
| K- POINTS .mode | gamma | gamma | gamma | gamma |

Characterization of pyrochlore
Lattice parameters, crystallite size, dislocation density, theoretical density, and Relative density (RD) were calculated from the XRD data using equations (S1) to (S6), respectively.

nλ=2d (sinθ)	                                             	(S1)

a=dh2+k2+l2                                       	(S2)

D=kλβ cosθ	                                               		(S3)

δ=1Davg		                                          	(S4)

ρth=ZMwV		                                   		(S5)

RD=ρ/ρth                                                 		(S6)

where d is the interplanar spacing, θ is the angle of diffraction, λ represents the X-ray wavelength (1.5406 Å), β is the FWHM (full width at half maximum) in radians, Z is the number of formula units per unit cell, Mw is the formula mass, V is the volume of the unit cell, and Davg is the average crystallite size calculated from the XRD pattern. The practical density of the samples are calculated using the mass and volume of the sintered pellets.

TableS2:   DFEs of B-site doped NZO

| Dopant &Sample NZO | Ionic radius Å | Vacant formation energy, Ev (eV) of different dopant % |  |  |
| --- | --- | --- | --- | --- |
|  |  | 10% | 15% | 20% |
| Li | 0.76 | -5.0319 | -4.8885 | -4.8885 |
| Mg | 0.72 | -5.5828 | -5.6273 | -5.6287 |
| Ca | 1.00 | -5.3569 | -5.2828 | -5.2904 |
| Ti | 0.61 | -5.5300 | 5.5553 | -5.5539 |
| V | 0.58 | -5.0029 | -4.8381 | -4.9012 |
| Sr | 1.26 | -5.3516 | -5.2713 | -5.3143 |
| Ce | 0.87 | -5.5881 | -5.6728 | -5.6319 |
| Yb | 0.85 | -5.5299 | -5.5736 | -5.5146 |
| Mo | 0.59 | -5.6231 | -5.7398 | -5.6827 |

TableS3:   DFEs of the codoped samples

| Dopant &Sample | Ionic radius Å | 3.125% dopant |  | 6.25% dopant |  | 12.5% |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | A0.06Nd1.94Mg0.3Zr1.7O7 | A0.06Nd1.94Mo0.3Zr1.7O7 | A0.1Nd1.9Mg0.3Zr1.7O7 | A0.1Nd1.9Mo0.3Zr1.7O7 | A0.24Nd1.76Mg0.3Zr1.7O7 | A0.24Nd1.76Mo0.3Zr1.7O7 |
| Er | 1.004 | -5.69 | -5.7361 | -5.6608 | -5.732 | -5.6543 | -5.7253 |
| Ho | 1.015 | -5.5421 | -5.7357 | -5.6592 | -5.7309 | -5.6511 | -5.7225 |
| Dy | 1.027 | -5.6046 | -5.7377 | -5.6668 | -5.7376 | -5.661 | -5.7360 |
| Gd | 1.053 | -5.6828 | -5.7382 | -5.6641 | -5.735 | -5.6594 | -5.7311 |
| Eu | 1.066 | -5.6031 | -5.7284 | -5.60.34 | -5.7116 | -5.6038 | -5.6765 |
| Sm | 1.079 | -5.6797 | -5.7414 | -5.6704 | -5.7422 | -5.6896 | -5.7460 |
| Pm | 1.093 | -5.6689 | -5.7467 | -5.6635 | -5.7140 | -5.5971 | -5.7480 |
| Pr | 1.126 | -5.6054 | -5.6794 | -5.544 | -5.6812 | -5.4029 | -5.4967 |
| Hf | 0.58 | -5.4319 | -5.7355 | --5.5727 | -5.7326 | -5.6590 | -5.7310 |