Supplementary Information

Elucidating the Catalytic Activity of Lattice-Distorted Double Perovskite Oxides as Bifunctional Electrocatalysts

Hyeocksu Kim1, Hak Sakong1, Sang-Hee Park1 and Joohyuk Park1,*

1Department of Chemical Engineering, Changwon National University, Gyeongsangnam-do 51140, Republic of Korea

E-mail: jhpark@changwon.ac.kr

Table S1 Comparison of ionic radii and coordination environments of constituent ions, with calculated Goldschmidt tolerance factors (t) and estimated crystal structures based on t values for Pr2MnCoO6 and La2MnCoO6

| Materials | A-site | B-site | B’-site | O-site | t | Crystal structure |
| --- | --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | Pr3+ (VIII) 1.126 Å | Mn4+ (VI) 0.53 Å | Co2+ (VI) 0.745 Å | O2– (VI) 1.4 Å | 0.877 | Monoclinic |
| La2MnCoO6 | La3+ (VIII) 1.16 Å | Mn4+ (VI) 0.53 Å | Co2+ (VI) 0.745 Å | O2– (VI) 1.4 Å | 0.888 | Monoclinic |

Fig. S1 Wide area SEM images of (a) Pr2MnCoO6 and (b) La2MnCoO6

Fig. S2 EDS mapping images and corresponding EDS spectra of (a) Pr2MnCoO6 and (b) La2MnCoO6. The EDS mapping images show the overall elemental distribution of Pr (or La), Mn, Co and O

Table S2 The elemental composition of Pr2MnCoO6 and La2MnCoO6 obtained from EDS mapping

| Materials | Element | Atomic % |
| --- | --- | --- |
| Pr2MnCoO6 | Pr | 24.33 |
|  | Mn | 11.98 |
|  | Co | 10.14 |
|  | O | 53.55 |
|  | Total | 100.00 |
| La2MnCoO6 | La | 20.65 |
|  | Mn | 8.77 |
|  | Co | 9.60 |
|  | O | 60.98 |
|  | Total | 100.00 |

Fig. S3 XPS survey spectra of (a) Pr2MnCoO6 and (b) La2MnCoO6, showing the characteristic peaks of Pr 3d (or La 3d), Pr 4d (or La 4d), Mn 2p, Co 2p, O 1s and C 1s

Fig. S4 Pr 3d XPS spectrum of Pr2MnCoO6

Fig. S5 La 3d XPS spectrum of La2MnCoO6

Table S3 The relative concentrations and fitting parameters of Pr 3d components for Pr2MnCoO6

| Materials | Component | Area | FWHM | Position (eV) | % Conc. |
| --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | Pr 3d5/2 | 138040.5 | 3.707 | 932.68 | 41.06 |
|  | Pr 3d3/2 | 85856.4 | 3.9782 | 952.95 | 25.54 |
|  | Satellite | 71063.4 | 3.95182 | 928.42 | 21.14 |
|  |  | 28135.8 | 3.3174 | 948.78 | 8.37 |
|  |  | 13087.2 | 2.88805 | 956.86 | 3.89 |

Table S4 The relative concentrations and fitting parameters of La 3d components for La2MnCoO6

| Materials | Component | Area | FWHM | Position (eV) | % Conc. |
| --- | --- | --- | --- | --- | --- |
| La2MnCoO6 | La 3d5/2 | 31636.8 | 1.48206 | 833.46 | 8.67 |
|  | La 3d5/2 antibonding satellite | 93604.7 | 3.97539 | 834.75 | 25.66 |
|  | La 3d5/2 bonding satellite | 58452.9 | 2.1619 | 837.94 | 16.02 |
|  | La 3d5/2 plasmons | 26539.7 | 4.66623 | 847.07 | 7.27 |
|  | La 3d3/2 | 26290.7 | 1.53986 | 850.28 | 7.21 |
|  | La 3d3/2 antibonding satellite | 60274.0 | 3.85453 | 851.58 | 16.52 |
|  | La 3d3/2 bonding satellite | 34362.9 | 2.07153 | 854.73 | 9.42 |
|  | La 3d3/2 plasmons | 33670.3 | 7.05614 | 864.15 | 9.23 |

Table S5 The relative concentrations and fitting parameters of O 1s components for Pr2MnCoO6 and La2MnCoO6

| Materials | Component | Area | FWHM | Position (eV) | % Conc. |
| --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | O2– | 35107.0 | 0.9782 | 528.9883 | 39.34 |
|  | O22–/O– | 19138.9 | 1.87936 | 529.9894 | 21.45 |
|  | O2/OH– | 27965.2 | 1.71679 | 531.1593 | 31.34 |
|  | H2O | 7026.0 | 1.89044 | 532.4922 | 7.87 |
| La2MnCoO6 | O2– | 40090.1 | 0.983187 | 529.0655 | 47.38 |
|  | O22–/O– | 6889.8 | 1.19224 | 529.8463 | 8.14 |
|  | O2/OH– | 27663.6 | 1.71109 | 531.0116 | 32.69 |
|  | H2O | 9967.9 | 2.22063 | 532.3073 | 11.78 |

Table S6 The relative concentrations and fitting parameters of Mn 2p components for Pr2MnCoO6 and La2MnCoO6

| Materials | Component | Area | FWHM | Position (eV) | % Conc. |
| --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | 2p3/2 Mn3+ | 14034.5 | 2.31052 | 641.4126 | 32.96 |
|  | 2p3/2 Mn4+ | 12559.7 | 3.46861 | 642.9254 | 29.49 |
|  | 2p1/2 Mn3+ | 13936.4 | 3.06034 | 653.2083 | 32.73 |
|  | 2p1/2 Mn4+ | 2053.4 | 3.32239 | 656.2487 | 4.82 |
| La2MnCoO6 | 2p3/2 Mn3+ | 15748.2 | 2.40876 | 641.3067 | 32.19 |
|  | 2p3/2 Mn4+ | 14822.2 | 3.54251 | 642.8324 | 30.29 |
|  | 2p1/2 Mn3+ | 15063.7 | 3.00984 | 653.2226 | 30.79 |
|  | 2p1/2 Mn4+ | 3296.1 | 3.25969 | 655.9247 | 6.73 |

Table S7 The relative concentrations and fitting parameters of Co 2p components for Pr2MnCoO6 and La2MnCoO6

| Materials | Component | Area | FWHM | Position (eV) | % Conc. |
| --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | 2p3/2 Co3+ | 8469.7 | 1.64246 | 779.2204 | 28.86 |
|  | 2p3/2 Co2+ | 2303.1 | 1.61096 | 780.4628 | 7.85 |
|  | 2p1/2 Co3+ | 3831.8 | 1.79341 | 795.0446 | 13.06 |
|  | 2p1/2 Co2+ | 6059.8 | 2.82241 | 796.2471 | 20.65 |
|  | Satellite | 5424.8 | 4.07229 | 786.6520 | 19.64 |
|  |  | 3672.2 | 4.08081 | 802.9032 | 13.30 |
| La2MnCoO6 | 2p3/2 Co3+ | 4967.9 | 1.3855 | 779.3575 | 23.64 |
|  | 2p3/2 Co2+ | 6639.9 | 2.43285 | 780.6245 | 31.59 |
|  | 2p1/2 Co3+ | 1928.5 | 1.52746 | 794.9460 | 9.18 |
|  | 2p1/2 Co2+ | 3699.3 | 2.33776 | 795.9942 | 17.6 |
|  | Satellite | 1672.4 | 6.26067 | 787.4454 | 7.96 |
|  |  | 2109.0 | 4.15138 | 802.9543 | 10.03 |

Fig. S6 Fourier-transformed k3-weighted EXAFS spectra of the Pr L3-edge (Pr2MnCoO6) and La L3-edge (La2MnCoO6)

Table S8 Comparison of electrocatalytic activities between Pr2MnCoO6, La2MnCoO6 and various perovskite oxides for ORR

| Catalysts | Onset potential (V vs. RHE) | Half-wave potential (V vs. RHE) | Potential (V vs. RHE) @ mA cm–2 | Loading mass (mgcat cm–2) | Electrolyte /Rotation rate (rpm) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | 0.8 | 0.68 | –5.89 @ 0.3 | 0.479 | 0.1 M KOH /1600 | This work |
| La2MnCoO6 | 0.77 | 0.69 | –4.13 @ 0.3 | 0.479 | 0.1 M KOH /1600 | This work |
| La0.9Ag0.1Co0.7Mn0.3O3 | 0.80 | 0.63 | –4.25 @ 0.0 | 0.150 | 0.1 M KOH /1600 | [1] |
| La0.85Y0.15Ni0.7Fe0.3O3 | 0.75 | 0.63 | –3.8 @ 0.4 | 0.2 | 0.1 M KOH /1600 | [2] |
| LaCo0.8Ru0.2O3 | 0.73 | n/a | –4.75 @ 0.3 | 0.204 | 0.1 M KOH /1600 | [3] |
| SrFe0.25 Co0.25Ni0.25Mo0.25O3−δ | n/a | 0.64 | n/a | 0.232 | 0.1 M KOH /1600 | [4] |
| Bi0.6Ca0.4FeO3 | 0.705 | 0.619 | –5.17 @ 0.2 | n/a | 0.1 M KOH /1600 | [5] |
| La0.95FeO3 | ~0.72 | n/a | ~–5.5 @ 0.2 | 0.232 | 0.1 M KOH /1600 | [6] |
| PrBa0.25Sr0.75Co2O5+ δ | 0.749 | n/a | –4.067 @ 0.2 | 0.328 | 0.1 M KOH /1600 | [7] |
| La1.7Sr0.3Co0.5Ni0.5O4+δ | 0.696 | 0.568 | −4.05 @ 0.15 | 0.232 | 0.1 M KOH /1600 | [8] |

Table S9 Comparison of electrocatalytic activities between Pr2MnCoO6, La2MnCoO6 and various perovskite oxides for OER

| Catalysts | Onset potential (V vs. RHE) | Potential (V vs. RHE) @ mA cm–2 | Loading mass (mgcat cm–2) | Electrolyte /Rotation rate (rpm) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Pr2MnCoO6 | 1.62 | 1.74 @ 10 | 0.12 | 0.1 M KOH /1600 | This work |
| La2MnCoO6 | 1.68 | - | 0.12 | 0.1 M KOH /1600 | This work |
| La0.85Y0.15Ni0.7Fe0.3O3 | n/a | 1.74 @ 10 | 0.2 | 0.1 M KOH /1600 | [2] |
| Sr2TiMnO6 | 1.65 | 1.91 @ 5 | 0.102 | 0.1 M KOH /1600 | [9] |
| Ba2Bi0.1Sc0.2Co1.7O6 | n/a | 1.75 @ 5.1 | 0.361 | 0.1 M KOH /1600 | [10] |
| Ba0.5Sr0.5Co0.8Fe0.2O3−δ | n/a | 1.74 @ 10 | 0.25 | 0.1 M KOH /1600 | [11] |
| LaTi0.65Fe0.35O3−δ | n/a | 1.77 @ 10 | n/a | 0.1 M KOH /1600 | [12] |
| La0.6Sr0.4CoO3−δ | n/a | 1.83 @ 10 | n/a | 0.1 M KOH /1600 | [13] |
| LaNi0.85Mg0.15O3 | n/a | 1.86 @ 10 | 0.2 | 0.1 M KOH /1600 | [14] |
| Co-dope LaMnO3/NCNT | n/a | 1.78 @ 10 | 0.41 | 0.1 M KOH /1600 | [15] |

References

1.	Y.-X. Gao, Y. Wang, H. Liu, H.-Y. Xu, X.-P. Liu, Y.-C. Hua, C.-P. Li, J. Bai, J. Alloys Compd. 1010, 178271 (2025)

2.	Z. Lu, H. Zhou, B. Qian, S. Wang, Y. Zheng, L. Ge, H. Chen, Int. J. Hydrogen Energy 48, 8082-8092 (2023)

3.	S. G. Chandrappa, P. Moni, D. Chen, G. Karkera, K. R. Prakasha, R. A. Caruso, A. S. Prakash, J. Mater. Chem. A 8, 20612-20620 (2020)

4.	K. Li, J. Gao, X. Han, Q. Shao, Z. Lü, Journal of Energy Chemistry 96, 669-678 (2024)

5.	R. A. Afzal, K.-Y. Park, S.-H. Cho, N.-I. Kim, S. R. Choi, J. H. Kim, H.-T. Lim, J.-Y. Park, RSC Adv. 7, 47643-47653 (2017)

6.	Y. Zhu, W. Zhou, J. Yu, Y. Chen, M. Liu, Z. Shao, Chem. Mat. 28, 1691–1697 (2016)

7.	Z. Wu, L.-P. Sun, T. Xia, L.-H. Huo, H. Zhao, A. Rougier, J.-C. Grenier, J. Power Sources 334, 86-93 (2016)

8.	P. Li, B. Wei, Z. Lü, Y. Wu, Y. Zhang, X. Huang, Appl. Surf. Sci. 464, 494-501 (2019)

9.	U. Bhardwaj, A. Sharma, A. Mathur, A. Halder, H. S. Kushwaha, Energy Storage 4, e293 (2021)

10.	H. Sun, G. Chen, Y. Zhu, B. Liu, W. Zhou, Z. Shao, Chem. Eur. J. 23, 5722-5728 (2017)

11.	K. J. May, C. E. Carlton, K. A. Stoerzinger, M. Risch, J. Suntivich, Y.-L. Lee, A. Grimaud, Y. Shao-Horn, J. Phys. Chem. Lett. 3, 3264-3270 (2012)

12.	M. Prabu, P. Ramakrishnan, P. Ganesan, A. Manthiram, S. Shanmugam, Nano Energy 15, 92-103 (2015)

13.	M. Y. Oh, J. S. Jeon, J. J. Lee, P. Kim, K. S. Nahm, RSC Adv. 5, 19190-19198 (2015)

14.	Z. Du, P. Yang, L. Wang, Y. Lu, J. B. Goodenough, J. Zhang, D. Zhang, J. Power Sources 265, 91-96 (2014)

15.	D. U. Lee, M. G. Park, H. W. Park, M. H. Seo, V. Ismayilov, R. Ahmed, Z. Chen, Electrochem. Commun. 60, 38-41 (2015)