Supplementary Information for

Asymmetric Plant Polyphenol Linkers Enable Robust Metal–Organic Frameworks with Structural Heterogeneity

Zijun Zhu,1 Tong Shao,1, Lantao He1, Jun Deng2, Yang Chu2, Xuemei Zhou2, Jiajing Zhou1,3, Shaojian Lin1, Jianwu Lan1, Jiaojiao Shang1,3,*

1	College of Biomass Science and Engineering, Sichuan University, Chengdu, Sichuan 610065, China

2	School of Chemical Engineering, Sichuan University, Chengdu, Sichuan 610065, China

3	National Engineering Laboratory for Clean Technology of Leather Manufacture, Sichuan University, Chengdu, Sichuan 610065, China

*Correspondence to: Email: jiaoj.shang@scu.edu.cn (J.S.)

Contents

1. Supplementary Figures	3

2. Supplementary Tables	23

3. Supplemental References	27

# 1. Supplementary Figures

Figure S1. PXRD of products synthesized under the solvothermal conditions in DMF.

Figure S2. SEM and EDX patterns of products synthesized under the solvothermal conditions in DMF.

Figure S3. Coordination unit structure of SCU-1. O1, O2, and O3 are derived from HMT, O4 belongs to a water molecule, and O5 and O6 are coordinated oxygen.

Figure S4. Chelation of HMT toward the bismuth oxo rods.

Figure S5. The observed hydrogen bond distances between the water molecules occupying the one-dimensional channels in SCU-1 and the hydroxyl oxygen and pyran oxygen of the HMT linker.

Figure S6. Structural formula of the HMT molecule and schematic diagram of the geometrically optimized molecular structure

Figure S7. Proposed coordinated complexes of HMT and Bi3+ ions. Ring A and Ring B of HMT have different chemical environments.

Figure S8. Optimized structure of different complexes

Figure S9. The structural formulas of ellagic acid and (1,2,4,5-tetrazine-3,6-diyl)bis(benzene-1,2,3-triol).

Figure S10. PXRD patterns of SCU-1 at the low 2θ region (1–6°).

Figure S11. PXRD of: (1) SCU-1 stirred in formic acid, (2) sulfuric acid (at corresponding pH), (3) bismuth nitrate stirred in formic acid, and (4) the standard bismuthtris(formate) sample.

Figure S12. Cell viability of the B16 cell line after 24 h incubation with SCU-1, HMT, and bismuth acetate.

Figure S13. PXRD of SCU-1 after being stirred in aqueous solutions of L-cysteine and L-cystine, as well as patterns of the as-synthesized material and L-cystine for comparison.

Figure S14. Colloidal stability of SCU-1 in water (red) and RPMI (grey), representing ζ-potential evolution vs. time.

Figure S15. Ar adsorption-desorption isotherm of as-synthesized SCU-1, all recorded at liquid Ar temperature (87 K). The adsorption points are shown as solid symbols and the desorption points as hollow symbols. BET surface area 190 m2g-1.

Figure S16. Pore size distribution as determined for SCU-1, using an Ar slit pore model. The dashed line is drawn at a pore-size value of 13.7 Å.

Figure S17. CO2 adsorption/desorption isotherms of SCU-1 at 0 °C

Figure S18. DFT-optimized structures of different CO2 adsorption sites. Color code: red, O; gray, C; purple, Bi; light gray, H

Figure S19. HPLC signals for liquid products formed in the CO2 reduction.

Figure S20. SEM and PXRD patterns of SCU-1 after 4 photocatalytic tests.

# 2. Supplementary Tables

Table S1. Crystallographic table for 3DED data of SCU-1.

| Specimen | SCU-1 |
| --- | --- |
| Crystal system | Tetragonal |
| Unit cell dimensions | a = 18.62 c = 5.54 |
| Volume (Å3) | 1924 Å3 |
| Z | 4 |
| Rotation range | 73.48° (–54.98° to 18.50°) |

Table S2. Crystallographic table for the structure refinement of SCU-1 against PXRD data.

| Identification code | SCU-1 |
| --- | --- |
| Crystal system | Tetragonal |
| Space group | P 42 (NO. 77) |
| Unit cell dimensions | a = 18.967 (19) Å c = 5.666 (5) Å |
| Volume (Å3) | 2038.15 (500) Å3 |
| Wavelength | 1.54060 Å |
| Refinement method | Profile method |
| Refinement statistics | Rwp = 3.69 % GOF = 2.24 |

Table S3. The condensed Fukui function and dual descriptor (based on Hirshfeld population analysis) for the catechol moiety in HMT.

| Different structures | condensed Fukui function | condensed dual descriptor |
| --- | --- | --- |
| O18 | 0.08642320 | -0.05579429 |
| O19 | 0.09422894 | -0.05761236 |
| O20 | 0.00844601 | -0.00387382 |
| O21 | 0.00479343 | -0.00106236 |

Table S4. Summary of the photocatalytic CO2 reduction performance of Bi-based photocatalysts.

| Catalysts | Reaction medium | light | Products (μmol g-1 h-1) | Refs. |
| --- | --- | --- | --- | --- |
| SCU-1 (this work) | H2O | Vis | C2H5OH: 50.13 CH3OH: 26.08 HCOOH: 6.46 | This work |
| BP/Bi2WO6 Heterojunction | Benzylamine | UV-vis | CO: 12.4 CH3OH: 8.6 C2H5OH: 61.3 | 1 |
| Bi19S27Cl3 | Na2SO3/Na2S/H2O | Vis | CO: 0.5 CH4: 0.4 CH3OH: 1.2 | 2 |
| RP-Bi2MoO6 | H2O | Vis | CH4: 11.3 HCOOH: 20.1 CH3OH: 31.2 C2H5OH: 51.8 | 3 |
| Bi4TaO8Cl/Bi | H2O | Vis | CH3OH: 2.3 C2H5OH: 5.1 | 4 |
| FAPbBr3/Bi2WO6 | Benzyl alcohol | Vis | CO: 170 | 5 |
| Bi2WO6-V | H2O | UV−vis | CO: 3.7 CH4: 9.95 | 6 |
| Bi2S3/TiO2/MoS2 | NaHCO3/HCl | UV-vis-NIR | CH3OH: 29.7 C2H5OH: 25.6 | 7 |
| Cu4Pd-BTO | H2O | 300 W Xe lamp | C2H5OH: 30.4 | 8 |
| Bi@Bi2MoO6 | NaHCO3 | Vis | CO: 0.85 CH3OH: 0.59 C2H5OH: 17.93 | 9 |

# 3. Supplemental References

1.	Zhang, M. et al. Coupling benzylamine oxidation with CO2 photoconversion to ethanol over a black phosphorus and bismuth tungstate s‐scheme heterojunction. Angew. Chem. 135, e202302919 (2023).

2.	Das, K. et al. Intrinsic charge polarization in Bi19S27Cl3 nanorods promotes selective C-C coupling reaction during photoreduction of CO2 to ethanol. Adv. Mater. 35, 2205994 (2023).

3.	Das, R., Das, K., Ray, B., Vinod, C. P. & Peter, S. C. Green transformation of CO2 to ethanol using water and sunlight by the combined effect of naturally abundant red phosphorus and Bi2MoO6. Energy Environ. Sci. 15, 1967–1976 (2022).

4.	Songmei, Li. et al. Bi4TaO8Cl/Bi heterojunction enables high-selectivity photothermal catalytic conversion of CO2-H2O flow to liquid alcohol. Chem. Eng. J. 435, 135133 (2022).

5.	Huang, H. et al. Direct Z-scheme heterojunction of semicoherent FAPbBr3/Bi2WO6 interface for photoredox reaction with large driving force. ACS Nano 14, 16689–16697 (2020).

6.	Lu, C. et al. Constructing surface plasmon resonance on Bi2WO6 to boost high-selective CO2 reduction for methane. ACS Nano 15, 3529–3539 (2021).

7.	Alkanad, K. et al. Construction of Bi2S3/TiO2/MoS2 S-scheme heterostructure with a switchable charge migration pathway for selective CO2 reduction. Sol. RRL 5, 2100501 (2021).

8.	Cheng, T. et al. Tandem synergistic catalysis on Cu-Pd/Bi4Ti3O12 nanorods promoting highly selective photoconversion of CO2 to ethyl alcohol. Inorg. Chem. 64, 5455–5462 (2025).

9.	Zhao, D., Xuan, Y., Zhang, K. & Liu, X. Highly selective production of ethanol over hierarchical Bi@Bi2MoO6 composite via bicarbonate-assisted photocatalytic CO2 reduction. ChemSusChem 14, 3293–3302 (2021).