Supplementary material

- Table S1. Parameters for Adsorbent Preparation and Adsorption Experiments

| - Item | - Parameter | - Description |
| --- | --- | --- |
| - LaRC Synthesis | - RC mass | - 50 g |
|  | - Lanthanum source & dosage | - LaCl₃·6H₂O, 6.2 g |
|  | - Reaction volume | - 175 mL deionized water |
|  | - Reaction conditions | - 25 °C, 150 rpm, 24 h |
|  | - Post-treatment | - Centrifugation (4000 rpm, 5 min), washed 5 times, dried at 60 °C, sieved through 100-mesh |
| - Adsorption Experiments | - Adsorbent dosage | - 0.1 g |
|  | - Solution volume | - 40 mL |
|  | - W concentration range | - 10 - 500 mg L-1 |
|  | - Background solution | - Deionized water |
|  | - Adsorption conditions | - 25 °C, 180 rpm, 24 h |
|  | - Solid-liquid separation | - Centrifugation (3500 rpm, 10 min), supernatant filtered through 0.45 μm filter |
|  | - Replicates | - Triplicate for each concentration |

- 2.Table S2. Design of Sediment Incubation Experiment

| - Item | - Parameter | - Description |
| --- | --- | --- |
| - Sampling Information | - Sampling site | - Yangcheng Lake |
|  | - Sampling date | - April 2024 |
| - Sediment Pretreatment | - Sieving mesh size | - 0.6 mm |
| - Experimental Setup | - Core tube material | - Plexiglass |
|  | - Core tube inner diameter | - 9 cm |
|  | - Core tube height | - 30 cm |
|  | - Sediment thickness | - ~ 18 cm |
|  | - Overlying water | - Undisturbed, maintained with source lake water |
| - Experimental Procedure | - Pre-incubation period | - 14 days |
|  | - Experimental groups | - Control (no capping), RC-capped, LaRC-capped |
|  | - Capping material dosage | - 3 g per core |
|  | - Replicates | - 3 cores per group |
|  | - Incubation temperature | - 25 °C |

- Table S3. Sampling and Analytical Methods

| - Item | - Parameter/Instrument | - Description |
| --- | --- | --- |
| - Microelectrode Measurements | - Measured parameters | - DO, pH |
|  | - Measurement time points | - Weeks 2, 5, and 8 |
| - Porewater Sampling | - Sampler type | - HP-Peeper equilibrium porewater samplers |
|  | - Equilibration time | - 48 h |
| - Porewater Analysis | - Dissolved Fe(II) | - 1,10-phenanthroline spectrophotometric method |
|  | - Dissolved W, Mn | - ICP-MS (NEXION 350 X, PerkinElmer); samples diluted with 3% HNO₃ prior to analysis |
| - Sediment Analysis | - Sampling time | - Week 8 |
|  | - Sampling depth | - Surface layer (0-5 cm) |
|  | - Pretreatment | - Freeze-drying |
|  | - W fractionation analysis | - Sequential extraction procedure |
| - Material Characterization | - Analyzed materials | - LaRC before and after W adsorption |
|  | - Characterization method | - XPS (ESCALAB 250 Xi, Thermo Fisher Scientific) |