SUPPLEMENTARY INFORMATION

The effective Ni(II) removal of red mud modified chitosan from aqueous solution

Thi-Thuy Luu1,2, Duy-Khoi Nguyen1,2, Tu Thi Phuong Nguyen3, Thien-Hoang Ho4, Van-Phuc Dinh1,2*, H.A. Tuan Kiet5,6,*

1Future Materials & Devices Laboratory, Institute of Fundamental and Applied Sciences, Duy Tan University, Ho Chi Minh City 700000, Viet Nam.

2Faculty of Natural Sciences, Duy Tan University, Da Nang, 550000, Vietnam

3Department of Chemistry, Faculty of Science, Chulalongkorn University, Payathai Road, Patumwan, Bangkok 10300, Thailand.

4Dong Nai University, 4 Le Quy Don Street, Tan Hiep Ward, Dong Nai province, Vietnam.

5Institute of Research and Development, Duy Tan University, Da Nang City 550000, Viet Nam.

6Graduate School of Education, University of Pennsylvania, Philadelphia, PA 19104, USA.

*Corresponding authors: dinhvanphuc@duytan.edu.vn; hatkiet@upenn.edu

Table S1.  Non-linear kinetic parameters

| Kinetic models | Non-linear form | Parameters | Values |
| --- | --- | --- | --- |
|  |  | Co (mg/L) | 47.21 |
|  |  | qe (exp) (mg/g) | 13.68 |
| Pseudo-first-order | Qt=Qe.(1-e-k1t) | qe (cal) (mg/g) | 12.34 |
|  |  | k1 (min-1) | 0.1354 |
|  |  | RMSE | 1.202 |
|  |  | R2 | 0.5986 |
|  |  | 2 | 1.648 |
| Pseudo-second-order | Qt=Qe2.k2.t1+k2.Qe.t | qe (cal) (mg/g) | 13.09 |
|  |  | k2 (min-1) | 0.0167 |
|  |  | RMSE | 0.7643 |
|  |  | R2 | 0.8376 |
|  |  | 2 | 0.6519 |
| Intra-diffusion model | Qt=kid.t1/2+C | KP | 0.4139 |
|  |  | C | 7.87 |
|  |  | RMSE | 0.3877 |
|  |  | R2 | 0.9582 |
|  |  | 2 | 0.1752 |

# Nomenclature:

Qt: adsorption capacity at time t (mg/g)

Qe: adsorption capacity at the equilibrium (mg/g).

k1: pseudo-first-order model constant (min-1).

k2: pseudo-second-order model constant (g.mg-1.min-1).

kd : intra-diffusion models constant.

Table S2.  Non-linear isotherm parameters at different temperature

| Isotherm models | Parameters | Temperatures |  |  |
| --- | --- | --- | --- | --- |
|  |  | 298 K | 313 K | 323 K |
| Langmuir Qe=Qm.KL.Ce1+KL.Ce | KL | 0.6278 | 0.5520 | 0.4992 |
|  | qm (mg/g) | 17.15 | 22.42 | 31.66 |
|  | RMSE | 1.335 | 1.425 | 1.708 |
|  | R2 | 0.7781 | 0.8980 | 0.9484 |
|  | 2 | 0.7150 | 0.6664 | 0.6360 |
| Freundlich Qe=KF.Ce1/n | n | 6.10 | 5.22 | 4.63 |
|  | KF (mg(1-1/n).L1/n.g-1) | 8.75 | 10.45 | 13.95 |
|  | RMSE | 0.5310 | 0.4020 | 2.047 |
|  | R2 | 0.9649 | 0.9919 | 0.9259 |
|  | 2 | 0.1100 | 0.0563 | 1.5900 |
| Sips Qe=Qs.Ceβs1+αs.Ceβs | QS (L/g) | 8.75 | 12.63 | 17.57 |
|  | s | 0.0000 | 0.2724 | 0.4942 |
|  | s | 0.1640 | 0.3089 | 0.6820 |
|  | RMSE | 0.5313 | 0.2811 | 1.5388 |
|  | R2 | 0.9649 | 0.9960 | 0.9581 |
|  | 2 | 0.1116 | 0.0230 | 0.6286 |

# Nomenclature:

# Qe: amount of adsorbate in the adsorbent at equilibrium (mg/g).

# Qm: maximum monolayer adsorption capacity (mg/g).

# KL (L/mg): Langmuir isotherm constant.

# KF: Freundlich isotherm constant [(mg/g).(L/mg)1/n].

# n: heterogeneity factor.

# Qs: Sips isotherm model constant (L/g)

# αs: Sips isotherm model constant (L/mg).

βs: Sips isotherm model exponent.