Table 1. The anisotropic hyperelastic material models and their classifications.

| Material model | Strain energy density function | Classification |
| --- | --- | --- |
| Fung model [17] | W=c2eQ-1 Q=b1Eθθ2+b2EZZ2+b3ERR2+2b4EθθEZZ+2b5EZZERR+2b6ERREθθ | Polynomial implementation of the Green-Lagrange tensor approach |
| Choi-Vito model [18] | W=b0expb1E112+expb2E222+exp2b3E11E22-3 | Exponential implementation of the Green-Lagrange tensor approach |
| Holzapfel (2000) [19] | W=c12c2expc2I4-12-1 | Exponential implementation of the strain invariant approach |
| Holzapfel (2005) [20] | W=c12c2expc21-κI1-32+κI4-12-1 | Exponential implementation of the strain invariant approach |
| Four-fiber family model [21, 22] | W=c2I1-3+i=14c1i4c2iexpc2iI4i-12-1 | Combination of polynomial and exponential implementation of the strain invariant approach |
| Polynomial anisotropy [23] | W=i=13aiI1-3i+j=13bjI2-3j+k=26ckI4-1k+m=26emI6-1m | Polynomial implementation of the strain invariant approach |

Table 2. Materials parameters (c, b1, b2, b3, b4, b5, b6 and R2) of average material parameters based on Fung hyperelastic model for the LV, RV and STW subjected to biaxial testing,

|  | c | b1 | b2 | b3 | b4 | b5 | b6 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LV | 5.60±1.68 | 2.70±0.44 | 1.81±0.46 | 1.07±0.20 | 0.56±0.20 | 0.34±0.12 | 0.56±0.21 | 0.75±0.08 |
| STW | 7.32±2.25 | 3.17±0.66 | 1.83±0.23 | 1.12±0.29 | 0.42±0.17 | 0.26±0.16 | 0.67±0.16 | 0.75±0.06 |
| RV | 2.95±1.33 | 2.31±0.64 | 4.24±0.78 | 0.53±0.42 | 0.73±0.12 | 0.49±0.04 | 0.35±0.10 | 0.82±0.08 |

Table 3. Materials parameters (c, b1, b2, b3 and R2) of average material parameters based on Choi-Vito hyperelastic model for the LV, RV and STW subjected to biaxial testing,

|  | c | b1 | b2 | b3 | R2 |
| --- | --- | --- | --- | --- | --- |
| LV | 3.17±0.72 | 5.96±0.03 | 3.97±0.28 | 1.95±0.28 | 0.81±0.09 |
| STW | 4.40±1.01 | 5.95±0.04 | 3.93±0.31 | 1.86±0.28 | 0.86±0.09 |
| RV | 3.84±1.21 | 6.38±1.10 | 4.04±0.04 | 2.43±0.49 | 0.85±0.09 |

Table 4. Materials parameters (a1, a2, a3, b1, b2, b3 , c2, c3, c5, c6, φ and R2) of average material parameters of LV, RV and STW based on Polynomial (Anisotropic) hyperelastic model for the subjected to biaxial testing.

|  | a1 | a2 | a3 | b1 | b2 | b3 | c2 | c3 | c4 | c5 | c6 | φ | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LV | 4.49±1.13 | 1.61±0.56 | 0.27±0.11 | 13.38±2.43 | 13.38±2.43 | 13.38±2.43 | -0.62±0.79 | 0.33±0.12 | 0.11±0.05 | 0.04±0.02 | 0.02±0.02 | 0.18±0.17 | 0.96±0.01 |
| STW | 5.46±1.49 | 1.93±0.60 | 0.31±0.12 | 11.39±2.15 | 11.39±2.15 | 11.39±2.15 | 0.02±0.91 | 0.37±0.10 | 0.12±0.04 | 0.04±0.02 | 0.01±0.01 | 0.18±0.12 | 0.96±0.02 |
| RV | 4.31±1.74 | 3.14±0.82 | 0.87±0.25 | 15.19±3.66 | 15.19±3.66 | 15.19±3.66 | -3.06±1.02 | 0.38±0.34 | 0.27±0.10 | 0.15±0.05 | 0.09±0.03 | 0.12±0.31 | 0.89±0.09 |

Table 5. Materials parameters (μ, k1, k2, φ, and R2) of average material parameters of LV, STW and RV based on Holzapfel (2000) hyperelastic model for the subjected to biaxial testing.

|  | μ | k1 | k2 | φ | R2 |
| --- | --- | --- | --- | --- | --- |
| LV | 9.34±3.59 | 1.54±0.36 | 1.16±0.08 | 0.69±0.77 | 0.93±0.02 |
| STW | 14.17±3.46 | 1.76±0.31 | 1.22±0.11 | -2.18±9.06 | 0.92±0.01 |
| RV | 4.36±3.44 | 2.42±0.63 | 1.35±0.11 | 1.47±0.84 | 0.78±0.11 |

Table 6. Materials parameters (μ, k1, k2, φ, ρ, and R2) of average material parameters of LV, STW and RV based on Holzapfel (2005) hyperelastic model for the subjected to biaxial testing.

|  | μ | k1 | k2 | φ | ρ | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| LV | 4.90±1.30 | 1.07±0.10 | 0.91±0.05 | 0.63±1.09 | 0.52±0.11 | 0.93±0.02 |
| STW | 7.26±1.35 | 1.43±0.26 | 0.97±0.03 | 0.28±0.53 | 0.60±0.18 | 0.93±0.01 |
| RV | 2.81±2.15 | 2.02±0.48 | 1.07±0.08 | 1.40±0.71 | 0.67±0.15 | 0.79±0.10 |

Table 7. Materials parameters (c, c11, c21, , c21, c12, c22, c134, c234, φ0, and R2) of 14 specimens Left Ventricle (LV) fitting on Four-Fiber Family hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | c | c11 | c21 | c12 | c22 | c134 | c234 | φ0 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LV | 9.64±3.33 | 2.09±1.54 | 1.49±1.17 | 1.98±0.80 | 1.57±0.81 | 0.71±0.12 | 1.40±0.23 | 0.98±0.35 | 0.93±0.02 |
| STW | 14.56±3.04 | 1.29±1.41 | 3.13±2.40 | 3.78±1.74 | 1.36±0.35 | 0.52±0.17 | 1.82±0.33 | 0.75±0.25 | 0.92±0.02 |
| RV | 4.19±3.63 | 7.86±2.81 | 1.12±0.14 | 0.58±0.52 | 5.86±6.66 | 0.23±0.31 | 8.10±8.78 | 0.58±0.80 | 0.82±0.09 |

Appendix A

Table A.1. Materials parameters (c, b1, b2, b3, b4, b5, b6 and R2) of 14 specimens based on Fung hyperelastic model for the Left Ventricle (LV) subjected to biaxial testing, including the average materials parameters.

|  | c | b1 | b2 | b3 | b4 | b5 | b6 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 01 | 6.018 | 2.174 | 1.493 | 1.308 | 0.768 | 0.491 | 0.310 | 0.796 |
| Sample 02 | 6.863 | 2.159 | 1.495 | 1.315 | 0.754 | 0.480 | 0.314 | 0.697 |
| Sample 03 | 3.789 | 2.165 | 2.572 | 1.302 | 0.765 | 0.493 | 0.325 | 0.811 |
| Sample 04 | 4.503 | 2.141 | 2.863 | 1.303 | 0.741 | 0.489 | 0.347 | 0.819 |
| Sample 05 | 6.535 | 2.124 | 1.310 | 0.725 | 0.475 | 0.355 | 0.375 | 0.779 |
| Sample 06 | 2.866 | 3.451 | 1.849 | 1.204 | 0.721 | 0.251 | 0.735 | 0.636 |
| Sample 07 | 4.179 | 2.951 | 1.848 | 1.005 | 0.543 | 0.251 | 0.735 | 0.783 |
| Sample 08 | 8.530 | 2.909 | 1.860 | 1.019 | 0.372 | 0.215 | 0.753 | 0.828 |
| Sample 09 | 5.166 | 2.930 | 1.858 | 1.006 | 0.388 | 0.239 | 0.755 | 0.725 |
| Sample 10 | 7.408 | 2.955 | 1.542 | 1.019 | 0.356 | 0.277 | 0.708 | 0.603 |
| Sample 11 | 4.670 | 2.961 | 1.838 | 1.005 | 0.401 | 0.258 | 0.728 | 0.822 |
| Sample 12 | 5.919 | 2.903 | 1.887 | 1.013 | 0.392 | 0.202 | 0.768 | 0.648 |
| Sample 13 | 7.871 | 2.932 | 1.828 | 1.018 | 0.361 | 0.247 | 0.731 | 0.758 |
| Sample 14 | 4.102 | 2.982 | 1.057 | 0.702 | 0.783 | 0.493 | 0.310 | 0.834 |
| Average | 5.601 | 2.696 | 1.807 | 1.067 | 0.559 | 0.339 | 0.564 | 0.753 |

Table A.2. Materials parameters (c, b1, b2, b3 and R2) of 14 specimens based on Choi-Vito hyperelastic model for the Left Ventricle (LV) subjected to biaxial testing, including the average materials parameters .

|  | c | b1 | b2 | b3 | R2 |
| --- | --- | --- | --- | --- | --- |
| Sample 01 | 3.069 | 5.986 | 4.010 | 1.940 | 0.911 |
| Sample 02 | 3.452 | 5.977 | 4.014 | 1.980 | 0.845 |
| Sample 03 | 2.444 | 5.962 | 4.038 | 2.511 | 0.771 |
| Sample 04 | 3.314 | 5.920 | 4.084 | 2.026 | 0.691 |
| Sample 05 | 3.972 | 5.917 | 4.085 | 2.023 | 0.771 |
| Sample 06 | 3.243 | 5.973 | 4.023 | 2.005 | 0.896 |
| Sample 07 | 2.281 | 5.970 | 4.032 | 2.010 | 0.793 |
| Sample 08 | 4.691 | 5.949 | 4.044 | 2.009 | 0.900 |
| Sample 09 | 2.460 | 5.963 | 4.039 | 2.011 | 0.736 |
| Sample 10 | 3.563 | 5.981 | 4.005 | 1.515 | 0.804 |
| Sample 11 | 2.298 | 5.977 | 4.025 | 2.008 | 0.846 |
| Sample 12 | 2.897 | 5.943 | 4.060 | 2.017 | 0.659 |
| Sample 13 | 3.961 | 5.904 | 4.097 | 2.027 | 0.747 |
| Sample 14 | 2.723 | 6.000 | 2.990 | 1.285 | 0.961 |
| Avg | 3.169 | 5.959 | 3.968 | 1.955 | 0.809 |

Table A.3. Materials parameters (a1, a2, a3, b1, b2, b3 , c2, c3, c5, c6, φ and R2) of 14 specimens Left Ventricle (LV) based on Polynomial (Anisotropic) hyperelastic model for the subjected to biaxial testing, including the average materials parameters .

|  | a1 | a2 | a3 | b1 | b2 | b3 | c2 | c3 | c4 | c5 | c6 | φ | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 3.600 | 1.183 | 0.180 | 11.258 | 11.258 | 11.258 | 0.208 | 0.266 | 0.083 | 0.026 | 0.007 | 0.204 | 0.964 |
| Sample 2 | 5.147 | 0.894 | 0.150 | 10.789 | 10.789 | 10.789 | 0.221 | 0.237 | 0.082 | 0.033 | 0.015 | 0.205 | 0.970 |
| Sample 3 | 3.836 | 1.990 | 0.341 | 17.726 | 17.726 | 17.726 | -1.266 | 0.371 | 0.099 | 0.018 | -0.008 | 0.440 | 0.960 |
| Sample 4 | 5.215 | 2.702 | 0.467 | 17.374 | 17.374 | 17.374 | -2.102 | 0.478 | 0.161 | 0.052 | 0.014 | 0.396 | 0.958 |
| Sample 5 | 6.316 | 2.136 | 0.367 | 13.532 | 13.532 | 13.532 | -1.488 | 0.517 | 0.205 | 0.092 | 0.046 | 0.000 | 0.967 |
| Sample 6 | 4.110 | 1.427 | 0.201 | 12.064 | 12.064 | 12.064 | -0.014 | 0.259 | 0.081 | 0.026 | 0.007 | 0.244 | 0.966 |
| Sample 7 | 4.089 | 1.443 | 0.207 | 12.048 | 12.048 | 12.048 | -0.022 | 0.263 | 0.083 | 0.027 | 0.008 | 0.244 | 0.966 |
| Sample 8 | 2.716 | 1.916 | 0.340 | 17.302 | 17.302 | 17.302 | -1.076 | 0.334 | 0.100 | 0.024 | -0.001 | 0.454 | 0.961 |
| Sample 9 | 5.656 | 1.422 | 0.159 | 13.920 | 13.920 | 13.920 | -0.898 | 0.365 | 0.126 | 0.049 | 0.022 | 0.000 | 0.954 |
| Sample 10 | 5.251 | 2.214 | 0.395 | 12.296 | 12.296 | 12.296 | -0.780 | 0.456 | 0.173 | 0.076 | 0.038 | 0.000 | 0.971 |
| Sample 11 | 3.806 | 1.508 | 0.309 | 13.681 | 13.681 | 13.681 | -1.179 | 0.387 | 0.143 | 0.062 | 0.028 | 0.109 | 0.959 |
| Sample 12 | 5.213 | 0.512 | 0.101 | 10.631 | 10.631 | 10.631 | 0.708 | 0.055 | 0.009 | 0.001 | 0.000 | 0.000 | 0.977 |
| Sample 13 | 2.531 | 1.598 | 0.282 | 12.845 | 12.845 | 12.845 | -0.734 | 0.313 | 0.127 | 0.057 | 0.029 | 0.000 | 0.953 |
| Sample 14 | 5.344 | 1.530 | 0.231 | 11.854 | 11.854 | 11.854 | -0.219 | 0.328 | 0.117 | 0.047 | 0.020 | 0.255 | 0.969 |
| Average | 4.488 | 1.605 | 0.266 | 13.380 | 13.380 | 13.380 | -0.617 | 0.331 | 0.114 | 0.042 | 0.016 | 0.182 | 0.964 |

Table A.4. Materials parameters (μ, k1, k2, φ and R2) of 14 specimens Left Ventricle (LV) based on Holzapfel (2000) hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | μ | k1 | k2 | φ | R2 |
| --- | --- | --- | --- | --- | --- |
| Sample 1 | 9.512 | 1.324 | 1.126 | -0.562 | 0.938 |
| Sample 2 | 11.868 | 1.233 | 1.101 | -0.543 | 0.960 |
| Sample 3 | 5.585 | 1.888 | 1.198 | 0.881 | 0.932 |
| Sample 4 | 7.153 | 2.251 | 1.227 | 2.192 | 0.917 |
| Sample 5 | 13.538 | 1.061 | 1.198 | 0.900 | 0.903 |
| Sample 6 | 10.498 | 1.372 | 1.130 | 0.650 | 0.934 |
| Sample 7 | 10.461 | 1.383 | 1.142 | 0.652 | 0.933 |
| Sample 8 | 3.679 | 1.864 | 1.236 | 0.856 | 0.930 |
| Sample 9 | 11.415 | 1.275 | 1.061 | 0.869 | 0.917 |
| Sample 10 | 13.421 | 1.750 | 1.279 | 1.758 | 0.921 |
| Sample 11 | 5.120 | 1.810 | 1.168 | 0.881 | 0.917 |
| Sample 12 | 11.845 | 1.041 | 0.956 | -0.302 | 0.962 |
| Sample 13 | 3.706 | 1.816 | 1.254 | 0.803 | 0.918 |
| Sample 14 | 12.922 | 1.450 | 1.177 | 0.679 | 0.940 |
| Average | 9.337 | 1.537 | 1.161 | 0.694 | 0.930 |

Table A.5. Materials parameters (μ, k1, k2, φ, ρ, and R2) of 14 specimens Left Ventricle (LV) based on Holzapfel (2005) hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | μ | k1 | k2 | φ | ρ | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 4.547 | 1.028 | 0.913 | 0.000 | 0.547 | 0.944 |
| Sample 2 | 5.777 | 0.979 | 0.908 | -0.005 | 0.586 | 0.961 |
| Sample 3 | 3.728 | 1.046 | 0.917 | 1.923 | 0.471 | 0.921 |
| Sample 4 | 5.049 | 1.284 | 0.955 | 1.571 | 0.550 | 0.896 |
| Sample 5 | 6.519 | 1.196 | 0.943 | 2.008 | 0.464 | 0.915 |
| Sample 6 | 4.984 | 1.007 | 0.906 | -0.347 | 0.477 | 0.940 |
| Sample 7 | 4.976 | 1.023 | 0.909 | -0.352 | 0.475 | 0.940 |
| Sample 8 | 2.767 | 1.060 | 0.926 | 2.051 | 0.469 | 0.918 |
| Sample 9 | 5.538 | 0.961 | 0.858 | -1.051 | 0.521 | 0.919 |
| Sample 10 | 6.436 | 1.289 | 0.991 | 0.700 | 0.465 | 0.935 |
| Sample 11 | 3.360 | 1.019 | 0.919 | 1.963 | 0.477 | 0.908 |
| Sample 12 | 5.966 | 1.026 | 0.796 | -0.005 | 0.885 | 0.964 |
| Sample 13 | 2.736 | 1.053 | 0.931 | 0.857 | 0.469 | 0.908 |
| Sample 14 | 6.198 | 1.068 | 0.930 | -0.447 | 0.471 | 0.946 |
| Average | 4.899 | 1.074 | 0.914 | 0.633 | 0.523 | 0.930 |

Table A.6. Materials parameters (c, c11, c21, , c21, c12, c22, c134, c234, φ0, and R2) of 14 specimens Left Ventricle (LV) fitting on Four-Fiber Family hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | c | c11 | c21 | c12 | c22 | c134 | c234 | φ0 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 9.589 | 0.329 | 1.924 | 2.905 | 0.133 | 0.799 | 1.294 | 0.809 | 0.938 |
| Sample 2 | 11.925 | 0.171 | 1.844 | 2.694 | 1.134 | 0.868 | 1.201 | 0.836 | 0.960 |
| Sample 3 | 6.177 | 3.464 | 1.040 | 1.451 | 1.832 | 0.668 | 1.461 | 0.979 | 0.929 |
| Sample 4 | 8.314 | 5.258 | 1.022 | 0.315 | 3.747 | 0.586 | 1.624 | 0.971 | 0.911 |
| Sample 5 | 13.657 | 3.262 | 0.953 | 1.198 | 2.008 | 0.587 | 1.596 | 1.044 | 0.913 |
| Sample 6 | 10.567 | 0.936 | 1.316 | 2.532 | 1.160 | 0.790 | 1.307 | 0.809 | 0.934 |
| Sample 7 | 10.534 | 0.953 | 1.337 | 2.557 | 1.173 | 0.775 | 1.338 | 0.811 | 0.933 |
| Sample 8 | 4.238 | 3.254 | 1.094 | 1.696 | 1.740 | 0.628 | 1.532 | 0.961 | 0.927 |
| Sample 9 | 11.450 | 2.075 | 0.780 | 1.067 | 1.616 | 0.882 | 1.119 | 0.988 | 0.923 |
| Sample 10 | 13.560 | 2.327 | 1.220 | 2.562 | 1.491 | 0.500 | 1.909 | 0.889 | 0.924 |
| Sample 11 | 5.798 | 3.232 | 0.793 | 1.291 | 2.133 | 0.691 | 1.369 | 1.234 | 0.926 |
| Sample 12 | 11.800 | 0.005 | 5.362 | 2.783 | 0.848 | 0.856 | 0.986 | 0.501 | 0.965 |
| Sample 13 | 4.308 | 2.777 | 0.956 | 2.134 | 1.705 | 0.634 | 1.487 | 2.056 | 0.921 |
| Sample 14 | 13.007 | 1.229 | 1.175 | 2.541 | 1.283 | 0.725 | 1.420 | 0.870 | 0.941 |
| Average | 9.637 | 2.091 | 1.487 | 1.980 | 1.572 | 0.714 | 1.403 | 0.983 | 0.932 |

Table 2.1. Materials parameters (c, b1, b2, b3, b4, b5, b6 and R2) of 14 specimens based on Fung hyperelastic model for the Septal Wall (STW) subjected to biaxial testing, including the average materials parameters.

|  | c | b1 | b2 | b3 | b4 | b5 | b6 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 01 | 10.180 | 2.784 | 1.930 | 1.234 | 0.315 | 0.142 | 0.700 | 0.718 |
| Sample 02 | 7.647 | 2.436 | 1.510 | 0.135 | 0.936 | 0.180 | 0.767 | 0.800 |
| Sample 03 | 10.093 | 2.945 | 1.498 | 1.219 | 0.342 | 0.273 | 0.650 | 0.842 |
| Sample 04 | 11.783 | 2.307 | 1.455 | 1.027 | 0.355 | 0.728 | 0.158 | 0.713 |
| Sample 05 | 7.954 | 3.852 | 1.822 | 1.223 | 0.276 | 0.247 | 0.650 | 0.711 |
| Sample 06 | 6.184 | 3.886 | 1.862 | 1.216 | 0.349 | 0.223 | 0.766 | 0.733 |
| Sample 07 | 6.267 | 3.850 | 1.929 | 1.221 | 0.381 | 0.158 | 0.797 | 0.755 |
| Sample 08 | 6.247 | 3.872 | 1.885 | 1.220 | 0.360 | 0.197 | 0.781 | 0.682 |
| Sample 09 | 6.660 | 3.442 | 1.823 | 1.212 | 0.366 | 0.260 | 0.729 | 0.832 |
| Sample 10 | 5.772 | 3.401 | 1.891 | 1.211 | 0.394 | 0.203 | 0.768 | 0.776 |
| Sample 11 | 5.650 | 3.840 | 1.928 | 1.220 | 0.371 | 0.158 | 0.700 | 0.641 |
| Sample 12 | 6.951 | 1.962 | 2.384 | 1.110 | 0.462 | 0.481 | 0.522 | 0.807 |
| Sample 13 | 8.178 | 2.816 | 1.909 | 1.209 | 0.328 | 0.183 | 0.700 | 0.737 |
| Sample 14 | 2.893 | 2.966 | 1.834 | 1.202 | 0.612 | 0.266 | 0.700 | 0.703 |
| Average | 7.319 | 3.169 | 1.833 | 1.119 | 0.418 | 0.264 | 0.671 | 0.746 |

Table B.2. Materials parameters (c, b1, b2, b3 and R2) of 14 specimens based on Choi-Vito hyperelastic model for the Septal Wall (STW) subjected to biaxial testing, including the average materials parameters .

|  | c | b1 | b2 | b3 | R2 |
| --- | --- | --- | --- | --- | --- |
| Sample 01 | 5.120 | 5.859 | 4.134 | 2.033 | 0.766 |
| Sample 02 | 4.297 | 5.992 | 3.460 | 1.603 | 0.942 |
| Sample 03 | 4.919 | 5.989 | 3.951 | 1.620 | 0.943 |
| Sample 04 | 5.094 | 5.990 | 2.994 | 1.129 | 0.876 |
| Sample 05 | 6.203 | 5.976 | 4.001 | 1.553 | 0.928 |
| Sample 06 | 4.609 | 5.965 | 4.025 | 2.004 | 0.935 |
| Sample 07 | 4.839 | 5.928 | 4.071 | 2.021 | 0.915 |
| Sample 08 | 4.687 | 5.950 | 4.043 | 2.009 | 0.900 |
| Sample 09 | 4.102 | 5.983 | 4.014 | 2.003 | 0.951 |
| Sample 10 | 3.651 | 5.947 | 4.055 | 2.017 | 0.870 |
| Sample 11 | 4.600 | 5.922 | 4.074 | 2.019 | 0.858 |
| Sample 12 | 3.785 | 5.917 | 4.077 | 2.020 | 0.665 |
| Sample 13 | 3.960 | 5.904 | 4.097 | 2.027 | 0.747 |
| Sample 14 | 1.742 | 5.979 | 4.022 | 2.006 | 0.720 |
| Avg | 4.401 | 5.950 | 3.930 | 1.862 | 0.858 |

Table B.3. Materials parameters (a1, a2, a3, b1, b2, b3 , c2, c3, c5, c6, φ and R2) of 14 specimens Septal Wall (STW) based on Polynomial (Anisotropic) hyperelastic model for the subjected to biaxial testing, including the average materials parameters .

|  | a1 | a2 | a3 | b1 | b2 | b3 | c2 | c3 | c4 | c5 | c6 | φ | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 7.506 | 2.008 | 0.311 | 12.062 | 12.062 | 12.062 | -0.090 | 0.364 | 0.119 | 0.043 | 0.016 | 0.255 | 0.974 |
| Sample 2 | 3.698 | 1.302 | 0.221 | 10.542 | 10.542 | 10.542 | 0.932 | 0.264 | 0.091 | 0.037 | 0.018 | 0.107 | 0.973 |
| Sample 3 | 5.341 | 1.637 | 0.275 | 11.049 | 11.049 | 11.049 | 0.490 | 0.332 | 0.117 | 0.044 | 0.016 | 0.176 | 0.975 |
| Sample 4 | 3.972 | 0.961 | 0.084 | 10.135 | 10.135 | 10.135 | 1.620 | 0.212 | 0.056 | 0.013 | 0 | 0 | 0.953 |
| Sample 5 | 6.595 | 1.894 | 0.313 | 10.801 | 10.801 | 10.801 | 0.980 | 0.374 | 0.125 | 0.046 | 0.019 | 0.135 | 0.976 |
| Sample 6 | 4.947 | 2.161 | 0.353 | 11.994 | 11.994 | 11.994 | 0.349 | 0.306 | 0.080 | 0.019 | 0.001 | 0.152 | 0.969 |
| Sample 7 | 5.397 | 2.767 | 0.521 | 12.395 | 12.395 | 12.395 | -0.701 | 0.513 | 0.192 | 0.083 | 0.041 | 0.333 | 0.975 |
| Sample 8 | 4.263 | 1.966 | 0.283 | 11.104 | 11.104 | 11.104 | 0.751 | 0.396 | 0.119 | 0.030 | 0 | 0.157 | 0.966 |
| Sample 9 | 5.713 | 2.140 | 0.312 | 11.968 | 11.968 | 11.968 | -0.123 | 0.433 | 0.139 | 0.045 | 0.012 | 0.244 | 0.963 |
| Sample 10 | 3.635 | 2.076 | 0.363 | 11.408 | 11.408 | 11.408 | 0.184 | 0.425 | 0.148 | 0.057 | 0.024 | 0.219 | 0.965 |
| Sample 11 | 4.124 | 2.414 | 0.430 | 13.117 | 13.117 | 13.117 | -0.911 | 0.443 | 0.153 | 0.059 | 0.026 | 0.334 | 0.963 |
| Sample 12 | 6.064 | 2.541 | 0.345 | 12.991 | 12.991 | 12.991 | -0.822 | 0.480 | 0.164 | 0.058 | 0.02 | 0 | 0.959 |
| Sample 13 | 8.550 | 0.696 | 0.103 | 5.176 | 5.176 | 5.176 | -0.596 | 0.174 | 0.056 | 0.019 | 0.005 | 0 | 0.914 |
| Sample 14 | 6.609 | 2.456 | 0.416 | 14.662 | 14.662 | 14.662 | -1.759 | 0.500 | 0.151 | 0.045 | 0.009 | 0.34 | 0.953 |
| Average | 5.458 | 1.930 | 0.309 | 11.386 | 11.386 | 11.386 | 0.022 | 0.373 | 0.122 | 0.043 | 0.0148 | 0.175 | 0.963 |

Table B.4. Materials parameters (μ, k1, k2, φ and R2) of 14 specimens Septal Wall (STW) based on Holzapfel (2000) hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | μ | k1 | k2 | φ | R2 |
| --- | --- | --- | --- | --- | --- |
| Sample 1 | 18.919 | 1.637 | 1.229 | 0.649 | 0.943 |
| Sample 2 | 12.179 | 1.429 | 1.159 | 0.229 | 0.926 |
| Sample 3 | 15.276 | 1.543 | 1.203 | -0.465 | 0.934 |
| Sample 4 | 11.371 | 2.023 | 1.042 | 0.000 | 0.925 |
| Sample 5 | 19.969 | 1.664 | 1.226 | 0.286 | 0.926 |
| Sample 6 | 15.203 | 1.690 | 1.228 | -0.568 | 0.914 |
| Sample 7 | 15.522 | 1.987 | 1.342 | 0.732 | 0.918 |
| Sample 8 | 14.788 | 1.647 | 1.209 | -0.385 | 0.903 |
| Sample 9 | 15.765 | 1.693 | 1.241 | 0.640 | 0.920 |
| Sample 10 | 8.533 | 2.353 | 1.378 | -0.636 | 0.940 |
| Sample 11 | 7.332 | 2.297 | 1.393 | 0.791 | 0.934 |
| Sample 12 | 15.637 | 1.776 | 1.241 | 0.769 | 0.905 |
| Sample 13 | 14.271 | 1.260 | 1.018 | 0.969 | 0.914 |
| Sample 14 | 13.595 | 1.644 | 1.197 | -33.595 | 0.900 |
| Average | 14.169 | 1.760 | 1.222 | -2.185 | 0.921 |

Table B.5. Materials parameters (μ, k1, k2, φ, ρ, and R2) of 14 specimens Septal Wall (STW) based on Holzapfel (2005) hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | μ | k1 | k2 | φ | ρ | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 9.206 | 1.217 | 0.960 | -0.332 | 0.469 | 0.952 |
| Sample 2 | 5.936 | 1.596 | 0.981 | 0.000 | 0.859 | 0.936 |
| Sample 3 | 7.606 | 1.314 | 0.970 | 0.000 | 0.666 | 0.941 |
| Sample 4 | 5.506 | 2.219 | 0.898 | 0.000 | 0.989 | 0.929 |
| Sample 5 | 10.220 | 1.641 | 1.011 | 0.000 | 0.830 | 0.924 |
| Sample 6 | 7.443 | 1.318 | 0.969 | 0.000 | 0.530 | 0.928 |
| Sample 7 | 7.492 | 1.477 | 1.026 | 0.619 | 0.462 | 0.936 |
| Sample 8 | 7.508 | 1.508 | 0.980 | 0.000 | 0.749 | 0.907 |
| Sample 9 | 7.635 | 1.262 | 0.962 | -0.279 | 0.466 | 0.931 |
| Sample 10 | 6.062 | 1.375 | 1.000 | 0.000 | 0.544 | 0.924 |
| Sample 11 | 5.298 | 1.295 | 0.983 | 0.816 | 0.460 | 0.921 |
| Sample 12 | 7.564 | 1.299 | 0.949 | 0.729 | 0.448 | 0.916 |
| Sample 13 | 7.564 | 1.299 | 0.949 | 0.729 | 0.448 | 0.916 |
| Sample 14 | 6.561 | 1.202 | 0.939 | 1.571 | 0.473 | 0.913 |
| Average | 7.257 | 1.430 | 0.970 | 0.275 | 0.600 | 0.927 |

Table B.6. Materials parameters (c, c11, c21, , c21, c12, c22, c134, c234, φ0, and R2) of 14 specimens Septal Wall (STW) fitting on Four-Fiber Family hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | c | c11 | c21 | c12 | c22 | c134 | c234 | φ0 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 19.051 | 1.195 | 1.552 | 3.284 | 1.249 | 0.590 | 1.689 | 0.815 | 0.944 |
| Sample 2 | 10.517 | 0.042 | 5.220 | 5.658 | 1.062 | 0.415 | 1.789 | 0.469 | 0.947 |
| Sample 3 | 15.361 | 0.001 | 8.828 | 4.346 | 1.156 | 0.706 | 1.659 | 0.860 | 0.934 |
| Sample 4 | 13.231 | -0.014 | 5.990 | 6.130 | 0.965 | 0.345 | 1.758 | 0.002 | 0.870 |
| Sample 5 | 19.979 | 0.030 | 4.820 | 6.002 | 1.119 | 0.298 | 2.352 | 0.661 | 0.931 |
| Sample 6 | 15.400 | 0.394 | 2.935 | 4.147 | 1.132 | 0.526 | 1.791 | 0.715 | 0.919 |
| Sample 7 | 15.071 | 2.427 | 1.432 | 3.331 | 1.444 | 0.347 | 2.431 | 0.826 | 0.921 |
| Sample 8 | 14.868 | 0.051 | 4.398 | 5.303 | 1.129 | 0.446 | 1.909 | 0.721 | 0.908 |
| Sample 9 | 15.911 | 1.209 | 1.519 | 3.503 | 1.277 | 0.570 | 1.727 | 0.844 | 0.921 |
| Sample 10 | 12.628 | 0.360 | 2.903 | 4.313 | 1.241 | 0.473 | 1.964 | 0.809 | 0.911 |
| Sample 11 | 8.006 | 3.764 | 1.259 | 3.137 | 1.685 | 0.398 | 2.005 | 0.998 | 0.931 |
| Sample 12 | 15.782 | 2.488 | 1.150 | 2.536 | 1.465 | 0.558 | 1.708 | 0.906 | 0.906 |
| Sample 13 | 14.287 | 2.526 | 0.817 | 0.573 | 1.856 | 0.943 | 1.067 | 0.955 | 0.918 |
| Sample 14 | 13.704 | 3.655 | 1.060 | 0.709 | 2.238 | 0.611 | 1.606 | 0.915 | 0.905 |
| Average | 14.557 | 1.295 | 3.135 | 3.784 | 1.358 | 0.516 | 1.818 | 0.750 | 0.919 |

Table C.1. Materials parameters (c, b1, b2, b3, b4, b5, b6 and R2) of 14 specimens based on Fung hyperelastic model for the Right Ventricle (RV) subjected to biaxial testing, including the average materials parameters .

|  | c | b1 | b2 | b3 | b4 | b5 | b6 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 01 | 1.387 | 2.171 | 5.503 | 0.297 | 0.775 | 0.499 | 0.329 | 0.639 |
| Sample 02 | 1.223 | 2.186 | 4.994 | 0.299 | 0.787 | 0.500 | 0.312 | 0.635 |
| Sample 03 | 5.266 | 2.154 | 2.884 | 1.300 | 0.754 | 0.485 | 0.342 | 0.875 |
| Sample 04 | 2.772 | 2.161 | 4.233 | 0.297 | 0.763 | 0.500 | 0.336 | 0.841 |
| Sample 05 | 4.064 | 2.093 | 4.513 | 0.293 | 0.692 | 0.498 | 0.405 | 0.787 |
| Sample 06 | 4.008 | 2.104 | 4.285 | 0.296 | 0.706 | 0.495 | 0.389 | 0.878 |
| Sample 07 | 3.390 | 2.138 | 4.129 | 0.740 | 0.496 | 0.360 | 0.546 | 0.823 |
| Sample 08 | 3.374 | 2.174 | 3.325 | 1.231 | 0.773 | 0.495 | 0.327 | 0.895 |
| Sample 09 | 4.669 | 2.159 | 3.482 | 1.263 | 0.758 | 0.490 | 0.340 | 0.910 |
| Sample 10 | 2.657 | 1.998 | 4.403 | 0.099 | 0.499 | 0.501 | 0.506 | 0.841 |
| Sample 11 | 1.611 | 2.188 | 4.822 | 0.298 | 0.791 | 0.499 | 0.313 | 0.833 |
| Sample 12 | 2.273 | 2.157 | 5.160 | 0.295 | 0.759 | 0.533 | 0.344 | 0.812 |
| Sample 13 | 3.563 | 2.133 | 4.518 | 0.294 | 0.734 | 0.497 | 0.373 | 0.808 |
| Sample 14 | 1.015 | 4.541 | 3.139 | 0.458 | 1.001 | 0.498 | 0.104 | 0.847 |
| Average | 2.948 | 2.311 | 4.242 | 0.533 | 0.735 | 0.489 | 0.355 | 0.816 |

Table C.2. Materials parameters (c, b1, b2, b3 and R2) of 14 specimens based on Choi-Vito hyperelastic model for the Right Ventricle (RV) subjected to biaxial testing, including the average materials parameters .

|  | c | b1 | b2 | b3 | R2 |
| --- | --- | --- | --- | --- | --- |
| Sample 01 | 4.7 | 5.875 | 4.11 | 2.523 | 0.773 |
| Sample 02 | 2.044 | 8.976 | 4.01 | 3.612 | 0.864 |
| Sample 03 | 4.957 | 5.989 | 3.97 | 1.564 | 0.943 |
| Sample 04 | 2.472 | 8.978 | 4 | 2.671 | 0.8 |
| Sample 05 | 6.21 | 5.976 | 4 | 1.549 | 0.928 |
| Sample 06 | 4.295 | 5.971 | 4.02 | 2.401 | 0.935 |
| Sample 07 | 4.441 | 5.939 | 4.06 | 2.515 | 0.921 |
| Sample 08 | 4.306 | 5.958 | 4.03 | 2.503 | 0.903 |
| Sample 09 | 4.016 | 5.983 | 4.01 | 2.134 | 0.951 |
| Sample 10 | 3.359 | 5.953 | 4.05 | 2.514 | 0.88 |
| Sample 11 | 4.227 | 5.931 | 4.06 | 2.511 | 0.864 |
| Sample 12 | 3.485 | 5.926 | 4.07 | 2.513 | 0.675 |
| Sample 13 | 3.643 | 5.915 | 4.08 | 2.521 | 0.759 |
| Sample 14 | 1.604 | 5.981 | 4.02 | 2.507 | 0.736 |
| Avg | 3.8399 | 6.382 | 4.04 | 2.431 | 0.852 |

Table A.3. Materials parameters (a1, a2, a3, b1, b2, b3 , c2, c3, c5, c6, φ and R2) of 14 specimens Right Ventricle (RV) based on Polynomial (Anisotropic) hyperelastic model for the subjected to biaxial testing, including the average materials parameters .

|  | a1 | a2 | a3 | b1 | b2 | b3 | c2 | c3 | c4 | c5 | c6 | φ | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 2.982 | 2.499 | 0.926 | 18.585 | 18.585 | 18.585 | -2.760 | -0.098 | 0.172 | 0.140 | 0.110 | 0.469 | 0.688 |
| Sample 2 | 2.114 | 1.992 | 0.766 | 26.077 | 26.077 | 26.077 | -1.638 | -0.377 | 0.076 | 0.069 | 0.052 | -0.534 | 0.673 |
| Sample 3 | 4.351 | 3.441 | 0.765 | 13.368 | 13.368 | 13.368 | -2.648 | 0.780 | 0.340 | 0.170 | 0.094 | 0.167 | 0.956 |
| Sample 4 | 3.684 | 2.988 | 0.910 | 15.540 | 15.540 | 15.540 | -2.694 | 0.072 | 0.194 | 0.130 | 0.088 | 0.405 | 0.873 |
| Sample 5 | 7.157 | 3.828 | 0.953 | 11.911 | 11.911 | 11.911 | -4.377 | 0.553 | 0.341 | 0.184 | 0.103 | 0.206 | 0.905 |
| Sample 6 | 7.635 | 2.815 | 0.808 | 11.477 | 11.477 | 11.477 | -3.599 | 0.394 | 0.276 | 0.161 | 0.099 | 0.175 | 0.938 |
| Sample 7 | 4.954 | 3.258 | 0.730 | 15.560 | 15.560 | 15.560 | -3.381 | 0.501 | 0.278 | 0.139 | 0.075 | 0.292 | 0.942 |
| Sample 8 | 5.656 | 1.422 | 0.159 | 13.920 | 13.920 | 13.920 | -0.898 | 0.365 | 0.126 | 0.049 | 0.022 | 0.000 | 0.954 |
| Sample 9 | 2.954 | 3.282 | 0.869 | 13.307 | 13.307 | 13.307 | -2.650 | 0.639 | 0.319 | 0.165 | 0.091 | 0.291 | 0.960 |
| Sample 10 | 4.232 | 4.298 | 1.136 | 13.424 | 13.424 | 13.424 | -3.543 | 0.758 | 0.392 | 0.204 | 0.113 | 0.322 | 0.964 |
| Sample 11 | 1.602 | 2.537 | 0.820 | 15.887 | 15.887 | 15.887 | -2.397 | 0.263 | 0.213 | 0.125 | 0.080 | 0.393 | 0.890 |
| Sample 12 | 4.279 | 4.030 | 1.070 | 15.725 | 15.725 | 15.725 | -4.148 | 0.601 | 0.353 | 0.183 | 0.102 | -0.322 | 0.919 |
| Sample 13 | 3.431 | 3.679 | 1.129 | 15.248 | 15.248 | 15.248 | -3.635 | 0.237 | 0.271 | 0.169 | 0.114 | -0.361 | 0.885 |
| Sample 14 | 5.295 | 3.823 | 1.124 | 12.598 | 12.598 | 12.598 | -4.428 | 0.680 | 0.404 | 0.237 | 0.150 | 0.230 | 0.928 |
| Average | 4.309 | 3.135 | 0.869 | 15.188 | 15.188 | 15.188 | -3.057 | 0.383 | 0.268 | 0.152 | 0.092 | 0.124 | 0.891 |

Table C.4. Materials parameters (μ, k1, k2, φ and R2) of 14 specimens Right Ventricle (RV) based on Holzapfel (2000) hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | μ | k1 | k2 | φ | R2 |
| --- | --- | --- | --- | --- | --- |
| Sample 1 | 2.301 | 1.727 | 1.33 | 1.208 | 0.619 |
| Sample 2 | 0.244 | 1.681 | 1.38 | 2.109 | 0.743 |
| Sample 3 | 4.461 | 3.236 | 1.43 | 0.876 | 0.888 |
| Sample 4 | 1.069 | 2.66 | 1.41 | 2.139 | 0.881 |
| Sample 5 | 9.834 | 2.26 | 1.31 | 1.731 | 0.600 |
| Sample 6 | 6.242 | 2.709 | 1.24 | 1.914 | 0.778 |
| Sample 7 | 4.99 | 2.321 | 1.22 | 1.962 | 0.758 |
| Sample 8 | 11.415 | 1.275 | 1.06 | 0.869 | 0.917 |
| Sample 9 | 1.41 | 3.06 | 1.46 | -0.892 | 0.899 |
| Sample 10 | 2.915 | 3.602 | 1.51 | 2.229 | 0.906 |
| Sample 11 | -0.006 | 2.127 | 1.41 | 2.128 | 0.818 |
| Sample 12 | 5.864 | 2.405 | 1.35 | 1.161 | 0.685 |
| Sample 13 | 3.64 | 2.296 | 1.41 | 1.15 | 0.7 |
| Sample 14 | 6.694 | 2.497 | 1.36 | 1.955 | 0.667 |
| Average | 4.3624 | 2.418 | 1.35 | 1.467 | 0.776 |

Table C.5. Materials parameters (μ, k1, k2, φ, ρ, and R2) of 14 specimens Right Ventricle (RV) based on Holzapfel (2005) hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | μ | k1 | k2 | φ | ρ | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 0.413 | 1.75 | 1.21 | 1.571 | 0.748 | 0.70586 |
| Sample 2 | 0.64 | 1.333 | 1.06 | 1.6 | 0.69 | 0.74865 |
| Sample 3 | 5.129 | 1.663 | 1.04 | 1.847 | 0.459 | 0.8497 |
| Sample 4 | 1.141 | 2.145 | 1.06 | 1.665 | 0.641 | 0.88126 |
| Sample 5 | 5.537 | 2.395 | 1.07 | 1.571 | 0.923 | 0.55531 |
| Sample 6 | 4.557 | 2.293 | 1.15 | 1.571 | 0.886 | 0.73415 |
| Sample 7 | 3.033 | 2.222 | 1.03 | 1.57 | 0.768 | 0.78537 |
| Sample 8 | 5.538 | 0.961 | 0.86 | -1.051 | 0.521 | 0.91852 |
| Sample 9 | 1.784 | 2.123 | 1.02 | 1.317 | 0.473 | 0.89073 |
| Sample 10 | 5.088 | 2.019 | 1.1 | 1.571 | 0.528 | 0.83549 |
| Sample 11 | -0.005 | 1.75 | 1.05 | 1.672 | 0.576 | 0.85572 |
| Sample 12 | 1.8413 | 2.751 | 1.08 | 1.57 | 0.724 | 0.78555 |
| Sample 13 | 0.348 | 2.582 | 1.13 | 1.57 | 0.687 | 0.84281 |
| Sample 14 | 4.255 | 2.256 | 1.1 | 1.571 | 0.795 | 0.62985 |
| Average | 2.8071 | 2.017 | 1.07 | 1.401 | 0.673 | 0.78707 |

Table C.6. Materials parameters (c, c11, c21, , c21, c12, c22, c134, c234, φ0, and R2) of 14 specimens Right Ventricle (RV) fitting on Four-Fiber Family hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | c | c11 | c21 | c12 | c22 | c134 | c234 | φ0 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample 1 | 0.563 | 6.487 | 1.173 | 0.233 | 3.964 | 0.113 | 3.479 | 2.021 | 0.744 |
| Sample 2 | 1.114 | 4.062 | 1.308 | 0.214 | 3.256 | 0.386 | 2.111 | 0.882 | 0.752 |
| Sample 3 | 5.428 | 8.950 | 1.030 | 1.699 | 2.796 | 0.043 | 3.516 | -0.980 | 0.904 |
| Sample 4 | 1.565 | 7.708 | 1.211 | 1.142 | 2.482 | 0.200 | 2.785 | 0.865 | 0.893 |
| Sample 5 | 10.371 | 10.553 | 1.073 | 0.235 | 3.723 | -0.032 | 2.345 | 0.000 | 0.618 |
| Sample 6 | 5.966 | 11.851 | 1.038 | 0.183 | 4.894 | 0.000 | 21.195 | 0.851 | 0.890 |
| Sample 7 | 5.777 | 7.959 | 0.976 | 0.551 | 3.357 | 0.144 | 2.953 | 1.821 | 0.812 |
| Sample 8 | 11.450 | 2.075 | 0.780 | 1.067 | 1.616 | 0.882 | 1.119 | 0.988 | 0.923 |
| Sample 9 | 2.755 | 8.146 | 1.146 | 1.224 | 2.987 | 0.043 | 4.087 | 0.829 | 0.904 |
| Sample 10 | -0.003 | 5.710 | 1.237 | 0.000 | 21.484 | 0.700 | 2.610 | 0.571 | 0.862 |
| Sample 11 | -0.003 | 5.710 | 1.237 | 0.000 | 21.484 | 0.700 | 2.610 | 0.571 | 0.862 |
| Sample 12 | 5.333 | 10.189 | 1.125 | 0.749 | 2.771 | 0.000 | 21.491 | 0.000 | 0.757 |
| Sample 13 | 2.619 | 9.392 | 1.265 | 0.532 | 3.496 | 0.000 | 21.512 | -0.274 | 0.814 |
| Sample 14 | 5.730 | 11.230 | 1.098 | 0.341 | 3.760 | 0.000 | 21.536 | 0.000 | 0.784 |
| Average | 4.190 | 7.859 | 1.121 | 0.584 | 5.862 | 0.227 | 8.096 | 0.582 | 0.823 |