Supplementary material

| a) | b) |
| --- | --- |
| Fig. A. SEM/EDX spectra after chromium adsorption onto functionalized biochar: a) micrograph of functionalized biochar loaded with Cr, b) EDX spectrum of the yellow square inside a, indicating the presence of P and Cr. The image inside b represents Cr distribution on the biochar. |  |

| a) | b) |
| --- | --- |
| Fig. B. N2 adsorption isotherms at 77 K of adsorbents before and after Cr adsorption, a) functionalized biochar and b) non-functionalized biochar. |  |

Fig. C. Deconvolution of XPS C1s for Sewage Sludge and functionalized biochar (before and after adsorption)

Table A. Element composition of the materials determined by SEM/EDS

| Material | Si | Fe | Al | Ca | K | Mg | P | Cr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ----------------------------- % ----------------------------- |  |  |  |  |  |  |  |
| SS | 7.84 | 4.89 | 4.09 | 2.18 | 1.50 | 0.97 | *ND | ND |
| SSB | 8.20 | 7.62 | 5.62 | 3.73 | 1.54 | 0.98 | ND | ND |
| SSBCr | 9.40 | 6.69 | 6.02 | 2.99 | 0.99 | 0.88 | ND | 0.14 |
| ASSB | 10.62 | 2.93 | 1.92 | 0.69 | ND | ND | 7.03 | ND |
| ASSBCr | 11.72 | 2.23 | 2.03 | 0.63 | ND | ND | 7.05 | 0.57 |

*ND – not detected. (Limit detection = 0.1 %)

Fig. D. Deconvolution of XPS O1s for sewage sludge and functionalized biochar (before and after adsorption)