Supporting information

Dual-Ion Pre-intercalation in Intralayer and Interlayer Sites for Enhanced Ammonium-Ion Storage Performance of MnO2

Ting Xiao1,2,*,Yiwen Zhang1, Can Tang2, Yuting Mei1, Xiuru Li1, Yulong Qiao2, Lihua Jiang1, Shibing Ni1, Yequan Xiao1 and Xinyu Tan1, 3,*

1 Hubei Provincial Engineering Research Center for Solar Energy High-value Utilization and Green Conversion, Key Laboratory of Inorganic Nonmetallic Crystalline and Energy Conversion Materials, College of Materials and Chemical Engineering, China Three Gorges University, Yichang 443002, PR China.

2 Hubei Provincial Engineering Technology Research Center for Microgrid, College of Electrical Engineering & New Energy, China Three Gorges University, Yichang 443002, PR China

3 School of New Energy, Jingchu University of Technology, Jingmen 448000, PR China

*Corresponding Author Email: tingxiao@ctgu.edu.cn; tanxin@ctgu.edu.cn

1. Electrochemical performance calculation

Based on GCD curves, the areal specific capacitances of the as-synthesized electrodes were calculated according to the equation S1:

Cg=I×∆tΔV ×m                                  (S1)

where Cg (F g-1) is the specific capacitance of the working electrode, I (A) is the discharge current, Δt (s) is the total discharge time for one complete cycle, ΔV (V) is the voltage window during the reaction, and m (g) is the mass of the electrode material involved in the reaction.

For the fabrication of ASC device, areal capacitance (Ccell, F cm-2), energy density (E, mWh cm-2) and power density (P, mW cm-2) of device were calculated from current charging/discharging curves using the following equations, respectively.

Ccell=I×∆tS×∆V                               (S2)

E=Ccell×∆v27.2                               (S3)

P=3600×E∆t                                (S4)

where I, S, Δt, ΔV are the discharge current (A), area of the device (cm2), discharge time (s), and voltage window (V) of the discharge process, respectively.

- Characterization

Powder X-ray diffraction (XRD, Rigaku SmartLab Cu Kα radiation λ=1.5406 Å) was used to analyze composition of the electrodes. Field-emission scanning electron microscopy (FE-SEM, JSM 7500F) and transmission electron microscope (TEM, Tecnai, G220 UTWIN) were used to observe micromorphology of the electrodes. X-ray photoelectron spectroscopy (XPS) were performed on a PHI Quantera II spectrometer to characterize the chemical composition and valence state information.

- Electrochemical Measurements

The electrochemical performance was tested using Shanghai Chenhua's 760e instrument. The performance of a single electrode was measured using three electrodes, in which the prepared sample (MnO2, Mo-MnO2 or Mo-MnO2/AC) was the working electrode, the saturated calomel electrode (SCE) was the reference electrode, the platinum sheet electrode was the counter electrode, and 1 M CH3COONH4 solution was the electrolyte. The performance of the device was tested using a two-electrode system, with Mo-MnO2/AC (1.0 cm×1.0 cm) materials as the positive electrode and the ACC (1.0 cm×1.0 cm) as the negative electrode.

- Supplementary figures

Fig. S1. (a)CV curves of the MnO2 anode at 5−50 mV s−1. (b) GCD curves of MnO2 sample at 2−20 mA cm−2

Fig. S2. (a)CV curves of the Mo-MnO2 anode at 5−50 mV s−1. (b) GCD curves of Mo-MnO2 sample at 2−20 mA cm−2

Fig. S3. (a)CV curves of the Mo-MnO2/AC anode at 5−50 mV s−1.