Development of a novel immunoassay method for sensitive and fast detection of benzopyrene in foods based on a PDA@Mn-ZIF-8 nanozyme label and a molecularly imprinted biomimetic antibody

Kaiyue Su1, Xinli Peng1, Yuze Zheng1, Xuguang Qiao1, Geoffrey I.N. Waterhouse2, Zhixiang Xu1*

1College of Food Science and Engineering, Shandong Agricultural University, Tai’an 271018, People’s Republic of China

2School of Chemical Sciences, The University of Auckland, Auckland 1142, New Zealand

*Corresponding author:

E-mail: zhixiangxu@sina.com (Zhixiang Xu)

Tel: +86 538 8242263

Fax: +86 538 8242482

A

A

B

A

D

C

Figure S1. (A) XPS survey spectrum for PDA@Mn-ZIF-8 NPs; (B) O 1s XPS spectra for PDA@Mn-ZIF-8 NPs; (C) Mn 2p XPS spectrum for PDA@Mn-ZIF-8NPs; and (D) Mn 3s XPS spectrum of PDA@Mn-ZIF-8NPs.

B

A

D

C

Figure S2. EDS spectrum for multiple PDA@Mn-ZIF-8 nanozyme.

Figure S3. SEM image of PDA@Mn-ZIF-8 NPs.

B

A

Figure S4. (A) Effect of pH on the oxidation of TMB by PDA@Mn-ZIF-8 NPs, (B) The influence of temperature on the oxidation of TMB by PDA@Mn-ZIF-8 NPs.

A

B

C

Figure S5. Effect of substrate concentration and solvent on TMB oxidation by PDA@Mn-ZIF-8 NPs in the presence of H2O2. TMB oxidation gave rise to an absorbance maximum at 652 nm: (A) Effect of the TMB concentration, (B) Effect of H2O2 concentration, and (C) Effect of the standard solution solvent on the inhibition rate of benzopyrene.

| Table S1. Recoveries of Benzopyrene in liquor sample. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | Benzopyrene content in sample (μg L-1) | Spiked level (μg L-1) | Found level (μg L-1) | Recovery (± RSD, %) |
| Chicken | 0 | 1.00 | 0.95 | 94.94±2.52 |
|  |  | 50.00 | 44.56 | 89.12±4.58 |
|  |  | 100.00 | 105.54 | 105.26±1.05 |
| Pork | 0 | 1.00 | 0.93 | 93.16±2.83 |
|  |  | 50.00 | 53.11 | 112.31±5.58 |
|  |  | 100.00 | 92.83 | 92.83±3.19 |

| Table S2. Comparison of the BELISA method and HPLC method for the detection of benzopyrene in different foods. |  |  |  |
| --- | --- | --- | --- |
| Sample | Analyte | Found level by HPLC (µg kg-1, ± SD) | Found level by BELISA (µg kg-1, ± SD) |
| Sausages | Benzopyrene | 0.83±0.06a | 0.80±0.02a |
| Grilled lamb | Benzopyrene | 1.07±0.16a | 0.98±0.05a |

| Table S3. Comparison of the BELISA method with other methods for benzopyrene detection. detection. detection |  |  |  |
| --- | --- | --- | --- |
| Method | Analyte | LOD (µg L-1) | Reference |
| SERS | Benzopyrene | 20.00 | Fu et al. 2015 |
| Fluorescence | Benzopyrene | 0.36 | Nahornia et al. 2006 |
| Electrochemical | Benzopyrene | 2.80 | Ni et al. 2014 |
| HPLC | Benzopyrene | 0.005 | Kato et al. 2003 |
| BELISA | Benzopyrene | 0.52 | This work |