Supporting Information for
Pilot-Scale Green Hydrogen Production via Concentrated Natural Sunlight-Driven Photocatalytic Overall Water Splitting and Photothermal Synergy
Yang Wang*, Dongping Duan*, Xiaodong Zhang, Qibo Jia, Xi Chen, Li Zhong, Yan Li, Ke Gan, E Zhou, Yan Liu, Yuhan Liu, Renlong Song, Yizhao Yang, Xinyu Wu
Corresponding Author: Yang Wang, wangyang6270@ipe.ac.cn; Dongping Duan, douglass@ipe.ac.cn.  
[image: image1.png][
|

|8 | 10 | 12

18

'

Ba

Mirror bracket

and gaskets

|

1050
1100

242





Figure S1 The heliostat array arrangement in our platform (A), the structure of single heliostat (B, C), the back of the single heliostat (D), the 1/16 structure of the heliostat (E).
[image: image2.png]c?of front

T

A
temperature





Figure S2 The structure of the 1.3 m3 photoreactor. The reactor is sealed after orderly placing the catalyst foams. 
[image: image3.png]o | ENTRES R EARAT

Sheas 13543759111





Figure S3 Low temperature (A) and room temperature (B) water vapor cooling device. 
[image: image4.png]Gas storage tank

OO i i

Check valve

 — Y — Gas storage tank
H,, O,, H,0 Flow meter Condenser pressure
booster

—

Feed

Adsorption bed
I— — | H,
Chiller unit
H,

Adsorption bed

H:, 0:
Dehydrator

Gas storage tank

Electromagnetic
Valve

H, O,
H,0 vapor §

c
=

Compression Cylinder

A

z{ & Compressed
CIC | mo HDSI > Hz, 02, H,0

vapor
Chiller Unit

‘Water Flow Switch





Figure S4 The running principle and the photo of the gas separation device. The device consists by condenser, pre-adsorption gas storage tank, pressure booster, chiller unit, dehydrator, adsorption bed, post-adsorption gas storage tank, and hydrogen detector. In a typical separation process, the produced oxyhydrogen and water vapor pass through the condenser, then enter the gas storage tank. Once the mixed gases in the storage tank reach a certain pressure, the gas booster is activated to compress the gases. After that, the compressed gas enters the dehydrator to remove residual water vapor from the mixture, followed by pressure swing adsorption to eliminate oxygen from the mixture to get purified H2.

[image: image5.jpg]=\

NAOU STRONTIUM HYDROGEN

DATA SCREEN A

[MAINSCREEN| | FOURTHTEST | FIFTHTEST
WORKING WEATHER MIRROR FIELD DEIONIZED LIVE VIEW OF
STATUS STATUS STATUS STATISTICS WATER GENERATOR : THE PRIMARY MIRROR FIELD
— 2025-03-291505
v, o RADANGE
*,
a0 MARY r
s & = © colRire 2 e
H = :
“, ’,t 300 @ cBRBOGTY 5u5/cm

o

IRRADIANCE 345 Wi? ‘

@ T w0 o

2 INSTANTANEOUS |7
ZZmeaeous (T,

by /@‘ \)

HYDROGEN PURITY

HYDROGEN - OXYGEN SEPARATION

.
o
0 m¥h

et
B e |
sosgpemion

TIME ‘
0s

BOOSTER STATUS STATISTICS

0

~(
v!ur[umuz or  TeupERATUREOF
SECOND

INLET AIR PRESSURE.

EXHAUST AIR PRESSURE WATER PRESSURE ,_n T
TEMPERATURE  TEMPERATURE

DATE

2024.108

2024.109

2024.10.10

20241011

TIME

1002

1102

1300

HELIOSTAT
FAILURE

HELIOSTAT
FAILURE

HELIOSTAT
FAILURE

HELIOSTAT
FAILURE

ALARM INFORMATION

RTC

MU

AM

FFP

~ REACTOR1 ~

=

TEMPERATURE  PRESSURE

~ REACTORS -

=

TEMPERATURE  PRESSURE

PHOTO - REACTOR KETTLE STATUS STATISTICS

e T o
e Il Y Nl e
Al el | T
| [ e
e\ (| [l o e\ o
L | i (NSl

LIVE VIEW OF
THE REACTOR





Figure S5 In-time indoor monitor screen, which can give the status of weather, irradiance, deionized water, hydrogen purity, oxygen purity, water temperature, reactor temperature, reactor inside pressure, alarm information, and the live view of the whole system automatically. This screen is installed in another building and about 200 m away from the experimental field.
[image: image6.jpg]Lol





Figure S6 Photograph of sunlight concentrated onto the target by heliostats. The minimum sunlight concentration area is approximately 0.4 m2.
[image: image7.png]Light intensity

o N

o o

S o

© o
1 " 1

o
L

| © Concentrated sunlight intensity

O Natural sunlight intensity

y =647.7x-373
R? = 0.9854

O

o

8

1 2 3 4 5 6 7
Amount of the heliostat

9

1 O Natural UV light intensity
T O Concentrated UV light intensity

0

y = 9.06x+3.56
R? = 0.9729

O

O o o o o o o O

1 2 3 4 5 6 7 8 9
Amount of the heliostat




Figure S7 The relation between the number of the heliostat and the condensed natural sunlight energy (A), UV light energy (B).

[image: image8.png]



Figure S8 The building process of the world largest high-energy “sunlight condense” equipment. Sunlight-concentrating tower with 16 m height (A). Parabolic secondary reflector (B). Single-reflection concentrating system (C, D). 
[image: image9.png]WANDIB=iB’

s ——% S SRR ) —
2025-04-02 18:15:58
v o= = N 2 A —— -~
02 H2 50
206, VoL [0-0. 6VOL.
= 22
15
]
o
12:15 18:15
i 60
N - =

* .]"

B AN





Figure S9The on-line electronic gas flow meter. The device can record and exhibit the purity of the H2 and O2 during experiment.
[image: image10.png]0:23 nmCoOOH





Figure S10 Characterization of the modified HSTO:Al(RhCrCo) catalyst. The HSTO:Al exhibits anisotropic crystal habits with distinct exposed facets. Specifically, the Rh/Cr2O3 cocatalyst shows a preferential deposition on the {100} crystal facets, while the CoOOH cocatalyst is deposited on the curved crystal facets, which are a combination of {111}, {110}, {112} etc. facets. This unique deposition pattern allows photo-excited electrons and holes to migrate to different crystal facets realizing spatially separate. As a result, the hydrogen evolution reaction (HER) and the oxygen evolution reaction (OER) can occur separately on these distinct crystal facets, facilitating the overall water splitting process.
[image: image11.png]A ooore

00010,
00008,
00006,

5 00004
00002

00000,

00002

00004

0005
o004

0003

o001
0000

-0001

o006

0004

5 ooz

0000

0002

4 oo
000e-
0006-
0004
0002
0000.
-0002

0004

B € oo
yeoes oo yeraa, yeats,
\=oszsse w143 wes10ps
P oons ueses ooss e
oo Gesa et
ooz
° o000
3 s
00005 oot
o
o000 oo
° 0w 00005 20w o001 0w
T o0 200 300 40 5000 6000 oo 20 3000 4500 560 6000 T %0 20 3600 400 5000 6000
Tine 09 T 2) Tive 21
E oo F oxs
a0 000t
- oo
5 oo 3 o2
000
oo0n
oon] §
oo, S "
o] © o
o001
T o 200 300 4o 5000 600 T o0 200 3600 400 5000 6000
Time ) v o)
H o, ! oo
o0 oo
o004 000t
% o2 3
oonz
oo
oo
002 o
00w 2] & oouw
0008
T o 200 300 4o 5000 600 T o0 20 3000 400 5000 6000
Tine ) T o)
o010
K L oono
Letes
ooos o0 hiin
o006 o0 ettt
o008 o o
o002 oon2
. oom.
o 002
° o ° omouw
To0un e
0004
T iom 20 300 40 560 o0 T 000 2000 3600 4000 5000 6000

Time 5s)

Time ps)




Figure S11 Femtosecond TA kinetic traces and fitting results at ~530 nm of HSTO:Al(RhCrCo) under different pump fluences.
[image: image12.png]H, production rate (mL/h)

[
o

40 - %
30
O

20

10 4

o <
04 <
02 04 06 08 10 12 14 16

Xe lamp light intensity (W/cm?)




Figure S12 H2 production performance in full-spectrum intensity (tested using a Xe lamp).
[image: image13.png]1.0

' — STOA

0.8 —— STO:AI(RhCrCo)
3 0.6
C
[4M]
2
(@]
8041
<

0.2

0.0 . . : .

400 600 800 1000

Wavelength (nm)




Figure S13 UV-vis diffuse spectra of the STO:Al and STO:Al(RhCrCo) catalysts. 
[image: image14.png]H, evolution (mL)

N
o

(00]

(o))

N

{ O 6 °C with 1828.6 mW/cm? of 365 nm light

| © 60 °C in the dark &

O 6 °Cinthe dark

A 90 °C in the dark O

&

&
&

o
coo008BA8A88480

0 60 120 180 240 300 360
Time (min)




Figure S14 H2 production experiments of the Al-H2O reaction under different conditions. Irritating Al powder in H2O at the light intensity of 1826.6 mW/cm2 and 6 °C, nearly no H2 can be detected. Heating Al and H2O mixture at 60 or 90 °C in the dark, large amount of H2 is evolved. 
[image: image15.png]Normalized Intensity (a.u.)

HSTO:AI(RhCrCo)+Al (after reaction)
. Al(OH), phase
P 2 I M N S n
HSTO:AI(RhCrCo)+Al (before reaction)
A A h
HSTO:AI(RhCrCo)
l I} l A A
Al powder
| \ \

10 20 30 40 50 60 70 80 90
2Theta (degree)




Figure S15 PXRD patterns of the Al powder, HSTO:Al(RhCrCo), HSTO:Al(RhCrCo) + Al mixture before and after reaction. In the XRD pattern of HSTO:Al(RhCrCo) + Al mixture (after reaction), except for the peaks attributed to the unreacted Al and HSTO:Al(RhCrCo) photocatalyst, Al(OH)3 is the only main byproduct. 
[image: image16.png]7
N o MeOH
5 51
E ] o
c 4‘ Qg)
S |
5 31 9
S S ° Qo
© 24 o o
I 1 o) o
14 © o S o 4
1 & © o & @9
0 @ 00 o o
0 200 400 600 800 1000 1200
Time (min)
C
30
' TEA
25 @(bo
O
— 1 O
E 201 ¢ (f
< o
c ] ® (éo
S 15+ & © 3
> ]
o) o &
S 104
T 5_' o
| &0 Y
0d « © &

0 300 600 900 1200 1500
Time (min)

4.0

3.5-
3.04
€ 251

L)

151
IN 1.0-_
0.5-

0.0-

evolution (

600 900 1200

Time (min)

0 300

H, evolution (mL)

{1 Al powder

&
§ g o g
s & 2 &
o &
&
°© g

o o

iF, 58

0 500 1000 1500 2000 2500
Time (min)




Figure S16 Multiple addition of the sacrificial agents to the HSTO:Al(RhCrCo)-pure water system for H2 production experiments. Methanol (A), ascorbic acid (B), TEA (C) and 320 mesh Al powder (D).

As shown in Figure S16A, when use methanol (MeOH) as sacrificial agent, in the 1st round of test, pure H2 can be obtained and the evolution rate is about 2 times that of without MeOH, no oxygen is detected. However, after a certain time, H2 evolution rate dramatically decrease to zero. After adding new MeOH (2nd or more round of test), H2 evolves again, however, the production rate goes through a continuous decrease and even worse than without MeOH. Similar phenomenon also occurs on other common used sacrificial agents like ascorbic acid (AA) and TEA (Figure S16B, C). The reason can be attributed that (i) the decomposition of the sacrifice reagents in the 1st round addition generates much complex byproducts which are unable to be separated from the reaction solution, thus forming chemical balance to prevent them from continuous consuming photoholes, and (ii) the byproducts block the active sites of the catalyst. Obviously, adding sacrificial agent is not a good solution in the continuous industrial production, especially considering the potential harmful gas byproducts which might also greatly decrease the quality of green hydrogen and need extra complex separation procedures.

[image: image17.jpg]



Figure S17 The water purify system which provides purified water in the experiment. The original water source is supplied by Zhengzhou city.


