# Supporting Information

Electrochemical and failure of high-mass loading lithium cobalt oxide electrode via cold sintering process

Zhong Lin1, Kelin Zhu1,Guoan Cheng1, Ruiting Zheng1*, Hongtao Zhang2*

Figure S1. Particle size of milled LCO powder used for CSP.

Figure S2. (a) Optical photograph of the C-LCO electrode surface. (b) Optical photograph of the gold-sputtered reverse surface of the C-LCO electrode sheet.

Figure S3. Resistance values of C-LCO/Li cell extracted by EIS fitting data.

Table S1. Electrochemical performance comparison of this work with previously reported studies.

| Electrode material | technical route | Mass loading@ Thickness | Capacity | No. of cycles (Capacity retention)@C-rate | Ref. |
| --- | --- | --- | --- | --- | --- |
| NCM811 | tape casting | ~23 mg cm-² | 4.1 mAh cm–2 | 70 (94.8%) @ 0.2 C | [1] |
| NCM622 | tape casting | 20 mg cm-² @70μm | ~56 mAh g-1 @ (100th cycle) | 100 (36%) @1 C | [2] |
| LFP | Sintering at 650℃ | 2.3 g cm-³ @500 μm | ~13.7 mAh cm-2 | 20 @0.1 C | [3] |
| LFP | CSP LFP+CNF | 8.0 mg cm-2 @33um thick | ~ 127 mAh g-1@ 1 C@(100th cycle) | 100 (90%) @1 C | [4] |
| LFP | CSP | 2.70 g cm−3 | 155 mAh g−1 @ 0.1 C@(40th cycle) | 40 (87%) @0.2 C | [5] |
| Li4Ti5O12@MOF | 3D-Printed hierarchical porous structure | 11 mg cm-² @316 μm | 5.37 mAh cm-2 | 150 (78.9 %) @5 C | [6] |
| LTO | CSP of tape casting LTO | ~9 mg cm-2 @35μm | 225 mAh cm-3 @ (150th cycle) | 150 (69%) @0.2 C | [7] |
| LCO | ice-templating method | 25 mg cm-² | 139 mAh g−1 @(100th cycle) | 200 (94.4%) @0.5 C cutoff voltages of 4.3 V | [8] |
| LCO | CSP LCO/LLZTO/PEO/C | 110 mg cm-2 @400 μm | ~15 mAh cm-2 | 150 (96%) @0.1 C | [9] |
| This study | CSP LCO/CNTs | 48mg cm-2 @200 μm | 5.6 mAh cm-2 | 100 (86.8%) @ 0.1 C |  |

References

1. 	Saqib, K.S.; Choi, J.H.; Park, S.; Lim, H.; Ali, J.; Hwang, M.; Kim, M.; Lim, H.; Oh, M.; Kaveevivitchai, W.; et al. High-Mass Loading Nickel-Rich Cathode Electrode Design Incorporating Multidimensional Carbon Conductive Additives to Minimize Ohmic Contact Resistance for High-Performance Lithium-Ion Batteries. ACS Appl. Mater. Interfaces 2025, 17, 48429–48439, doi:10.1021/acsami.5c12663.

2. 	Park, K.-Y.; Park, J.-W.; Seong, W.M.; Yoon, K.; Hwang, T.-H.; Ko, K.-H.; Han, J.-H.; Jaedong, Y.; Kang, K. Understanding Capacity Fading Mechanism of Thick Electrodes for Lithium-Ion Rechargeable Batteries. J. Power Sources 2020, 468, 228369, doi:10.1016/j.jpowsour.2020.228369.

3. 	de la Torre-Gamarra, C.; Sotomayor, M.E.; Sanchez, J.-Y.; Levenfeld, B.; Várez, A.; Laïk, B.; Pereira-Ramos, J.-P. High Mass Loading Additive-Free LiFePO4 Cathodes with 500 μm Thickness for High Areal Capacity Li-Ion Batteries. J. Power Sources 2020, 458, 228033, doi:10.1016/j.jpowsour.2020.228033.

4. 	Seo, J.-H.; Verlinde, K.; Guo, J.; Heidary, D.S.B.; Rajagopalan, R.; Mallouk, T.E.; Randall, C.A. Cold Sintering Approach to Fabrication of High Rate Performance Binderless LiFePO4 Cathode with High Volumetric Capacity. Scr. Mater. 2018, 146, 267–271, doi:10.1016/j.scriptamat.2017.12.005.

5. 	Seo, J.-H.; Guo, J.; Guo, H.; Verlinde, K.; Heidary, D.S.B.; Rajagopalan, R.; Randall, C.A. Cold Sintering of a Li-Ion Cathode: LiFePO4-Composite with High Volumetric Capacity. Ceram. Int. 2017, 43, 15370–15374, doi:10.1016/j.ceramint.2017.08.077.

6. 	Mwizerwa, J.P.; Li, J.; Nsengiyumva, W.; Li, C.; Xu, K.; Rasaki, S.A.; Liu, C. Thick 3D-Printed Hierarchical Li4Ti5O12@MOF Anode and Grid-Lined Micropores for High-Performance Lithium-Ion Batteries. J. Colloid Interface Sci. 2025, 696, 137883, doi:10.1016/j.jcis.2025.137883.

7. 	Seo, J.-H.; Verlinde, K.; Rajagopalan, R.; Gomez, E.D.; Mallouk, T.E.; Randall, C.A. Cold Sintering Process for Fabrication of a High Volumetric Capacity Li4Ti5O12 Anode. Mater. Sci. Eng. B 2019, 250, 114435, doi:10.1016/j.mseb.2019.114435.

8. 	He, R.; Tian, G.; Li, S.; Han, Z.; Zhong, W.; Cheng, S.; Xie, J. Enhancing the Reversibility of Lithium Cobalt Oxide Phase Transition in Thick Electrode via Low Tortuosity Design. Nano Lett. 2022, 22, 2429–2436, doi:10.1021/acs.nanolett.2c00123.

9. 	Wu, X.; Xia, S.; Huang, Y.; Hu, X.; Yuan, B.; Chen, S.; Yu, Y.; Liu, W. High-Performance, Low-Cost, and Dense-Structure Electrodes with High Mass Loading for Lithium-Ion Batteries. Adv. Funct. Mater. 2019, 29, 1903961, doi:10.1002/adfm.201903961.