Technoeconomic assessment of bacterial nanocellulose production from second generation sugars derived via the OxiOrganosolv pretreatment process

Konstantinos G Kalogiannis1,2*, Anthi Karnaouri3, Koar Chorozian3, Stylianos S. Stefanidis2

1Department of Chemical Engineering – University of Western Macedonia, 50100, Kozani, Greece

2Chemical Process and Energy Resources Institute (CPERI), Centre for Research and Technology Hellas (CERTH), 6th km Harilaou-Thermis, 57001 Thessaloniki, Greece

3Laboratory of General and Agricultural Microbiology, Department of Crop Science, Agricultural University of Athens, Athens 11855, Greece

* Corresponding author

Address: University of Western Macedonia, 50100, Kozani, Greece

E-mail address: kkalogiannis@uowm.gr

SUPPLEMENTARY INFORMATION

- Material balances

Preparation of the culture medium

For the preparation stage of the culture medium, the quantities required for one batch that produces 50 kg of dry BNC are presented in Table S1.

Table S1. Quantities of HS medium components per batch for 50 kg of dry BNC.

| Component | kg/batch |
| --- | --- |
| Glucose | 200 |
| Peptone | 50 |
| Yeast extract | 50 |
| Na2HPO4 | 27 |
| Citric acid | 11,5 |
| Water | 9.661,5 |
| Total | 10,000 |

Aeration requirements

Moving on to the fermentation stage, the aeration requirements of the static bioreactor were initially calculated. According to the literature, a typical aeration rate during fermentation for the production of bacterial nanocellulose is around 0.5 VVM (Vessel Volumes per Minute) (Babaeipour, 2021). Thus, the volumetric airflow rate during one batch with a medium volume of 10 m³ will be:

0,5*10m3min=300m3h

For 168 h (7 days) of fermentation, the amount of air required is equal to 50,400 m³ per batch, and for 2,000 batches per year, with an air density of 1.164 kg/m³, the annual quantity of air required is 117,331.2 t/y.

### Washing stage with NaOH and Deionised Water

After the completion of the cultivation, the produced BNC exits in the form of a hydrogel (stream S-9) from the TB-01/48 units, consisting of 99 % water (wet BNC) along with a fraction of liquid waste, and is prepared to be directed to the bleaching stage with sodium hydroxide. It should be noted that the waste stream is considered non-hazardous and is directed to treatment. Table S2 presents the outputs from the fermentation stage in kg/batch. The density of the culture medium is assumed equal to that of water, i.e., 1,000 kg/m³.

Table S2. Outputs in kg/batch from the fermentation stage.

| Output Stream |  | Description | Mass (kg/batch) |
| --- | --- | --- | --- |
| Wet BNC | Stream with 1 % w/w BNC |  | 5,000 |
| ▸ Dry BNC | Dry BNC |  | 50 |
| ▸ Water | Remaining water |  | 4,950 |
| Liquid waste | Cellular residues |  | 5,000 |
| Total outputs | Total |  | 10,000 |

Drying stage

Drying takes place at 50 °C with a continuous supply of hot dry air. The outlet stream of the product is approximately 14.8 kg/h, consisting of 85 % dry BNC and 15 % water, corresponding to ~12.5 kg/h of dry BNC, which equals 102 t/year. For the estimation of the required air quantity as well as the air properties at 50 °C, data from the literature were used (Dute et al., 2025). Dry air at 50 °C can absorb 0.0845 kg H₂O/kg of air. Given the requirement to evaporate 1,235.29 kg/h of water, the corresponding mass flow of air is 14,618.8 kg/h. With a density of 1.087 kg/m³, the volumetric airflow is calculated as 13,448.76 m³/h.

- Energy balances

### Medium Preparation

The calculation begins with the energy required during the sterilization stage of the culture medium. With the requirement for 6 batches per day, and assuming that the time needed to feed the reactors is 10 hours, a culture medium flow rate of 6,000 kg/h is used (60 m³ required for 6 batches). Furthermore, for the calculations, the specific heat capacity (Cp) of the culture medium is considered equal to that of liquid water at 25 °C, i.e., 4.18 kJ/kgK.

Thus, for heat exchanger E-101, knowing that the medium is heated from ambient temperature (20 °C) up to 128 °C the required energy is :

QE-01=m*Cp*ΔΤ=6000kgh*4,18kJkgK*128°C-20°C=2.583.240kJh=752,4kW Assuming an overall heat exchanger efficiency of 0.9, the actual heating needs will be  836kW.

Next, stream S-5 enters E-102 and is further heated up to the sterilization temperature (140 °C) using low-pressure steam. Similarly to E-101, for ΔT = (140 – 128) = 12 °C, the energy required for E-102 is:

QE-02=83.6 kW.

Once again an overall heat exchanger efficiency of 0.9 results in a heating demand of 92.9 kW.

### Fermentation – Static Bioreactors

Regarding the energy balances for the fermentation stage, the calculation here focuses on the energy required to heat the air from ambient temperature (20 °C) to the culture temperature (30 °C). With an air flow per reactor equal to 300 m³/h, as calculated in the mass balances, and density 1.164 kg/m³, the heat required for preheating the air is:

Qair=Vair*ρair*Cp,air*ΔΤ=300m3h*1,164kgm3*1,005kJkg K*10 Κ=3,509.5kJh=0.975 kW

With one batch lasting 168 h (7 days) and the annual requirement of 2,000 batches, the annual energy consumption for air heating amounts to 327,600 kWh/year.

### Washing with NaOH

Proceeding to the washing stage, the NaOH solution (stream S-10), is first preheated in heat exchanger E-103 to reach the required temperature of 60 °C. The specific heat capacity of the solution is assumed equal to that of water, i.e., 4.18 kJ/(kg K). The flow rate of the solution was calculated at 706.25 kg/h and thus; Q=706,25*4,18*60-20=118.085kJh=32.8 kW, resulting in a heating demand of 36.5 kW, assuming an overall heat exchanger efficiency of 0.9.

### Drying

Finally, the drying stage represents the most energy-intensive part of the plant, as it involves the removal of water from the wet BNC until the desired final moisture content of 15 % w/w is achieved. The energy balance for the drying stage is presented below. Drying is carried out at a temperature of 50 °C. The heat required for drying is calculated using the latent heat of water evaporation, the heat required to raise the material to the drying temperature, and the heat to raise the air from 20 °C to 50 °C.

From the mass balances, the amount of water to be evaporated is 1,235.29 kg/h. Using the latent heat of water evaporation at 50 °C, equal to 2,257 kJ/kg, the required heat is:

Qevaporation=mw*λ=1.235,29kgh*2.257kJkg=2.788.049kJh=774.76 kW

To calculate the heat required to raise the wet BNC (1,250 kg/h) from 25 °C (after the washing stage) to 50 °C, it was assumed that, since it consists of 99 % water, its specific heat capacity would be approximately equal to that of water, i.e., Cp= 4,18 kJ/kgΚ. Thus, the required heat is:

Qheating=mwet BNC*Cp*ΔΤ=1.250kgh*4,18kJkg K*25 K=130.625kJh=36.3 kW

The air enters at 20 °C from the environment with a flow of 14,618.8 kg/h and exits the dryer at approximately 50 °C. The specific heat capacity of air was taken as 1.007 kJ/kg K. Therefore, the total heat transfer required to heat the air is:

Qair=mair*Cp,air*ΔΤ=14.618,8kgh*1,007kJkg K*30°C=441.634kJh=122.68 kW

Consequently, the total heat consumption required for the drying process will be the sum of the three components above. However, since the drying efficiency is 85 % (Sturgeon, 1995), the overall heat requirement is the sum divided by the efficiency:

Qtotal=(Qevaporation+Qheating+Qair)0,85 =1,098.5 kW

- Equipment sizing

Conveyor Belt filters

For the alkaline washing of bacterial conveyor belts are used, on which the BNC is carried and sprayed with the solution through nozzles. Technical specifications for sizing the equipment were taken by examining various belt conveyors available on Alibaba.com. Since this unit processes 6 batches per day, corresponding to 30,000 kg of wet BNC, the collection was distributed into six 4-hour periods to reduce equipment load. The calculated flow rate is 1,250 kg/h. Based on this data, the conveyor belts were dimensioned. Table S3 below presents the technical characteristics of the equipment that will be used for the final design.

Table S3. Equipment characteristics according to market data.

| Belt conveyor |  |
| --- | --- |
| Active filter width | 1.0 m |
| Active filter length | 10-30 m |
| Active filter surface area | 18-33 m2 |
| Motor power | ~5.25 kW |
| Dimensions |  |
| Length | 25 m |
| Width | 3 m |

Additionally, table S4 presents the data used for equipment design based on the mass balances.

Table S4. Data for equipment sizing based on balances.

| Parameter | Value |
| --- | --- |
| Quantity of wet BNC per batch | 5,000 kg (≈ 5.0 m³) |
| Density of wet BNC. | 1.0 kg/L |
| Layer thickness on belt (assumption) | 2.5 cm |
| Residence time | 2 h |
| Quantity per filter per batch | 2,500 kg (≈2,5 m³) |
| Operating duration per cycle | 2 h/filter |
| NaOH concentration | 0.5 M |
| Washing temperature | 60 °C |

Based on these data, the required filter area is calculated as:

Α=VolumeLayer thickness=2,50,025=100 m2

With a filter width of 1.0 m, the filter length is calculated as: L=AD=100 m. Since this length exceeds the available equipment specifications, five conveyor belts of 20 m length each will be used, and the required filter area will be 100/5 = 20 m2. In addition, the required belt speed during washing is calculated, so that the BNC remains on the belt and is washed for two hours: v=Lt=20m2h*3600s=0.278 cm/s

Finally, the required amount of 0.5 M NaOH solution for washing the wet BNC is calculated. Based on a wet BNC flow of 1,250 kg/h, the required solution volume from the mass balances is 706.25 L/h. Since the flow is distributed across five conveyor belts operating in parallel, the required solution volume is approximately 141.25 L/h per belt. Thus, based on the calculated parameters for this unit and the technical specifications of the selected belt conveyor, the final equipment data are presented in Table S5.

Table S5. Characteristics of each belt conveyor in the unit.

| Parameter | Value |
| --- | --- |
| Filtration area | 20 m² |
| Belt width | 1.0 m |
| Belt length | 20 m |
| BNC layer thickness | 0.025 m |
| Inlet flow | 2.5 m³ per 2 h |
| Belt speed | 0.365 cm/s |
| Motor power | 5.25 kW |
| Solution temperature | 60 °C |
| NaOH solution | 141.25 L/h |

In summary, the total power consumption for operating the five conveyor belts is: 5*5.25kW*24h/d*340d/y = 214,200 kWh/y.

The conveyor belts used for washing with deionized water are sized in the same way and their main characteristics are presented in table S6.

Table S6. Characteristics of WSH-102.

| Parameter | Value |
| --- | --- |
| Filtration area | 20.2 m² |
| Belt width | 1.0 m |
| Belt length | 20.2 m |
| BNC layer thickness | 0.025 m |
| Inlet flow | 2,525 m³ per 2 h |
| Belt speed | ~0.368 cm/s |
| Motor power | 5.25 kW |
| Deionized water | 1,262.7 kg/h |

In summary, the total power consumption for operating the five filters is again:

5*5.25kW*24h/d*340d/y = 214,200 kWh/y

### Deionized-water production system

Deionized water is produced on site using a reverse-osmosis deionized water production system (DIS). The selected unit has a capacity of 8,000 L/h (~65,280 t/y), which is sufficient to cover the plant’s demand for deionized water, approximately ~56,000 t/y. Table S7 presents the characteristics of the system.

Table S7. Characteristics of the deionized-water system.

| Production capacity | 8,000 L/h |
| --- | --- |
| Salt rejection | ≥ 99.5 % |
| Frames | SUS304 |
| Recovery rate | ≥ 70 % |
| Membrane elements | Vontron |
| Operating pressure | 0.5-1.0 MPa |
| Power consumption | 10 kW |
| Filter accuracy | 0.0001 microns |
| Membrane size – Number of membranes | 8,040-8 membranes |

The unit’s demand for deionized water is 7,005.3 kg/h, required for NaOH solution preparation and BNC neutralization. With a recovery rate of 70 %, the water feed to the system must be 7.005,33kgh0,7≈10,008kgh.

The corresponding annual water volume is 10,008 kg/h * 24h * 340d = 81,665.3 t/y. Finally, the annual electricity consumption is 10kW*24h/d*340d/y = 81,600 kWh/y.

### Conveyor Dryer

The key assumptions focus on the evaporation rate and the residence time of the BNC sheets in the dryer; they are presented in Table S8 along with the conveyor dryer’s characteristics.

Table S8. Sizing data for CD-01.

| Parameter | Value |
| --- | --- |
| Wet BNC flow | 1,250 kg/h |
| BNC moisture | 99 % → 1,237.5 kg/h water |
| Final moisture | 15 % |
| Water to be evaporated | 1,235.29 kg/h |
| BNC layer thickness | 2.5 cm |
| Evaporation rate | 9.91 kg/m²/h (Perry’s Chemical Engineers’ Handbook, Eighth Edition, 2008) |
| Residence time | 240 min |
| BNC density | ≈ 1,000 kg/m³ (like water) |
| Belt width | 3 m (Perry’s Chemical Engineers’ Handbook, Eighth Edition, 2008) |

According to Perry’s Chemical Engineers’ Handbook typical evaporation rates for sheet like wet materials are around 10 kg/m²/h. However, the water is strongly bound within the BNC. In addition, it is typically much easier to dry sheets of small thickness, 5 to 10 mm; increasing the sheet thickness introduces additional resistance to water removal. Therefore, given that the BNC in this study will have a thickness of 25 mm, we assumed that the average evaporation rate was reduced by 4 times to a value of 2.5 kg/m²/h. Based on the required quantity of water to be evaporated (1,235.3 kg/h), the residence time of 4 hours and the evaporation rate (2.5 kg/m²/h), the required drying surface area is

Ad=1.235,294*2.5=123.5 m2.

Furthermore, with a belt width of 3 m, the required belt length is

L=123,53=41.17 m.

Since this length is considered relatively large, multiple levels are used to reduce the dryer footprint and improve unit efficiency. In this case two levels are used. Thus, the required surface area per level is 123.5/2 = 61.7 m2 and the required length per level is approximately 20.6 m. Finally, the required belt speed for a residence time of 4 h (240 min), assuming the material stays for two hours on each level, is calculated as:

u=Lt=20,6120=0.172mmin≈0.29cms.

Regarding the fans used, it is assumed that they operate with a pressure increase of 1,000 Pa, and for a volumetric flow rate of 13,448.8 m³/h the power consumption is approximately 4 kW, according to the power-consumption vs. volumetric-airflow diagram taken from the literature*. According to the energy balances, the total thermal load required during drying is 1,098.5 kW. Therefore, including the fan consumption, the annual operating energy requirement is:

1,098.5 kW+4kW*24hd*340dy=8,996,400kWhy

Finally, the size of the glucose storage tank vessel was calculated. V-101 is the glucose storage tank, capable of storing glucose needed for 5 days of production and was designed to have a volume of 182.4 m3.

* https://www.engineeringtoolbox.com/fans-efficiency-power-consumption-d_197.html

- Equipment cost estimation

### Conveyor belts

Regarding the costs of belt conveyors, market data were used (e.g., Alibaba.com) along with diagrams from Peters et al. (2004). Typically, the purchase cost for a washing system with conveyor belts is approximately 1,200 $/m, for belts with a width of 1 m. For the conveyor belts used in washing with caustic WSH-101, the length is 20 m with a width of 1 m. Therefore, the purchase cost of the belt conveyors for the NaOH washing system was calculated to be 120,000$ @2024. For the WSH-102 conveyors used in the deionized-water washing stage, the length of each is 20.2 m with the same width. Therefore, the purchase cost of this equipment was 121,219 $ @2024.

Table S9. Summary of purchase costs for conveyor belts.

| Item | Characteristic size | Purchase cost $@2024 | Purchase cost (M €@2024) |
| --- | --- | --- | --- |
| WSH-101 | L = 20 m | 120,000 | 0.105 |
| WSH-102 | L= 20.2 m | 121,219 | 0.106 |
| Total |  |  | 0.211 |

### Conveyor dryer

Regarding the purchase cost of this type of conveyor dryer the purchase cost per square meter for dryers of a specific belt length and width was taken from the reference (Perry’s Chemical Engineers’ Handbook, Eighth Edition, 2008). The conveyor dryer used in the bacterial nanocellulose production plant consists of two belts with a surface area of 61.7 m², with each belt having a length of 20.6 m. The final cost for two such dryers was calculated to be 1,343,000 $ @2024.

Heat exchangers

The cost of heat exchangers and relevant details is provided in the following tables.

Table S10. Summary of heat-exchanger purchase costs.

| Item | Characteristic size | Material | Purchase cost $ | CEPCI | Purchase cost (M €@2024) |  |
| --- | --- | --- | --- | --- | --- | --- |
| E-101 | 69.67 m2 | SS304 | 24,888.41 | 240 | 0.072 |  |
| E-102 | 2.2m2 | SS304 | 5,093.83 | 240 | 0.015 |  |
| Holding tube | Lht = 60 m, dht 0.065 m | SS316 | 72,000 | 390.4 | 0.129 |  |
| E-103 | 0.12m2 | CS,SS | 1,800 | 395.6 | 0.003 |  |
| Total |  |  |  |  |  | 0.219 |

### Mixing tanks

The cost of the mixing tanks and relevant details are given in the table below.

Table S11. Summary of stirred tank purchase costs.

| Item | Characteristic size | Material | Purchase cost $ | CEPCI | Purchase cost (M €@2024) |  |
| --- | --- | --- | --- | --- | --- | --- |
| Μ-101 | 21.2 m3 | SS304 | 164,746.5 | 550 | 0.209 |  |
| Μ-102 | 1.25 m3 | SS304 | 34,735.4 | 550 | 0.044 |  |
| Total |  |  |  |  |  | 0.253 |

### The water deionization system cost was taken from various industrial-equipment supplier websites; it was between 20,000-25,000€, an average value of 22,500€ was used. The storage tank cost was also calculated via relevant equations and found to be only a fragment of the total equipment costs. Specifically, it was calculated at 68,000€.

- Utilities cost

Table 8 summarizes the utility consumption data for the production plant of 100 t/y dry BNC. Regarding water usage, the total amount required is the sum of the water fed directly into the culture-medium vessel plus the water used for preparing the 15 % glucose solution. The water requirement for the 15 % glucose solution is 1,333.3 kg/batch (quantity for the 15 % solution fed to M-01) – 2,857 kg/batch (70 % glucose solution purchased from the market) = 1,047.6 kg/batch. Thus, together with 8,528.2 kg/batch, the total amount required will be 19,152 t/y.

Table S12. Summary of utility consumption data for the plant.

| Item | Electricity kWh/y | Lower pressure steam t/y | Water t/y |
| --- | --- | --- | --- |
| DIS | 81,600 |  | 81,662 |
| M-101 | 24,480 | - | 19,152 |
| M-102 | 1,175 | - | - |
| TR-101/148 | 382,990 | - | - |
| WSH-201/205 | 214,200 | - | - |
| WSH-206/210 | 214,200 | - | - |
| CDR-201 | 8,993,490 | - | - |
| E-102 | - | 520 | - |
| E-103 | - | 457 | - |
| P-01 | 12,240 |  | - |
| Total | 9,924,375 | 977 | 100,814 |
| Unit cost | 0.053 €/kWh | 26.2 €/t | 0.59 €/t |
| Utility Costs | € 525,991 | € 25,597 | € 59,480 |
| TOTAL UTILITY COSTS CUT = 0.611 M € |  |  |  |  |

- Waste treatment cost

Table S13. Summary of waste treatment cost data.

| Item | kg/batch | t/y |
| --- | --- | --- |
| TR-101/148 | 5,000 | 10,000 |
| WSH-201/205 | 2,775 | 5,550 |
| WSH-206/210 | 25,300 | 50,600 |
| Total |  | 66,150 |
| Unit cost |  | 31.5 €/t (Peters et al., 2004) |
| TOTAL WASTE TREATMENT COST CWT = 2.08 M € |  |  |

- Labor cost

Table S14. Summary of waste treatment cost data.

| Equipment Items | Workers / Shift | Number |
| --- | --- | --- |
| Mixing tanks | 0.2 | 2 |
| Batch reactors | 1 | 6 |
| Belt filters | 0.1 | 10 |
| Conveyor dryer | 0.6 | 1 |
| Pumps | 0 | 1 |
| Storage tanks | 0 | 1 |
| Heat exchangers | 0.05 | 4 |
| Total workers / shift = 8.2 |  |  |

For full operation in three shifts (3·8 hours/day), 8 workers per shift are required to cover all critical process stages (reactors, washing, drying, etc.). Considering days off, holidays, and potential sick leaves, the total workforce is estimated at 8*4.5 = 36 workers. The need for significant manual operation increases the labor cost. Introducing more automated processes for high-capacity production will also bring this cost down in the future.

- Sensitivity analysis

Tables S15 and S16 present the results of this analysis. In the first column, the percentage variation of each parameter is shown, and in the subsequent columns, the value of the NPV calculated for the change of the respective parameter.

Table S15. Sensitivity analysis results for ±20 % range, showing the NPV value (in M €) for scenario A (15 wt. % moisture content).

| Deviation | Peptone price | FCI | CWT | Glucose price | Electricity cost |
| --- | --- | --- | --- | --- | --- |
|  | NPV (M €) |  |  |  |  |
| -20 % | 22.39 | 38.002 | 24.614 | 21.86 | 22.243 |
| -15 % | 22.159 | 33.9 | 23.827 | 21.762 | 22.049 |
| -10 % | 21.928 | 29.779 | 23.04 | 21.66 | 21.855 |
| -5 % | 21.697 | 25.638 | 22.253 | 21.565 | 21.661 |
| 0 % | 21.466 |  |  |  |  |
| 5 % | 21.236 | 17.244 | 20.676 | 21.368 | 21.272 |
| 10 % | 21.005 | 12.962 | 19.881 | 21.27 | 21.078 |
| 15 % | 20.771 | 8.495 | 19.086 | 21.171 | 20.882 |
| 20 % | 20.538 | 3.916 | 18.29 | 21.073 | 20.686 |

Table S16. Sensitivity analysis results for ±20 % range, showing the NPV value (in M €) for scenario B (no drying).

| Deviation | Peptone price | FCI | CWT | Glucose price | Electricity cost |
| --- | --- | --- | --- | --- | --- |
|  | NPV |  |  |  |  |
| -20 % | 19.366 | 36.62 | 21.6 | 18.837 | 18.499 |
| -15 % | 19.136 | 29.103 | 20.8 | 18.738 | 18.485 |
| -10 % | 18.905 | 25.507 | 20 | 18.64 | 18.471 |
| -5 % | 18.674 | 22.02 | 19.2 | 18.542 | 18.457 |
| 0 % | 18.443 |  |  |  |  |
| 5 % | 18.213 | 14.824 | 17.7 | 18.345 | 18.429 |
| 10 % | 17.981 | 11.154 | 16.9 | 18.247 | 18.416 |
| 15 % | 17.748 | 7.325 | 16.1 | 18.148 | 18.4 |
| 20 % | 17.515 | 3.4 | 15.3 | 18.05 | 18.388 |

# Literature

Air Density, Specific Weight, and Thermal Expansion Coefficients at Varying Temperatures and Pressures [WWW Document], n.d. URL https://www.engineeringtoolbox.com/air-density-specific-weight-d_600.html (accessed 6.11.25).

Babaeipour, V., 2021. Optimization of Bacterial Nano-Cellulose Production in Bench-Scale Rotating Biological Contact Bioreactor by Response Surface Methodology. Iran. J. Chem. and Chem. Eng.; Chemical Engineering-international English Edition. https://doi.org/10.30492/IJCCE.2020.38040

Dute, S., Bijwe, M., Pawar, D., 2025. Design Modification of Tray Dryer to Increase Efficiency. Int. J. Advanced Res. Sci., Com. Technol., 267–277. https://doi.org/10.48175/IJARSCT-23239

Perry's Chemical Engineers' Handbook, 8th ed., 2008. McGraw-Hill, New York, NY, USA.

Peters, M.S., Timmerhaus, K.D., West, R.E., West, R.E., 2004. Plant design and economics for chemical engineers, 5th ed, McGraw-Hill chemical engineering series. McGraw-Hill, New York, NY, USA.

Sturgeon, L.F., 1995. Conveyor Dryers, in: Handbook of Industrial Drying. CRC Press, Boca Raton, Florida, USA.