Supporting Information

Enhancement in the yield and properties of cellulose nanocrystals by two-batch addition of ammonium persulfate

Zhangyun Chen, Zhongyuan Xie, Hua Jiang*

College of Chemical Engineering, Nanjing Forestry University, Nanjing 210037, China

M1 The procedures for conductometric titrations

CNCs (50 mg) were suspended in 10 ml of 0.01 mol.l-1 HCl solution and ultrasonicated for 5 min to disperse them. The suspension was then titrated against 0.01 mol.l-1 NaOH. The carboxyl content (mmol/g) is given by the following equation:

CC (mmol/g)=c×(V2-V1)m                        (1)

where c is the NaOH concentration (mol.l-1), V1 and V2  are the amount of NaOH (ml), corresponding to the first and the second inflection points in the titration curve, respectively; m is the weight of the dried sample (g).

M2 The calculation for the crystallite parameters

The average size of crystallite and the d-spacing were calculated from the Scherrer’s and Bragg’s equations, respectively.

L(hkl)=kλB(hkl)cosθ       （2）

d(hkl)=λ2sinθ          （3）

where (hkl) is the lattice plane, L(hkl) is the size of crystallite, k isthe Scherrer’s constant (0.94), λ is the X-ray wavelength (0.154 nm), B 3. is the FWHM (full width half maximum) of the measured hkl reflection and 2θ is the corresponding Bragg’s angle. d(hkl)is the d-spacing of the lattice plane (hkl).

Fig. S2 The procedures for the separation of CNCs from the reaction suspension

Fig. S3. TEM images of the CNCs.

Fig. S4 The XRD patterns of the CNCs

* Correspondence: E-mail: jianghua@njfu.edu.cn