Supplementary Information (SI)

Enhanced Removal of Cesium Ions by Prussian Blue/Calcium Alginate Composite Membranes: Mechanism of Atomic-Level Trapping Elucidated by Combined Experimental and DFT Studies

Supplementary tables

# Table 1 Parameters derived from the pseudo-first-order and pseudo-second-order kinetic models for Cs(I) adsorption on the PB/CA membrane

| Quasi-first-order kinetic model |  | Quasi-second-order kinetic model |  |
| --- | --- | --- | --- |
| Qe (mg/g) | 4.63 | Qe (mg/g) | 5.06 |
| K1(min-1) | 2.15×10-2 | K2(g/mg·min-1) | 0.58×10-2 |
| R2 | 0.97 | R2 | 0.99 |

# Table 2 Parameters derived from the intraparticle diffusion and Boyd liquid membrane diffusion models for Cs(I) adsorption on the PB/CA membrane

| Intragranular diffusion model |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| KI(mg/g∙min1/2) | 0.18 | KII(mg/g∙min1/2) | 5.35×10-2 | KIII(mg/g∙min1/2) | 0.27×10-2 |
| C | -0.36 | C | 2.06 | C | 4.78 |
| R2 | 0.99 | R2 | 0.98 | R2 | 0.85 |

Table 3 Langmuir isotherm model parameters for the adsorption of Cs(I) onto the PB/CA membrane at different temperatures

| T(K) | Q e (mg/g) | Q m(mg/g) | KL(L/mg) | R2 |
| --- | --- | --- | --- | --- |
| 298.15 | 24.61 | 29.59 | 4.48×10-2 | 0.99 |
| 308.15 | 25.74 | 31.01 | 4.13×10-2 | 0.97 |
| 318.15 | 26.56 | 32.88 | 3.78×10-2 | 0.98 |

Table 4 Freundlich isotherm model fitting parameters for the adsorption of Cs(I) onto the PB/CA membrane

| T(K) | Q e(mg/g) | n | KF(L/mg) | R2 |
| --- | --- | --- | --- | --- |
| 298.15 | 24.61 | 0.45 | 3.23 | 0.96 |
| 308.15 | 25.74 | 0.47 | 3.12 | 0.961 |
| 318.15 | 26.56 | 0.48 | 3.06 | 0.97 |

Table 5 Thermodynamic fitting parameters for the adsorption of Cs(I) onto the PB/CA membrane at different temperatures

| T(K) | ΔG0(kJ/mol) | ΔH0(kJ/mol) | ΔS0(J/mol·K) |
| --- | --- | --- | --- |
| 298.15 | -31.50 | 6.76 | 0.08 |
| 308.15 | -32.35 |  |  |
| 318.15 | -33.16 |  |  |

Table 6 Hydrated ionic radius of competing cations

| Type | Hydrated ionic radius(Å) |
| --- | --- |
| Na+ | 3.58 |
| Mg2+ | 4.28 |
| K+ | 3.31 |
| Ca2+ | 4.12 |
| Mn2+ | 4.38 |
| Co2+ | 4.23 |
| Ni2+ | 4.04 |
| Zn2+ | 4.30 |

Table 7 Mössbauer spectral parameters of the PB/CA membrane before and after Cs(I) adsorption

| Sample | Ion type | A(%) | IS(mm·s-1) | QS(mm·s-1) | LW(mm·s-1) |
| --- | --- | --- | --- | --- | --- |
| Before adsorption | Fe2+ | 21.0 | -0.19±0.00 | 0.00±0.00 | 0.17±0.01 |
|  | Fe3+ | 79.0 | 0.17±0.00 | 0.52±0.00 | 0.44±0.00 |
| After adsorption | Fe2+ | 21.7 | -0.20±0.00 | 0.00±0.00 | 0.17±0.02 |
|  | Fe3+ | 78.3 | 0.18±0.00 | 0.54±0.00 | 0.47±0.00 |