Machine Learning Models with a Reject Option to Minimize Prediction Error:  Application to Optical Properties of Dye Molecules

James Wellnitz1, Travis Maxfield1, Matthew Hart1, Marielle Rath1, Kathryn Kirchoff1, Konstantin I. Popov1*, Alexander Tropsha1*.

1UNC Eshelman School of Pharmacy, University of North Carolina, Chapel Hill, NC, USA.

*Email: kpopov@unc.edu; alex_tropsha@unc.edu.

| Model | abs-λmax (nm) | emi-λmax (nm) | abs-σ (nm) | emi-σ (nm) | log PLQY | log ε (M−1⋅cm−1) |
| --- | --- | --- | --- | --- | --- | --- |
| CasRidge | 38.9 ± 5.4 | 51.45 ± 5.04 | 15.06 ± 1.24 | 21.9 ± 2.7 | 0.61 ± 0.06 | 0.29 ± 0.04 |
| GBT | 36.24 ± 4.0 | 45.88 ± 2.15 | 14.28 ± 0.61 | 19.92 ± 2.1 | 0.57 ± 0.04 | 0.3 ± 0.03 |
| ChemProp | 31.12 ± 3.1 | 39.6 ± 2.8 | 13.38 ± 1.31 | 19.5 ± 0.9 | 0.55 ± 0.04 | 0.29 ± 0.04 |

Table S1: Mean absolute error (MAE) for the three regression models (rows) using absolute-out cross validation for all six endpoints (columns).

| Model | Max Absorbance (nm) | Max Emission (nm) | Bandwidth Absorbance (nm) | Bandwidth Emission (nm) | Log Quantum Yield | Log Extinction Coefficient |
| --- | --- | --- | --- | --- | --- | --- |
| Deep4Chem | 31.6 | 32.6 | 14450.87 | 17667.84 | 0.431 | 0.24 |
| CasRidge | 23.74 ± 0.84 | 35.23 ± 1.13 | 12.39 ± 0.77 | 19.84 ± 0.37 | 0.54 ± 0.02 | 0.24 ± 0.02 |
| GBT | 20.14 ± 1.24 | 25.76 ± 0.48 | 10.24 ± 0.89 | 14.76 ± 0.73 | 0.41 ± 0.01 | 0.22 ± 0.02 |
| ChemProp | 19.87 ± 0.67 | 26.01 ± 0.49 | 11.03 ± 0.39 | 15.74 ± 1.14 | 0.44 ± 0.01 | 0.21 ± 0.01 |

Table S2: Comparison of full coverage models to the deep learning Deep4Chem model from Joung et. al. [REF]. Errors are measured in RMSE and evaluated on random split folds, as outlined in in Joung et. al. bandwidth was converted from wavenumber to wavelength for Deep4Chem. Bolded entries are significantly better than the Deep4Chem results by means of a Students T-Test.

|  | Max Absorbance (nm) | Max Emission (nm) | Bandwidth Absorbance (nm) | Bandwidth Emission (nm) | Log Quantum Yield | Log Extinction Coefficient |
| --- | --- | --- | --- | --- | --- | --- |
| 75% CasRidge | 29.52 ± 3.28 | 44.91 ± 4.28 | 14.15 ± 2.02 | 20.83 ± 3.34 | 0.55 ± 0.04 | 0.26 ± 0.05 |
| 75% GBT | 29.94 ± 3.61 | 42.22 ± 2.08 | 13.74 ± 1.2 | 18.61 ± 2.18 | 0.54 ± 0.04 | 0.27 ± 0.04 |
| 75% ChemProp | 26.80 ± 3.10 | 37.23 ± 2.63 | 6.80 ± 0.97 | 18.35 ± 0.96 | 0.52 ± 0.03 | 0.27 ± 0.04 |
| 50% CasRidge | 25.67 ± 2.26 | 38.98 ± 4.31 | 14.05 ± 3.03 | 20.43 ± 3.73 | 0.49 ± 0.07 | 0.24 ± 0.05 |
| 50% GBT | 26.13 ± 2.18 | 38.60 ± 3.10 | 13.35 ± 1.35 | 17.74 ± 2.74 | 0.48 ± 0.04 | 0.25 ± 0.04 |
| 50% ChemProp | 24.74 ± 3.45 | 33.99 ± 3.49 | 7.23 ± 1.19 | 17.41 ± 1.12 | 0.47 ± 0.03 | 0.25 ± 0.05 |
| 25% CasRidge | 19.46 ± 3.18 | 32.01 ± 4.26 | 10.95 ± 2.01 | 20.9 ± 5.37 | 0.39 ± 0.10 | 0.18 ± 0.02 |
| 25% GBT | 21.62 ± 2.11 | 33.49 ± 2.85 | 12.57 ± 1.56 | 16.81 ± 3.16 | 0.42 ± 0.03 | 0.21 ± 0.02 |
| 25% ChemProp | 22.42 ± 3.73 | 32.21 ± 4.12 | 7.51 ± 0.95 | 16.06 ± 1.29 | 0.42 ± 0.06 | 0.21 ± 0.03 |

Table S3: MAE of models utilizing reject option on absolute out validation splits.

| Endpoint | Max Absorbance (nm) | Max Emission (nm) | FWHM Absorbance (nm) | FWHM Emission (nm) | Log Quantum Yield | Log Extinction Coefficient |
| --- | --- | --- | --- | --- | --- | --- |
| Num unique dyes | 6257 | 6140 | 1543 | 2714 | 5258 | 3730 |
| Num dyes occurrence >1 | 2054 | 2348 | 493 | 936 | 1763 | 1014 |

Table S4: the number a unique dyes in each of the six datasets and the number of unique dyes in the dataset that occur more than once (in different solvents).

| Solvents |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| O Water | CS(C)=O Methylsulfinylmethane | CCO Ethanol | CCCO Propanol | CC(C)=O Acetone | C1COCCO1 Dioxane | CCOCC Ethoxyethane |
| ClC(Cl)Cl Chloroform | C1CCCCC1 Cyclohexane | CO Methonal | CCCCO Butanol | Cc1ccccc1 Toluene | ClCCl Dichloromethane | CN(C)C=O Dimethylformamide |
| CC#N Acetonitrile | CCOC(C)=O Ethyl Acetate | CC(C)O Isopropyl Alcohol | c1ccccc1 Benzene | CCCCCC Hexane | C1CCOC1 Oxolane | CCCCCCC Heptane |
| O=P(c1ccccc1)(c1ccccc1)c1ccccc1Oc1ccccc1P(=O)(c1ccccc1)c1ccccc1 1-diphenylphosphoryl-2-(2-diphenylphosphorylphenoxy)benzene |  |  |  |  |  |  |

Table S5: SMILES strings of the 22 solvents that occurred more than 100 times used in the curated the dataset. O=P(c1ccccc1)(c1ccccc1)c1ccccc1Oc1ccccc1P(=O)(c1ccccc1)c1ccccc1 was considered a solvent for the purposes of this work

| Endpoint | Max Absorbance(nm) | Max Emission (nm) | FWHM Absorbance (nm) | FWHM Emission (nm) | Log Quantum Yield | Log Extinction Coefficient |
| --- | --- | --- | --- | --- | --- | --- |
| Total size | 14915 | 15397 | 2363 | 6175 | 11755 | 7437 |
| Training | 8440.6 | 7701.0 | 1439.4 | 3971.8 | 5878.4 | 3726.0 |
| Val Dye Out | 3589.8 | 3324.0 | 602.6 | 1258.6 | 2515.8 | 1631.2 |
| Val Absolute Out | 442.8 | 647.0 | 188.6 | 297.4 | 506.0 | 300.0 |

Table S6: Number of datapoints in the datasets and model folds generated for each endpoint. Total refers to all datapoints, Training refers to the average size of the five training subsets used for training models. Val Dye Out refers to the average size of dye out validation subsets used for validation. Val Absolute out refers to the average size of absolute out subsets used for validation.

Figure S1: Coverage loss curves for reject option models (solid line) compared to random rejections controls (faded line)

Figure S2: Distributions of MAE across confidence levels. Confidence was binned by groups of 10%, with each density line representing the distribution of errors for that bin of confidence.

Figure S3: Scatter plot of real and predict values colored by rejection confidence for GBT (top) and ChemProp (bottom) for all 6 endpoints.

Figure S4: UMap of the chemicals space colored by similarity (left) and rejection confidence (right) for the four endpoints not shown in the main text

Figure S5: Distributions of error across various similarity levels. Smaller distance means higher similarity. Distance binned by 0.25. Each density line represents the distribution of errors present in that bin.

Figure S6: Distribution of the maximum absolute difference in endpoint measurement values across all solvents a given dye was measured in. Dyes that were only measured in a single solvent are not included in the graph.

Figure S7: Comparison of performance on endpoints for each model across all four validation split methods. For each, Random split validation always performs significantly better than all other validation approaches, with the exception of ChemProp on absorption bandwidth